- Table 1 Coil type electromagnet specifications

| Sr. No. | Constituents | Description |
| --- | --- | --- |
| 1. | Core material | Mild steel (M.S.) |
| 2. | Core size | Core length = 175 mm Core radius = 25 mm Core rod diameter = 35 mm |
| 3. | Electromagnet coils | Copper wire, 23 gauge, ɸ 0.5733mm No. of turns = 2500 per coil Coil Weight = 3.820 kg |
| 4. | Power supply (DC) | 0–240V |
| 5. | Magnetic flux density (Mf) | 0–2T |

Table 2 Composition of magnetic abrasive media

| Sr. No. | Constituents | Value of the constituents | % Volume concentration in media |
| --- | --- | --- | --- |
| 1. | Silicon carbide (SiC) abrasive particle | 150 mesh size 220 mesh size 400 mesh size | 45%, 50%, 55% |
| 2. | Iron (Fe) particle | 300 mesh size | 10% |
| 3. | Hydraulic oil | 68 number | 10% |
| 4. | Liquid silicon rubber | White colour (RTV–2615) | 35%, 30%, 25% |

Table 3 Design of experiments and results

| Run No. | Extrusion Pressure (Ep) | Mesh No. (M) | Concentration of Abrasives (C) | Type of Work Material (Wp) | Number of Cycles (N) | Magnetic Flux Density (Mf) | MRR (μg/s) | ΔRa (μm) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 5 | 220 | 45 | 1 | 150 | 0.15 | 6.31 | 1.52 |
| 2 | 7 | 400 | 50 | 1 | 150 | 0.3 | 6.78 | 2.24 |
| 3 | 5 | 150 | 55 | 2 | 200 | 0.3 | 7.78 | 2.68 |
| 4 | 3 | 400 | 50 | 3 | 150 | 0.3 | 2.32 | 0.79 |
| 5 | 3 | 150 | 50 | 1 | 150 | 0.3 | 5.01 | 1.42 |
| 6 | 5 | 220 | 50 | 2 | 150 | 0.3 | 6.28 | 1.73 |
| 7 | 7 | 220 | 50 | 1 | 100 | 0.3 | 6.79 | 1.91 |
| 8 | 5 | 400 | 55 | 2 | 200 | 0.3 | 6.94 | 2.21 |
| 9 | 3 | 400 | 50 | 1 | 150 | 0.3 | 4.56 | 1.31 |
| 10 | 7 | 220 | 50 | 3 | 100 | 0.3 | 4.87 | 1.72 |
| 11 | 5 | 150 | 45 | 2 | 200 | 0.3 | 7.66 | 2.51 |
| 12 | 3 | 220 | 55 | 2 | 150 | 0.45 | 4.97 | 1.39 |
| 13 | 5 | 400 | 45 | 2 | 200 | 0.3 | 6.82 | 1.98 |
| 14 | 5 | 220 | 45 | 3 | 150 | 0.45 | 4.94 | 1.73 |
| 15 | 5 | 220 | 45 | 1 | 150 | 0.45 | 6.83 | 1.98 |
| 16 | 5 | 400 | 50 | 2 | 100 | 0.45 | 7.08 | 2.19 |
| 17 | 7 | 220 | 50 | 3 | 200 | 0.3 | 5.87 | 2.13 |
| 18 | 7 | 220 | 50 | 1 | 200 | 0.3 | 8.21 | 2.79 |
| 19 | 5 | 400 | 50 | 2 | 200 | 0.15 | 6.58 | 1.27 |
| 20 | 5 | 400 | 45 | 2 | 100 | 0.3 | 6.35 | 1.81 |
| 21 | 3 | 220 | 45 | 2 | 150 | 0.15 | 4.68 | 1.12 |
| 22 | 5 | 220 | 55 | 1 | 150 | 0.15 | 6.49 | 1.65 |
| 23 | 5 | 220 | 50 | 2 | 150 | 0.3 | 6.42 | 1.75 |
| 24 | 5 | 400 | 55 | 2 | 100 | 0.3 | 6.45 | 1.87 |
| 25 | 3 | 220 | 50 | 3 | 200 | 0.3 | 3.29 | 1.07 |
| 26 | 7 | 220 | 55 | 2 | 150 | 0.45 | 8.24 | 2.83 |
| 27 | 5 | 150 | 50 | 2 | 100 | 0.45 | 7.62 | 2.74 |
| 28 | 5 | 220 | 55 | 3 | 150 | 0.45 | 5.02 | 1.96 |
| 29 | 5 | 220 | 55 | 3 | 150 | 0.15 | 4.37 | 1.38 |
| 30 | 3 | 150 | 50 | 3 | 150 | 0.3 | 3.37 | 1.01 |
| 31 | 5 | 150 | 50 | 2 | 200 | 0.15 | 7.29 | 2.15 |
| 32 | 3 | 220 | 50 | 1 | 200 | 0.3 | 4.98 | 1.38 |
| 33 | 5 | 400 | 50 | 2 | 200 | 0.45 | 7.23 | 2.41 |
| 34 | 7 | 220 | 45 | 2 | 150 | 0.45 | 7.93 | 2.61 |
| 35 | 5 | 150 | 45 | 2 | 100 | 0.3 | 7.2 | 2.01 |
| 36 | 5 | 150 | 50 | 2 | 100 | 0.15 | 6.82 | 1.89 |
| 37 | 5 | 220 | 50 | 2 | 150 | 0.3 | 7.05 | 2.01 |
| 38 | 5 | 220 | 55 | 1 | 150 | 0.45 | 6.95 | 2.29 |
| 39 | 3 | 220 | 50 | 3 | 100 | 0.3 | 3.21 | 0.73 |
| 40 | 3 | 220 | 45 | 2 | 150 | 0.45 | 4.89 | 1.21 |
| 41 | 5 | 400 | 50 | 2 | 100 | 0.15 | 5.74 | 1.03 |
| 42 | 5 | 150 | 55 | 2 | 100 | 0.3 | 7.32 | 2.17 |
| 43 | 3 | 220 | 50 | 1 | 100 | 0.3 | 4.91 | 1.19 |
| 44 | 5 | 220 | 50 | 2 | 150 | 0.3 | 6.93 | 1.76 |
| 45 | 5 | 150 | 50 | 2 | 200 | 0.45 | 8.41 | 2.88 |
| 46 | 7 | 150 | 50 | 1 | 150 | 0.3 | 7.69 | 2.68 |
| 47 | 7 | 400 | 50 | 3 | 150 | 0.3 | 3.93 | 1.91 |
| 48 | 5 | 220 | 50 | 2 | 150 | 0.3 | 6.86 | 1.89 |
| 49 | 7 | 150 | 50 | 3 | 150 | 0.3 | 5.28 | 2.1 |
| 50 | 3 | 220 | 55 | 2 | 150 | 0.15 | 3.95 | 1.13 |
| 51 | 5 | 220 | 45 | 3 | 150 | 0.15 | 4.12 | 1.19 |
| 52 | 7 | 220 | 45 | 2 | 150 | 0.15 | 7.41 | 2.16 |
| 53 | 5 | 220 | 50 | 2 | 150 | 0.3 | 7.11 | 2.15 |
| 54 | 7 | 220 | 55 | 2 | 150 | 0.15 | 6.68 | 2.23 |

Table 4 The weight percentage of material composition

| Element | Al | Fe | Mg | Cu | Si | Zn | Mn | Pb | B | Cr | Ti |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Workpiece-1 | Balance | 0.28 | 0.76 | 0.03 | 9.15 | 0.0010 | 0.0064 | 0.0025 | 1.01 | 0.0016 | 0.0096 |
| Workpiece-2 | Balance | 0.16 | 0.53 | 0.02 | 8.02 | 0.0012 | 0.0050 | 0.0026 | 1.96 | 0.0021 | 0.0090 |
| Workpiece-3 | Balance | 0.18 | 0.72 | 0.04 | 6.82 | 0.0012 | 0.0068 | 0.0027 | 2.86 | 0.0021 | 0.0091 |

Table 5 Factors with their levels (actual and coded)

| Parameter | Symbols | Units | Lower range | Upper range | Coded low | Coded high | Mean | SD |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A | Ep | MPa | 3.00 | 7 | ‒1 ↔ 3 | +1 ↔ 7 | 5.00 | 1.35 |
| B | M | Number | 150 | 400 | ‒1 ↔ 150 | +1 ↔ 400 | 244.44 | 88.52 |
| C | C | Wt. % | 45 | 55 | ‒1 ↔ 45 | +1 ↔ 55 | 50.00 | 3.36 |
| D | Wp | type | 1 | 3 | ‒1 ↔ 1 | +1 ↔ 3 | 2.00 | 0.6729 |
| E | N | ‒ | 100 | 200 | ‒1 ↔ 100 | +1 ↔ 200 | 150.00 | 33.65 |
| F | Mf | Tesla | 0.15 | 0.45 | ‒1 ↔ 0.15 | +1 ↔ 0.45 | 0.3000 | 0.1009 |

Table 6 Experimental and ANN predicted results for MRR and ΔRa.

| Run No. | Input Parameters and their Values |  |  |  |  |  | Experimental |  | ANN Predicted |  | Error |  | Absolute Error % |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Extrusion Pressure (Ep) | Mesh No. (M) | Conc. of abrasives (C) | Type of work material (Wp) | Number of Cycles (N) | Magnetic flux density (Mf) | MRR (μg/s) | ΔRa (μm) | MRR (μg/s) | ΔRa (μm) | MRR (μg/s) | ΔRa (μm) | MRR (μg/s) | ΔRa (μm) |
| 1 | 5 | 220 | 45 | 1 | 150 | 0.15 | 6.31 | 1.52 | 6.3035 | 2.0972 | 0.0065 | -0.5772 | 0.10301 | -37.974 |
| 2 | 7 | 400 | 50 | 1 | 150 | 0.3 | 6.78 | 2.24 | 6.3437 | 1.9609 | 0.4363 | 0.2791 | 6.4351 | 12.4598 |
| 3 | 5 | 150 | 55 | 2 | 200 | 0.3 | 7.78 | 2.68 | 7.1767 | 2.1018 | 0.6033 | 0.5782 | 7.7545 | 21.5746 |
| 4 | 3 | 400 | 50 | 3 | 150 | 0.3 | 2.32 | 0.79 | 2.812 | 1.014 | -0.492 | -0.224 | -21.207 | -28.354 |
| 5 | 3 | 150 | 50 | 1 | 150 | 0.3 | 5.01 | 1.42 | 5.0476 | 1.5966 | -0.0376 | -0.1766 | -0.7505 | -12.437 |
| 6 | 5 | 220 | 50 | 2 | 150 | 0.3 | 6.28 | 1.73 | 6.0937 | 2.0668 | 0.1863 | -0.3368 | 2.96656 | -19.468 |
| 7 | 7 | 220 | 50 | 1 | 100 | 0.3 | 6.79 | 1.91 | 6.1354 | 2.1064 | 0.6546 | -0.1964 | 9.64065 | -10.283 |
| 8 | 5 | 400 | 55 | 2 | 200 | 0.3 | 6.94 | 2.21 | 6.414 | 1.9686 | 0.526 | 0.2414 | 7.57925 | 10.9231 |
| 9 | 3 | 400 | 50 | 1 | 150 | 0.3 | 4.56 | 1.31 | 4.7999 | 2.0319 | -0.2399 | -0.7219 | -5.261 | -55.107 |
| 10 | 7 | 220 | 50 | 3 | 100 | 0.3 | 4.87 | 1.72 | 4.7657 | 2.0746 | 0.1043 | -0.3546 | 2.14168 | -20.616 |
| 11 | 5 | 150 | 45 | 2 | 200 | 0.3 | 7.66 | 2.51 | 7.157 | 1.9499 | 0.503 | 0.5601 | 6.56658 | 22.3147 |
| 12 | 3 | 220 | 55 | 2 | 150 | 0.45 | 4.97 | 1.39 | 4.2988 | 2.2508 | 0.6712 | -0.8608 | 13.505 | -61.928 |
| 13 | 5 | 400 | 45 | 2 | 200 | 0.3 | 6.82 | 1.98 | 6.1226 | 1.9592 | 0.6974 | 0.0208 | 10.2258 | 1.05051 |
| 14 | 5 | 220 | 45 | 3 | 150 | 0.45 | 4.94 | 1.73 | 4.9479 | 1.966 | -0.0079 | -0.236 | -0.1599 | -13.642 |
| 15 | 5 | 220 | 45 | 1 | 150 | 0.45 | 6.83 | 1.98 | 6.0776 | 1.9666 | 0.7524 | 0.0134 | 11.0161 | 0.67677 |
| 16 | 5 | 400 | 50 | 2 | 100 | 0.45 | 7.08 | 2.19 | 6.8954 | 1.9772 | 0.1846 | 0.2128 | 2.60734 | 9.71689 |
| 17 | 7 | 220 | 50 | 3 | 200 | 0.3 | 5.87 | 2.13 | 6.2676 | 1.9399 | -0.3976 | 0.1901 | -6.7734 | 8.92488 |
| 18 | 7 | 220 | 50 | 1 | 200 | 0.3 | 8.21 | 2.79 | 8.4127 | 1.9177 | -0.2027 | 0.8723 | -2.4689 | 31.2652 |
| 19 | 5 | 400 | 50 | 2 | 200 | 0.15 | 6.58 | 1.27 | 6.9458 | 1.9659 | -0.3658 | -0.6959 | -5.5593 | -54.795 |
| 20 | 5 | 400 | 45 | 2 | 100 | 0.3 | 6.35 | 1.81 | 6.8886 | 1.9812 | -0.5386 | -0.1712 | -8.4819 | -9.4586 |
| 21 | 3 | 220 | 45 | 2 | 150 | 0.15 | 4.68 | 1.12 | 4.2477 | 2.367 | 0.4323 | -1.247 | 9.23718 | -111.34 |
| 22 | 5 | 220 | 55 | 1 | 150 | 0.15 | 6.49 | 1.65 | 6.8583 | 2.8593 | -0.3683 | -1.2093 | -5.6749 | -73.291 |
| 23 | 5 | 220 | 50 | 2 | 150 | 0.3 | 6.42 | 1.75 | 6.0937 | 2.0668 | 0.3263 | -0.3168 | 5.08255 | -18.103 |
| 24 | 5 | 400 | 55 | 2 | 100 | 0.3 | 6.45 | 1.87 | 6.3684 | 2.2043 | 0.0816 | -0.3343 | 1.26512 | -17.877 |
| 25 | 3 | 220 | 50 | 3 | 200 | 0.3 | 3.29 | 1.07 | 3.0594 | 2.0373 | 0.2306 | -0.9673 | 7.00912 | -90.402 |
| 26 | 7 | 220 | 55 | 2 | 150 | 0.45 | 8.24 | 2.83 | 8.4916 | 1.9787 | -0.2516 | 0.8513 | -3.0534 | 30.0813 |
| 27 | 5 | 150 | 50 | 2 | 100 | 0.45 | 7.62 | 2.74 | 7.4669 | 2.1746 | 0.1531 | 0.5654 | 2.00919 | 20.635 |
| 28 | 5 | 220 | 55 | 3 | 150 | 0.45 | 5.02 | 1.96 | 5.8292 | 2.0378 | -0.8092 | -0.0778 | -16.12 | -3.9694 |
| 29 | 5 | 220 | 55 | 3 | 150 | 0.15 | 4.37 | 1.38 | 4.0086 | 2.7685 | 0.3614 | -1.3885 | 8.27002 | -100.62 |
| 30 | 3 | 150 | 50 | 3 | 150 | 0.3 | 3.37 | 1.01 | 3.7901 | 2.492 | -0.4201 | -1.482 | -12.466 | -146.73 |
| 31 | 5 | 150 | 50 | 2 | 200 | 0.15 | 7.29 | 2.15 | 7.9561 | 2.1307 | -0.6661 | 0.0193 | -9.1372 | 0.89767 |
| 32 | 3 | 220 | 50 | 1 | 200 | 0.3 | 4.98 | 1.38 | 5.1189 | 2.0513 | -0.1389 | -0.6713 | -2.7892 | -48.645 |
| 33 | 5 | 400 | 50 | 2 | 200 | 0.45 | 7.23 | 2.41 | 7.0164 | 1.9602 | 0.2136 | 0.4498 | 2.95436 | 18.6639 |
| 34 | 7 | 220 | 45 | 2 | 150 | 0.45 | 7.93 | 2.61 | 7.1626 | 1.9596 | 0.7674 | 0.6504 | 9.67718 | 24.9195 |
| 35 | 5 | 150 | 45 | 2 | 100 | 0.3 | 7.2 | 2.01 | 7.4179 | 2.2182 | -0.2179 | -0.2082 | -3.0264 | -10.358 |
| 36 | 5 | 150 | 50 | 2 | 100 | 0.15 | 6.82 | 1.89 | 6.6944 | 1.1468 | 0.1256 | 0.7432 | 1.84164 | 39.3228 |
| 37 | 5 | 220 | 50 | 2 | 150 | 0.3 | 7.05 | 2.01 | 7.0937 | 2.0668 | -0.0437 | -0.0568 | -0.6199 | -2.8259 |
| 38 | 5 | 220 | 55 | 1 | 150 | 0.45 | 6.95 | 2.29 | 6.1282 | 2.0597 | 0.8218 | 0.2303 | 11.8245 | 10.0568 |
| 39 | 3 | 220 | 50 | 3 | 100 | 0.3 | 3.21 | 0.73 | 3.0021 | 0.777 | 0.2079 | -0.047 | 6.47664 | -6.4384 |
| 40 | 3 | 220 | 45 | 2 | 150 | 0.45 | 4.89 | 1.21 | 4.8918 | 1.986 | -0.0018 | -0.776 | -0.0368 | -64.132 |
| 41 | 5 | 400 | 50 | 2 | 100 | 0.15 | 5.74 | 1.03 | 5.2717 | 1.253 | 0.4683 | -0.223 | 8.15854 | -21.65 |
| 42 | 5 | 150 | 55 | 2 | 100 | 0.3 | 7.32 | 2.17 | 7.5247 | 2.0874 | -0.2047 | 0.0826 | -2.7964 | 3.80645 |
| 43 | 3 | 220 | 50 | 1 | 100 | 0.3 | 4.91 | 1.19 | 4.772 | 1.8913 | 0.138 | -0.7013 | 2.81059 | -58.933 |
| 44 | 5 | 220 | 50 | 2 | 150 | 0.3 | 6.93 | 1.76 | 6.0937 | 2.0668 | 0.8363 | -0.3068 | 12.0678 | -17.432 |
| 45 | 5 | 150 | 50 | 2 | 200 | 0.45 | 8.41 | 2.88 | 8.1814 | 1.958 | 0.2286 | 0.922 | 2.71819 | 32.0139 |
| 46 | 7 | 150 | 50 | 1 | 150 | 0.3 | 7.69 | 2.68 | 7.159 | 1.9973 | 0.531 | 0.6827 | 6.90507 | 25.4739 |
| 47 | 7 | 400 | 50 | 3 | 150 | 0.3 | 3.93 | 1.91 | 4.002 | 1.9634 | -0.072 | -0.0534 | -1.8321 | -2.7958 |
| 48 | 5 | 220 | 50 | 2 | 150 | 0.3 | 6.86 | 1.89 | 6.0937 | 2.0668 | 0.7663 | -0.1768 | 11.1706 | -9.3545 |
| 49 | 7 | 150 | 50 | 3 | 150 | 0.3 | 5.28 | 2.1 | 4.993 | 2.0032 | 0.287 | 0.0968 | 5.43561 | 4.60952 |
| 50 | 3 | 220 | 55 | 2 | 150 | 0.15 | 3.95 | 1.13 | 4.6401 | 1.2329 | -0.6901 | -0.1029 | -17.471 | -9.1062 |
| 51 | 5 | 220 | 45 | 3 | 150 | 0.15 | 4.12 | 1.19 | 4.0588 | 2.0743 | 0.0612 | -0.8843 | 1.48544 | -74.311 |
| 52 | 7 | 220 | 45 | 2 | 150 | 0.15 | 7.41 | 2.16 | 7.0509 | 1.9744 | 0.3591 | 0.1856 | 4.84615 | 8.59259 |
| 53 | 5 | 220 | 50 | 2 | 150 | 0.3 | 7.11 | 2.15 | 7.0937 | 2.0668 | 0.0163 | 0.0832 | 0.22925 | 3.86977 |
| 54 | 7 | 220 | 55 | 2 | 150 | 0.15 | 6.68 | 2.23 | 6.6069 | 2.3228 | 0.0731 | -0.0928 | 1.09431 | -4.1614 |

Table 7 Modeling Error Reduction by Parameter Optimization Techniques

| Coefficient Type | Experimental | Particle Swarm Optimization (PSO) | Genetic Algorithm (GA) | Simulated Annealing (SA) | Pattern Search (PS) |
| --- | --- | --- | --- | --- | --- |
| Mean Square Error | 4.1919 | 1.3575 | 1.9225 | 1.3561 | 1.9423 |