Supporting information

Magnetic quasi-atomic electrons driven reversible structural and magnetic transitions between electride and its hydrides

Seung Yong Lee1,2,†, Dong Cheol Lim1,3,†, Md Salman Khan1,3,†, Jeong Yun Hwang4, Hyungsub Kim5, Kyu Hyung Lee4*, Sung Wng Kim1,3*

1Department of Energy Science, Sungkyunkwan University; Suwon 16419, Republic of Korea.

2KIURI Institute, Yonsei University, Seoul, 03722, Republic of Korea.

3Center for Electride Materials, Sungkyunkwan University; Suwon 16419, Republic of Korea.

4Department of Materials Science and Engineering, Yonsei University, Seoul, 03722, Republic of Korea.

5Neutron Science Division, Korea Atomic Energy Research Institute, Daejeon, 34057, Republic of Korea.

†These authors contributed equally to this work

*Email: khlee2018@yonsei.ac.kr (K.H.L) and kimsungwng@skku.edu (S.W.K.)

Supplementary Fig. 1 | Schematic illustration of synthetic process for the hydrogenation yielding Gd2CHx (x≤1.0) (top) and Gd2CHy (y2.0) (bottom). The hydrogen pressures for each process producing hydrogenated Gd2CHx (x≤1.0) and Gd2CHy (y2.0) were controlled with a vacuum pump station.

Supplementary Fig. 2 | Rietveld refinement of powder XRD pattern of Gd2CHy (y2.0). The structural parameters obtained by the refinement with the P3m1 space group are listed in Table S1.

Supplementary Fig. 3 | Rietveld refinement of powder ND pattern of hydrogenated Y2CHy (y2.0). The [Y2C]2+·2e− electride, which is isostructural with the [Gd2C]2+·2e− electride, was hydrogenated with the same condition to produce Gd2CHy (y2.0) as shown in bottom of Supplementary Fig. 1.

Supplementary Fig. 4 | Temperature dependence of electrical resistivity for the [Gd2C]2+∙2e− electride and hydrogenated Gd2CHx (x≤1.0). a, Power law fitting of R/R400K for metallic [Gd2C]2+∙2e− electride and hydrogenated Gd2CHx (x≤1.0), showing different scattering mechanism of carriers. b, Plot of R/R400K versus T0.8 for the hydrogenated Gd2CHx (x≤1.0).

Supplementary Fig. 5 | Magnetic phase transition temperatures of the [Gd2C]2+∙2e− electride and its hydrides. a, Temperature dependence of dM/dT for the three samples. b, Curie-Weiss fitting for the three samples.

Supplementary Fig. 6 | Antiferromagnetic nature of hydrogenated Gd2CHy (y>2.0). The TN decreasing with the increase of DC magnetic field is clearly revealed from MT/MTN.

Supplementary Fig. 7 | AC susceptibility of ferromagnetic [Gd2C]2+∙2e− electride. Real part (a) and imaginary part (b) of AC susceptibility are measured under different frequencies at 0 HDC.

Supplementary Fig. 8 | Magnetic properties between Cl-substituted Gd2CCl and H-substituted Gd2CHy (y>2.0). a, MT curves measured under magnetic field of 0.1 T, showing no splitting and a clear splitting between ZFC and FC for Gd2CCl and Gd2CHy (y>2.0), respectively. b, MH curves measured at 2 K. These results strongly indicate the antiferromagnetism of Gd2CCl and canted antiferromagnetsm of Gd2CHy (y>2.0).

Supplementary Fig. 9 | The modified Arrott plot of [Gd2C]2+∙2e− electride and its hydrides. a–f, Modified Arrott plots of [Gd2C]2+∙2e− electride with meanfield (a), tricritical (b), 3D Heisenberg (c), 3D Ising (d), 2D Ising (e), xy (f) models. g–l, Modified Arrott plots of Gd2CHx (x≤1.0) with meanfield (g), tricritical (h), 3D Heisenberg (i), 3D Ising (j), 2D Ising (k), xy (l) models. m–r, Modified Arrott plots of Gd2CHy (y>2.0) with meanfield (m), tricritical (n), 3D Heisenberg (o), 3D Ising (p), 2D Ising (q), xy (r) models.

Supplementary Fig. 10 | Critical exponent fitting from Arrott plot. a–c, Temperature dependence of relative slope (RS) curves near the magnetic transition temperatures for the [Gd2C]2+∙2e− electride (a), Gd2CHx (x≤1.0) (b) and Gd2CHy (y>2.0) (c). d–f, Plots of the critical exponent model calculated by MS and χ0-1 from Arrott plots for each sample. g–i, Critical exponent value derives from KF method.

Supplementary Fig. 11 | Schematic illustration of canted antiferromagnetic ordering in Gd2CHy (y>2.0). Out-of-plane interaction between GdHGd determines the canted antiferromagnetism.

Supplementary Fig. 12 | Curie-Weiss fitting. Temperature dependence of reciprocal magnetic susceptibility (1) of [Gd2C]2+∙2e− electride, hydrogenated and dehydrogenated samples.

Supplementary Fig. 13 | MH curves of the [Gd2C]2+∙2e− electride and its hydrides. The data was obtained at 2 K.

Supplementary Fig. 14 | RCP performance of the [Gd2C]2+∙2e− electride and its hydrides. The canted antiferromagnetic Gd2CHy (y>2.0) shows a larger RCP value than those of ferromagnetic [Gd2C]2+∙2e− electride and Gd2CHx (x≤1.0) samples.

Supplementary Table. 1 | XRD Rietveld results of Gd2CHx (x≤1.0) and Gd2CHy (y>2.0).

| Sample | Gd2CHx (x≤1.0) |  | Gd2CHy (y>2.0) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Space group | R3m |  | P31m |  | P3m1 |  | P3m1 (Supplementary Fig. 2) |
| a, b (Å) | 3.64 |  | 6.47 |  | 3.74 |  | 3.73 |
| c (Å) | 18.13 |  | 6.02 |  | 6.02 |  | 6.03 |
| Volume (Å3) | 207.55 |  | 218.79 |  | 72.88 |  | 72.59 |
| Atom | Position / Occupancy |  |  |  |  |  |  |
| Gd1 | (0 0 0.257) / 1.0 |  | (0.350 0 0.247) / 1.0 |  | (0.333 0.667 0.269) / 1.0 |  | (0.667 0.333 0.548) / 1.0 |
| Gd2 |  |  |  |  |  |  | (0 0 0) / 1.0 |
| C1 | (0 0 0) / 1.0 |  | (0 0 0) / 1.0 |  | (0 0 0) / 1.0 |  | (0.333 0.667 0.77) / 1.0 |
| C2 | (0.333 0.667 0) / 1.0 |  | (0.333 0.667 0) / 1.0 |  |  |  |  |
| Rwp (%) | 8.71 |  | 8.17 |  | 8.80 |  | 10.50 |

Supplementary Table. 2 | ND Rietveld results of hydrogenated [Y2C]2+·2e.

| Space group | P31m |
| --- | --- |
| a, b (Å) | 6.34 |
| c (Å) | 5.94 |
| Volume (Å3) | 206.695 |
| Atom | Position / Occupancy |
| Y | (0.345 0 0.250) / 1.0 |
| C1 | (0 0 0) / 1.0 |
| C2 | (0.333 0.667 0) / 1.0 |
| H1 | (0 0 0.500) / 1.0 |
| H2 | (0.333 0.667 0.500) / 0.62 |
| H3 | (0.298 0 0.625) / 0.79 |
| Rwp (%) | 15.6 |