Table 1 Comparison of the He-irradiation conditions, volume fractions of He bubbles, and increments of nanohardness among the Nb55V25Ta5Si15 REHEA and other radiation-tolerant alloys[14, 16, 48-54]

| Alloy | Phase | Energy (MeV) | Dose (ions/cm2) | Temp. (℃) | Volume fraction of He Bubbles (×10-5) | Increment of nanohardness (%) |
| --- | --- | --- | --- | --- | --- | --- |
| Nb55V25Ta5Si15 | eutectic | 3 | 5×1017 | 850 | 3.72 | 8.4 |
| NiMo DPS | Ni-based | 3 | 5×1017 | 850 | 45.07 | 24.1 |
| GH3535[48] | Ni-based | 1 | 1×1016 | 650 | 81.98 | 27.6 |
|  |  | 1 | 3×1016 | 650 | 231.06 | 29.0 |
|  |  | 1 | 6×1016 | 650 | 428.21 | 31.1 |
| Hastelloy N[49] | Ni-based | 0.4 | 3×1016 | 650 | 288.78 | 32.9 |
| Hastelloy N[16] | Ni-based | 2 | 7×1016 | 650 | 460.62 | 34.8 |
| Hastelloy N[50] | Ni-based | 1.2 | 1×1017 | 650 | 509.07 | 36.0 |
| Hastelloy N[51] | Ni-based | 0.5 | 2×1016 | 700 | 582.02 | 47.6 |
|  |  | 0.5 | 5×1016 | 700 | 755.93 | 74.9 |
| 800H[51] | Ni-based | 0.5 | 2×1016 | 700 | 886.01 | 97.2 |
|  |  | 0.5 | 5×1016 | 700 | 3,283.83 | 118.1 |
| Inconel 617[51] | Ni-based | 0.5 | 2×1016 | 700 | 1,370.03 | 64.8 |
|  |  | 0.5 | 5×1016 | 700 | 4,644.8- | 96.8 |
| Nickel[52] | Ni-based | 0.2 | 2×1017 | 450 | 2,480.29 | 102.7 |
| 316L[53] | Fe-based | 0.5 | 4×1015 | 700 | 137.98 | 32.2 |
|  |  | 0.5 | 1.5×1016 | 700 | 383.26 | 50.5 |
|  |  | 0.5 | 5×1016 | 700 | 1,270.12 | 71.8 |
|  |  | 0.5 | 1×1017 | 700 | 1,919.41 | 75.2 |
| 304SS[50] | Fe-based | 0.2 | 2×1017 | 450 | 1,753.92 | 64.7 |
| W600[54] | W-based | 0.04 | 1×1017 | 600 | 457.49 | 70.3 |
| CrMnFeCoNi[53] | BCC | 0.2 | 2×1017 | 450 | 3,015.92 | 88.6 |
| TiZrHfVMo[14] | BCC | 3 | 5×1015 | 600 | 45.79 | - |
|  |  | 3 | 1×1016 | 600 | 94.29 | - |
|  |  | 3 | 3×1016 | 600 | 160.28 | - |