B, N Co-doped Wood Scrap Charcoal for High Supercapacitor with Decorated Conductivity

Gaojun Chena, Yudong Lib, Enshan Hana, Ziqiang Zhanga, Xiaohui Yangc,*, Desheng Zhoud and Yanzhen Hea,*

a School of Chemical Engineering and Technology, Hebei University of Technology, Tianjin 300130, China

b Key Laboratory of Bio-based Material Science & Technology, Northeast Forestry University, Ministry of Education, Harbin 150040, China

c Key Laboratory of Reservoir Aquatic Environment, Chongqing Institute of Green and Intelligent Technology, Chinese Academy of Sciences, Chongqing 400714, China

d School of Energy Science and Engineering, Harbin Institute of Technology, Harbin 150001, China

*Corresponding authors: yzhe87@163.com (Y. He), yangxiaohui@cigit.ac.cn (X. Yang)

Figure S1 The SEM of polyaniline was impregnated into nature wood after aggregation

Figure S2 The SEM of the polyaniline aggregation after NW carbonized

Table S1 Table of element content distribution of samples

| Sample Name | C1s | N1s | O1s | B1s |
| --- | --- | --- | --- | --- |
| NCM | 89.43 | 1.03 | 9.54 | 0 |
| PNCM | 87.76 | 1.18 | 11.06 | 0 |
| BNPCM | 88.77 | 1.20 | 7.79 | 2.24 |

Figure S3 The XPS of the samples. (a) The full XPS survey spectrum of three samples, (b) the O1s high resolution spectra of BNPCM (c) the N1s high resolution spectra of PNCM. (d) the N1s high resolution spectra of NCM

Figure S4 The enlarged view of high frequency region of Fig. 6(c)

Figure S5 Comparison of electrochemical data of different introduction times of aniline

Figure S6 Comparison of electrochemical data of PNWC carbonized at 700℃, 800℃ and 900℃

Figure S7 Comparison of electrochemical data of PNWC at C:KOH=1, 3, 5 and 7 respectively