Supplementary materials

Enhance arsenic adsorptions by optimizing Fe-loaded biochar and preliminary application in paddy soil under different water management strategies

Yijie Xua, Manjie Huanga, Hongyan Wanga,b*, Guoxin Sunc,d, Amit Kumara, Zhiguo Yua

a School of Hydrology and Water Resources, Nanjing University of Information Science and Technology, Nanjing 210044, China

b Key Laboratory of Watershed Earth Surface Processes and Ecological Security，Zhejiang Normal University, Jinhua, 321004, China

c State Key Lab of Urban and Regional Ecology, Research Center for Eco-Environmental Sciences, Chinese Academy of Sciences, Beijing 100085, China

d College of Resources and Environment, University of Chinese Academy of Sciences, Beijing 101408, PR China

*: corresponding author: why_cugb@163.com

Fig. S1 The SEM image of FRB

Fig. S2 Adsorption content of NRB, FRB and CRB for As(Ⅲ) and As(Ⅴ)

Table S1 Best-fit parameters for kinetic models of As(V) and As(III) sorption onto FRB

| Modules/equations | Solution type |  | Parameter 1 | Parameter 2 | R2 |
| --- | --- | --- | --- | --- | --- |
| Pseudo-first-order | As(III) | qe=0.936 g/kg |  | k1=0.248 /h | 0.946 |
|  | As(V) | qe=8.149 g/kg |  | k1=0.248 /h | 0.936 |
| Pseudo-second-order | As(III) | qe=1.402 g/kg |  | k2=0.277 kg/g·h | 0.981 |
|  | As(V) | qe=0.359 g/kg |  | k2=9.159 kg/g·h | 0.976 |
| Elovich | As(III) | α=1.155 g/kg·h |  | β=3.65 kg/g | 0.973 |
|  | As(V) | α=6.636 g/kg·h |  | β=0.558 kg /g | 0.983 |

Table S2 Best-fit parameters of models for As(V) and As(III) adsorption isotherms to FRB

| Modules/equations | Solution type |  | Parameter 1 | Parameter 2 | R2 |  |
| --- | --- | --- | --- | --- | --- | --- |
| Langumir dqtdt=k1(qe-qt) | As(III) | qe=7908 mg/kg |  | K=0.077 L/mg |  | 0.997 |  |
|  | As(V) | qe=11268 mg/kg |  | K=0.298 L/mg |  | 0.966 |  |
| Freundilich | As(III) | n=0.58 |  | Kf=842.62 mg1-n ·Ln/kg |  | 0.981 |  |
|  | As(V) | n=0.300 |  | Kf=3338.64 mg1-n ·Ln/kg |  | 0.936 |  |
| Temkin | As(III) | K=1.11 L/mg |  | b=1.72 |  | 0.973 |  |
|  | As(V) | K=4.91 L/mg |  | b=1.27 |  | 0.986 |  |