Table 1: FT-IR Vibrational frequencies with assignments of BGLP

| # Wavenumber(cm-1) |  | # Assignments |
| --- | --- | --- |
| # FT – IR | # FT – Raman |  |
| # 3575 | # - | # ( O – H) symmetric stretching |
| # - | # 3013 | # NH2 stretching |
| # 3117 | # - | # N – H asymmetric stretching |
| # 2929 | # 2875 | # N – H symmetric stretching |
| # 2692 | # 2616 | # CH2 asymmetric stretching |
| # 2579 | # - | # CH2 symmetric stretching |
| # 2220 | # - | # N – H bending |
| # 2019 | # - | # N – H torsional |
| # 1624 | # 1718 | # C = O asymmetric stretching |
| # - | # 1602 | # NH2 deformation |
| # 1558 | # 1584 | # NH2+ in – plane deformation |
| # 1475 | # 1493 | # CH2scissoring |
| # 1442 | # 1450 | # CH2 rocking |
| # 1410 | # - | # CH2 wagging |
| # 1144 | # - | # CH2rocking |
| # 1328 | # 1336 | # CH2wagging |
| # 1307 | # - | # CH2 wagging |
| # 1113 | # 1166 | # CH2rocking |
| # - | # 1184 | # NH2twisting |
| # - | # 1148 | # ClO4 – symmetric stretching |
| # 1030 | # 1056 | # C – N stretching |
| # - | # 990 | # C – C stretching |
| # 901 | # - | # ClO4 – asymmetric bending |
| # - | # 874 | # C- C-N symmetric stretching |
| # - | # 832 | # C- C-N symmetric stretching |
| # - | # 741 | # C = O deformation |
| # - | # 717 | # C = O deformation |
| # - | # 662 | # COO- wagging vibration |
| # 681 | # - | # COO- wagging |
| # - | # 620 | # ClO4 – asymmetric stretching |
| # 580 | # - | # COO- wagging |
| # 538 | # - | # N – H torsional |
| # 456 | # 462 | # Cl- in plane deformation |
| # 410 |  | # COO- wagging |
| # - | # 148 | # COO- wagging |

Table 2 Nonlinear optical parameters measured in Z – scan experiment

| Parameters | n2×10-11 (m2/W) | β × 10-3 cm/W | Re(χ3) × 10-9 esu | Im (χ3) × 10-10 esu |  | (χ3) × 10-7 esu |
| --- | --- | --- | --- | --- | --- | --- |
| Measured values | 1.17102 | 0.362618 | 181.1103 | 710.095 | 2.7962 |  |

Table 3 Compositional analysis of BGLP single crystal

| Element | Weight % | Atomic% |
| --- | --- | --- |
| C | 21.08 | 27.44 |
| N | 21.46 | 21.195 |
| O | 41.139 | 42.41 |
| Cl | 11.198 | 6.17 |
| Ca | 0.09 | 0.03 |
| Total | 100 | 100 |

Table 4 Antibacterial Activities of BGLP

| Types of microorganism | Test organisms | Zone of inhibition in millimetre (diameter) |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | 25 µg/mL | 50 µg/mL | 100 µg/mL | Standard - Norfloxacin |
| Gram positive bacteria | Staphylococcus aureus | 10 | 11 | 12 | 18 |
| Gram negative bacteria | E. coli | 11 | 12 | 14 | 20 |