Supporting Information

Regulating local molecular polarization of triazine-PDI based polymer for high-efficient photocatalytic coupling of benzylamine

Rong Yana,#, Meiyang Songa,#,Peng Chena,*, Henghui Songa, Chengbing Fua,*, Haiyang Penga, Shuang-Feng Yinb,*

a Provincial Guizhou Key Laboratory of Green Chemical and Clean Energy Technology, School of Chemistry and Chemical Engineering, Guizhou University, Guiyang 550025, Guizhou, China

b College of Chemistry and Chemical Engineering, Advanced Catalytic Engineering Research Center of the Ministry of Education, State Key Laboratory of Chemo/Biosensing and Chemometrics, Hunan University, Changsha 410082, PR China

Email: pchen3@gzu.edu.cn (P. Chen), gs.songmy21@gzu.edu.cn (M. Song) sf_yin@hnu.edu.cn (S. F. Yin)

Table S1. Apparent quantum yield (AQY) of N-benzylidenebenzylamine formation over PDIMB-2.

| Wavelength (nm) | 420 | 450 | 500 | 550 | 600 | 700 | 750 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| N-benzylidenebenzylamine formation rate (mmol g-1h-1) | 13.67 | 11.07 | 8.61 | 8.20 | 6.84 | 2.42 | 0.40 |
| Light intensity (mW cm-2) | 21.04 | 17.02 | 19.92 | 20.08 | 25.22 | 8.51 | 3.05 |
| Irradiation area (cm2) | 8.04 | 8.04 | 8.04 | 8.04 | 8.04 | 8.04 | 8.04 |
| Irradiation time (h) | 2.00 | 2.00 | 2.00 | 2.00 | 2.00 | 2.00 | 2.00 |
| AQY (%) | 6.40 | 5.98 | 3.57 | 3.07 | 1.87 | 1.68 | 0.73 |

Table S2. Detailed comparison of PDIMB-2 with other photocatalysts.

| Catalysts | Reaction conditions | Sel. (%) | Generation rate (mmol g-1 h-1) | Ref |
| --- | --- | --- | --- | --- |
| PCN/Ag3PO4 | O2 (1 atm) 298 K | >99 | 2.48 | 1 |
| HUN-64 | O2 (1 atm) 298 K | >99 | 1.99 | 2 |
| BMO-NP | O2 (1 atm) 298 K | >99 | 0.30 | 3 |
| mpg-C3N4 | O2 (5 atm) 353 K | 99 | 3.00 | 4 |
| NST | O2 (1 atm) 298 K | 96.9 | 1.09 | 5 |
| Zn-PDI | O2 (1atm) 298K | >99 | 9.9 | 6 |
| PDIMB-2 | O2 (1atm) 298K | >99 | 24.5 | This work |

Table S3. Zeta potentials of as-prepared photocatalysts.

| Samples | 1 | 2 | 3 | 4 | 5 | 6 | Average |
| --- | --- | --- | --- | --- | --- | --- | --- |
| PDIM | -40.5 | -41.2 | -42.3 | -41.5 | -41.2 | -41.8 | -41.4 |
| PDIMB-1 | -49.5 | -49.2 | -49.0 | -49.9 | -50.2 | -49.5 | -49.6 |
| PDIMB-2 | -51.4 | -52.5 | -52.6 | -52.8 | -52.9 | -52.0 | -52.4 |
| PDIMB-3 | -46.7 | -46.8 | -46.9 | -46.5 | -46.2 | -46.3 | -46.6 |
| PDIMB-4 | -45.3 | -45.2 | -45.9 | -46.0 | -44.9 | -44.8 | -45.4 |
| PDIMB-5 | -42.3 | -42.5 | -43.5 | -42.9 | -43.0 | -43.2 | -42.9 |

Table S4. Fitting results of time-resolved photoluminescence spectra.

| Samples | A1 (%) | τ1 (ns) | A2 (%) | τ2 (ns) | A3 (%) | τ3 (ns) | τave (ns) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| PDIMB-2 | 47.62 | 0.20 | 30.38 | 1.59 | 22.00 | 5.32 | 4.01 |
| PDIM | 54.37 | 0.25 | 29.48 | 1.87 | 16.15 | 6.24 | 4.34 |

The τave can be calculated by the following equation:

τave=(A1τ12+A2τ22+A3τ32)/(A1τ1+A2τ2+A3τ3)

Table S5. Total Mulliken charge populations of PDIM and PDIMB.

|  | C (e) | N (e) | O (e) | H (e) | SUM |
| --- | --- | --- | --- | --- | --- |
| PDIM | 1.370 | -0.482 | -1.942 | 0.864 | -0.190 |
| PDIMB | 1.364 | -0.474 | -1.961 | 0.862 | -0.209 |

Fig. S1. SEM images of as-prepared samples.

Fig. S2. XRD pattern of as-prepared samples.

Fig. S3. FTIR spectra of as-prepared samples.

As shown in Fig. S3, the FT-IR spectrum of the synthesized polymers of PDIMB and PDIM are almost the same as that of PDI. Additionally, a peak of PDIM at 1618 cm-1 is the stretching of C=N, suggesting the triazine was successfully embedded in the PDIM.

Fig. S4. The corresponding Tauc plots of fabricated samples.

Fig. S5. Mott-Schottky curves of fabricated samples.

Fig. S6. Energy band structure of PDIM and PDIMB-X.

Fig. S7. The HOMO and LUMO orbitals of PDIM and PDIMB

Fig. S8. Projected density of states of PDIM and PDIMB.

Fig. S9. 1H NMR spectrum of benzylamine oxidation products.

Fig. S10. Photocatalytic selective oxidation of 4-chlorobenzylamine, 4-bromobenzylamine, 4-methylbenzylamine and 4-methoxybenzylamine over PDIMB-2.

Fig. S11. XRD pattern of PDIMB-2 before and after five cycles for photocatalytic selective oxidation of benzylamine.

# Fig. S12. Room temperature hysteresis loops of (a) PDIM, (b) PDIMB-2, (c) P–E loops of PDIM and PDIMB-2.

Fig. S13. Zeta potential of PDIM and PDIMB-X.

Fig. S14. TD-PL spectrum of (a) PDIM and (b) PDIMB-2.

Fig. S15. Mulliken charges of (a) PDIM and (b) PDIMB.

Fig. S16. Differential charge density of PDIM.

Fig. S17. Contact-angle of benzylamine on the surface of (a) PDIM and (b) PDIMB-2.

Fig. S18. O2-temperature programmed desorption spectra of PDIM and PDIMB-2.

Fig. S19. Photocatalytic selective oxidation of benzylamine over PDIMB-2 with or without a scavenger. (Ammonium oxalate (AO), potassium persulfate (KSO), p-benzoquinone (BQ) and tert-butanol (TBA) acted as scavengers for hole (h+), electron (e−), superoxide radical (O2•−) and hydroxyl radical (·OH) trapping, respectively.)

Fig. S20. Detection of H2O2 in reaction liquid.

(1)

(2)

(3)

Fig. S21. Proposed reaction progress of the photocatalytic oxidative coupling of benzylamine.

Fig. S22. DFT-calculated Gibbs free energy of selective amines oxidation.

Fig. S23. Differential charge diagram before and after adsorption of benzylamine of PDIMB and PDIM.

References

- W. Li, L. Qin, Z.-H. Wang, G.-C. Xu, H.-C. Zheng, L.-M. Zhou, Z.-Q. Chen, Efficient porous carbon nitride/Ag3PO4 photocatalyst for selective oxidation of amines to imines: Z-scheme heterojunction and interfacial adsorption. Colloids Surf A Physicochem Eng Asp 2022; 652: 129806.

- G. Che, W.-T. Yang, C. Wang, M.-L. Li, X.-Y. Li, Q.-H. Pan, Efficient photocatalytic oxidative coupling of benzylamine over uranyl–organic frameworks. Inorg Chem 2022; 61: 12301–12307.

- W. Phasayavan, M. Japa, S. Pornsuwan, D. Tantraviwat, F. Kielar, V.-B. Golovko, S. Jungsuttiwong, B. Inceesungvorn, Oxygen-deficient bismuth molybdate nanocatalysts: Synergistic effects in boosting photocatalytic oxidative coupling of benzylamine and mechanistic insight. J Colloid Interface Sci 2021; 581: 719–728.

- F.-Z. Su, S.-C. Mathew, L. Möhlmann, M. Antonietti, X.-C. Wang, S. Blechert, Aerobic oxidative coupling of amines by carbon nitride photocatalysis with visible light. Angew Chem Int Ed 2011; 50: 657–660.

- Y.-h. Ren, J.-H. Zou, K.-Q. Jing, Y.-Y. Liu, B.-B. Guo, Y.-J. Song, Y. Yu, L. Wu, Photocatalytic synthesis of N-benzyleneamine from benzylamine on ultrathin BiOCl nanosheets under visible light. J Catal 2019; 380: 123–131.

- L. Zeng, T. Liu, C. He, D.-Y. Shi, F.-L. Zhang, C.-Y. Duan, Organized aggregation makes insoluble perylene diimide efficient for the reduction of aryl halides via consecutive visible light-induced electron-transfer processes. J Am Chem Soc 2016; 138: 3958–3961.