S Table 1:

Analysis of equilibrium Cd (II) biosorption capacity of Candida tropicalis XTA1874 by Langmuir Isotherm before optimization

| Experiment No. | Ci (ppm) | Ce (ppm) | 1/Ce |  |  | qe(mg/g) | 1/qe |  | Equilibrium Biosorption capacity(%)(Ci-Ce)*100/Ci | Mean Equilibrium Biosorption capacity(%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 15 | 3.2 | 0.3125 |  |  | 7.866667 | 0.127119 |  | 78.66666667 |  |
| 2 | 45 | 10.8 | 0.092593 |  |  | 22.8 | 0.04386 |  | 76 |  |
| 3 | 55 | 11.16 | 0.089606 |  |  | 29.22667 | 0.034215 |  | 79.70909091 | 75.52596537 |
| 4 | 100 | 20.32 | 0.049213 |  |  | 53.12 | 0.018825 |  | 79.68 |  |
| 5 | 250 | 62.34 | 0.016041 |  |  | 125.1067 | 0.007993 |  | 75.064 |  |
| 6 | 300 | 109.23 | 0.009155 |  |  | 127.18 | 0.007863 |  | 63.59 |  |
| 7 | 500 | 120.14 | 0.008324 |  |  | 253.24 | 0.003949 |  | 75.972 |  |

S Table 2:

Linear plot for Langmuir Isotherm before optimization

| 1/Ce | 1/qe |  | Intercept | Slope | R2 | qmax (mg/g) | KL | RL |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0.3125 | 0.127119 |  | 0.0017 | 0.40165 | 0.995455 | 588.2450556 | 0.004232 | 0.940303 |
| 0.092593 | 0.04386 |  |  |  |  |  |  | 0.840011 |
| 0.089606 | 0.034215 |  |  |  |  |  |  | 0.811171 |
| 0.049213 | 0.018825 |  |  |  |  |  |  | 0.702619 |
| 0.016041 | 0.007993 |  |  |  |  |  |  | 0.485881 |
| 0.009155 | 0.007863 |  |  |  |  |  |  | 0.440579 |
| 0.008324 | 0.003949 |  |  |  |  |  |  | 0.3209 |

S Table 3:

Statistical analysis for the data obtain from Langmuir Adsorption Isotherm before optimization

| No of Observations | Removal (%) | Mean Removal (%) | SD | SEM | qmax (mg/g) | Mean Maximum Surface Adsorption (mg/g) | SD | SEM |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 75.972 | 75.9671 | 0.070761 | 0.028888 | 588.2353 | 588.4334 | 0.331157 | 0.135194 |
| 2 | 76.035 |  |  |  | 588.3251 |  |  |  |
| 3 | 75.9248 |  |  |  | 588.285 |  |  |  |
| 4 | 75.9236 |  |  |  | 588.3451 |  |  |  |
| 5 | 76.0648 |  |  |  | 589.105 |  |  |  |
| 6 | 75.8824 |  |  |  | 588.3051 |  |  |  |

S Table 4:

Analysis of equilibrium Cd(II) biosorption capacity of Candida tropicalis XTA1874 by Langmuir Isotherm after optimization

| Experiment No. | Ci (ppm) | Ce (ppm) | 1/Ce |  |  | qe(mg/g) | 1/qe |  | Equilibrium Biosorption capacity(%)(Ci-Ce)*100/Ci | Mean Equilibrium Biosorption capacity(%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 15 | 1.3 | 0.769231 |  |  | 9.133333 | 0.109489 |  | 91.33333 |  |
| 2 | 45 | 2.8 | 0.357143 |  |  | 28.13333 | 0.035545 |  | 93.77778 |  |
| 3 | 55 | 5.16 | 0.193798 |  |  | 33.22667 | 0.030096 |  | 90.61818 | 87.90028 |
| 4 | 100 | 10.32 | 0.096899 |  |  | 59.78667 | 0.016726 |  | 89.68 |  |
| 5 | 250 | 43.34 | 0.023073 |  |  | 137.7733 | 0.007258 |  | 82.664 |  |
| 6 | 300 | 86.23 | 0.011597 |  |  | 142.5133 | 0.007017 |  | 71.25667 |  |
| 7 | 500 | 20.14 | 0.049652 |  |  | 319.9067 | 0.003126 |  | 95.972 |  |

S Table 5:

Linear plot for Langmuir Isotherm after optimization

| 1/Ce | 1/qe | Intercept | Slope | R2 | qmax (mg/g) | KL | RL |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.769231 | 0.109489 | 1.18E-03 | 0.13389 | 0.96928 | 847.4576 | 0.008813 | 0.883238 |
| 0.357143 | 0.035545 |  |  |  |  |  | 0.716028 |
| 0.193798 | 0.030096 |  |  |  |  |  | 0.673525 |
| 0.096899 | 0.016726 |  |  |  |  |  | 0.531542 |
| 0.023073 | 0.007258 |  |  |  |  |  | 0.312178 |
| 0.011597 | 0.007017 |  |  |  |  |  | 0.274427 |
| 0.049652 | 0.003126 |  |  |  |  |  | 0.184959 |

S Table 6:

Statistical analysis for the data obtain from Langmuir Adsorption Isotherm after optimization

| No of Observations | Removal (%) | Mean Removal (%) | SD | SEM | qmax (mg/g) | Mean Maximum Surface Adsorption (mg/g) | SD | SEM |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Observation 1 | 95.972 | 95.96233 | 0.068916 | 0.028135 | 847.4576 | 0.028135 | 0.004698 | 0.008007 |
| Observation 2 | 95.974 |  |  |  | 847.4643 |  |  |  |
| Observation 3 | 95.98 |  |  |  | 847.4772 |  |  |  |
| Observation 4 | 95.976 |  |  |  | 847.4966 |  |  |  |
| Observation 5 | 95.832 |  |  |  | 847.4583 |  |  |  |
| Observation 6 | 96.04 |  |  |  | 847.5026 |  |  |  |

S Table 7:

Analysis of equilibrium Cd(II) biosorption capacity of Candida tropicalis XTA1874 by Freundlich Isotherm before optimization

| Experiment No. | Ci (ppm) | Ce (ppm) |  | logCe |  | qe(mg/g) |  | logqe | Equilibrium Biosorption capacity(%)(Ci-Ce)*100/Ci | Mean Equilibrium Biosorption capacity(%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 15 | 3.2 |  | 0.50515 |  | 7.866667 |  | 0.895791 | 78.66667 |  |
| 2 | 45 | 10.8 |  | 1.033424 |  | 22.8 |  | 1.357935 | 76 |  |
| 3 | 55 | 11.16 |  | 1.047664 |  | 29.22667 |  | 1.465779 | 79.70909 | 76.09739 |
| 4 | 100 | 20.32 |  | 1.307924 |  | 53.12 |  | 1.725258 | 79.68 |  |
| 5 | 250 | 62.34 |  | 1.794767 |  | 125.1067 |  | 2.09728 | 75.064 |  |
| 6 | 300 | 109.23 |  | 2.038342 |  | 127.18 |  | 2.104419 | 63.59 |  |
| 7 | 500 | 100.14 |  | 2.000608 |  | 266.5733 |  | 2.425817 | 79.972 |  |

S Table 8:

Linear plot for Freundlich Isotherm before optimization

| logCe | logqe | Intercept | Slope | 1/n | n | KF | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.50515 | 0.895791 | 0.48367 | 0.89296 | 0.89296 | 1.119871 | 3.04558 | 0.95455 |
| 1.033424 | 1.357935 |  |  |  |  |  |  |
| 1.047664 | 1.465779 |  |  |  |  |  |  |
| 1.307924 | 1.725258 |  |  |  |  |  |  |
| 1.794767 | 2.09728 |  |  |  |  |  |  |
| 2.038342 | 2.104419 |  |  |  |  |  |  |
| 2.000608 | 2.425817 |  |  |  |  |  |  |

S Table 9:

Statistical analysis for the data obtain from Freundlich Adsorption Isotherm before optimization

| No of Observation | KF | Mean | SD | SEM | n | Mean | SD | SEM |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 3.04558 | 3.09558 | 0.061644 | 0.025166 | 1.119871 | 1.12067 | 0.001245 | 0.000508 |
| 2 | 3.20558 |  |  |  | 1.121471 |  |  |  |
| 3 | 3.08558 |  |  |  | 1.122871 |  |  |  |
| 4 | 3.06558 |  |  |  | 1.119971 |  |  |  |
| 5 | 3.12558 |  |  |  | 1.119963 |  |  |  |
| 6 | 3.04558 |  |  |  | 1.119871 |  |  |  |

S Table 10:

Analysis of equilibrium Cd(II) biosorption capacity of Candida tropicalis XTA1874 by Freundlich Isotherm after optimization

| Experiment No. | Ci (ppm) | Ce (ppm) |  | logCe |  | qe(mg/g) |  | logqe | Equilibrium Biosorption capacity(%)(Ci-Ce)*100/Ci | Mean Equilibrium Biosorption capacity(%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 15 | 1.3 |  | 0.113943 |  | 9.133333 |  | 0.960629 | 91.33333 |  |
| 2 | 45 | 2.8 |  | 0.447158 |  | 28.13333 |  | 1.449221 | 93.77778 |  |
| 3 | 55 | 5.16 |  | 0.71265 |  | 33.22667 |  | 1.521487 | 90.61818 | 87.90028 |
| 4 | 100 | 10.32 |  | 1.01368 |  | 59.78667 |  | 1.776604 | 89.68 |  |
| 5 | 250 | 43.34 |  | 1.636889 |  | 137.7733 |  | 2.139165 | 82.664 |  |
| 6 | 300 | 86.23 |  | 1.935658 |  | 142.5133 |  | 2.153855 | 71.25667 |  |
| 7 | 500 | 20.14 |  | 1.304059 |  | 319.9067 |  | 2.505023 | 95.972 |  |

S Table 11:

Linear plot for Freundlich Isotherm after optimization

| logCe | logqe | Intercept | Slope | 1/n | n | KF | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.113943 | 0.960629 | 1.06984 | 0.70032 | 0.70032 | 1.427919 | 11.74465 | 0.75973 |
| 0.447158 | 1.449221 |  |  |  |  |  |  |
| 0.71265 | 1.521487 |  |  |  |  |  |  |
| 1.01368 | 1.776604 |  |  |  |  |  |  |
| 1.636889 | 2.139165 |  |  |  |  |  |  |
| 1.935658 | 2.153855 |  |  |  |  |  |  |
| 1.304059 | 2.505023 |  |  |  |  |  |  |

S Table 12:

Statistical analysis for the data obtain from Freundlich Adsorption Isotherm after optimization

| No of Observation | KF | Mean | SD | SEM | n | Mean | SD | SEM |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 11.74465 | 11.77248 | 0.024967 | 0.010193 | 1.427919 | 1.457797 | 0.036753 | 0.015005 |
| 2 | 11.75865 |  |  |  | 1.439919 |  |  |  |
| 3 | 11.78265 |  |  |  | 1.432919 |  |  |  |
| 4 | 11.74965 |  |  |  | 1.460187 |  |  |  |
| 5 | 11.80465 |  |  |  | 1.527919 |  |  |  |
| 6 | 11.79465 |  |  |  | 1.457919 |  |  |  |

S Table 13:

Analysis of Cd(II) biosorption kinetics by Pseudo First Order Kinetic Model before optimization using 100 ppm Cd(II)

| Experiment No. | Time (min) | Ci (ppm) | Ce (ppm) | qt (mg/g) |  | ln (qe-qt) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 0 | 0 | 0 | 0 |  | 0 |
| 2 | 40 | 100 | 25.26 | 49.82667 |  | 1.1919 |
| 3 | 60 | 100 | 24.56 | 50.29333 |  | 1.039098 |
| 4 | 80 | 100 | 23.43 | 51.04667 |  | 0.729158 |
| 5 | 100 | 100 | 22.37 | 51.75333 |  | 0.312375 |
| 6 | 150 | 100 | 21.28 | 52.48 |  | -0.44629 |
| 7 | 180 | 100 | 21.28 | 52.48 |  | -0.44629 |
| 8 | 200 | 100 | 21.28 | 52.48 |  | -0.44629 |
| 9 | 250 | 100 | 21.28 | 52.48 |  | -0.44629 |
| 10 | 280 | 100 | 21.28 | 52.48 |  | -0.44629 |
| 11 | 300 | 100 | 21.28 | 52.48 |  | -0.44629 |
| 12 | 350 | 100 | 21.28 | 52.48 |  | -0.44629 |
| 13 | 380 | 100 | 21.28 | 52.48 |  | -0.44629 |
| 14 | 400 | 100 | 21.28 | 52.48 |  | -0.44629 |
| 15 | 450 | 100 | 21.28 | 52.48 |  | -0.44629 |
| 16 | 480 | 100 | 21.28 | 52.48 |  | -0.44629 |
| 17 | 500 | 100 | 21.28 | 52.48 |  | -0.44629 |

S Table 14:

Linear plot of Pseudo First Order Kinetics Before optimization Using 100 ppm Cd(II)

| Time (min) | ln (qe-qt) | Intercept | Slope | qe(mg/g) | k1 | R2 |
| --- | --- | --- | --- | --- | --- | --- |
| 0 | 0 | 1.89883 | -0.01551 | 6.678077 | -0.0001 | 0.98893 |
| 40 | 1.1919 |  |  |  |  |  |
| 60 | 1.039098 |  |  |  |  |  |
| 80 | 0.729158 |  |  |  |  |  |
| 100 | 0.312375 |  |  |  |  |  |
| 150 | -0.44629 |  |  |  |  |  |

S Table 15:

Statistical analysis of Pseudo First Order Kinetics Before optimization Using 100 ppm Cd(II)

| Observation no | qe | Mean | SD | SEM | k1 | Mean | SD | SEM |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 6.678077 | 6.991768 | 1.050226 | 0.428753 | -0.0001 | -0.00012 | 2.27E-05 | 9.26E-06 |
| 2 | 6.917799 |  |  |  | -0.00012 |  |  |  |
| 3 | 6.519999 |  |  |  | -0.00014 |  |  |  |
| 4 | 6.917799 |  |  |  | -0.00016 |  |  |  |
| 5 | 8.999139 |  |  |  | -0.0001 |  |  |  |
| 6 | 5.917793 |  |  |  | -0.0001 |  |  |  |

S Table 16:

Analysis of Cd(II) biosorption kinetics by Pseudo First Order Kinetic Model before optimization using 250 ppm Cd(II)

| Experiment No. | Time (min) | Ci (ppm) | Ce (ppm) | qt (mg/g) |  | ln (qe-qt) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 0 | 0 | 0 | 0 |  | 0 |
| 2 | 40 | 250 | 65.35 | 123.1 |  | 0.696475 |
| 3 | 60 | 250 | 64.28 | 123.8133 |  | 0.257223 |
| 4 | 80 | 250 | 63.34 | 124.44 |  | -0.40547 |
| 5 | 100 | 250 | 62.57 | 124.9533 |  | -1.87514 |
| 6 | 150 | 250 | 62.42 | 125.0533 |  | -2.93119 |
| 7 | 180 | 250 | 62.42 | 125.0533 |  | -2.93119 |
| 8 | 200 | 250 | 62.42 | 125.0533 |  | -2.93119 |
| 9 | 250 | 250 | 62.42 | 125.0533 |  | -2.93119 |
| 10 | 280 | 250 | 62.42 | 125.0533 |  | -2.93119 |
| 11 | 300 | 250 | 62.42 | 125.0533 |  | -2.93119 |
| 12 | 350 | 250 | 62.42 | 125.0533 |  | -2.93119 |
| 13 | 380 | 250 | 62.42 | 125.0533 |  | -2.93119 |
| 14 | 400 | 250 | 62.42 | 125.0533 |  | -2.93119 |
| 15 | 450 | 250 | 62.42 | 125.0533 |  | -2.93119 |
| 16 | 480 | 250 | 62.42 | 125.0533 |  | -2.93119 |
| 17 | 500 | 250 | 62.42 | 125.0533 |  | -2.93119 |

S Table 17:

Linear plot of Pseudo First Order Kinetics Before optimization Using 250 ppm Cd(II)

| Time (min) | ln (qe-qt) | Intercept | Slope | qe(mg/g) | k1 | R2 |
| --- | --- | --- | --- | --- | --- | --- |
| 0 | 0 | 2.16975 | -0.03513 | 8.756095 | -0.00023 | 0.95549 |
| 40 | 0.696475 |  |  |  |  |  |
| 60 | 0.257223 |  |  |  |  |  |
| 80 | -0.40547 |  |  |  |  |  |
| 100 | -1.87514 |  |  |  |  |  |
| 150 | -2.93119 |  |  |  |  |  |

S Table 18:

Statistical analysis of Pseudo First Order Kinetics Before optimization Using 250 ppm Cd(II)

| Observation no | qe | Mean | SD | SEM | k1 | Mean | SD | SEM |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 8.756095 | 12.22295 | 4.767139 | 1.946176 | -0.00023 | -0.00028 | 2.82E-05 | 1.15E-05 |
| 2 | 5.917799 |  |  |  | -0.00028 |  |  |  |
| 3 | 10.7489 |  |  |  | -0.00032 |  |  |  |
| 4 | 12.99799 |  |  |  | -0.0003 |  |  |  |
| 5 | 15.99914 |  |  |  | -0.00028 |  |  |  |
| 6 | 18.91779 |  |  |  | -0.00028 |  |  |  |

S Table 19:

Analysis of Cd(II) biosorption kinetics by Pseudo First Order Kinetic Model before optimization using 300 ppm Cd(II)

| Experiment No. | Time (min) | Ci (ppm) | Ce (ppm) | qt (mg/g) |  | ln (qe-qt) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 0 | 0 | 0 | 0 |  | 0 |
| 2 | 40 | 300 | 112.46 | 125.0267 |  | 0.767017 |
| 3 | 60 | 300 | 111.27 | 125.82 |  | 0.307485 |
| 4 | 80 | 300 | 110.84 | 126.1067 |  | 0.070769 |
| 5 | 100 | 300 | 109.57 | 126.9533 |  | -1.48427 |
| 6 | 150 | 300 | 109.45 | 127.0333 |  | -1.91959 |
| 7 | 180 | 300 | 109.45 | 127.0333 |  | -1.91959 |
| 8 | 200 | 300 | 109.45 | 127.0333 |  | -1.91959 |
| 9 | 250 | 300 | 109.45 | 127.0333 |  | -1.91959 |
| 10 | 280 | 300 | 109.45 | 127.0333 |  | -1.91959 |
| 11 | 300 | 300 | 109.45 | 127.0333 |  | -1.91959 |
| 12 | 350 | 300 | 109.45 | 127.0333 |  | -1.91959 |
| 13 | 380 | 300 | 109.45 | 127.0333 |  | -1.91959 |
| 14 | 400 | 300 | 109.45 | 127.0333 |  | -1.91959 |
| 15 | 450 | 300 | 109.45 | 127.0333 |  | -1.91959 |
| 16 | 480 | 300 | 109.45 | 127.0333 |  | -1.91959 |
| 17 | 500 | 300 | 109.45 | 127.0333 |  | -1.91959 |

S Table 20:

Linear plot of Pseudo First Order Kinetics Before optimization Using 300 ppm Cd(II)

| Time (min) | ln (qe-qt) | Intercept | Slope | qe(mg/g) | k1 | R2 |
| --- | --- | --- | --- | --- | --- | --- |
| 0 | 0 | 1.81104 | -0.02631 | 6.116806 | -0.00018 | 0.88723 |
| 40 | 0.767017 |  |  |  |  |  |
| 60 | 0.307485 |  |  |  |  |  |
| 80 | 0.070769 |  |  |  |  |  |
| 100 | -1.48427 |  |  |  |  |  |
| 150 | -1.91959 |  |  |  |  |  |

S Table 21:

Statistical analysis of Pseudo First Order Kinetics Before optimization Using 300 ppm Cd(II)

| Observation no | qe | Mean | SD | SEM | k1 | Mean | SD | SEM |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 6.116806 | 5.1474 | 2.81834 | 1.150583 | -0.00018 | -0.00018 | 2.06E-06 | 8.42E-07 |
| 2 | 4.01978 |  |  |  | -0.00018 |  |  |  |
| 3 | 4.748899 |  |  |  | -0.00018 |  |  |  |
| 4 | 2.998955 |  |  |  | -0.00018 |  |  |  |
| 5 | 5.999999 |  |  |  | -0.00018 |  |  |  |
| 6 | 6.999961 |  |  |  | -0.00018 |  |  |  |

S Table 22:

Analysis of Cd(II) biosorption kinetics by Pseudo First Order Kinetic Model before optimization using500 ppm Cd(II)

| Experiment No. | Time (min) | Ci (ppm) | Ce (ppm) | qt (mg/g) |  | ln (qe-qt) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 0 | 0 | 0 | 0 |  | 0 |
| 2 | 40 | 500 | 123.26 | 251.16 |  | 0.732368 |
| 3 | 60 | 500 | 122.48 | 251.68 |  | 0.444686 |
| 4 | 80 | 500 | 121.35 | 252.4333 |  | -0.21484 |
| 5 | 100 | 500 | 120.53 | 252.98 |  | -1.34707 |
| 6 | 150 | 500 | 120.22 | 253.1867 |  | -2.93119 |
| 7 | 180 | 500 | 120.22 | 253.1867 |  | -2.93119 |
| 8 | 200 | 500 | 120.22 | 253.1867 |  | -2.93119 |
| 9 | 250 | 500 | 120.22 | 253.1867 |  | -2.93119 |
| 10 | 280 | 500 | 120.22 | 253.1867 |  | -2.93119 |
| 11 | 300 | 500 | 120.22 | 253.1867 |  | -2.93119 |
| 12 | 350 | 500 | 120.22 | 253.1867 |  | -2.93119 |
| 13 | 380 | 500 | 120.22 | 253.1867 |  | -2.93119 |
| 14 | 400 | 500 | 120.22 | 253.1867 |  | -2.93119 |
| 15 | 450 | 500 | 120.22 | 253.1867 |  | -2.93119 |
| 16 | 480 | 500 | 120.22 | 253.1867 |  | -2.93119 |
| 17 | 500 | 500 | 120.22 | 253.1867 |  | -2.93119 |

S Table 23:

Linear plot of Pseudo First Order Kinetics Before optimization Using 500 ppm Cd(II)

| Time (min) | ln (qe-qt) | Intercept | Slope | qe(mg/g) | k1 | R2 |
| --- | --- | --- | --- | --- | --- | --- |
| 0 | 0 | 2.36149 | -0.03517 | 10.60674 | -0.00023 | 0.97996 |
| 40 | 0.732368 |  |  |  |  |  |
| 60 | 0.444686 |  |  |  |  |  |
| 80 | -0.21484 |  |  |  |  |  |
| 100 | -1.34707 |  |  |  |  |  |
| 150 | -2.93119 |  |  |  |  |  |

S Table 24:

Statistical analysis of Pseudo First Order Kinetics Before optimization Using 500 ppm Cd(II)

| Observation no | qe | Mean | SD | SEM | k1 | Mean | SD | SEM |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 10.60674 | 14.43672 | 3.530067 | 1.441144 | -0.00023 | -0.00021 | 2.4E-05 | 9.79E-06 |
| 2 | 12.01978 |  |  |  | -0.00018 |  |  |  |
| 3 | 11.9949 |  |  |  | -0.00022 |  |  |  |
| 4 | 15.99895 |  |  |  | -0.00024 |  |  |  |
| 5 | 16 |  |  |  | -0.00019 |  |  |  |
| 6 | 19.99996 |  |  |  | -0.0002 |  |  |  |

S Table 25:

Analysis of Cd(II) biosorption kinetics by Pseudo Second Order Kinetic Model before optimization using 100 ppm Cd(II)

| Experiment No. | Time (min) | Ci (ppm) | Ce (ppm) | qt (mg/g) | t/qt |  |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 0 | 0 | 0 | 0 | 0 |  |
| 2 | 40 | 100 | 25.26 | 49.82667 | 0.802783 |  |
| 3 | 60 | 100 | 24.56 | 50.29333 | 1.193001 |  |
| 4 | 80 | 100 | 23.43 | 51.04667 | 1.567193 |  |
| 5 | 100 | 100 | 22.37 | 51.75333 | 1.932243 |  |
| 6 | 150 | 100 | 21.28 | 52.48 | 2.858232 |  |
| 7 | 180 | 100 | 21.28 | 52.48 | 3.429878 |  |
| 8 | 200 | 100 | 21.28 | 52.48 | 3.810976 |  |
| 9 | 250 | 100 | 21.28 | 52.48 | 4.76372 |  |
| 10 | 280 | 100 | 21.28 | 52.48 | 5.335366 |  |
| 11 | 300 | 100 | 21.28 | 52.48 | 5.716463 |  |
| 12 | 350 | 100 | 21.28 | 52.48 | 6.669207 |  |
| 13 | 380 | 100 | 21.28 | 52.48 | 7.240854 |  |
| 14 | 400 | 100 | 21.28 | 52.48 | 7.621951 |  |
| 15 | 450 | 100 | 21.28 | 52.48 | 8.574695 |  |
| 16 | 480 | 100 | 21.28 | 52.48 | 9.146341 |  |
| 17 | 500 | 100 | 21.28 | 52.48 | 9.527439 |  |

S Table 26:

Linear plot of Pseudo Second Order Kinetics Before optimization Using 100 ppm Cd(II)

| Time (min) | t/qt | Intercept | Slope | qe (mg/g) (cal) | qe2 | K2 | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0 | 0 | 0.03312 | 0.01897 | 52.71481 | 2778.851 | 0.010865 | 0.99998 |
| 40 | 0.324939 |  |  |  |  |  |  |
| 60 | 0.4846 |  |  |  |  |  |  |
| 80 | 0.64288 |  |  |  |  |  |  |
| 100 | 0.800299 |  |  |  |  |  |  |
| 150 | 1.199488 |  |  |  |  |  |  |
| 180 | 1.439386 |  |  |  |  |  |  |
| 200 | 1.599318 |  |  |  |  |  |  |
| 250 | 1.999147 |  |  |  |  |  |  |
| 280 | 2.239045 |  |  |  |  |  |  |
| 300 | 2.398976 |  |  |  |  |  |  |
| 350 | 2.798806 |  |  |  |  |  |  |
| 380 | 3.038703 |  |  |  |  |  |  |
| 400 | 3.198635 |  |  |  |  |  |  |
| 450 | 3.598465 |  |  |  |  |  |  |
| 480 | 3.838362 |  |  |  |  |  |  |
| 500 | 3.998294 |  |  |  |  |  |  |

S Table 27 :

Statistical analysis of Pseudo Second Order Kinetics Before optimization Using 100 ppm Cd(II)

| Observation no | qe | Mean | SD | SEM | k2 | Mean | SD | SEM |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 52.71481 | 53.06293 | 0.198789 | 0.081155 | 0.021938 | 0.021905 | 0.006998 | 0.002857 |
| 2 | 53.11498 |  |  |  | 0.022438 |  |  |  |
| 3 | 52.99813 |  |  |  | 0.019638 |  |  |  |
| 4 | 53.31481 |  |  |  | 0.026538 |  |  |  |
| 5 | 53.11001 |  |  |  | 0.021938 |  |  |  |
| 6 | 53.12481 |  |  |  | 0.018938 |  |  |  |

S Table 28:

Analysis of Cd(II) biosorption kinetics by Pseudo Second Order Kinetic Model before optimization using 250 ppm Cd(II)

| Experiment No. | Time (min) | Ci (ppm) | Ce (ppm) | qt (mg/g) | t/qt |
| --- | --- | --- | --- | --- | --- |
| 1 | 0 | 0 | 0 | 0 | 0 |
| 2 | 40 | 250 | 65.35 | 123.1 | 0.324939 |
| 3 | 60 | 250 | 64.28 | 123.8133 | 0.4846 |
| 4 | 80 | 250 | 63.34 | 124.44 | 0.64288 |
| 5 | 100 | 250 | 62.57 | 124.9533 | 0.800299 |
| 6 | 150 | 250 | 62.42 | 125.0533 | 1.199488 |
| 7 | 180 | 250 | 62.42 | 125.0533 | 1.439386 |
| 8 | 200 | 250 | 62.42 | 125.0533 | 1.599318 |
| 9 | 250 | 250 | 62.42 | 125.0533 | 1.999147 |
| 10 | 280 | 250 | 62.42 | 125.0533 | 2.239045 |
| 11 | 300 | 250 | 62.42 | 125.0533 | 2.398976 |
| 12 | 350 | 250 | 62.42 | 125.0533 | 2.798806 |
| 13 | 380 | 250 | 62.42 | 125.0533 | 3.038703 |
| 14 | 400 | 250 | 62.42 | 125.0533 | 3.198635 |
| 15 | 450 | 250 | 62.42 | 125.0533 | 3.598465 |
| 16 | 480 | 250 | 62.42 | 125.0533 | 3.838362 |
| 17 | 500 | 250 | 62.42 | 125.0533 | 3.998294 |

S Table 29:

Linear plot of Pseudo Second Order Kinetics Before optimization Using 250 ppm Cd(II)

| Time (min) | t/qt | Intercept | Slope | qe (mg/g) (cal) | qe2 | K2 | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0 | 0 | 0.00291 | 0.00799 | 125.1564 | 15664.14 | 0.021938 | 1 |
| 40 | 0.324939 |  |  |  |  |  |  |
| 60 | 0.4846 |  |  |  |  |  |  |
| 80 | 0.64288 |  |  |  |  |  |  |
| 100 | 0.800299 |  |  |  |  |  |  |
| 150 | 1.199488 |  |  |  |  |  |  |
| 180 | 1.439386 |  |  |  |  |  |  |
| 200 | 1.599318 |  |  |  |  |  |  |
| 250 | 1.999147 |  |  |  |  |  |  |
| 280 | 2.239045 |  |  |  |  |  |  |
| 300 | 2.398976 |  |  |  |  |  |  |
| 350 | 2.798806 |  |  |  |  |  |  |
| 380 | 3.038703 |  |  |  |  |  |  |
| 400 | 3.198635 |  |  |  |  |  |  |
| 450 | 3.598465 |  |  |  |  |  |  |
| 480 | 3.838362 |  |  |  |  |  |  |
| 500 | 3.998294 |  |  |  |  |  |  |

S Table 30 :

Statistical analysis of Pseudo Second Order Kinetics Before optimization Using 250ppm Cd(II)

| Observation no | qe | Mean | SD | SEM | k2 | Mean | SD | SEM |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 125.1564 | 125.1147 | 0.067495 | 0.027555 | 0.021938 | 0.021904859 | 0.002672 | 0.001091 |
| 2 | 125.2001 |  |  |  | 0.022438 |  |  |  |
| 3 | 125.1274 |  |  |  | 0.019638 |  |  |  |
| 4 | 125.1034 |  |  |  | 0.026538 |  |  |  |
| 5 | 124.9995 |  |  |  | 0.021938 |  |  |  |
| 6 | 125.1012 |  |  |  | 0.018938 |  |  |  |

S Table 31:

Analysis of Cd(II) biosorption kinetics by Pseudo Second Order Kinetic Model before optimization using 300 ppm Cd(II)

| Experiment No. | Time (min) | Ci (ppm) | Ce (ppm) | qt (mg/g) | t/qt |
| --- | --- | --- | --- | --- | --- |
| 1 | 0 | 0 | 0 | 0 | 0 |
| 2 | 40 | 300 | 112.46 | 125.0267 | 0.319932 |
| 3 | 60 | 300 | 111.27 | 125.82 | 0.476872 |
| 4 | 80 | 300 | 110.84 | 126.1067 | 0.634384 |
| 5 | 100 | 300 | 109.57 | 126.9533 | 0.787691 |
| 6 | 150 | 300 | 109.45 | 127.0333 | 1.180792 |
| 7 | 180 | 300 | 109.45 | 127.0333 | 1.416951 |
| 8 | 200 | 300 | 109.45 | 127.0333 | 1.57439 |
| 9 | 250 | 300 | 109.45 | 127.0333 | 1.967987 |
| 10 | 280 | 300 | 109.45 | 127.0333 | 2.204146 |
| 11 | 300 | 300 | 109.45 | 127.0333 | 2.361585 |
| 12 | 350 | 300 | 109.45 | 127.0333 | 2.755182 |
| 13 | 380 | 300 | 109.45 | 127.0333 | 2.991341 |
| 14 | 400 | 300 | 109.45 | 127.0333 | 3.14878 |
| 15 | 450 | 300 | 109.45 | 127.0333 | 3.542377 |
| 16 | 480 | 300 | 109.45 | 127.0333 | 3.778536 |
| 17 | 500 | 300 | 109.45 | 127.0333 | 3.935975 |

S Table 32:

Linear plot of Pseudo Second Order Kinetics Before optimization Using 300 ppm Cd(II)

| Time (min) | t/qt | Intercept | Slope | qe (mg/g) (cal) | qe2 | K2 | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0 | 0 | 0.00312 | 0.00786 | 127.2265 | 16186.57 | 0.019801 | 1 |
| 40 | 0.319932 |  |  |  |  |  |  |
| 60 | 0.476872 |  |  |  |  |  |  |
| 80 | 0.634384 |  |  |  |  |  |  |
| 100 | 0.787691 |  |  |  |  |  |  |
| 150 | 1.180792 |  |  |  |  |  |  |
| 180 | 1.416951 |  |  |  |  |  |  |
| 200 | 1.57439 |  |  |  |  |  |  |
| 250 | 1.967987 |  |  |  |  |  |  |
| 280 | 2.204146 |  |  |  |  |  |  |
| 300 | 2.361585 |  |  |  |  |  |  |
| 350 | 2.755182 |  |  |  |  |  |  |
| 380 | 2.991341 |  |  |  |  |  |  |
| 400 | 3.14878 |  |  |  |  |  |  |
| 450 | 3.542377 |  |  |  |  |  |  |
| 480 | 3.778536 |  |  |  |  |  |  |
| 500 | 3.935975 |  |  |  |  |  |  |

S Table 33 :

Statistical analysis of Pseudo Second Order Kinetics Before optimization Using 300 ppm Cd(II)

| Observation no | qe | Mean | SD | SEM | k2 | Mean | SD | SEM |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 127.2265 | 127.0333 | 1.59E-14 | 6.49E-15 | 0.019801 | 0.021467 | 0.002282 | 0.000932 |
| 2 | 127.197 |  |  |  | 0.024022 |  |  |  |
| 3 | 127.2376 |  |  |  | 0.023912 |  |  |  |
| 4 | 127.2265 |  |  |  | 0.019801 |  |  |  |
| 5 | 127.2265 |  |  |  | 0.019801 |  |  |  |
| 6 | 127.2265 |  |  |  |  |  |  |  |

S Table 34:

Analysis of Cd(II) biosorption kinetics by Pseudo Second Order Kinetic Model before optimization using 500 ppm Cd(II)

| Experiment No. | Time (min) | Ci (ppm) | Ce (ppm) | qt (mg/g) | t/qt |
| --- | --- | --- | --- | --- | --- |
| 1 | 0 | 0 | 0 | 0 | 0 |
| 2 | 40 | 500 | 123.26 | 251.16 | 0.159261 |
| 3 | 60 | 500 | 122.48 | 251.68 | 0.238398 |
| 4 | 80 | 500 | 121.35 | 252.433333 | 0.3169154 |
| 5 | 100 | 500 | 120.53 | 252.98 | 0.3952882 |
| 6 | 150 | 500 | 120.22 | 253.186667 | 0.5924483 |
| 7 | 180 | 500 | 120.22 | 253.186667 | 0.7109379 |
| 8 | 200 | 500 | 120.22 | 253.186667 | 0.789931 |
| 9 | 250 | 500 | 120.22 | 253.186667 | 0.9874138 |
| 10 | 280 | 500 | 120.22 | 253.186667 | 1.1059034 |
| 11 | 300 | 500 | 120.22 | 253.186667 | 1.1848965 |
| 12 | 350 | 500 | 120.22 | 253.186667 | 1.3823793 |
| 13 | 380 | 500 | 120.22 | 253.186667 | 1.5008689 |
| 14 | 400 | 500 | 120.22 | 253.186667 | 1.579862 |
| 15 | 450 | 500 | 120.22 | 253.186667 | 1.7773448 |
| 16 | 480 | 500 | 120.22 | 253.186667 | 1.8958344 |
| 17 | 500 | 500 | 120.22 | 253.186667 | 1.9748275 |

S Table 35 :

Linear plot of Pseudo Second Order Kinetics Before optimization Using 500 ppm Cd(II)

| Time (min) | t/qt | Intercept | Slope | qe (mg/g) (cal) | qe2 | K2 | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0 | 0 | 8.36E-04 | 0.00395 | 253.1646 | 64092.29 | 0.01866 | 1 |
| 40 | 0.159261 |  |  |  |  |  |  |
| 60 | 0.238398 |  |  |  |  |  |  |
| 80 | 0.316915 |  |  |  |  |  |  |
| 100 | 0.395288 |  |  |  |  |  |  |
| 150 | 0.592448 |  |  |  |  |  |  |
| 180 | 0.710938 |  |  |  |  |  |  |
| 200 | 0.789931 |  |  |  |  |  |  |
| 250 | 0.987414 |  |  |  |  |  |  |
| 280 | 1.105903 |  |  |  |  |  |  |
| 300 | 1.184897 |  |  |  |  |  |  |
| 350 | 1.382379 |  |  |  |  |  |  |
| 380 | 1.500869 |  |  |  |  |  |  |
| 400 | 1.579862 |  |  |  |  |  |  |
| 450 | 1.777345 |  |  |  |  |  |  |
| 480 | 1.895834 |  |  |  |  |  |  |
| 500 | 1.974828 |  |  |  |  |  |  |

S Table 36 :

Statistical analysis of Pseudo Second Order Kinetics Before optimization Using 500 ppm Cd(II)

| Observation no | qe | Mean | SD | SEM | k2 | Mean | SD | SEM |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 253.1646 | 253.0809 | 0.129383 | 0.05282 | 0.01866 | 0.019186 | 0.000847 | 0.000346 |
| 2 | 252.8669 |  |  |  | 0.018851 |  |  |  |
| 3 | 252.9769 |  |  |  | 0.018848 |  |  |  |
| 4 | 253.1866 |  |  |  | 0.01923 |  |  |  |
| 5 | 253.1634 |  |  |  | 0.020861 |  |  |  |
| 6 | 253.1269 |  |  |  | 0.018663 |  |  |  |

S Table 37:

Analysis of Cd(II) biosorption kinetics by Pseudo First Order Kinetic Model after optimization using 100 ppm Cd(II)

| Experiment No. | Time (min) | Ci (mg/g) | Ce (mg/g) | qt (mg/g) |  | ln (qe-qt) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 0 | 0 | 0 | 0 |  | 0 |
| 2 | 40 | 100 | 15.63 | 56.24667 |  | 1.264127 |
| 3 | 60 | 100 | 14.45 | 57.03333 |  | 1.012812 |
| 4 | 80 | 100 | 14.35 | 57.1 |  | 0.988301 |
| 5 | 100 | 100 | 14.28 | 57.14667 |  | 0.970779 |
| 6 | 150 | 100 | 14.23 | 57.18 |  | 0.958072 |
| 7 | 180 | 100 | 14.23 | 57.18 |  | 0.958072 |
| 8 | 200 | 100 | 14.23 | 57.18 |  | 0.958072 |
| 9 | 250 | 100 | 14.23 | 57.18 |  | 0.958072 |
| 10 | 280 | 100 | 14.23 | 57.18 |  | 0.958072 |
| 11 | 300 | 100 | 14.23 | 57.18 |  | 0.958072 |
| 12 | 350 | 100 | 14.23 | 57.18 |  | 0.958072 |
| 13 | 380 | 100 | 14.23 | 57.18 |  | 0.958072 |
| 14 | 400 | 100 | 14.23 | 57.18 |  | 0.958072 |
| 15 | 450 | 100 | 14.23 | 57.18 |  | 0.958072 |
| 16 | 480 | 100 | 14.23 | 57.18 |  | 0.958072 |
| 17 | 500 | 100 | 14.23 | 57.18 |  | 0.958072 |

S Table 38 :

Linear plot of Pseudo First Order Kinetics After optimization Using 100 ppm Cd(II)

| Time (min) | ln (qe-qt) | Intercept | Slope | qe(mg/g) | k1 | R2 |
| --- | --- | --- | --- | --- | --- | --- |
| 0 | 0 | 3.82871 | -0.02247 | 46.00316 | -0.00015 | 0.85282 |
| 40 | 3.264127 |  |  |  |  |  |
| 60 | 2.512812 |  |  |  |  |  |
| 80 | 1.888301 |  |  |  |  |  |
| 100 | 0.989879 |  |  |  |  |  |
| 150 | 0.828072 |  |  |  |  |  |

S Table 39:

Statistical analysis of Pseudo First Order Kinetics After optimization Using 100 ppm Cd(II)

| Observation no | qe | Mean | SD | SEM | k1 | Mean | SD | SEM |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 46.00316 | 56.24805 | 5.286257 | 2.158106 | -0.00015 | -0.00018 | 2.12E-05 | 8.64E-06 |
| 2 | 55.57329 |  |  |  | -0.00018 |  |  |  |
| 3 | 60.46217 |  |  |  | -0.0002 |  |  |  |
| 4 | 57.53782 |  |  |  | -0.00019 |  |  |  |
| 5 | 59.28898 |  |  |  | -0.00016 |  |  |  |
| 6 | 58.62289 |  |  |  | -0.0002 |  |  |  |

S Table 40:

Analysis of Cd(II) biosorption kinetics by Pseudo First Order Kinetic Model after optimization using 250 ppm Cd(II)

| Experiment No. | Time (min) | Ci (mg/g) | Ce (mg/g) | qt (mg/g) |  | ln (qe-qt) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 0 | 0 | 0 | 0 |  | 0 |
| 2 | 40 | 250 | 46.67 | 135.5533 |  | 0.797507 |
| 3 | 60 | 250 | 45.75 | 136.1667 |  | 0.474162 |
| 4 | 80 | 250 | 44.64 | 136.9067 |  | -0.1431 |
| 5 | 100 | 250 | 44.57 | 136.9533 |  | -0.19845 |
| 6 | 150 | 250 | 43.48 | 137.68 |  | -2.37158 |
| 7 | 180 | 250 | 43.48 | 137.68 |  | -2.37158 |
| 8 | 200 | 250 | 43.48 | 137.68 |  | -2.37158 |
| 9 | 250 | 250 | 43.48 | 137.68 |  | -2.37158 |
| 10 | 280 | 250 | 43.48 | 137.68 |  | -2.37158 |
| 11 | 300 | 250 | 43.48 | 137.68 |  | -2.37158 |
| 12 | 350 | 250 | 43.48 | 137.68 |  | -2.37158 |
| 13 | 380 | 250 | 43.48 | 137.68 |  | -2.37158 |
| 14 | 400 | 250 | 43.48 | 137.68 |  | -2.37158 |
| 15 | 450 | 250 | 43.48 | 137.68 |  | -2.37158 |
| 16 | 480 | 250 | 43.48 | 137.68 |  | -2.37158 |
| 17 | 500 | 250 | 43.48 | 137.68 |  | -2.37158 |

S Table 41 :

Linear plot of Pseudo First Order Kinetics After optimization Using 250 ppm Cd(II)

| Time (min) | ln (qe-qt) | Intercept | Slope | qe(mg/g) | k1 | R2 |
| --- | --- | --- | --- | --- | --- | --- |
| 0 | 0 | 2.16022 | -0.02847 | 8.673046 | -0.00019 | 0.94159 |
| 40 | 0.797507 |  |  |  |  |  |
| 60 | 0.474162 |  |  |  |  |  |
| 80 | -0.1431 |  |  |  |  |  |
| 100 | -0.19845 |  |  |  |  |  |
| 150 | -2.37158 |  |  |  |  |  |

S Table 42 :

Statistical analysis of Pseudo First Order Kinetics After optimization Using 250 ppm Cd(II)

| Observation no | qe | Mean | SD | SEM | k1 | Mean | SD | SEM |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 8.673046 | 9.290274 | 0.615514 | 0.251283 | -0.00019 | -0.00017 | 3.78E-05 | 1.54E-05 |
| 2 | 9.2864 |  |  |  | -0.0001 |  |  |  |
| 3 | 8.5621 |  |  |  | -0.00015 |  |  |  |
| 4 | 9.2546 |  |  |  | -0.00019 |  |  |  |
| 5 | 10.0894 |  |  |  | -0.00016 |  |  |  |
| 6 | 9.8761 |  |  |  | -0.0002 |  |  |  |

S Table 43:

Analysis of Cd(II) biosorption kinetics by Pseudo First Order Kinetic Model after optimization using 300 ppm Cd(II)

| Experiment No. | Time (min) | Ci (mg/g) | Ce (mg/g) | qt (mg/g) |  | ln (qe-qt) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 0 | 0 | 0 | 0 |  | 0 |
| 2 | 40 | 300 | 88.28 | 141.1467 |  | 0.312375 |
| 3 | 60 | 300 | 87.64 | 141.5733 |  | -0.06188 |
| 4 | 80 | 300 | 86.68 | 142.2133 |  | -1.20397 |
| 5 | 100 | 300 | 86.35 | 142.4333 |  | -2.52573 |
| 6 | 150 | 300 | 86.24 | 142.5067 |  | -5.01064 |
| 7 | 180 | 300 | 86.24 | 142.5067 |  | -5.01064 |
| 8 | 200 | 300 | 86.24 | 142.5067 |  | -5.01064 |
| 9 | 250 | 300 | 86.24 | 142.5067 |  | -5.01064 |
| 10 | 280 | 300 | 86.24 | 142.5067 |  | -5.01064 |
| 11 | 300 | 300 | 86.24 | 142.5067 |  | -5.01064 |
| 12 | 350 | 300 | 86.24 | 142.5067 |  | -5.01064 |
| 13 | 380 | 300 | 86.24 | 142.5067 |  | -5.01064 |
| 14 | 400 | 300 | 86.24 | 142.5067 |  | -5.01064 |
| 15 | 450 | 300 | 86.24 | 142.5067 |  | -5.01064 |
| 16 | 480 | 300 | 86.24 | 142.5067 |  | -5.01064 |
| 17 | 500 | 300 | 86.24 | 142.5067 |  | -5.01064 |

S Table 44 :

Linear plot of Pseudo First Order Kinetics After optimization Using 300 ppm Cd(II)

| Time (min) | ln (qe-qt) | Intercept | Slope | qe(mg/g) | k1 | R2 |
| --- | --- | --- | --- | --- | --- | --- |
| 0 | 0 | 2.6694 | -0.05078 | 14.43131 | -0.00034 | 0.98608 |
| 40 | 0.312375 |  |  |  |  |  |
| 60 | -0.06188 |  |  |  |  |  |
| 80 | -1.20397 |  |  |  |  |  |
| 100 | -2.52573 |  |  |  |  |  |
| 150 | -5.01064 |  |  |  |  |  |

S Table 45 :

Statistical analysis of Pseudo First Order Kinetics After optimization Using 300 ppm Cd(II)

| Observation no | qe | Mean | SD | SEM | k1 | Mean | SD | SEM |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 14.43131 | 15.47383 | 1.574082 | 0.642616 | -0.00034 | -0.00036 | 4.06E-05 | 1.66E-05 |
| 2 | 15.2894 |  |  |  | -0.00036 |  |  |  |
| 3 | 16.2622 |  |  |  | -0.00038 |  |  |  |
| 4 | 14.2846 |  |  |  | -0.00029 |  |  |  |
| 5 | 14.2994 |  |  |  | -0.00039 |  |  |  |
| 6 | 18.2761 |  |  |  | -0.0004 |  |  |  |

S Table 46:

Analysis of Cd(II) biosorption kinetics by Pseudo First Order Kinetic Model after optimization using 500 ppm Cd(II)

| Experiment No. | Time (min) | Ci (mg/g) | Ce (mg/g) | qt (mg/g) |  | ln (qe-qt) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 0 | 0 | 0 | 0 |  | 0 |
| 2 | 40 | 500 | 23.28 | 317.8133 |  | 0.738758 |
| 3 | 60 | 500 | 22.68 | 318.2133 |  | 0.526699 |
| 4 | 80 | 500 | 21.25 | 319.1667 |  | -0.30111 |
| 5 | 100 | 500 | 20.64 | 319.5733 |  | -1.09861 |
| 6 | 150 | 500 | 20.28 | 319.8133 |  | -2.37158 |
| 7 | 180 | 500 | 20.28 | 319.8133 |  | -2.37158 |
| 8 | 200 | 500 | 20.28 | 319.8133 |  | -2.37158 |
| 9 | 250 | 500 | 20.28 | 319.8133 |  | -2.37158 |
| 10 | 280 | 500 | 20.28 | 319.8133 |  | -2.37158 |
| 11 | 300 | 500 | 20.28 | 319.8133 |  | -2.37158 |
| 12 | 350 | 500 | 20.28 | 319.8133 |  | -2.37158 |
| 13 | 380 | 500 | 20.28 | 319.8133 |  | -2.37158 |
| 14 | 400 | 500 | 20.28 | 319.8133 |  | -2.37158 |
| 15 | 450 | 500 | 20.28 | 319.8133 |  | -2.37158 |
| 16 | 480 | 500 | 20.28 | 319.8133 |  | -2.37158 |
| 17 | 500 | 500 | 20.28 | 319.8133 |  | -2.37158 |

S Table 47 :

Linear plot of Pseudo First Order Kinetics After optimization Using 500 ppm Cd(II)

| Time (min) | ln (qe-qt) | Intercept | Slope | qe(mg/g) | k1 | R2 |
| --- | --- | --- | --- | --- | --- | --- |
| 0 | 0 | 2.07197 | -0.02992 | 7.94045 | -0.0002 | 0.98222 |
| 40 | 0.738758 |  |  |  |  |  |
| 60 | 0.526699 |  |  |  |  |  |
| 80 | -0.30111 |  |  |  |  |  |
| 100 | -1.09861 |  |  |  |  |  |
| 150 | -2.37158 |  |  |  |  |  |

S Table 48 :

Statistical analysis of Pseudo First Order Kinetics After optimization Using 500 ppm Cd(II)

| Observation no | qe | Mean | SD | SEM | k1 | Mean | SD | SEM |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 7.98085 | 13.74043 | 3.430697 | 1.400576 | -0.0002 | -0.00023 | 2.81E-05 | 1.15E-05 |
| 2 | 15.2894 |  |  |  | -0.00026 |  |  |  |
| 3 | 12.2982 |  |  |  | -0.00024 |  |  |  |
| 4 | 14.2986 |  |  |  | -0.00025 |  |  |  |
| 5 | 14.2994 |  |  |  | -0.00019 |  |  |  |
| 6 | 18.2761 |  |  |  | -0.00022 |  |  |  |

S Table 49:

Analysis of Cd(II) biosorption kinetics by Pseudo Second Order Kinetic Model after optimization using 100 ppm Cd(II)

| Experiment No. | Time (min) | Ci (mg/g) | Ce (mg/g) | qt (mg/g) | t/qt |  |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 0 | 0 | 0 | 0 | 0 |  |
| 2 | 40 | 100 | 15.63 | 56.24667 | 0.711153 |  |
| 3 | 60 | 100 | 14.45 | 57.03333 | 1.052016 |  |
| 4 | 80 | 100 | 14.35 | 57.1 | 1.401051 |  |
| 5 | 100 | 100 | 14.28 | 57.14667 | 1.749883 |  |
| 6 | 150 | 100 | 14.23 | 57.18 | 2.623295 |  |
| 7 | 180 | 100 | 14.23 | 57.18 | 3.147954 |  |
| 8 | 200 | 100 | 14.23 | 57.18 | 3.497726 |  |
| 9 | 250 | 100 | 14.23 | 57.18 | 4.372158 |  |
| 10 | 280 | 100 | 14.23 | 57.18 | 4.896817 |  |
| 11 | 300 | 100 | 14.23 | 57.18 | 5.24659 |  |
| 12 | 350 | 100 | 14.23 | 57.18 | 6.121021 |  |
| 13 | 380 | 100 | 14.23 | 57.18 | 6.64568 |  |
| 14 | 400 | 100 | 14.23 | 57.18 | 6.995453 |  |
| 15 | 450 | 100 | 14.23 | 57.18 | 7.869885 |  |
| 16 | 480 | 100 | 14.23 | 57.18 | 8.394544 |  |
| 17 | 500 | 100 | 14.23 | 57.18 | 8.744316 |  |

S Table 50 :

Linear plot of Pseudo Second Order Kinetics After optimization Using 100 ppm Cd(II)

| Time (min) | t/qt | Intercept | Slope | qe (mg/g) (cal) | qe2 | K2 | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0 | 0 | 0.00378 | 0.01748 | 57.20824 | 3272.782 | 0.080833 | 1 |
| 40 | 0.711153 |  |  |  |  |  |  |
| 60 | 1.052016 |  |  |  |  |  |  |
| 80 | 1.401051 |  |  |  |  |  |  |
| 100 | 1.749883 |  |  |  |  |  |  |
| 150 | 2.623295 |  |  |  |  |  |  |
| 180 | 3.147954 |  |  |  |  |  |  |
| 200 | 3.497726 |  |  |  |  |  |  |
| 250 | 4.372158 |  |  |  |  |  |  |
| 280 | 4.896817 |  |  |  |  |  |  |
| 300 | 5.24659 |  |  |  |  |  |  |
| 350 | 6.121021 |  |  |  |  |  |  |
| 380 | 6.64568 |  |  |  |  |  |  |
| 400 | 6.995453 |  |  |  |  |  |  |
| 450 | 7.869885 |  |  |  |  |  |  |
| 480 | 8.394544 |  |  |  |  |  |  |

S Table 51 :

Statistical analysis of Pseudo Second Order Kinetics After optimization Using 100 ppm Cd(II)

| Observation no | qe | Mean | S.D. | SEM | k2 | Mean | S.D. | SEM |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 57.20824 | 59.44014 | 1.106602 | 0.451768 | 0.080833 | 0.083153 | 0.002533 | 0.001034 |
| 2 | 60.02468 |  |  |  | 0.0825 |  |  |  |
| 3 | 59.6968 |  |  |  | 0.082 |  |  |  |
| 4 | 59.77725 |  |  |  | 0.08574 |  |  |  |
| 5 | 59.78634 |  |  |  | 0.081 |  |  |  |
| 6 | 60.14753 |  |  |  | 0.086842 |  |  |  |

S Table 52:

Analysis of Cd(II) biosorption kinetics by Pseudo Second Order Kinetic Model after optimization using 250 ppm Cd(II)

| Experiment No. | Time (min) | Ci (mg/g) | Ce (mg/g) | qt (mg/g) | t/qt |  |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 0 | 0 | 0 | 0 | 0 |  |
| 2 | 40 | 250 | 46.67 | 135.5533 | 0.295087 |  |
| 3 | 60 | 250 | 45.75 | 136.1667 | 0.440636 |  |
| 4 | 80 | 250 | 44.64 | 136.9067 | 0.58434 |  |
| 5 | 100 | 250 | 44.57 | 136.9533 | 0.730176 |  |
| 6 | 150 | 250 | 43.48 | 137.68 | 1.089483 |  |
| 7 | 180 | 250 | 43.48 | 137.68 | 1.307379 |  |
| 8 | 200 | 250 | 43.48 | 137.68 | 1.452644 |  |
| 9 | 250 | 250 | 43.48 | 137.68 | 1.815805 |  |
| 10 | 280 | 250 | 43.48 | 137.68 | 2.033701 |  |
| 11 | 300 | 250 | 43.48 | 137.68 | 2.178966 |  |
| 12 | 350 | 250 | 43.48 | 137.68 | 2.542127 |  |
| 13 | 380 | 250 | 43.48 | 137.68 | 2.760023 |  |
| 14 | 400 | 250 | 43.48 | 137.68 | 2.905288 |  |
| 15 | 450 | 250 | 43.48 | 137.68 | 3.268449 |  |
| 16 | 480 | 250 | 43.48 | 137.68 | 3.486345 |  |
| 17 | 500 | 250 | 43.48 | 137.68 | 3.63161 |  |

S Table 53 :

Linear plot of Pseudo Second Order Kinetics After optimization Using 250 ppm Cd(II)

| Time (min) | t/qt | Intercept | Slope | qe (mg/g) (cal) | qe2 | K2 | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0 | 0 | 0.00342 | 0.00725 | 137.931 | 19024.97 | 0.015369 | 1 |
| 40 | 0.295087 |  |  |  |  |  |  |
| 60 | 0.440636 |  |  |  |  |  |  |
| 80 | 0.58434 |  |  |  |  |  |  |
| 100 | 0.730176 |  |  |  |  |  |  |
| 150 | 1.089483 |  |  |  |  |  |  |
| 180 | 1.307379 |  |  |  |  |  |  |
| 200 | 1.452644 |  |  |  |  |  |  |
| 250 | 1.815805 |  |  |  |  |  |  |
| 280 | 2.033701 |  |  |  |  |  |  |
| 300 | 2.178966 |  |  |  |  |  |  |
| 350 | 2.542127 |  |  |  |  |  |  |
| 380 | 2.760023 |  |  |  |  |  |  |
| 400 | 2.905288 |  |  |  |  |  |  |
| 450 | 3.268449 |  |  |  |  |  |  |
| 480 | 3.486345 |  |  |  |  |  |  |
| 500 | 3.63161 |  |  |  |  |  |  |

S Table 54 :

Statistical analysis of Pseudo Second Order Kinetics After optimization Using 250 ppm Cd(II)

| Observation no | qe | Mean | SD | SEM | k2 | Mean | SD | SEM |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 137.931 | 137.8865 | 0.242782 | 0.099115 | 0.015369 | 0.037909 | 0.046398 | 0.018942 |
| 2 | 137.9674 |  |  |  | 0.0226 |  |  |  |
| 3 | 138.2943 |  |  |  | 0.018831 |  |  |  |
| 4 | 137.5793 |  |  |  | 0.132406 |  |  |  |
| 5 | 137.7738 |  |  |  | 0.022453 |  |  |  |
| 6 | 137.7732 |  |  |  | 0.015794 |  |  |  |

S Table 55:

Analysis of Cd(II) biosorption kinetics by Pseudo Second Order Kinetic Model after optimization using 300 ppm Cd(II)

| Experiment No. | Time (min) | Ci (mg/g) | Ce (mg/g) | qt (mg/g) | t/qt |
| --- | --- | --- | --- | --- | --- |
| 1 | 0 | 0 | 0 | 0 | 0 |
| 2 | 40 | 300 | 88.28 | 141.1467 | 0.283393 |
| 3 | 60 | 300 | 87.64 | 141.5733 | 0.423809 |
| 4 | 80 | 300 | 86.68 | 142.2133 | 0.562535 |
| 5 | 100 | 300 | 86.35 | 142.4333 | 0.702083 |
| 6 | 150 | 300 | 86.24 | 142.5067 | 1.052582 |
| 7 | 180 | 300 | 86.24 | 142.5067 | 1.263099 |
| 8 | 200 | 300 | 86.24 | 142.5067 | 1.403443 |
| 9 | 250 | 300 | 86.24 | 142.5067 | 1.754304 |
| 10 | 280 | 300 | 86.24 | 142.5067 | 1.96482 |
| 11 | 300 | 300 | 86.24 | 142.5067 | 2.105165 |
| 12 | 350 | 300 | 86.24 | 142.5067 | 2.456025 |
| 13 | 380 | 300 | 86.24 | 142.5067 | 2.666542 |
| 14 | 400 | 300 | 86.24 | 142.5067 | 2.806886 |
| 15 | 450 | 300 | 86.24 | 142.5067 | 3.157747 |
| 16 | 480 | 300 | 86.24 | 142.5067 | 3.368263 |
| 17 | 500 | 300 | 86.24 | 142.5067 | 3.508608 |

S Table 56 :

Linear plot of Pseudo Second Order Kinetics After optimization Using 300 ppm Cd(II)

| Time (min) | t/qt | Intercept | Slope | qe (mg/g) (cal) | qe2 | k2 | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0 | 0 | 1.50E-03 | 0.00701 | 142.6534 | 20349.98 | 0.03276 | 1 |
| 40 | 0.283393 |  |  |  |  |  |  |
| 60 | 0.423809 |  |  |  |  |  |  |
| 80 | 0.562535 |  |  |  |  |  |  |
| 100 | 0.702083 |  |  |  |  |  |  |
| 150 | 1.052582 |  |  |  |  |  |  |
| 180 | 1.263099 |  |  |  |  |  |  |
| 200 | 1.403443 |  |  |  |  |  |  |
| 250 | 1.754304 |  |  |  |  |  |  |
| 280 | 1.96482 |  |  |  |  |  |  |
| 300 | 2.105165 |  |  |  |  |  |  |
| 350 | 2.456025 |  |  |  |  |  |  |
| 380 | 2.666542 |  |  |  |  |  |  |
| 400 | 2.806886 |  |  |  |  |  |  |
| 450 | 3.157747 |  |  |  |  |  |  |
| 480 | 3.368263 |  |  |  |  |  |  |
| 500 | 3.508608 |  |  |  |  |  |  |

S Table 57 :

Statistical analysis of Pseudo Second Order Kinetics After optimization Using 300 ppm Cd(II)

| Observation no | qe | Mean | SD | SEM | k2 | Mean | SD | SEM |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 142.6534 | 142.5395 | 0.055934 | 0.022835 | 0.03276 | 0.036641 | 0.002974 | 0.001214 |
| 2 | 142.5183 |  |  |  | 0.0376 |  |  |  |
| 3 | 142.5246 |  |  |  | 0.034631 |  |  |  |
| 4 | 142.5133 |  |  |  | 0.035206 |  |  |  |
| 5 | 142.5139 |  |  |  | 0.038853 |  |  |  |
| 6 | 142.5136 |  |  |  | 0.040794 |  |  |  |

S Table 58:

Analysis of Cd(II) biosorption kinetics by Pseudo Second Order Kinetic Model after optimization using 500 ppm Cd(II)

| Experiment No. | Time (min) | Ci (ppm) | Ce (ppm) | qt (mg/g) | t/qt |
| --- | --- | --- | --- | --- | --- |
| 1 | 0 | 0 | 0 | 0 | 0 |
| 2 | 40 | 500 | 23.28 | 317.8133 | 0.12586 |
| 3 | 60 | 500 | 22.68 | 318.2133 | 0.188553 |
| 4 | 80 | 500 | 21.25 | 319.1667 | 0.250653 |
| 5 | 100 | 500 | 20.64 | 319.5733 | 0.312917 |
| 6 | 150 | 500 | 20.28 | 319.8133 | 0.469024 |
| 7 | 180 | 500 | 20.28 | 319.8133 | 0.562828 |
| 8 | 200 | 500 | 20.28 | 319.8133 | 0.625365 |
| 9 | 250 | 500 | 20.28 | 319.8133 | 0.781706 |
| 10 | 280 | 500 | 20.28 | 319.8133 | 0.875511 |
| 11 | 300 | 500 | 20.28 | 319.8133 | 0.938047 |
| 12 | 350 | 500 | 20.28 | 319.8133 | 1.094388 |
| 13 | 380 | 500 | 20.28 | 319.8133 | 1.188193 |
| 14 | 400 | 500 | 20.28 | 319.8133 | 1.25073 |
| 15 | 450 | 500 | 20.28 | 319.8133 | 1.407071 |
| 16 | 480 | 500 | 20.28 | 319.8133 | 1.500876 |
| 17 | 500 | 500 | 20.28 | 319.8133 | 1.563412 |

S Table 59 :

Linear plot of Pseudo Second Order Kinetics After optimization Using 500 ppm Cd(II)

| Time (min) | t/qt | Intercept | Slope | qe (mg/g) (cal) | qe2 | k2 | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0 | 0 | 5.22E-04 | 0.00313 | 319.4888 | 102073.1 | 0.018762 | 1 |
| 40 | 0.12586 |  |  |  |  |  |  |
| 60 | 0.188553 |  |  |  |  |  |  |
| 80 | 0.250653 |  |  |  |  |  |  |
| 100 | 0.312917 |  |  |  |  |  |  |
| 150 | 0.469024 |  |  |  |  |  |  |
| 180 | 0.562828 |  |  |  |  |  |  |
| 200 | 0.625365 |  |  |  |  |  |  |
| 250 | 0.781706 |  |  |  |  |  |  |
| 280 | 0.875511 |  |  |  |  |  |  |
| 300 | 0.938047 |  |  |  |  |  |  |
| 350 | 1.094388 |  |  |  |  |  |  |
| 380 | 1.188193 |  |  |  |  |  |  |
| 400 | 1.25073 |  |  |  |  |  |  |
| 450 | 1.407071 |  |  |  |  |  |  |
| 480 | 1.500876 |  |  |  |  |  |  |
| 500 | 1.563412 |  |  |  |  |  |  |

S Table 60 :

Statistical analysis of Pseudo Second Order Kinetics After optimization Using 500 ppm Cd(II)

| Observation no | qe | Mean | SD | SEM | k2 | Mean | SD | SEM |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 319.4888 | 319.8361 | 0.170161 | 0.069468 | 0.018762 | 0.074993 | 0.087399 | 0.035681 |
| 2 | 319.8996 |  |  |  | 0.018147 |  |  |  |
| 3 | 319.9065 |  |  |  | 0.018463 |  |  |  |
| 4 | 319.9105 |  |  |  | 0.018965 |  |  |  |
| 5 | 319.9065 |  |  |  | 0.189925 |  |  |  |
| 6 | 319.9046 |  |  |  | 0.185697 |  |  |  |

B

A

D

C

E

F

H

G

I

J

L

K

N

M

O

S Fig 1. Contour Plots For Surface Optimization of (A) Glucose concentration (%) (B) Urea concentration (%) (C) K2HPO4 concentration (%) (D) KH2PO4 concentration (%) (E) MgSO4.7H2O concentration (%) (F) KCl concentration (%) (G) CoCl2.6H2O concentration (%) (H) NH4VO2 concentration (%) (I) FeSO4.7H2O concentration (%) (J) Na2MoO4 concentration (%)  (K) CaCO3 concentration (%)  (L) ZnSO4.7H2O concentration (%) (M) MnSO4.7H2O concentration (%) (N) NiSO4.7H2O concentration (%) (O) Na2B4O7concentration (%)