Supplementary materials

A facile and straightforward immersion approach to enhance the hydrophobicity of melamine sponge for efficient cleanup of crude oils and organic solvents

Jiangwei Chen, Mingyang Hu, Yun Liu *

(Beijing Key Laboratory of Bioprocess, College of Life Science and Technology, Beijing University of Chemical Technology, Beijing 100029, China)

Table S1 Composition changes of biomass before and after extraction by tetrahydrofuran (Using corn stove and pine wood as examples)

| Biomass | Before extraction (%) |  |  | After extraction (%) |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Cellulose | Hemicellulose | Lignin | Cellulose | Hemicellulose | Lignin |
| corn stove | 46.60 | 21.16 | 23.59 | 49.75 | 21.73 | 20.57 |
| pine wood | 48.10 | 19.71 | 26.13 | 51.60 | 19.73 | 22.46 |

Table S2 Comparison of hydrophobicity of the modified MS sponge in our work with those reported in the literature

| Modified sponges adsorbent | Adsorption capacity (g. g-1) |  | Refs. |
| --- | --- | --- | --- |
|  | Crude oil | Organic solvent |  |
| Biomass extraction solution-modified MS sponge | 104 | 137 | In our work |
| Dopamine,Fe3O4, and FAS-17-modified PU | 17 | 35 | [1] |
| Fe3O4 and Actyflon-G502-modified PU | / | 87 | [2] |
| Methyltrichlorosilane-modified PU | 25 | 19 | [3] |
| Nanodiamonds, polydopamine, and PFDT-modified PU | / | 60 | [4] |
| Graphene and KH-570-modified PU | 39 | / | [5] |
| Eeduced graphene oxide, APTES, and TTEAI-modified PU | 46 | 35 | [6] |
| Carbon nanotube and PDMS-modified PU | 25 | 20 | [7] |
| Graphene-modified PU | 47.2 | 90 | [8] |
| Fe3O4 and TEHFDS-modified PU | 46.3 | / | [9] |
| HDPE and Fe3O4-modified PU | 40 | 52 | [10] |
| ZnO, Fe3O4 and stearic acid-modified PU | 108.9 | 60 | [11] |
| PDA and HMDS-modified PU | 53 | / | [12] |
| MoS2 and aromatic diazonium salts-modified PU | 50 | 90 | [13] |
| PDA, Ag nanoparticles, and dodecyl mercaptan-modified PU | 25 | 43 | [14] |
| 1,3-oxazolidine, 1,4-dioxane, stearoyl chloride, and NaHCO3-modified PU | 25.06 | 40.91 | [15] |
| HDTMS-lignin（HCl）-modified PU | 80 | 91 | [16] |
| MMDI-Alkali lignin-modified PU | 95 | 90 | [17] |
| PDMS-lignin –modified PU | 42.13 | 46.09 | [18] |
| Acetylation lignin (THF) -modified PU | 90 | 80 | [19] |
| Lignin (THF)-modified PU | 90 | 140 | [19] |
| Lignin-modified PU | 95 | 98 | [20] |
| Lignin-modified PU | 29.7 | 68.2 | [21] |
| Cellulose nanocrystals (CNC-H2SO4）-modified PU | 125 | 140 | [22] |
| Lignin-modified PU | 78 | 60 | [23] |
| Lignin-modified PU | 2 | 18 | {Yu, 2020 #15}[24] |

References

1. Liu, S., Xu, Q., Latthe, S.S., Gurav, A.B., Xing, R.: Superhydrophobic/ superoleophilic magnetic polyurethane sponge for oil/water separation. Rsc. Adv. 5, 68293-68298 (2015)

2. Liu, L., Lei, J., Li, L., Zhang, R., Mi, N., Chen, H., Huang, D., Li, N.: A facile method to fabricate the superhydrophobic magnetic sponge for oil-water separation. Mater. Lett. 195, 66-70 (2017)

3. Zhu, Q., Chu, Y., Wang, Z.N., Chen, L., Lin, F., Liu, Q.: Pan, Robust superhydrophobic polyurethane sponge as a highly reusable oil-absorption material. J Mater. Chem. A. 1, 17 (2013)

4. Cao, N., Yang, B., Barras, A., Szunerits, S., Boukherroub, R.: Polyurethane sponge functionalized with superhydrophobic nanodiamond particles for efficient oil/water separation. Chem. Eng. J. 307, 319-325 (2017)

5. Li, B., Liu, X., Zhang, X., Zou, J., Chai, W., Xu, J.: Oil-absorbent polyurethane sponge coated with KH-570-modified graphene. J. Appl. Polym. Sci. 132, 16 (2015)

6. Tjandra, R., Lui, G., Veilleux, A., Broughton, J., Chiu, G., Yu, A.: Introduction of an Enhanced Binding of Reduced Graphene Oxide to Polyurethane Sponge for Oil Absorption. Ind. Eng. Chem. Res. 54, 3657-3663 (2015)

7. Wang, C.F., Lin, S.J.: Robust superhydrophobic/superoleophilic sponge for effective continuous absorption and expulsion of oil pollutants from water. Acs. Appl. Mater. Inter. 5, 8861-4 (2013)

8. Zhang, L., Li, H., Lai, X., Su, X., Liang, T., Zeng. X.: Thiolated graphene-based superhydrophobic sponges for oil-water separation. Chem. Eng. J. 316, 736-743 (2017)

9. Li, Z.T., Lin, B., Jiang, L.W., Lin, E. C., Chen, J., Zhang, S.J., Tang, Y.W., He, F.A., Li, D.H.: Effective preparation of magnetic superhydrophobic Fe3O4/PU sponge for oil-water separation. Appl. Surf. Sci. 427, 56-64 (2018)

10. Reis-Dennis, S.: Review of Rethinking Health Care Ethics by Stephen Scher and Kasia Kozlowska. Monash Bioeth Rev. 38, 83-86 (2020)

11. Tran, V.T., Lee, B.K.: Novel fabrication of a robust superhydrophobic PU@ZnO@Fe(3)O(4)@SA sponge and its application in oil-water separations. Sci Rep. 7, 17520 (2017)

12. Liu, C., Fang, Y., Miao, X., Pei, Y., Yan, Y., Xiao, W., Wu, L.: Facile fabrication of superhydrophobic polyurethane sponge towards oil-water separation with exceptional flame-retardant performance. Sep. Purif. Technol 229, 115801 (2019)

13. Yu, T.L., Mathias, D., Lu, S.X., Xu, W.G., Naushad, M., Szunerits, S., Boukherroub, R.: Functionalized MoS2/polyurethane sponge: An efficient scavenger for oil in water. Sep. Purif. Technol 238, 116420 (2020)

14. Li, B., Li, L., Wu, L., Zhang, J., Wang, A.: Durable Superhydrophobic/ Superoleophilic Polyurethane Sponges Inspired by Mussel and Lotus Leaf for the Selective Removal of Organic Pollutants from Water. ChemPlusChem 79, 850-856 (2014)

15. Wang, G., Zeng, Z., Wu, X., Ren, T., Han, J., Xue. Q.: Three-dimensional structured sponge with high oil wettability for the clean-up of oil contaminations and separation of oil–water mixtures. Polym. Chem. 5, 5942-5948 (2014)

16. Sun, H., Liu, Z., Liu, K., Gibril, M.E., Kong, F., Wang, S.: Lignin-based superhydrophobic melamine resin sponges and their application in oil/water separation. Ind. Crop. Prod. 170, 113798 (2021)

17. Lei, Z., Deng, Y., Wang, C.: Ambient-temperature fabrication of melamine-based sponges coated with hydrophobic lignin shells by surface dip adsorbing for oil/water separation. Rsc. Adv. 6, 106928-106934 (2016)

18. Zhang, Y.Q., Jiang, Y.H., Qin, Y.N., An, Q.D., Xiao, L.P., Wang, Z.H., Xiao, Z.Y., Zhai, S.R.: Cooperative construction of oil/water separator using renewable lignin and PDMS. Colloid. Surface. A. 643, 128790 (2022)

19. Yu, H., Zhan, W., Liu, Y.: Engineering Lignin Nanoparticles Deposition on Melamine Sponge Skeleton for Absorbent and Flame Retardant Materials. Waste. Biomass. Valori. 11, 4561-4569 (2019)

20. Yang, Y., Yi, H., Wang, C.: Oil Absorbents Based on Melamine/Lignin by a Dip Adsorbing Method. Acs. Sustain. Chem. Eng. 3, 3012-3018 (2015)

21. Oribayo, O., Feng, X., Rempel, G.L., Pan Q.: Synthesis of lignin-based polyurethane/graphene oxide foam and its application as an absorbent for oil spill clean-ups and recovery. Chem. Eng. J. 323, 191-202 (2017)

22. Lei, Z., Zheng, P., Niu, L., Yang, Y., Shen, J., Zhang, W., Wang. C.: Ultralight, robustly compressible and super-hydrophobic biomass-decorated carbonaceous melamine sponge for oil/water separation with high oil retention. Appl. Surf. Sci. 489, 922-929 (2019)

23. Vannarath, A., Thalla, A.K.: Synthesis and characterisation of an ultra-light, hydrophobic and flame-retardant robust lignin-carbon foam for oil-water separation. J. Clean. Prod. 325, 129263 (2021)

24. Wu, J., Ma, X., Gnanasekar, P., Wang, F., Zhu, J., Yan, N., Chen, J.: Superhydrophobic lignin-based multifunctional polyurethane foam with SiO2 nanoparticles for efficient oil adsorption and separation. Sci. Total. Environ. 860, 160276 (2023)