Supplementary materials

- Table S1. Selected geometrical parameters for studied compounds

- Table S2. Geometry of the intermolecular contacts in 1 and 2 (in italics) in γ phase (Å, º)

- Table S3. Unit cell parameters in different temperatures

- Table S4. Isostructurality index calculated for analogues phases

- Table S5. The systematic analysis of reflection extinction in different temperatures also indicates some structural and symmetry changes.

- Table S7. Relevant crystallographic and refinement data

- Table S6. Kitaigorodskii packing index (%) calculated for more occupied position of disordered structures

- Figure S1. The crystal packing along [001] direction for compounds 1 (left) and 2 (right) at 100K (lower panel) and at room temperature (upper panel)

- Figure S2. Ewald representation along [001]for complexes 1 (top) and 2 (bottom) at different temperatures.

- Figure S3. The layers of crystal a) 1 and   b) 2 in temperatures close to the phase transition from phase 2 to phase 1

- Figure S4. a) The superposition of complex 1 molecules from different phases

- Figure S5 a),b) The superposition of complex 2 molecules from different phases (- black β-green - light blue from different views)  Orientation of disordered phenyl rings in c) , d) β e)  phases.

- Figure S6. Molecular overlay of the a) α, b) β c) γ phases of complexes 1 (green) and 2 (purple)

- Figure S7. Hirshfeld fingerplots of complex molecules in different phases.

- Figure S8. The unit cell similarity index and elongation vs. temperature [K]

- Figure S9.1. Theoretically generated powder pattern for complex 1:

- Figure S9.2. Theoretically generated powder pattern for complex 2.

- Figure S10. The powder X-Ray diffractogrmas collected for 130 K black, 240 K green, 290K blue one form complex 2

- Figure S11.  Selected fragment of the temperature PXRD patterns for compound 2 at four temperatures: red – first  measurement in the cycle, black -second measurement in the cycle.

- Figure S12.  Fragments of the temperature PXRD patterns for compound 2 at different temperatures

Table S1. Selected geometrical parameters for studied compounds

Complex 1

(α-phase)

Bi2—Cl4	2.8116 (19)	Bi1—Cl4	2.9234 (18)

Bi2—Cl3	2.8126 (17)	Bi1—Cl3	2.9337 (19)

Bi2—Cl6	2.6075 (18)	Bi1—Cl1	2.5575 (18)

Bi2—Cl5	2.5978 (19)	Bi1—Cl2	2.539 (2)

Bi2—S70	2.8527 (18)	Bi1—S30	2.827 (2)

Bi2—S50	2.8073 (18)	Bi1—S10	2.827 (2)

Cl4—Bi2—Cl3	95.33 (5)	Cl1—Bi1—Cl4	162.44 (6)

Cl4—Bi2—S70	69.86 (5)	Cl1—Bi1—Cl3	89.11 (6)

Cl3—Bi2—S70	85.81 (5)	Cl1—Bi1—S30	80.54 (6)

Cl6—Bi2—Cl4	88.00 (6)	Cl1—Bi1—S10	88.48 (6)

Cl6—Bi2—Cl3	168.12 (6)	Cl2—Bi1—Cl4	88.89 (6)

Cl6—Bi2—S70	106.02 (6)	Cl2—Bi1—Cl3	166.38 (6)

Cl6—Bi2—S50	96.62 (6)	Cl2—Bi1—Cl1	95.58 (7)

Cl5—Bi2—Cl4	167.05 (6)	Cl2—Bi1—S30	88.90 (6)

Cl5—Bi2—Cl3	88.99 (6)	Cl2—Bi1—S10	81.66 (6)

Cl5—Bi2—Cl6	90.24 (6)	S30—Bi1—Cl4	116.60 (5)

Cl5—Bi2—S70	98.38 (6)	S30—Bi1—Cl3	79.25 (6)

Cl5—Bi2—S50	104.67 (6)	S10—Bi1—Cl4	75.35 (5)

S50—Bi2—Cl4	88.28 (5)	S10—Bi1—Cl3	111.31 (6)

S50—Bi2—Cl3	72.14 (5)	S10—Bi1—S30	164.77 (6)

S50—Bi2—S70	147.47 (5)	Bi2—Cl4—Bi1	87.22 (5)

Cl4—Bi1—Cl3	90.44 (5)	Bi2—Cl3—Bi1	87.01 (5)

(β-phase)

Bi2—Cl2	2.853 (4)	Bi1—Cl2i	2.879 (4)

Bi2—Cl3	2.603 (8)	Bi1—Cl1i	2.565 (8)

Bi2—Cl3i	2.603 (8)	Bi1—Cl1	2.565 (8)

Bi2—Cl3Ai	2.560 (10)	Bi1—Cl1Ai	2.557 (10)

Bi2—Cl3A	2.560 (10)	Bi1—Cl1A	2.557 (10)

Bi2—S2i	2.797 (12)	Bi1—S1	2.829 (12)

Bi2—S2	2.797 (12)	Bi1—S1i	2.829 (12)

Bi2—S6	2.831 (13)	Bi1—S10i	2.838 (14)

Bi2—S6i	2.831 (13)	Bi1—S10	2.838 (14)

Bi1—Cl2	2.879 (4)

Cl2—Bi2—Cl2i	91.91 (18)	S6—Bi2—S6i	164.5 (10)

Cl3i—Bi2—Cl2i	90.1 (2)	Cl2i—Bi1—Cl2	90.87 (17)

Cl3—Bi2—Cl2i	165.61 (19)	Cl1i—Bi1—Cl2i	89.4 (2)

Cl3—Bi2—Cl2	90.1 (2)	Cl1—Bi1—Cl2	89.4 (2)

Cl3i—Bi2—Cl2	165.61 (19)	Cl1i—Bi1—Cl2	166.5 (2)

Cl3i—Bi2—Cl3	91.6 (4)	Cl1—Bi1—Cl2i	166.5 (2)

Cl3i—Bi2—S2	101.7 (4)	Cl1—Bi1—Cl1i	93.5 (4)

Cl3—Bi2—S2	96.4 (3)	Cl1—Bi1—S10i	84.2 (4)

Cl3i—Bi2—S2i	96.4 (3)	Cl1i—Bi1—S10	84.2 (4)

Cl3—Bi2—S2i	101.7 (4)	Cl1—Bi1—S10	85.6 (5)

Cl3Ai—Bi2—Cl2	165.5 (3)	Cl1i—Bi1—S10i	85.6 (5)

Cl3Ai—Bi2—Cl2i	90.1 (3)	Cl1Ai—Bi1—Cl2i	90.0 (3)

Cl3A—Bi2—Cl2	90.1 (3)	Cl1A—Bi1—Cl2i	167.1 (3)

Cl3A—Bi2—Cl2i	165.5 (3)	Cl1A—Bi1—Cl2	90.0 (3)

Cl3Ai—Bi2—Cl3A	91.5 (5)	Cl1Ai—Bi1—Cl2	167.1 (3)

Cl3A—Bi2—S6i	56.7 (4)	Cl1A—Bi1—Cl1Ai	92.1 (5)

Cl3A—Bi2—S6	111.1 (5)	S1i—Bi1—Cl2i	91.7 (3)

Cl3Ai—Bi2—S6	56.7 (4)	S1—Bi1—Cl2	91.7 (3)

Cl3Ai—Bi2—S6i	111.1 (5)	S1i—Bi1—Cl2	68.2 (3)

S2—Bi2—Cl2	92.3 (3)	S1—Bi1—Cl2i	68.2 (3)

S2i—Bi2—Cl2	69.3 (3)	S1—Bi1—S1i	151.9 (8)

S2—Bi2—Cl2i	69.3 (3)	S10i—Bi1—Cl2i	109.1 (4)

S2i—Bi2—Cl2i	92.3 (3)	S10—Bi1—Cl2	109.1 (4)

S2—Bi2—S2i	154.0 (8)	S10—Bi1—Cl2i	81.6 (5)

S6i—Bi2—Cl2	81.7 (4)	S10i—Bi1—Cl2	81.6 (5)

S6—Bi2—Cl2i	81.7 (4)	S10—Bi1—S10i	165.2 (10)

S6i—Bi2—Cl2i	109.4 (4)	Bi2—Cl2—Bi1	88.61 (10)

S6—Bi2—Cl2	109.4 (4)

Symmetry code(s): (i) −x, y, −z+1/2.

(δ -phase)

Bi1—Cl1i	2.571 (4)	Bi1—S1i	2.831 (8)

Bi1—Cl1	2.571 (4)	Bi1—S1A	2.827 (15)

Bi1—Cl2	2.868 (3)	Bi1—S1Ai	2.827 (15)

Bi1—Cl2ii	2.868 (3)	Cl2—Bi1iii	2.868 (3)

Bi1—S1	2.831 (8)

Cl1i—Bi1—Cl1	92.4 (2)	Cl2—Bi1—Cl2ii	90.89 (12)

Cl1i—Bi1—Cl2	89.98 (12)	S1i—Bi1—Cl2ii	93.0 (6)

Cl1i—Bi1—Cl2ii	166.30 (8)	S1i—Bi1—Cl2	69.6 (4)

Cl1—Bi1—Cl2	166.30 (8)	S1—Bi1—Cl2	93.0 (6)

Cl1—Bi1—Cl2ii	89.98 (12)	S1—Bi1—Cl2ii	69.6 (4)

Cl1—Bi1—S1i	96.7 (4)	S1—Bi1—S1i	155.7 (14)

Cl1—Bi1—S1	100.1 (6)	S1Ai—Bi1—Cl2ii	107.6 (10)

Cl1i—Bi1—S1i	100.1 (6)	S1A—Bi1—Cl2ii	79.8 (8)

Cl1i—Bi1—S1	96.7 (4)	S1A—Bi1—Cl2	107.6 (10)

Cl1i—Bi1—S1A	86.9 (7)	S1Ai—Bi1—Cl2	79.8 (8)

Cl1—Bi1—S1A	86.0 (10)	S1A—Bi1—S1Ai	170 (2)

Cl1i—Bi1—S1Ai	86.0 (10)	Bi1iii—Cl2—Bi1	89.11 (12)

Cl1—Bi1—S1Ai	86.9 (7)

Symmetry code(s):  (i) x, -y+3/2, -z+3/2; (ii) -x+1, y, -z+3/2; (iii) -x+1, -y+3/2, z.

(γ-phase)

Bi1—Cl1	2.863 (3)	Bi1—S10i	2.827 (6)

Bi1—Cl1i	2.863 (3)	Bi1—S10A	2.87 (2)

Bi1—Cl2	2.557 (3)	Bi1—S10Ai	2.87 (2)

Bi1—Cl2i	2.557 (3)	Cl1—Bi1ii	2.863 (3)

Bi1—S10	2.827 (6)

Cl1i—Bi1—Cl1	90.37 (12)	Cl2i—Bi1—S10i	97.50 (18)

Cl1i—Bi1—S10A	108.9 (4)	Cl2—Bi1—S10A	84.4 (4)

Cl1—Bi1—S10A	82.2 (4)	Cl2—Bi1—S10Ai	85.0 (4)

Cl1—Bi1—S10Ai	108.9 (4)	Cl2i—Bi1—S10A	85.0 (4)

Cl1i—Bi1—S10Ai	82.2 (4)	Cl2i—Bi1—S10Ai	84.4 (4)

Cl2—Bi1—Cl1	89.85 (11)	S10i—Bi1—Cl1i	70.93 (15)

Cl2i—Bi1—Cl1	166.61 (8)	S10—Bi1—Cl1	70.93 (15)

Cl2—Bi1—Cl1i	166.61 (8)	S10—Bi1—Cl1i	95.22 (16)

Cl2i—Bi1—Cl1i	89.85 (11)	S10i—Bi1—Cl1	95.22 (16)

Cl2—Bi1—Cl2i	93.0 (2)	S10—Bi1—S10i	160.7 (4)

Cl2—Bi1—S10	97.50 (18)	S10Ai—Bi1—S10A	164.7 (9)

Cl2i—Bi1—S10	95.72 (17)	Bi1ii—Cl1—Bi1	89.63 (12)

Cl2—Bi1—S10i	95.72 (17)

Symmetry code(s): (i) −x+1, y, −z+1/2; (ii) −x+1, −y+3/2, z.

Complex 2

(α-phase )

Bi1—Br1i	2.9753 (12)	Bi1—S30A	2.953 (15)

Bi1—Br1	3.0158 (12)	Bi1—S10	2.785 (6)

Bi1—Br2	2.7354 (13)	Bi1—S10A	2.928 (14)

Bi1—Br3	2.7118 (13)	Br1—Bi1i	2.9753 (12)

Bi1—S30	2.785 (6)

Br1i—Bi1—Br1	93.49 (3)	Br3—Bi1—S10A	87.9 (3)

Br2—Bi1—Br1	88.47 (4)	S30—Bi1—Br1i	71.81 (15)

Br2—Bi1—Br1i	168.19 (4)	S30—Bi1—Br1	93.72 (13)

Br2—Bi1—S30	96.45 (15)	S30—Bi1—S10	157.52 (19)

Br2—Bi1—S30A	89.8 (3)	S30A—Bi1—Br1	107.5 (3)

Br2—Bi1—S10	99.48 (13)	S30A—Bi1—Br1i	78.5 (3)

Br2—Bi1—S10A	83.8 (3)	S10—Bi1—Br1	71.07 (14)

Br3—Bi1—Br1i	89.45 (4)	S10—Bi1—Br1i	92.17 (14)

Br3—Bi1—Br1	166.67 (4)	S10A—Bi1—Br1i	108.0 (3)

Br3—Bi1—Br2	91.31 (4)	S10A—Bi1—Br1	78.8 (3)

Br3—Bi1—S30	99.55 (13)	S10A—Bi1—S30A	170.9 (4)

Br3—Bi1—S30A	85.8 (3)	Bi1i—Br1—Bi1	86.50 (3)

Br3—Bi1—S10	95.85 (14)

Symmetry code(s): (i) −x+1, y, −z+1/2.

(β-phase)

Bi2—Br2i	2.9746 (10)	Bi1—Br2i	3.0173 (10)

Bi2—Br2	2.9746 (10)	Bi1—Br2	3.0173 (10)

Bi2—Br3	2.7269 (10)	Bi1—Br1i	2.7065 (10)

Bi2—Br3i	2.7268 (10)	Bi1—Br1	2.7065 (10)

Bi2—S30i	2.818 (6)	Bi1—S10i	2.815 (4)

Bi2—S30	2.818 (6)	Bi1—S10	2.815 (4)

Bi2—S30A	2.94 (3)	Bi1—S10Ai	2.914 (15)

Bi2—S30Ai	2.94 (3)	Bi1—S10A	2.914 (15)

Br2i—Bi2—Br2	93.32 (4)	Br1i—Bi1—Br2	167.60 (3)

Br3—Bi2—Br2i	167.24 (3)	Br1i—Bi1—Br2i	89.15 (3)

Br3i—Bi2—Br2	167.24 (3)	Br1—Bi1—Br2	89.15 (3)

Br3—Bi2—Br2	89.04 (3)	Br1—Bi1—Br2i	167.60 (3)

Br3i—Bi2—Br2i	89.04 (3)	Br1i—Bi1—Br1	92.75 (5)

Br3i—Bi2—Br3	91.41 (5)	Br1—Bi1—S10i	95.99 (10)

Br3—Bi2—S30i	99.21 (12)	Br1—Bi1—S10	95.41 (10)

Br3—Bi2—S30	95.36 (14)	Br1i—Bi1—S10	95.99 (10)

Br3i—Bi2—S30i	95.36 (14)	Br1i—Bi1—S10i	95.41 (10)

Br3i—Bi2—S30	99.21 (12)	Br1i—Bi1—S10A	83.2 (3)

Br3i—Bi2—S30A	87.9 (5)	Br1i—Bi1—S10Ai	84.9 (3)

Br3—Bi2—S30A	88.5 (7)	Br1—Bi1—S10Ai	83.2 (3)

Br3—Bi2—S30Ai	87.9 (5)	Br1—Bi1—S10A	84.9 (3)

Br3i—Bi2—S30Ai	88.5 (7)	S10—Bi1—Br2	96.03 (10)

S30i—Bi2—Br2	71.99 (14)	S10i—Bi1—Br2	72.21 (10)

S30—Bi2—Br2	93.44 (12)	S10—Bi1—Br2i	72.21 (10)

S30—Bi2—Br2i	71.99 (14)	S10i—Bi1—Br2i	96.03 (10)

S30i—Bi2—Br2i	93.44 (12)	S10i—Bi1—S10	163.5 (2)

S30i—Bi2—S30	159.1 (3)	S10Ai—Bi1—Br2	83.1 (4)

S30Ai—Bi2—Br2	78.8 (7)	S10A—Bi1—Br2i	83.1 (4)

S30A—Bi2—Br2i	78.8 (7)	S10Ai—Bi1—Br2i	109.2 (3)

S30A—Bi2—Br2	104.9 (5)	S10A—Bi1—Br2	109.2 (3)

S30Ai—Bi2—Br2i	104.9 (5)	S10A—Bi1—S10Ai	162.8 (8)

S30Ai—Bi2—S30A	174.8 (13)	Bi2—Br2—Bi1	87.54 (2)

Br2i—Bi1—Br2	91.61 (4)

Symmetry code(s): (i) −x, y, −z+1/2.

(γ-phase)

Bi1—Br1	3.0018 (8)	Bi1—S10	2.841 (12)

Bi1—Br1i	3.0018 (8)	Bi1—S10Ai	2.84 (4)

Bi1—Br2i	2.7207 (10)	Bi1—S10A	2.84 (4)

Bi1—Br2	2.7207 (10)	Br1—Bi1ii	3.0018 (8)

Bi1—S10i	2.842 (12)

Br1—Bi1—Br1i	91.70 (3)	Br2i—Bi1—S10A	89.5 (8)

Br2i—Bi1—Br1i	89.49 (3)	S10—Bi1—Br1i	94.21 (16)

Br2—Bi1—Br1	89.49 (3)	S10i—Bi1—Br1	94.21 (16)

Br2—Bi1—Br1i	167.63 (2)	S10i—Bi1—Br1i	72.4 (2)

Br2i—Bi1—Br1	167.63 (2)	S10—Bi1—Br1	72.4 (2)

Br2—Bi1—Br2i	91.99 (5)	S10—Bi1—S10i	161.1 (4)

Br2—Bi1—S10i	95.2 (2)	S10A—Bi1—Br1i	104.4 (5)

Br2—Bi1—S10	97.89 (16)	S10Ai—Bi1—Br1	104.4 (5)

Br2i—Bi1—S10	95.2 (2)	S10Ai—Bi1—Br1i	78.2 (8)

Br2i—Bi1—S10i	97.89 (16)	S10A—Bi1—Br1	78.2 (8)

Br2—Bi1—S10A	87.9 (5)	S10Ai—Bi1—S10A	176.3 (12)

Br2i—Bi1—S10Ai	87.9 (5)	Bi1ii—Br1—Bi1	88.30 (3)

Br2—Bi1—S10Ai	89.5 (8)

Symmetry code(s): (i) −x+1, y, −z+1/2; (ii) −x+1, −y+3/2, z.

Table S2. Geometry of the intermolecular contacts in 1 and 2 (in italics) in γ phase (Å, º)

| D-H···A | D-H | D···A | H···A | < D-H···A | Symmetry codes for acceptor |
| --- | --- | --- | --- | --- | --- |
| N-H···Cl | 0.86 | 3.68(1) | 3.02 | 135 | ½+x,1-y,1/2-z |
| N-H···Br | 0.86 | 3.723(7) | 3.01 | 142 | ½+x,1-y,1/2-z |
| C-H···Cl | 0.97 | 3.78(2) | 2.86 | 157 | 3/2-x,1-y,z |
| C-H···Br | 0.97 | 3.86(1) | 2.96 | 155 | 3/2-x,1-y,z |
| C-H···S (1) | 0.93 | 3.85(1) | 3.07 | 143 | 3/2-x,y,1/2+z |
| C-H···S (2) | 0.93 | 3.97(1) | 3.19 | 142.5 | 3/2-x,y,1/2+z |

Table S3. Unit cell parameters in different temperatures

Complex 1

| T[K] | a [Å] |  | b[Å] |  | c[Å] |  | α[o] |  | β [o] |  | γ [o] |  | V [Å3] |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 100 | 14,79 | 16,49 |  | 23,30 |  | 90,00 |  | 94,46 |  | 90,00 |  | 5666,20 |  |
| 105 | 14,79 | 16,49 |  | 23,29 |  | 90,00 |  | 94,42 |  | 90,00 |  | 5664,05 |  |
| 110 | 14,80 | 16,49 |  | 23,29 |  | 90,00 |  | 94,41 |  | 90,00 |  | 5667,91 |  |
| 115 | 14,82 | 16,51 |  | 23,30 |  | 90,00 |  | 94,34 |  | 90,00 |  | 5684,80 |  |
| 120 | 14,82 | 16,52 |  | 23,30 |  | 90,00 |  | 94,29 |  | 90,00 |  | 5690,95 |  |
| 125 | 14,82 | 16,51 |  | 23,30 |  | 90,00 |  | 94,33 |  | 90,00 |  | 5685,66 |  |
| 130 | 14,83 | 16,51 |  | 23,30 |  | 90,00 |  | 94,26 |  | 90,00 |  | 5691,15 |  |
| 135 | 14,84 | 16,53 |  | 23,32 |  | 90,00 |  | 94,07 |  | 90,00 |  | 5703,34 |  |
| 140 | 14,85 | 16,55 |  | 23,30 |  | 90,00 |  | 93,95 |  | 90,00 |  | 5711,50 |  |
| 145 | 14,86 | 16,54 |  | 23,31 |  | 90,00 |  | 93,91 |  | 90,00 |  | 5714,49 |  |
| 150 | 14,86 | 16,55 |  | 23,30 |  | 90,00 |  | 93,77 |  | 90,00 |  | 5720,93 |  |
| 155 | 14,87 | 16,54 |  | 23,29 |  | 90,00 |  | 93,73 |  | 90,00 |  | 5714,99 |  |
| 160 | 14,87 | 16,54 |  | 23,29 |  | 90,00 |  | 93,63 |  | 90,00 |  | 5719,24 |  |
| 165 | 14,88 | 16,55 |  | 23,30 |  | 90,00 |  | 93,56 |  | 90,00 |  | 5726,99 |  |
| 170 | 14,89 | 16,56 |  | 23,30 |  | 90,00 |  | 93,46 |  | 90,00 |  | 5732,70 |  |
| 175 | 14,90 | 16,56 |  | 23,29 |  | 90,00 |  | 93,50 |  | 90,00 |  | 5737,69 |  |
| 180 | 14,90 | 16,57 |  | 23,30 |  | 90,00 |  | 93,50 |  | 90,00 |  | 5743,00 |  |
| 185 | 14,91 | 16,58 |  | 23,30 |  | 90,00 |  | 93,44 |  | 90,00 |  | 5747,00 |  |
| 190 | 14,93 | 16,58 |  | 23,31 |  | 90,00 |  | 93,30 |  | 90,00 |  | 5762,04 |  |
| 195 | 14,94 | 16,59 |  | 23,31 |  | 90,00 |  | 93,33 |  | 90,00 |  | 5768,76 |  |
| 200 | 14,95 | 16,59 |  | 23,32 |  | 90,00 |  | 93,31 |  | 90,00 |  | 5774,14 |  |
| 205 | 14,97 | 16,61 |  | 23,33 |  | 90,00 |  | 93,20 |  | 90,00 |  | 5788,89 |  |
| 210 | 14,98 | 16,62 |  | 23,33 |  | 90,00 |  | 93,16 |  | 90,00 |  | 5796,33 |  |
| 215 | 14,98 | 16,62 |  | 23,33 |  | 90,00 |  | 93,12 |  | 90,00 |  | 5798,29 |  |
| 220 | 14,99 | 16,62 |  | 23,33 |  | 90,00 |  | 92,97 |  | 90,00 |  | 5806,69 |  |
| 225 | 15,01 | 16,63 |  | 23,33 |  | 90,00 |  | 92,76 |  | 90,00 |  | 5816,06 |  |
| 230 | 15,02 | 16,63 |  | 23,33 |  | 90,00 |  | 92,51 |  | 90,00 |  | 5821,86 |  |
| 235 | 15,05 | 16,65 |  | 23,31 |  | 90,00 |  | 90,00 |  | 90,00 |  | 5840,00 |  |
| 240 | 15,06 | 16,66 |  | 23,32 |  | 90,00 |  | 90,00 |  | 90,00 |  | 5849,21 |  |
| 245 | 15,07 | 16,66 |  | 23,32 |  | 90,00 |  | 90,00 |  | 90,00 |  | 5855,01 |  |
| 250 | 15,08 | 16,66 |  | 23,32 |  | 90,00 |  | 90,00 |  | 90,00 |  | 5859,92 |  |
| 255 | 15,09 | 16,66 |  | 23,32 |  | 90,00 |  | 90,00 |  | 90,00 |  | 5864,92 |  |
| 260 | 15,10 | 16,67 |  | 23,33 |  | 90,00 |  | 90,00 |  | 90,00 |  | 5874,27 |  |
| 265 | 15,12 | 16,68 |  | 23,33 |  | 90,00 |  | 90,00 |  | 90,00 |  | 5883,85 |  |
| 270 | 15,13 | 16,68 |  | 23,34 |  | 90,00 |  | 90,00 |  | 90,00 |  | 5892,18 |  |
| 275 | 15,15 | 16,68 |  | 23,34 |  | 90,00 |  | 90,00 |  | 90,00 |  | 5897,62 |  |
| 280 | 15,16 | 16,69 |  | 23,34 |  | 90,00 |  | 90,00 |  | 90,00 |  | 5908,24 |  |
| 285 | 15,18 | 16,70 |  | 23,35 |  | 90,00 |  | 90,00 |  | 90,00 |  | 5921,10 |  |
| 290 | 15,20 | 16,71 |  | 23,36 |  | 90,00 |  | 90,00 |  | 90,00 |  | 5934,69 |  |
| 295 | 15,22 | 16,72 |  | 23,38 |  | 90,00 |  | 90,00 |  | 90,00 |  | 5950,28 |  |
| 300 | 15,24 | 16,73 |  | 23,38 |  | 90,00 |  | 90,00 |  | 90,00 |  | 5961,74 |  |

Complex 2

| T[K] | a [Å] | b[Å] | c[Å] | α[o] | β [o] | γ [o] | V [Å3] |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 100 | 15,15 | 16,95 | 23,47 | 89,99 | 92,88 | 89,95 | 6019,38 |
| 105 | 15,15 | 16,95 | 23,45 | 90,00 | 92,98 | 90,02 | 6010,38 |
| 110 | 15,19 | 17,00 | 23,52 | 89,99 | 92,94 | 89,94 | 6065,45 |
| 115 | 15,16 | 16,96 | 23,46 | 89,99 | 92,93 | 89,95 | 6023,90 |
| 120 | 15,20 | 17,00 | 23,51 | 90,01 | 92,90 | 90,05 | 6062,78 |
| 125 | 15,22 | 17,01 | 23,54 | 90,02 | 92,83 | 90,06 | 6086,14 |
| 130 | 15,23 | 17,02 | 23,53 | 90,02 | 92,85 | 90,07 | 6089,53 |
| 135 | 15,19 | 16,97 | 23,46 | 89,99 | 92,81 | 89,95 | 6038,53 |
| 140 | 15,20 | 16,98 | 23,46 | 89,97 | 92,76 | 89,94 | 6045,69 |
| 145 | 15,22 | 17,00 | 23,51 | 89,98 | 92,69 | 89,93 | 6076,38 |
| 150 | 15,22 | 17,00 | 23,50 | 89,97 | 92,63 | 89,93 | 6076,49 |
| 155 | 15,21 | 16,98 | 23,48 | 90,02 | 92,64 | 90,06 | 6058,09 |
| 160 | 15,23 | 16,98 | 23,47 | 89,97 | 92,58 | 89,90 | 6064,23 |
| 165 | 15,27 | 16,95 | 23,48 | 90,01 | 92,50 | 90,01 | 6067,13 |
| 170 | 15,26 | 16,93 | 23,45 | 89,99 | 92,49 | 89,94 | 6053,46 |
| 175 | 15,33 | 17,01 | 23,53 | 90,05 | 92,42 | 90,08 | 6129,31 |
| 180 | 15,32 | 17,07 | 23,46 | 89,91 | 89,98 | 89,88 | 6133,04 |
| 185 | 15,31 | 17,10 | 23,45 | 89,94 | 89,97 | 89,87 | 6136,28 |
| 190 | 15,33 | 17,12 | 23,47 | 89,94 | 89,98 | 89,89 | 6158,88 |
| 195 | 15,32 | 17,11 | 23,44 | 89,97 | 89,95 | 89,90 | 6143,36 |
| 200 | 15,35 | 17,13 | 23,48 | 90,07 | 90,03 | 90,08 | 6173,54 |
| 205 | 15,34 | 17,13 | 23,45 | 89,97 | 89,98 | 89,89 | 6163,14 |
| 210 | 15,38 | 17,16 | 23,50 | 90,07 | 90,03 | 90,11 | 6200,25 |
| 215 | 15,38 | 17,15 | 23,47 | 89,97 | 90,00 | 89,89 | 6189,61 |
| 220 | 15,38 | 17,15 | 23,46 | 90,02 | 90,00 | 90,10 | 6188,39 |
| 225 | 15,39 | 17,15 | 23,48 | 90,02 | 90,01 | 90,10 | 6195,78 |
| 230 | 15,41 | 17,17 | 23,48 | 89,96 | 89,99 | 89,87 | 6213,88 |
| 235 | 15,43 | 17,19 | 23,50 | 89,97 | 89,98 | 89,88 | 6232,64 |
| 240 | 15,43 | 17,18 | 23,50 | 89,98 | 89,98 | 89,88 | 6229,66 |
| 245 | 15,43 | 17,18 | 23,49 | 90,00 | 90,03 | 90,12 | 6230,05 |
| 250 | 15,45 | 17,19 | 23,51 | 89,99 | 89,97 | 89,89 | 6245,61 |
| 255 | 15,46 | 17,19 | 23,51 | 90,03 | 90,01 | 90,11 | 6247,04 |
| 260 | 15,46 | 17,18 | 23,50 | 90,05 | 90,02 | 90,12 | 6244,73 |
| 265 | 15,48 | 17,19 | 23,51 | 89,95 | 90,00 | 89,84 | 6259,14 |
| 270 | 15,48 | 17,19 | 23,50 | 90,06 | 90,00 | 90,14 | 6254,42 |
| 275 | 15,49 | 17,20 | 23,52 | 90,02 | 90,01 | 90,11 | 6266,03 |
| 280 | 15,51 | 17,20 | 23,52 | 90,05 | 90,01 | 90,15 | 6272,01 |
| 285 | 15,52 | 17,21 | 23,52 | 90,02 | 90,04 | 90,13 | 6282,00 |
| 290 | 15,54 | 17,21 | 23,53 | 89,95 | 90,00 | 89,85 | 6293,53 |
| 295 | 15,54 | 17,22 | 23,54 | 89,99 | 89,98 | 89,89 | 6298,98 |
| 300 | 15,55 | 17,22 | 23,58 | 90,00 | 90,09 | 90,08 | 6316,49 |
| 305 | 15,55 | 17,22 | 23,57 | 90,09 | 90,03 | 90,05 | 6308,95 |
| 310 | 15,55 | 17,20 | 23,56 | 90,13 | 90,03 | 90,04 | 6302,79 |
| 295 | 15,54 | 17,22 | 23,54 | 89,99 | 89,98 | 89,89 | 6298,98 |
| 300 | 15,55 | 17,22 | 23,58 | 90,00 | 90,09 | 90,08 | 6316,49 |
| 305 | 15,55 | 17,22 | 23,57 | 90,09 | 90,03 | 90,05 | 6308,95 |
| 310 | 15,55 | 17,20 | 23,56 | 90,13 | 90,03 | 90,04 | 6302,79 |

Table S4. Isostructurality index calculated for analogues phases

| Phases |  | Isostructural index % |
| --- | --- | --- |
| γ-γ |  | 99,30 |
| δ-γ |  | 99,29 |
| β-β |  | 98,77 |
| α-α |  | 97,69 / 97,38 |

Table S5. The systematic analysis of reflection extinction in different temperatures also indicates some structural and symmetry changes.

|  |  | Hkl | R.condition/temperature | 100 | 190 | 220 | 230 | 240 | 298 | 303 | 333 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| C1 | b¦x | 0kl | k=2n+1 | 2.6 | 2.7 | 2.0 | 2.4 | 1.9 | 1.1 | 0.5 | 0.5 |
|  | c¦x | 0kl | l=2n+1 | 3.2 | 3.1 | 2.1 | 2.6 | 0.7 | 0.6 | 1.1 | 0.5 |
|  | n¦x | 0kl | k+l=2n+1 | 3.1 | 3.4 | 2.4 | 3.0 | 2.0 | 1.1 | 1.1 | 0.5 |
|  | a¦y | h0l | h=2n+1 | 2.1 | 2.5 | 1.8 | 2.0 | 3.1 | 1.6 | 1.5 | 0.8 |
|  | c¦y | h0l | l=2n+1 | 4.5 | 3.5 | 2.1 | 2.4 | 7.5 | 1.5 | 2.0 | 0.9 |
|  | n¦y | h0l | h+l=2n+1 | 5.8 | 4.5 | 3.0 | 3.4 | 7.7 | 2.7 | 3.1 | 0.5 |
|  | a¦z | hk0 | h=2n+1 | 3.6 | 4.6 | 4.0 | 4.6 | 7.5 | 2.8 | 2.9 | 0.4 |
|  | b¦z | hk0 | k=2n+1 | 3.3 | 3.4 | 3.0 | 3.6 | 6.8 | 1.4 | 1.8 | 1.0 |
|  | n¦z | hk0 | h+k=2n+1 | 3.0 | 2.9 | 2.3 | 2.6 | 3.4 | 2.1 | 1.9 | 1.0 |
|  | A | hkl | k+l=2n+1 | 4.3 | 4.0 | 2.9 | 3.4 | 6.5 | 2.5 | 2.8 | 1.5 |
|  | B | hkl | h+l=2n+1 | 4.4 | 4.3 | 3.1 | 3.7 | 6.3 | 2.8 | 3.1 | 1.5 |
|  | C | hkl | h+k=2n+1 | 2.6 | 2.5 | 1.9 | 2.2 | 2.8 | 1.6 | 1.4 | 0.4 |
|  | I | hkl | h+k+l=2n+1 | 6.5 | 6.5 | 4.8 | 5.5 | 7.5 | 5.9 | 6.2 | 3.7 |
|  | F | hkl | t all od | 3.8 | 3.6 | 2.6 | 3.1 | 5.2 | 2.3 | 2.4 | 1.1 |
|  |  | hkl | R.condition/temperature | 100 | 170 | 190 | 240 | 260 | 298 | 303 | 333 |
| 2 | b¦x | 0kl | k=2n+1 | 2.0 | 2.0 | 0.6 | 0.5 | 0.5 | 0.5 | 0.6 | 0.6 |
|  | c¦x | 0kl | l=2n+1 | 2.3 | 1.7 | 0.6 | 0.5 | 0.5 | 0.5 | 0.5 | 0.6 |
|  | n¦x | 0kl | k+l=2n+1 | 3.0 | 2.5 | 0.6 | 0.5 | 0.5 | 0.5 | 0.5 | 0.6 |
|  | a¦y | h0l | h=2n+1 | 1.2 | 1.3 | 0.4 | 0.4 | 0.4 | 0.4 | 0.4 | 0.4 |
|  | c¦y | h0l | l=2n+1 | 1.5 | 1.9 | 3.4 | 2.2 | 0.8 | 0.6 | 0.5 | 0.5 |
|  | n¦y | h0l | h+l=2n+1 | 2.1 | 2.1 | 3.4 | 2.3 | 0.8 | 0.6 | 0.5 | 0.5 |
|  | a¦z | hk0 | h=2n+1 | 2.5 | 2.3 | 3.0 | 2.0 | 0.7 | 0.6 | 0.6 | 0.6 |
|  | b¦z | hk0 | k=2n+1 | 2.7 | 2.6 | 3.1 | 2.1 | 0.8 | 0.6 | 0.5 | 0.6 |
|  | n¦z | hk0 | h+k=2n+1 | 1.0 | 1.2 | 0.5 | 0.4 | 0.4 | 0.5 | 0.5 | 0.5 |
|  | A | hkl | k+l=2n+1 | 2.3 | 2.2 | 2.7 | 2.1 | 1.3 | 1.2 | 1.3 | 1.3 |
|  | B | hkl | h+l=2n+1 | 2.4 | 2.2 | 2.7 | 2.1 | 1.3 | 1.2 | 1.3 | 1.3 |
|  | C | hkl | h+k=2n+1 | 1.4 | 1.3 | 0.4 | 0.4 | 0.4 | 0.4 | 0.4 | 0.4 |
|  | I | hkl | h+k+l=2n+1 | 3.0 | 2.8 | 2.9 | 2.6 | 2.3 | 2.2 | 2.4 | 2.3 |
|  | F | hkl | t all od | 2.0 | 1.9 | 1.9 | 1.5 | 1.0 | 1.0 | 1.0 | 1.0 |

Table S6. Kitaigorodskii packing index (%) calculated for more occupied position of disordered structures

|  | α | β | γ | δ |
| --- | --- | --- | --- | --- |
| 1 | 68,3 | 65,9 | 64,9 | 64,0 |
| 2 | 66,0 | 64,4 | 63,5 | - |

Table S7. Relevant crystallographic and refinement data

|  | Complex 1 |  |  |  | Complex 2 |  |  | Solid solution |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Name | phase | phase | phase | phase | phase | phase | phase | Lt phase |
| Chemical formula | C44H60Bi2Cl6N12S4 |  |  |  | C44H60Bi2Br6N12S4 |  |  | C44H60Bi2Br1.68Cl4.32N12S4 |
| Mr | 1515.94 |  |  |  | 1682.70 |  |  | 1708.90 |
| Crystal system, space group | Monoclinic P21/c | Monoclinic C2/c | Orthorhombic Ccce | Orthorhombic Ccce | Monoclinic C2/c | Monoclinic C2/c | Orthorhombic Ccce | Monoclinic C2/c |
| Temperature (K) | 100(1) | 250(1) | 298(1) | 333(1) | 100 (1) | 200 (1) | 293(2) | 100(1) |
| a, b, c (Å) | 14.8035 (4) 16.5246 (5) 23.2996 (7) | 6.6914(4) 15.0827(4) 23.3076 (5) | 15.2405(4) 16.7327(3) 23.3773 (4) | 16.7598 (3) 15.3581 (3) 23.3959 (4) | 15.1589 (7) 16.9552 (7) 23.4305 (8) | 17.0706 (3) 15.3215 (3) 23.3800 (4) | 17.1784 (4) 15.5345 (5) 23.4823 (6) | 17.0706 (3), 15.3215 (3), 23.3800 (4) |
| (°) | 94.317 (2) | 90.056 (2) | 90 | 90 | 92.920 (4) | 90.2758 (14) | 90 | 90.2758 (14) |
| V (Å3) | 5683.4 (3) | 5867.7 (2) | 5961.5 (2) | 6022.10 (19) | 6014.3 (4) | 6114.90 (17) | 6266.4 (3) | 6114.90 (19) |
| Z | 4 | 4 | 4 | 4 | 4 | 4 | 4 | 4 |
| (mm-1) | 6.66 | 6.45 | 6.35 | 6.28 | 10.01 | 9.85 | 9.61 | 8.83 |
| Measured, independent and observed [I > 2s(I)] reflections | 12411, 12411, 9888 | 21650, 6360, 5585 | 12721, 3059, 2428 | 55089, 3658, 3039 | 6501, 6501, 4857 | 23200, 6286, 5161 | 14674, 3234, 2264 | 11447, 4782, 3803 |
| Rint | - | 0.027 | 0.026 | 0.031 | - | 0.037 | 0.039 | 0.049 |
| (sin /)max (Å-1) | 0.641 | 0.668 | 0.639 | 0.672 | 0.640 | 0.641 | 0.639 | 0.665 |
| R[F2 > 2s(F2)], wR(F2), S | 0.039, 0.106, 1.04 | 0.080, 0.201, 1.20 | 0.077 0.148, 1.49 | 0.079, 0.156, 1.46 | 0.053, 0.116, 1.00 | 0.047, 0.100, 1.19 | 0.050, 0.087, 1.31 | 0.043, 0.095, 1.03 |
| No. of reflections | 12411 | 6360 | 3059 | 3658 | 6501 | 6286 | 3234 | 4782 |
| No. of parameters | 623 | 374 | 198 | 207 | 360 | 392 | 207 | 394 |
| max, min (e Å-3) | 2.40, -1.73 | 4.17, −2.67 | 0.83, -1.11 | 1.53, -1.63 | 2.87, -2.44 | 1.26, -1.63 | 0.74, -0.64 | 2.14, -1.45 |

Room temperature

100K	room temperature

Figure S1. The crystal packing along [001] direction for compounds 1 (left) and 2 (right) at 100K (lower panel) and at room temperature (upper panel)

100	240	298	333

Figure S2 Ewald representation along [001]for complexes 1 (top) and 2 (bottom) at different temperatures.

h1l	h0l	h0l

- b)

235K	230K	190K	170K

Figure S3. The layers of crystal a) 1 and   b) 2 in temperatures close to the phase transition from phase 2 to phase 1

a)	b)	c)

Figure S4. A) The superposition of complex 1 molecules from different phases (- black β-green -red - light blue. B) Disordered terminal chlorine atoms in β phase.
 c)  Orientation of disordered phenyl rings in top--phase and down -phase.

- b)	c) 	d) β	e)

Figure S5 a),b) The superposition of complex 2 molecules from different phases (- black β-green - light blue from different views)  Orientation of disordered phenyl rings in c) , d) β e)  phases.

- b)	c)

Figure S6. Molecular overlay of the a) α, b) β c) γ phases of complexes 1 (green) and 2 (purple)

| Complex 1 |  |  |  |
| --- | --- | --- | --- |
|  | α | β | δ |
| Complex 2 |  |  |  |
|  | α | β | γ |

Figure S7. Hirshfeld fingerplots of complex molecules in different phases.

Fig. S8. The unit cell similarity index and elongation vs. temperature [K]

Fig. S9.1. Theoretically generated powder pattern for complex 1:  Black-α phase , green- β phase, red- γ phase, blue- δ phase

Fig. S9.2. Theoretically generated powder pattern for complex 2 :  Black-α phase , green- β phase, red- γ phase.

Figure S10. The powder X-Ray diffractogrmas collected for 130 K black, 240 K green, 290K blue one form complex 2

Fig. S11.  Selected fragment of the temperature PXRD patterns for compound 2 at four temperatures: red – first  measurement in the cycle, black -second measurement in the cycle.

Figure S12.  Fragments of the temperature PXRD patterns for compound 2 at different temperatures

Fig. S9.  The graphs presenting the percentage of specific contacts in complex 1 (green) and 2 (red)