(Supplementary information)

Single PbS colloidal quantum dot transistor

Kenji Shibata,1,† Masaki Yoshida,1 Kazuhiko Hirakawa,2,3 Tomohiro Otsuka,4,5,6,7,8 Satria Zulkarnaen Bisri,9,10 and Yoshihiro Iwasa,9,11

1Department of Electrical and Electronic Engineering, Tohoku Institute of Technology, 35-1 Yagiyama, Kasumi-cho, Taihaku-ku, Sendai, 982-8577, Japan

2Institute of Industrial Science, University of Tokyo, 4-6-1 Komaba, Meguro-ku, Tokyo 153-8505, Japan

3Institute for Nano Quantum Information Electronics, University of Tokyo, 4-6-1 Komaba, Meguro-ku, Tokyo 153-8505, Japan

4Research Institute of Electrical Communication, Tohoku University, 2-1-1 Katahira, Aoba-ku, Sendai, 980-8577, Japan

5WPI Advanced Institute for Materials Research, Tohoku University, Sendai 980-8577, Japan

6Department of Electronic Engineering, Tohoku University, Aoba 6-6-05, Aramaki, Aoba-Ku, Sendai 980-8579, Japan

7Center for Science and Innovation in Spintronics, Tohoku University, 2-1-1 Katahira, Aoba-ku, Sendai 980-8577, Japan

8Quantum Functional System Research Group, RIKEN Center for Emergent Matter Science, 2-1 Hirosawa, Wako, Saitama 351-0198, Japan

9Emergent Device Research Team, RIKEN Center for Emergent Matter Science, 2-1 Hirosawa Wako, Saitama 351-0198, Japan

10Department of Applied Physics and Chemical Engineering, Tokyo University of Agriculture and Technology, 2-24-16 Naka-cho, Koganei-shi, Tokyo 184-8588, Japan

11Department of Applied Physics and Quantum-Phase Electronics Center, University of Tokyo, Hongo, Bunkyo-ku, Tokyo, 113-8656, Japan

____________________

†Electronic address: kshibata@tohtech.ac.jp

Supplementary Figure S1: Low-temperature transport properties for samples D and E.

Coulomb stability diagrams obtained for samples (a) D with d ~ 4.8 nm and (b) E with d ~ 8.7 nm. The number of confined electrons in the CQD is shown in each figure. The dashed lines are guides for the eyes.

Supplementary Figure S2: Detailed analysis of the excited states in sample A.

(a) Coulomb stability diagram obtained for sample A. The positions of the excited-state lines are indicated by orange arrows with assigned numbers 1, 2, 3, and 4, which correspond to E(N), E(N+1)low, E(N+1)high, and E(N+2) in the main text, respectively. (b) Schematic illustrations of the band diagrams at positions A (upper left), B (upper right), A’ (lower left), and B’ (lower right) in (a), where (N+1) is the electrochemical potential for adding the (N+1)-th electron. E(N) is the ground- to excited-state energy separation for N electrons. The dashed line indicates the electrochemical potential due to the excited state of N electrons. At positions B and B’, electrochemical potentials in the CQD are pushed up by the electric field from VSD and enter the bias window with an increase in the negative VSD, resulting in electrons being able to be transported through either the ground state of (N+1) electrons (solid line) or the excited state of N electrons (dashed line). (c) Differential conductance as a function of VSD along the solid line AB (black curve, VG = -5 V) and the dashed line A’B’ (red curve, VG = 15 V). Data for VG = 15 V are shifted by 0.14 V in the x-direction so that the conductance peaks determined by the boundary of the (N+1) Coulomb diamond match for comparison of the voltage spacing between the boundary of the (N+1) Coulomb diamond and the excited-state line of the N electrons. The voltage difference between the boundary of the (N+1) Coulomb diamond and the excited-state line of the N electrons shows a significant difference between the two datasets, indicating that E(N) increases by ~50 meV with the increase in VG from VG = -5 V to 15 V. Such behavior is not observed in the positive VSD region, probably because of the asymmetric tunnel coupling in this sample; the tunnel coupling to the source is strong, whereas that to the drain is weak, leading to the polarity-dependent appearance of the anomaly.

Supplementary Figure S3: Kondo effect in sample G (d ~ 4.8 nm) measured at T = 4 K.

(a) I-V curves plotted for various VG. The conductance is almost one order of magnitude higher than that in sample F. (b) Coulomb stability diagram of sample G. A clear Kondo peak is observed at VSD = 0 V. (c) Differential conductance as a function of VSD (i.e., Kondo peak) plotted for various VG. The width of the Kondo peak, w, depends on VG; w becomes larger when VG approaches the charge degeneracy point. Such behavior is known to be typical of the Kondo effect in quantum dot systems. From the width of the Kondo peak, the Kondo temperature TK is estimated to be TK ~50 K at VG = 10 V and TK ~80 K at VG = 40 V. (d) Schematic band diagram of a quantum dot with one spin-degenerate energy level 0 occupied by a single electron, where D and S are the tunnel coupling energies to the drain and source electrodes, respectively. The energy states of the source and drain electrodes are filled up to electrochemical potentials D and S, respectively. The tunnel coupling energy,  between the quantum dot and the source-drain electrodes is calculated by  = D + S, while the electrochemical potential of the source-drain electrodes at VSD = 0 V is expressed as D = S =  in the main text.

Supplementary Figure S4: Fabrication of nanogap source-drain electrodes by the EBJ method.

(a) Schematic cross-sectional image (upper) and SEM image (top view) of a sample with the experimental setup for the EBJ method (lower). (b) Typical nanogap source-drain electrode formed by the EBJ method. (c) Histogram of the fabricated nanogap sizes.

Supplementary Figure S5: SEM images of fabricated single-PbS-CQD transistors

SEM images of typical single-PbS-CQD transistors (top view) for diameter d values of (a) d = 3.6 nm, (b) d = 4.8 nm, and (c) d = 8.7 nm.

Supplementary Figure S6: Size distribution of PbS CQDs.

SEM image (left) and histogram of the diameters with the Gaussian result fitting shown as a red line (right) for oleic acid-capped PbS CQDs with (a) 1100 nm peak emission (d ~ 3.6 nm), (b) 1500 nm peak emission (d ~ 4.8 nm), and (c) 2000 nm peak absorption (d ~ 8.7 nm).

Supplementary Figure S7: Determination of Eadd for each Coulomb diamond.

Eadd for each Coulomb diamond is determined by e|VSD(apex)|, where e is the elementary charge. When |VSD(apex)| is polarity dependent, Eadd is determined as the average of the two values.

Supplementary Figure S8: Observation of the bandgap region.

(a) Coulomb stability diagram for PbS CQD sample H (d ~ 4.8 nm) with HfO2 as the gate dielectric. We observed that the large Coulomb gap monotonically increases with increasing negative VG, suggesting the bandgap region of the PbS CQD. Since the Coulomb gap decreases with increasing positive VG, we are detecting the bandgap region near the conduction band edge. The reason for the bandgap observation in this sample is the slight difference in the amount of surface charges caused by the use of a different gate dielectric. (b) Schematic cross-sectional image of the PbS CQD sample with HfO2 as the gate dielectric.