Effect of Anionic and Cationic Surfactants on the Rheological Properties of Human Serum Albumin Hydrogel

Tochukwu Olunna Nnyigide1, Osita Sunday Nnyigide1 and Kyu Hyun1*

School of Chemical and Biomolecular Engineering, Pusan National University, Busan 46241, Korea

Email：kyuhyun@pusan.ac.kr

Supporting Information

Fig. S1. Simulation box of HSA in 0.05 M CTAB. Cartoon structure of HSA is shown in orange and ball/stick representation of CTAB is shown in CPK colors with. Water molecules and counter ions are hidden for brevity.

Table S1. Contents of HSA/CTAB solutiona simulation box

Table S2. Contents of HSA/SDS solutionb simulation box

| SDS [M] | Nwater | NSDS |
| --- | --- | --- |
| 0.00 | 43897 | 0 |
| 0.01 | 43801 | 8 |
| 0.05 | 43335 | 42 |
| 0.20 | 42792 | 165 |
| 0.30 | 41685 | 248 |

Table S3. Comparison of average molar ratios of surfactant in experiment (10wt% HSA) and simulation

| CTAB [M] | Nwater | NCTAB |
| --- | --- | --- |
| 0.00 | 43897 | 0 |
| 0.01 | 43801 | 8 |
| 0.05 | 43335 | 42 |
| 0.20 | 42792 | 165 |
| 0.30 | 41685 | 248 |

| Experiment surfactant concentration [M] | Simulation concentration [M] | Surfactant/HSA molar ratio [-] |
| --- | --- | --- |
| 0.000 | 0 | 0 |
| 0.008 | 0.01 | 5 |
| 0.038 | 0.05 | 25 |
| 0.075 | 0.20 | 100 |
| 0.150 | 0.30 | 150 |

(a)

(b)

(d)

(c)

(f)

(e)

Fig. S2 (a-f). Temperature ramp results of 5, 7, 10 wt% HSA in different CTAB/SDS concentrations.

(b)

(a)

(d)

(c)

Fig. S3 (a-d). Time sweeps of 10 and 12 wt% in different CTAB/SDS concentrations.

(b)

(a)

Fig. S4 (a-b). Fitting for the determination of plateau modulus G0