Supplementary material

Porous polymer magnetic adsorbents for dye wastewater treatment

Tao Xue, Feifei Shao, Han Miao*, and Xinxin Li*

Key Laboratory of Specially Functional Polymeric Materials and Related Technology (Ministry of Education), School of Materials Science and Engineering, East China University of Science and Technology, 130 N, Meilong Road, Shanghai 200237, People’s Republic of China

Synthesis of oleophilic Fe3O4 nanoparticle

Oleophilic Fe3O4 nanoparticle was synthesized by easy coprecipitation method. Fe3+ (3.24 g) and Fe2+ (3.336 g) were dissolved in deionized water (30 mL) under mechanical stirring (500 rpm), after heating to 60°C, NH3H2O (15 mL) was added in flask under N2 protection. The system was heated to 80°C after stirring 30min, then OA (1.16 g) was joined. The whole system was stirred and aged for each 1 h. The obtained product (OA-Fe3O4) was precipitated by pH = 1 HCl solution and washed with deionized water until neutral.

Scheme S1. The preparation procedures of porous magnetic adsorbents.

Fe3O4 was prepared by coprecipitation method. Its structure was characterized by XRD. From Figure S1a, all the characteristic diffraction peaks were observed and the peak 2θ = 35.439 (311 Crystal Plane) was chosen to calculate its grain size according to the Debye-Scherrer formula. The grain size of obtained Fe3O4 was about 21.714 nm. In order to improve the compatibility of Fe3O4 with St, Fe3O4 was modified with OA, and the obtained OA-Fe3O4 showed an obvious transformation from hydrophilic to hydrophobic (Figure S1b). Then, their compositions were investigated by FT-IR (Figure S1c). The peak at 579 cm-1 was attributed to Fe-O bonds. Compared with Fe3O4, stretching vibrations of the C-H bonds at 2846 cm-1 and 2920 cm-1 were observed on the curve of OA-Fe3O4. These illustrated that the Fe3O4 was modified successfully.

Figure S1. (a) XRD pattern of Fe3O4, (b) the wettability transformation of Fe3O4 and OA-Fe3O4, (c) FT-IR spectra of Fe3O4 and OA-Fe3O4.

Figure S2. Zoom-in view of the TEM images of (a) SF and (b) SVF.

Figure S3. The composition and structure of (a) SY, (b) RhB, and (c) MB dye molecules.

PFO: qt=qe×1-e-K1t

PSO: qt=qe2K2t1+K2qet

Intra-particle diffusion: qt=Kpt0.5+C

Where t is the contact time, qt and qe are the adsorption capacity at time t and equilibrium, K1, K2, Kp were the PFO, PSO and intra-particle diffusion model rate constants respectively. C is the thickness of the boundary layer.

Table S1. Summary of kinetic fitting dates of HSVF and HSF.

| 298K | PFO |  | PSO |  | Intra-particle diffusion |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| HSVF | K1 | 0.088 | K2 | 8.19×10-4 | First stage | Kp | 5.034 |
|  |  |  |  |  |  | C | 97.708 |
|  | qe | 153.36 | qe | 164.69 |  | R2 | 0.986 |
|  |  |  |  |  | Second stage | Kp | 1.072 |
|  | R2 | 0.874 | R2 | 0.961 |  | C | 139.484 |
|  |  |  |  |  |  | R2 | 0.989 |
| HSF | K1 | 0.0911 | K2 | 0.00344 | First stage | Kp | 1.591 |
|  |  |  |  |  |  | C | 28.331 |
|  | qe | 44.981 | qe | 47.856 |  | R2 | 0.993 |
|  |  |  |  |  | Second stage | Kp | 0.3994 |
|  | R2 | 0.921 | R2 | 0.978 |  | C | 38.583 |
|  |  |  |  |  |  | R2 | 0.982 |

Note: K1 (min-1); K2 (g/mgmin); qe (mg/g); Kp (mg/gt0.5); C (mg/g).

Figure S4. The equilibrium time of HSVF at 100 mg/L.

Langmuir: qe=qmbCe1+bCe , separation factor of the Langmuir model RL=11+bC0

Freundlich: qe=KFCe1n

Temkin: qe=BlnKTCe

Where qe, Ce are equilibrium adsorption capacity and equilibrium concentration respectively. qm is the maximum adsorption capacity, b, KF and KT are Langmuir, Freundlich and Temkin isotherm models constants respectively. n (dimensionless) is the Freundlich intensity parameter, B (dimensionless) is the Temkin model parameter.

Table S2. Summary of isotherm fitting dates of HSVF.

| HSVF |  | 298K | 308K | 318K |
| --- | --- | --- | --- | --- |
| Langmuir | qm (mg/g) | 343.904 | 338.35 | 313.04 |
|  | b (L/mg) | 0.0742 | 0.055 | 0.057 |
|  | RL | 0.063 | 0.083 | 0.0806 |
|  | R2 | 0.965 | 0.975 | 0.980 |
| Freundlich | KF [(mg/g) (L/mg)1/n] | 143.47 | 123.83 | 105.1 |
|  | n | 6.849 | 6.01 | 5.65 |
|  | R2 | 0.758 | 0.829 | 0.920 |
| Temkin | KT | 7.405 | 3.081 | 2.706 |
|  | B | 43.157 | 47.133 | 43.457 |
|  | R2 | 0.818 | 0.890 | 0.948 |

Table S3. Summary of isotherm fitting dates of HSF.

| HSF |  | 298K | 308K | 318K |
| --- | --- | --- | --- | --- |
| Langmuir | qm (mg/g) | 269.044 | 285.090 | 172.15 |
|  | b (L/mg) | 0.00595 | 0.0041 | 0.087 |
|  | RL | 0.627 | 0.709 | 0.103 |
|  | R2 | 0.982 | 0.997 | 0.965 |
| Freundlich | KF [(mg/g) (L/mg)1/n] | 13.645 | 7.638 | 130.314 |
|  | n | 2.299 | 1.927 | 24.272 |
|  | R2 | 0.890 | 0.957 | 0.981 |
| Temkin | KT | 0.0495 | 0.0414 | 1.142×10-8 |
|  | B | 63.175 | 62.479 | 6.797 |
|  | R2 | 0.982 | 0.998 | 0.982 |