Supplementary Information

Machine learning discovered nano-circuitry for nonlinear ion transport in nanoporous materials

Hualin Zhan1, Richard Sandberg2, Zhiyuan Xiong1, Qinghua Liang1, Ke Xie1, Lianhai Zu1,3, Dan Li1, Jefferson Zhe Liu2

1 Department of Chemical Engineering, The University of Melbourne, VIC 3010, Australia

2 Department of Mechanical Engineering, The University of Melbourne, VIC 3010, Australia

3 ARC Hub for Computational Particle Technology, Department of Chemical Engineering, Monash University, VIC 3800, Australia

# METHODS

Selective use of nanoscopic models. Modified Poisson-Nernst-Planck theory. Electrical double layer (EDL) at material-electrolyte interfaces is a region where ions from electrolyte redistribute due to Debye screening, enabling nonlinear charging dynamics in supercapacitors1. In their porous electrodes, EDL from neighbouring interfaces could overlap. The overlapped EDL could further change dynamically when subject to varying electrical conditions such as CV during charging/discharging processes, adding more layers of complexity to the charging dynamics. Mean-field theories, or known as continuum models, collectively calculate the motion and electrical fluctuation of a group of ions or atoms, allowing for extraction of spatiotemporal information of ion transport for large nanoporous systems in dynamic electrical environment. Although early studies indicate that classical mean-field theories, such as Poisson-Nernst-Planck model, may be inaccurate to describe ions in nanopores when their finite size is not negligible2,3, recently modified theories can capture these nanoconfinement effects for nanoconfined ions4,5. Among several mean-field theories developed for ion dynamics4,6,7, mPNP relaxes the thin EDL assumption and includes the finite ion size. Although mPNP first demonstrates its use in a one-dimensional model of supercapacitor4, recent advances in computational science allows for simulation of three-dimensional models where the calculated performance can be correlated with experiments8. These advantages render mPNP a suitable method for the study in this work, as it is of interest to study general effects of nanoconfinement, namely ions with finite size in ubiquitous overlapped EDL, on charging mechanisms in nanoporous network.

Molecular dynamics. In contrast to mean-field theories which statistically average the behaviour of a group of individual molecules, molecular dynamics (MD) tracks the motion of every particle in a system by numerically solving Newton’s equation. These particles can be atoms, molecules, or coarse-grained macromolecules9,10. The force acting on each particle is derived from the spatial gradient of the potential energy. In MD simulation for supercapacitors, it is often of interest to construct atomic systems to investigate the origin of charging mechanisms11,12, where both the electrostatic and atomic interaction potentials must be considered. This has at least four advantages for the study of nanoconfined charging dynamics. (1) Non-equilibrium ion dynamics can be studied13. This is because the trajectory of individual ions can be predicted based on the exerted forces. Their collective behaviour determines the thermodynamic state of the system, which can be far away from equilibrium. In contrast, mean-field theories describe ion dynamics when systems are close to thermodynamic equilibrium, as a result of free energy perturbation of the statistical ensemble4,14. (2) High-fidelity information of ion dynamics can be obtained at atomic scale with femtosecond resolution, as the location and velocity of each ion in electrolyte are directly calculated at every timestep. In mean-field theories, electrolyte is treated as a continuum based on the fluid element treatment in fluid mechanics15,16. This treatment becomes inaccurate when atomic resolution is required for, for example, ion concentration profile in sub-nanometre pores. Modifications to mean-field theories should then be considered3. (3) Finite size of ions is more accurately accounted for using the inter-atomic potentials, rather than the rigid-sphere approximation of ions used in mPNP. This is because the ionic/atomic size is defined as the closest equilibrium distance between two ions/atoms in the presence of inter-atomic potentials17. This accurate description of ionic size, in principle, describes the steric flux more accurately. (4) Interaction between solvent molecules and ions or materials is included, e.g., solvation and desolvation effect. This effect could compete with other atomic interactions and affect charging/discharging processes12,18.

Disadvantages of MD. Those four advantages, however, could impose certain restrictions to the system studied, which can imply disadvantages at the same time. (1) Calculation for every atom in a system would require a substantial amount of computational resource and time10. This suggests that the studied system and the dynamic evolution should be small and short enough so that the calculation can complete within a reasonable computational time19. Supercapacitor models in MD simulations contain typically thousands of atoms studied at timescales of nanoseconds9,11,12,20. (2) The electrical condition applied in supercapacitor models for MD is generally simple. This is because inclusion of additional calculation for, for example, time-dependent Poisson’s equation with complicated boundary conditions in MD, would drastically increase more workload to the already-intense calculation. A commonly used constant-charge method20,21 circumvents this complexity by assigning static charges on electrodes, where the burden of solving Poisson’s equation with Dirichlet boundary condition is alleviated by calculation of Coulombic interactions. This method, however, does not consider the charge fluctuation on electrode due to the equipotential condition, and it is incapable to include arbitrary time-dependent potential. Recently developed constant-potential and coarse-grained methods22,23 could account for these effects which, however, inevitably require more computational resources19. (3) Collective behaviour of ions is generally not manifested explicitly in MD results. As a result, we rely on physical models to interpret the massive numerical data of MD simulations, e.g., use Fick’s law, which could be derived from statistical mechanics15, to quantitatively understand ion diffusion by calculating the concentration gradient. (4) There is an uncertainty in transferring the inter-atomic force models (potential energy) from one chemical system to another. This is because the widely adopted force models are fitted from some given chemical systems.

Requirements to research methods. In this work, we are interested in understanding the impacts of nanoconfinement effect on charging mechanisms of supercapacitors during dynamic charging/discharging processes. This requires that the research methods possess certain virtues. (i) The model constructed should be as large as possible and it should contain sufficient nanoscopic details of ion dynamics, so that the microscopic understanding and macroscopic charging behaviour could be bridged. Simulations of such models are preferred to be completed within an acceptable time, e.g., less than a week for one case study. (ii) The voltage applied on the electrodes should be able to resemble the changes in CV experiments, i.e., time-dependent electrical potential. (iii) Analysis of charging mechanisms, including electro-migration, diffusion, and steric flux, should be straightforward and accurate enough within the provided theoretical framework. (iv) General steric effect and overlapped EDL should be accounted for.

Allowed approximations for this work. Note that the following virtues could be included in the research methods which, however, are not essential for this work. (v) Charging dynamics could be investigated when the system is perturbed far away from thermodynamic equilibrium. This could be of interest to further studies involving redox-active electrodes24 or to systems operated at non-steady states with time-dependent momentum15,25. However, this information is not critical for this work as no redox reaction is involved, and the studied charging/discharging processes can reach steady states. (vi) Atomic resolution is preferred, not necessary in this work, when obtaining the distribution of ions, current, and potential in the system. This is because electro-migration, diffusion, and steric flux are collective effects of ions, and these atomic details will be averaged during data analysis for this work.

Use of mPNP and MD. With all these factors considered, we use mPNP as the primary method for nanoscopic investigation for this paper and use MD to qualitatively confirm the observation from mPNP. This is because mPNP possesses virtues (i-iv), while MD has virtues (v) and (vi). In recent studies, mPNP has been adopted as a common technique to understand the underlying mechanism of charging/discharging in supercapacitors5. The constant-charge method is used in the qualitative MD study, as the response of ion dynamics to electrical and collective inter-atomic potentials can be efficiently investigated with available computational resources. Our MD results confirm the key discoveries of mPNP.

Modified Poisson-Nernst-Planck theory. Governing equations. The equations for mPNP are written

n±v±=-D±∇n±diffusion-n±μ±∇ϕmigration-a±3D±n±∇c1-a±3csteric flux,	(3)

∇2ϕ=-eρε,	(4)

∂n±∂t+∇⋅(n±v±)=0,	(5)

where the subscript ± denotes cation and anion. n, v, D, z, and a are the concentration, velocity, diffusion coefficient, valency, and diameter of ions. μ=zeDkBT is the ion mobility described by the Einstein relation. ε, kB, T, e, and ϕ are permittivity, Boltzmann constant, temperature, elementary charge, and electrical potential. ρ=z+n++z-n- and c=n++n- are the net and total ion concentration. In mPNP equations, Fick's diffusion law [diffusion term in equation (3)] and Drude's conduction model [migration term in equation (3)] are integrated into Poisson's equation [equation (4)] and time-dependant mass conservation theorem [equation (5)], in order to account for (concentration-gradient-driven) diffusion and (potential-gradient-driven) migration of ions26. The impact of finite ion size (steric effect) on ion transport is included using a lattice gas model27, where ions are considered as rigid spheres rather than point charges. Inclusion of this model in a mixing entropy term contribute to the grand canonical free energy of the electrolyte, where the functional derivative over ion concentration produces a generalized electrochemical potential for the system28. With the idea of a dynamic density functional theory for close-to-equilibrium transport14, an additional flux induced by steric effects [steric flux term in equation (3)] can be derived4, which depends on the total concentration of cations and anions. This is particularly interesting for ions in EDL, either under nanoconfinement or in an open space with a high electrode potential ϕm, as the limited space at electrode-electrolyte interface only permits accommodation of certain number of ions.

Parameters settings. Substituting equation (3) into equation (5) and treating cations and anions separately, we then have five independent equations. In order to solve this set of equations to study charging dynamics in nanoporous electrodes, we keep five independent variables ϕ, n±, and v± unknown and pre-define the rest. e=1.6×10-19 C. kB=1.38×10-23 m2 kg s-2 K-1. T=298.15 K. ε=εrε0. εr=78.5 is the relative permittivity or dielectric constant of water20. ε0=8.85×10-12 F m-1 is the vacuum permittivity. z+=1. z-=-1. The ionic parameters including the diffusion coefficient and the ion diameter are set the same for cations and anions for simplicity. This enables straightforward analysis of general nanoconfinement effects for charging dynamics, which serves the purpose of this study. The impacts of specific properties of ions on charging dynamics can be investigated in future, which is outside the scope of this work. D±=2×10-9 m2/s is the diffusion coefficient commonly used in mPNP simulations29. a±=0.6 nm is the diameter of both cations and anions4. These ionic parameters are within the same order of magnitude as those for aqueous potassium chloride electrolyte30.

Model implementation. This set of partial differential equations can be numerically solved with finite element methods, where a commercial package – COMSOL 5.4 – is used in this work. This allows for construction of supercapacitor models with layered 2D materials as electrodes, where the electrolyte is considered as continuum (Supplementary Fig. 1). The internal structure of the electrodes can be described with three parameters in 2D geometry31,32, i.e., the lateral material size (Ls), lateral gap (ds), and interlayer spacing (or nanoslit height, d). In this work, Ls=6 nm, ds=1.6 nm, and d changes from 1.5 to 5 nm. The thickness of a monolayer 2D material (dm) takes the value of the graphene thickness, 0.34 nm33. The position of each 2D material is fixed in the model and their corners are rounded to avoid electrical edge-effects34. The model contains half of Ls and ds in y-axis due to the geometric symmetry on the edges, in order to effectively deliver computational results within reasonable time. Since electrical potential is split equally on symmetric cathode and anode in an electrochemical cell where the local potential in the mid-plane is 01,35, a half-cell consisting of a positively charged electrode and an electrolyte reservoir extended from the electrode to the mid-plane of the full-cell is studied here. The x-dimension of the reservoir is set as 3000 λD for half-cells, i.e., the distance between the positive and negative electrodes in full-cells is equivalently 6000 λD, where the electrical effect from the opposite electrode in full-cells can be effectively screened and the concentration variation in the bulk electrolyte can be minimized. λD is the Debye length characterizing the thickness of EDL15,25, which is around 0.3 nm for a 1 M KCl aqueous electrolyte. This practice is commonly used in mPNP studies4, and is in line with experiments36. As approximated solution is provided with finite element methods based on variational approach34 which could be inaccurate in the presence of steep slope of electrical potential37, the element size in EDL is set as λD/30 due to the drastic change in ϕ. In order to describe the modification to electrical condition in EDL by finite ion size, Stern layer is constructed around each monolayer material, following the Gouy-Chapman-Stern theory26. The thickness of the Stern layer is set as half of the ion diameter (a/2), as it represents the closest distance from ion centre to the material-electrolyte interface.

Boundary and initial conditions. The uniqueness theorem requires definition of sufficient and non-conflicting boundary conditions. Dirichlet boundary condition is used for Poisson’s equation, as the electrical potential is directly applied on electrodes in supercapacitors. While the potential on the rightmost side of the half-cell in Supplementary Fig. 1 is kept at 0 V, ϕ applied on each 2D material is set as a function of time (bottom panel in Fig. 2f), in order to study CV charging/discharging processes. Note that the transition of ϕ at its maxima and minima is smoothed to reduce numerical singularities in this time-dependent study. This is the reason why the upper-right and bottom-left corners of the CV diagrams in Fig. 4c-e are not sharp enough. In supercapacitors, anions/cations travel towards the positively/negatively charged electrode from the opposite side. In order to reproduce this process in half-cells, a boundary condition is imposed for equation (5) where the concentration of cations and anions at the rightmost side is kept constant (1 M). Lastly, for time-dependent studies, initial conditions must be defined. In this work, the initial concentration is 1 M and the initial electrical potential is 0 V.

Molecular Dynamics (MD). Model setup for MD. Here we use an open-source MD package, LAMMPS (Large-scale Atomic/Molecular Massively Parallel Simulator), to examine the atomistic mechanisms of nanoconfined charging dynamics in supercapacitors with membrane electrodes. As supercapacitor is generally operated in thermostatic environment, we simulate the system in the canonical (or NVT) ensemble, i.e., fixing the total number of atoms, and the volume and temperature of the entire system. The volume of the system is represented by the size of the simulation cell, which has periodic boundaries in y and z directions and fixed boundary in x direction. The dimension of the simulation cell in x, y, and z is 6.15×15.48×2.13 nm3. As shown in Supplementary Fig. 4a, two electrodes are located in regimes 0<x<3.74 nm and 11.74<x<15.48 nm. Each membrane electrode contains 5 graphene layers stacked in x-direction, where the inter-layer distance (dg) is 0.93 nm. This is equivalent to d=0.59 nm in Supplementary Fig. 1 as d=dg−dm. Each layer is comprised of y-aligned graphene nanomaterials, separated by gaps with the width ds=1.23 nm. The width of nanomaterial (Ls) is 2.46 nm. The length of bulk electrolyte in x-direction is 8 nm. An equivalently 1 M KCl aqueous solution is set as the electrolyte, where the number of KCl ion pairs and H2O molecules are 120 and 6600. The total number of atoms including those for graphene is 24240.

Parameters settings. The molecular structure of water is constructed with a commonly used SPC/E (extended simple point charge) model31,38, where the H-O bond length and the H-O-H angle are 0.1 nm and 109.47°, respectively. The atomic interaction is described with the standard 12-6 Lennard-Jones potential ULJ=4ϵσr12-σr6, where r is the distance between two atoms. ϵ and σ are two parameters with the units of energy and distance, respectively. These parameters for the same type of atoms are given in Extended Data Table 1; and those for different type of atoms are calculated arithmetically using the Lorentz-Berthelot mixing rules, i.e., ϵ=ϵmϵn and σ=12σm+σn. The subscripts m and n indicate different types of atom. The cut-off distance for both the atomic interaction and Coulombic potential is set as 1 nm. The charge for each type of atom is given in Extended Data Table 1.

Numerical algorithm. MD simulation packages generally treat Newton’s equation based on Hamiltonian mechanics39. Unlike microcanonical ensembles where Hamiltonian equations can be directly used, the equation of motion is modified and non-Hamiltonian for canonical ensembles. The modified equation used here has Nosé-Hoover style40,41. Although ordinary differential equations can be solved by other finite difference methods including Runge-Kutta method42,43, here the Nosé-Hoover equation is solved with schemes following the Verlet and rRESPA (reversible Reference System Propagator Algorithms) time integrators44, in order to preserve time reverse symmetry and to enable long-term stability. The motion of water molecules is described by constraint dynamics, which is invoked subsequent to solution of equation of motion, in order to reduce the complexity in simulation introduced by molecular geometry. Here we use the SHAKE algorithm where the bond length and angle of water molecule are reset to predefined constants at each time step45. The Coulombic interaction is computed with the particle-particle particle-mesh solver, which is generally faster than the traditional Ewald summation46.

Simulation procedure. The simulation procedure is mainly comprised of two stages. (i) At first, the charge on graphene electrodes is set as 0 (top panel in Supplementary Fig. 4a). The system is simulated for 1 ns with a time step of 1 fs after the initial energy minimization of the system, in order to allow the electrolyte to fully enter each nanoslit. This is to resemble the experimental practice where electrodes are fully immersed in electrolyte for sufficient time prior to electrochemical experiments36. (ii) The charge on each carbon atom of the left and right electrodes in the bottom panel of Supplementary Fig. 4a is assigned 0.041 e and -0.041 e, respectively, where e is the elementary charge. The system is simulated for 0.5 ns with a time step of 1 fs.

Analysis of migration, diffusion, and steric flux. As the MD simulation result only contains the information of individual atoms, we derive the collective dynamic mechanisms including migration, diffusion, and steric flux based on their definition in equation (3). Since we are interested in the dynamic mechanisms inside nanopores, particularly between the ith and (i+1)th nanoslit, it is convenient to approximate the spatial gradient operator with ∆∆r, where ∆ calculates the difference of electrical potential or ion concentration, and ∆r represents the distance, between two nanoslits. The electrical potential of the ith nanoslit (ϕi) is evaluated at the location in the centre where y=0 (Fig. 2b), by solving the Poisson’s equation with Neumann boundary condition on the edges in x-axis as the constant-charge method is used. The ion concentration, either total (ci) or net (ρi), of the ith nanoslit is averaged over the slit. ∆r is a constant as there is no structural change in MD simulation. Therefore, migration, diffusion, and steric flux can be qualitatively represented by the differences of their electrical potential (Δϕi = ϕi+1 - ϕi), net ion concentration (Δρi = ρi+1 - ρi), and total ion concentration (Δci = ci+1 - ci). ρ = z+n+ + z−n− and c = n+ + n−, where n and z are the ion concentration and valency, the subscripts + and − denote cations and anions, respectively. The simultaneous increase of Δϕ1, Δρ1, and Δc1 from some negative value to nearly 0 indicates a constructive interplay of EDS where their directions are the same (Fig. 2h). Although Δρ1 and Δc1 increases to a value slightly above 0 after 0.1 ns, it does not change the inference, as the constant charge method used in MD induces variation in the electrical potential on neighbouring graphene layers. If a more accurate but time-consuming method of constant potential were used in MD, Δρ1 and Δc1 would be smaller due to the negligible difference of electrical screening in different nanoslits at equilibrium. This consistency confirms the applicability of mPNP and its findings in this study, at least qualitatively.

Evolutionary Algorithm. Introduction. Evolutionary algorithm (EA) is a metaheuristic machine learning approach inspired by Darwin’s theory of evolution47. It can be used to search for globally optimized solution to a problem, for example, the shortest route for a travelling salesman48. This solution is obtained through an iterative and evolving process of a massive population of candidate solutions, i.e., chromosomes. In each iteration/generation of this process, the genotypes of chromosome, which contain the generic information, are generated/reproduced and selected by high-level competition rules to formulate the population for the next generation, which could also mutate. Recent development in EA provides a constraint-free symbolic regression method to identify explicit mathematical formula for a given set of data, where the phenotype of chromosome is mathematical expression49,50. The obtained formula may not be the exact solution for the problem, but it could provide a closely approximated form with excellent fitness, which would allow for physical discussion and quantitative description.

Data preparation. Here we use EA to analyse the massive simulation data generated by mPNP, in order to unveil previously unnoticed mathematical/physical relation for in-pore ion dynamics. Before construction of the chromosome for evolution process, we must prepare the simulation data such that the symbolic regression could converge rapidly. As the in-pore ion dynamics is symmetric about the point where charging process ends, i.e., the centre of Fig. 2g or Fig. 3a, we can focus on the analysis of the charging process only. The discharging process can then be described by symmetry. However, the voltage and current are still nonmonotonic functions of time. This implies that the algorithm needs to search in a large solution space with possibly non-elementary functions, which could introduce challenges for regression convergence. An observation of the simulation data suggests that the time integrations of voltage (∆ϕidt) and current (Iidt) have a monotonic relation, where elementary functions would be sufficient for the solution space. In order to keep the integrated values within the same order of magnitude, as a common practice to facilitate regression processes51, ∆ϕidt and Iidt are normalized. Note that Iidt=Qi, which represents the transient net ion stored in the ith nanoslit. It is straightforward to normalize Iidt with the maximum value of Qi, where Ii=IidtQimax=QiQimax. Hence, the integrated voltage can be normalised by ∆ϕi=∆ϕidtQimaxRc, where Rc is the constant resistance obtained by a linear regression of voltage-current relation in the initial charging process. We then focus on finding the mathematical relation between Ii and ∆ϕi using the method of symbolic regression.

Construction of chromosome. The treated data for training purpose have single variable Ii and single output ∆ϕi with a nonlinear relation, as shown in Supplementary Fig. 15. Multigenic chromosome is then used to add a degree of nonlinearity between the genotype and phenotype49. The multigenic chromosome consists of 7 genes with flexible length, in which each has a head and a tail section. In order to avoid overfitting, the number of alleles in chromosome is kept small to minimise the length of the phenotype. The head contains at most 3 alleles choosing from the terminal set x, 1.0, -1.0, r1, r2, r3, r4, r5 and the function set +, -, ×, sin, while all alleles in the tails are selected from the terminal set. x is the simulation data. r1, r2, r3, r4, r5 are random numbers between 0 and 1, and sin represents the sine function. The length of the tail (lt) is determined by lt=lh∙am-1+1, where lh is the length of the head and am is the maximum value of arity in head. These genes are connected via 6 linking functions. The genotype of an example chromosome from this study is +-+--*<*0.715+1.0x><+x0.423><*sinsin1.0-1.0><sinsin0.423><sinx><1.0><-+x-1.00.544>, where +-+--* are the linking functions and those inside <…> are the genes. This linear genotype is translated into nonlinear phenotype by Parse Tree (or Expression Tree)49,50, which reads 0.72x2+2.02x+sinx-1.35 after rearrangement.

Evolution. 250 chromosomes/individuals construct the population for evolution process. The cost of each chromosome in the population is computed by single-objective criteria fIi-∆ϕi2N. fIi is the phenotype of the chromosome with Ii as the argument, and N is the number of datapoints used for learning. The individual with the lowest cost gives the fittest mathematical expression for the training set provided. An elitism principle is used in the tournament selection process, where the individual with the lowest cost is carried forward directly into the next generation. Among the rest of the individuals, two are randomly selected, in which the one with lower cost would survive. This process is repeated for 50 times. The survived ones are used to produce offspring for the next generation through one-point and two-point crossover with the possibility of 0.5 and 0.2, respectively. This is followed by the genetic operations of mutation and inversion, each with a possibility of 0.05. In the symbolic regression process, the population of chromosome would evolve for a maximum 3000 generations if the cost is larger than 10-5. After thousands of generations, we obtain ∆ϕi=Ii1-0.5γIi with a cost of 2.35×10-6 for a supercapacitor with d=2 nm. where γ=0.39. Rearrangement and derivation over t at both sides of this equation give equation (2).

Equivalent Circuits. Background. Equivalent circuits are frequently used to interpret electrochemical experiments, particularly the impedance spectroscopy, in which ion transport and storage may be characterized using electrical circuits comprised of resistors or capacitors26, e.g., Randles circuit15,33. This could enable quantitative analysis for the macroscopic performance of the studied electrochemical device under, for example, dynamical charging rates52. When porous electrodes are used in electrochemical experiments, the equivalent circuit may consist of many layers of resistors and capacitors, where the transmission line model (TLM) is a common example53,54. This is because the electrical signal applied between the parallelly aligned EDL and in-pore surface is analogous to that between two parallel transmission lines53. In addition to interpretation of experiments, this model, when combined with a self-affine fractal model, is attempted to optimize the design of supercapacitor architecture based on activated carbon for large capacitance and rapid charging/discharging, by relating the structural characteristics to dynamic performance55.

Knowledge gaps. This predictive capability enables equivalent circuits as an effective macroscopic tool for the study of supercapacitors and batteries, in which the rational design towards higher performance may be possible56,57. In order to achieve this goal, future developments should include nanoscopic charging mechanisms, where the impact of nanoscopic effects on macroscopic charging can be evaluated. Therefore, at least two questions should be addressed to. (i) Are conventional resistors and capacitors capable to describe ion transport and storage, particularly when nanoporous electrodes are used? Even the basic Nernst-Planck model indicates that diffusion, unrelated to voltage stimulation directly, is included in ion transport; and the Gouy-Chapman-Stern model suggests that the nonlinear diffuse layer could affect the capacitance26. In this context, how to further define the values of circuit elements used, including resistors, capacitors, and/or more, especially with additional consideration of the steric effects and EDL overlapping under nanoconfinement? (ii) How many circuit elements should be included in equivalent circuits and how should they be connected; or more generally, does an electrochemical device correspond to a unique equivalent circuit? Unfortunately, the indirect relation between the physio-chemical origin of ion transport and the electrical basis of conventional circuit analysis does not warrant a unique equivalent circuit, unlike those models derived directly from the relevant physical mechanisms such as the Poisson’s equation for electrostatics.

Physics-based circuits. Developing a strategy to construct circuits based on the microscopic physical models could be a key to address to these questions58,59. In other words, this involves a multiscale, interdisciplinary study where the circuit elements can be defined from the mechanistic studies of charging dynamics, particularly under nanoconfinement, if the mathematical relation between the microscopic and macroscopic quantities are known. Previous atomistic studies demonstrate that physio-chemical results could be used to define circuit elements in general, in order to describe the charging properties13,19. In order to guide inverse design in future, the collective behaviour of ions should be further evaluated in larger systems for long-time evolution under practical electrical conditions56,57, rather than in atomic systems for nanoseconds under simple electrical conditions. Therefore, mPNP is selected as a primary microscopic model in this work as their measurable physical quantities are, in principle, derived based on the statistical results of atomic systems60. The physical relation of nanoconfined ion conduction, discovered by EA in this work, can be used to construct physics-based circuits for nanoconfined charging dynamics based on the results of mPNP.

Circuit construction. Based on the mechanistic studies of nanoconfined charging dynamics by mPNP and the analysis by EA, here we use MATLAB Simulink to construct a nano-circuitry model (NCM) and TLM. As schematically shown in Supplementary Fig. 5a, ion storage in EDL within each nanoslit can be described by capacitance Cslit=Qiϕm-ϕi, which is a constant when d>1 nm (quantitatively studied in Supplementary Fig. 11a, b). Due to EDL overlapping from the closely stacked 2D materials, ion transport inside a single nanoslit is enhanced where a short-circuit mechanism can be applied59. The resultant ionic conductance in a single nanoslit is much smaller than that between two neighbouring nanoslits, as indicated in Supplementary Fig. 10b. Therefore, resistor elements in NCM and TLM are mainly used to describe trans-slit ion transport. As R+ and R− in Supplementary Fig. 10b and c are connected in series to represent trans-slit ion transport, their combined effect should also be time-dependent, i.e., R++R−=Rc+Rd. Rc is a constant resistance and Rd is a dynamic resistance described in Fig. 3. In a serial circuit of resistors, the definition of each resistance value can be arbitrary as long as the sum of R+ and R− is the same as that of Rc and Rd. Therefore, due to mathematical convenience, we define R+=Rc and R−=Rd. While both Rc and Rd are included in NCM, only Rc with the same constant value is used in TLM (Supplementary Fig. 11c). In both NCM and TLM, ϕm(t) is applied between two terminals at the bottom, which represent the bulk electrolyte and electrode terminal of the half-cell; and the total current Im(t) is measured. As indicated in equation (2), Rd is a function of Qi(t). This suggests that the trans-slit ion transport is dependent on the voltage across Cslit, producing a system of entangled equations which is difficult to model with Simulink. In order to circumvent this obstacle, Qi(t) could be obtained externally from other sources including mPNP, TLM, or even experiments in future works. As mPNP is used in nanoscopic investigation, its results of Qi(t) is considered reliable for NCM studies. We then demonstrate that, for supercapacitors with 6 layers of 2D materials, consistent results can be obtained when using Qi(t) from TLM (Supplementary Fig. 11d). This is possibly because, even if the magnitude of Qi(t) obtained by TLM could be different from that strictly obtained from NCM, the normalized Qi(t) in equation (2) cancels the effect of magnitude. This enables us to conveniently investigate membrane-based supercapacitors comprised of many layers of 2D materials using NCM (Supplementary Fig. 12). Moreover, the nanoconfined resistance values, including both Rc and Rd, are the same for different nanoslits with the same dimension, as demonstrated in Fig. 3c. Note that there are no resistors connected with Cslit in parallel for all circuits in this work, indicating that no leakage current (or electron transfer) is present in EDL; and hence no Faradaic reactions are involved.

# Supplementary Figures

Supplementary Fig. 1 | Half-cell model of a membrane-based supercapacitor to investigate charging dynamics using modified Poisson-Nernst-Planck theory. The membrane electrode is comprised of several monolayer 2D materials (orange slats). It follows the statistical representative microstructure model32 that consists of regularly distributed 2D material layers. Each pair of two adjacent 2D materials construct a nanoslit, with i as the index. The top and bottom edges (y-axis) are the mirror planes.  The dark cyan region represents the electrolyte filled in the porous electrode and in the open space (reservoir). The contact of electrolyte with each 2D material prior to the application of voltage is to reflect an experimental practice where electrodes are immersed in electrolyte for sufficient time before electrochemical measurements. The rightmost side on x-axis of the half-cell also represents the mid-plane in an equivalent full-cell model. The light cyan regions surrounding each 2D material indicate the Stern layer. Taking advantage of the symmetry of the adopted electrode structure, we only need to simulate the ion transport and storage in this depicted region by using appropriate boundary condition (e.g., vertical flux equals to zero at the top and bottom edges). See Methods for details of our simulations.

Supplementary Fig. 2 | Ion migration, diffusion, and steric flux as a function of distance (x) from the electrode surface in open space. a, Normalized current components (migration, diffusion, and steric flux) as a function of normalized distance in open space (Fig. 2b), calculated using the mPNP theory at the instant where the cycle number is around k+0.25. The current components are normalized by the total current in supercapacitor, obtained at the rightmost side of the half-cell model. x is normalized by the Debye length (λD), which is around 0.3 nm for 1 M aqueous KCl solution. The dashed vertical line roughly indicates the location where current values in Fig. 2c are reported. b, Magnification of the dashed box in (a). The current in the open space (or the bulk electrolyte) is mainly migration. The steric flux is overlapped by diffusion, and they are all negligible here.

Supplementary Fig. 3 | Trans-slit migration, diffusion, and steric flux of ions under nanoconfinement. The variation of trans-slit ionic current (Ii) between the ith and (i+1)th nanoslits (Fig. 2e) during kth cyclic voltammetry charging/discharging cycle is decomposed into the components of ion migration, diffusion, and steric flux. a-c, The slit size (d) or interlayer distance of 2D materials is 2 nm. i is 1 (a), 2 (b), and 3 (c), respectively. d-f, d=3 nm. g-i, d=4 nm. The scale of Ii in all panels are set the same for comparison. The direction of diffusion is the same as that of migration, leading to the observed diffusion-enhanced migration (Fig. 2e-g). Note that the direction of steric flux tends to become the same as d decreases.

Supplementary Fig. 4 | Molecular dynamics studies of trans-slit ion migration, diffusion, and steric flux in a graphene membrane-based supercapacitor during charging process. a, Atomic structure of the supercapacitor (details in Methods). Top panel denotes the uncharged case where all carbon atoms possess zero charge. Bottom panel represents the charged supercapacitor, where each carbon atom in left/right electrode possesses a charge of +0.041e/-0.041e, respectively. Here e is the elementary charge. For the feasibility of molecular dynamics simulations to investigate the complex charging dynamics, we adopted the fixed charge method (instead of the constant potential method) and applied the charges on carbon atoms suddenly and hold thereafter in a step-function fashion (instead of the gradual charge increase/decrease in experiments and our PNP simulations). The directions of trans-slit ion migration, diffusion, and steric fluxes are illustrated by blue, red, and purple arrows, respectively (see following for details). b, The differences of electrical potential (Δϕ1, squares), net ion concentration (Δρ1, circles), and total ion density (Δc1, diamonds) between the first and second slit as a function of time. The differences follow the same variation trend, which is qualitatively consistent with the results by mPNP simulations. Particularly, the same variation trends of Δϕ1 and Δρ1 suggest same direction of migration flux and diffusion flux, due to a strong correlation between charge and electrical potential (see discussion in Supplementary Fig. 5), confirming the observed diffusion-enhanced migration in our mPNP simulations.

Supplementary Fig. 5 | Electric potential and net ion concentration inside nanoslits of membrane-based supercapacitors. a, Electric potential well (solid black curve) along x-direction inside the ith nanoslit, calculated by mPNP at y=0 in Fig. 2e. The shaded regions indicate two 2D material sheets used to construct the boundaries/walls of the nanoslit, which have an identical positive surface potential ϕm in this case. The counter-ions in nanoslit must screen ϕm from both sheets, while in open space they only screen ϕm from one electrode surface by forming an EDL (Fig. 2d). Therefore, the potential well in nanoslit is contributed the overlap of two EDLs from each of the 2D material sheets (dotted grey curves). b, ϕi and the net ion concentration (ρi) in three adjacent nanoslits in a nanoslit network at the instant where the cycle number is around k+0.25. Here d=2 nm. It is clear that a more negative value of ρi corresponds to a lower ϕi. This is reasonable because according to the sketch in (a), a higher anion concentration gives rise to better screening of positive fm and thus a smaller ϕi. c, The trans-slit voltage (or potential difference, Δϕ2=ϕ3−ϕ2) and net ion concentration difference (Δρ2=ρ3−ρ2) between the 3rd and 2nd nanoslit during a typical charging/discharging cycle. The observed strong correlation confirms that the observation in (b) persists during the whole charging cycle. Therefore, we can understand why the ion migration (driven by Δϕ) and net ion diffusion (driven by Δr) have the same direction (Fig. 2 and Supplementary Fig. 3). Note that the trans-slit voltage decreases after reaching the maximum at point α (see discussion in Supplementary Fig. 8).

Supplementary Fig. 6 | Trans-slit voltage (Δϕi), current (Ii), and the directly derived dynamically varying ionic resistivity during a typical charging/discharging cycle. a-l, Δϕi (blue squares) and Ii (dashed lines) between the ith and (i+1)th nanoslit in membranes with slit height d =1.5 (a-c), 2 (d-f), 3 (g-i), and 4 nm (j-l), respectively. The index i of a nanoslit indicates its location in x-axis in the supercapacitor electrode (Supplementary Fig. 1). The trans-slit ionic resistivity derived directly using Δϕi and Ii, and it is studied here for comparison for intrinsic ion transport in nanoslits with different heights. The significant variation of ionic resistivity during a charging cycle clearly indicates its dynamic feature. m-p, The resistivity remains identical for different nanoslits in the same membrane, although both Δϕi and Ii decrease with the increasing i. This observation is valid for different values of d. Overall, we can draw three conclusions regarding dynamic ion resistivity. First, in a membrane electrode with a given slit size, the dynamic ion resistivity value is independent of the slit location. Second, the magnitude of dynamic resistivity increases as slit size d increases, which is counter-intuitive (see main text for discussion). Third, the difference between the maximum and minimum of the dynamic ionic resistivity (variation magnitude) seems unchanged (or only slightly increased) with the increasing d, which is summarized in Fig. 3d. As such, the difference between the maximum and minimum resistance is larger in small slit size, which can also be inferred from the dependence of deviation between Δϕi and Ii during charging/discharging on d. This indicates that the effect of dynamic variation of ionic resistance becomes more profound as d decreases (Fig. 3c and Supplementary Fig. 9).

Supplementary Fig. 7 | Net ion storage in ith nanoslit and the trans-slit resistivity and resistance. a-c, Net ion storage in the ith nanoslit of a membrane electrode [ρi: concentration, Qi/Qimax: normalized storage used in equation (2)], where the slit size (d) is 2 (a), 3 (b), and 4 nm (c), respectively. The insets are the magnification of the lines in the grey boxes, showing that ρi>ρi+1. The slight differences of ρi among nanoslits are responsible for the trans-slit voltage Δϕi, due to the charge-potential correlation (Supplementary Fig. 5). d-f, Trans-slit resistivity (normalized with respect to its maximum) and resistance described by net ion storage through equation (2) (Rc+Rd, solid lines), which is consistent with that directly obtained from the voltage-current relation in mPNP simulation (filled circles, same as that in Supplementary Fig. 6h, l, p). d is 2 (d), 3 (e), and 4 nm (f). As we are interested in understanding the effect of intrinsic ion properties (e.g., ρi) on geometry-related quantities (e.g., resistance) in nanoslits, the relative change in resistivity is discussed. (1), In nanoscopic level, ions accumulate in nanoslits and increase ρi during charging, leading to the dynamically varying trans-slit resistivity. (2), In terms of the nano-macro translation, ρi is a quantity also available in macroscopic models allowing for the description of resistivity, while the conventional definition of resistivity involves the total ion concentration (ci) which is only available in nanoscale. (3), In macroscopic level, Rc+Rd automatically includes the contribution of migration, diffusion, and steric flux, while the nanoscopic quantity ci is only able to account for migration (Supplementary Fig. 8c). Note that the small difference in ρi results in nearly identical resistivity for different i. Also note that the difference between the maximum and minimum of resistivity decreases as d increases. This is because ion accumulation in ρi becomes more notable as d decreases where EDL overlaps substantially. This indicates that the dynamically varying resistivity, although with an unchanged absolute difference (Δr in Fig. 3d), has a relatively smaller overall effect with larger d.

Supplementary Fig. 8 | Trans-slit current of nanoconfined ions: impact on trans-slit voltage and its origin from diffusion-enhanced migration. a, Variation of the net ions and electrical potential (indicated by grayscale) in the ith and (i+1)th nanoslits, as ions are carried by the trans-slit current (Ii, green arrow) during a charging process at the time points α and β in Supplementary Fig. 5c. The sign of the net ion is negative here due to the positive potential on 2D material. Note that the direction of Ii is opposite to the flow of net ions (red arrow) due to the negative sign. b, Calculated fractions of Ii (green diamonds) and net ions (Qi, purple circles) in three neighbouring nanoslits at the point α, with respect to Qm and Im. Qi=ρidVi, where Vi is the volume of the ith nanoslit. Qm=iQi represent the net ions stored in the entire membrane electrode, and Im is the total current in the circuit. Note that Qm cancels the negative sign of Qi in the fraction. Before the point α is reached during charging, Δϕi and Δρi in Supplementary Fig. 5c increase because anions from the bulk electrolyte always reach the ith nanoslit before the (i+1)th, i.e., a higher fraction of Qi than Qi+1. The higher fraction of Qi continuously moves/supplies the ions from the ith nanoslit to the (i+1)th through the current Ii. Note that Ii>Ii+1, because when ions are travelled to the (i+1)th nanoslit, some ions are stored/left and less ions keep travelling to the (i+2)th nanoslit. As charging proceeds beyond α, this ion supply process decreases the difference between Qi and Qi+1, i.e., accounting for the observed decrease in Δϕi and Δρi in Supplementary Fig. 5c. c, Quantitative description of migration by Δϕ2 and the total ion concentration (c2), accounting for the nonlinear relation between the trans-slit voltage and migration only. θ is a constant analogous to mobility. d, Contribution to the accumulation of c2 (dash-dotted curve) from migration (blue), diffusion (red) and steric flux (violet) during a charging cycle. e, Diffusion current compensated by steric flux, further contributing to the nonlinearity between the trans-slit voltage and current.

Supplementary Fig. 9 | Trans-slit conductance and conductivity as a function of the slit size (d). a, The conductance at the beginning of charging has the minimum value (blue triangles), and it is nearly constant in spite of different values of d. When d decreases, only the space between 2D materials (dark slats in Fig. 2b) is reduced; the interfacial area between the 2D materials and nanoconfined electrolyte remains unchanged. This suggests that the conduction is most likely relevant to the ions in the interface, i.e., surface-conduction. b, The conductivity is the inverse of the resistivity in Fig. 3d. The difference between the conductivity maximum and minimum reaches increases when d decreases while Δr in Fig. 3d remains nearly unchanged, confirming that the nonlinear voltage-current relation, although exists in nanoslits with all sizes, dominates as d decreases.

Supplementary Fig. 10 | Spatial investigation of the local potential and current in nanoscopic simulation for the study of resistance distribution in macroscale. a, Spatial investigation of potential (colour-scale unit: mV) and current (arrows) in nanoslits by mPNP at a time point during the charging process. The potential applied on 2D materials has not reached its maximum (200 mV) yet. d=1.5 nm here. The length of the white arrows indicates the magnitude of the local current density or ion flux. Note that the arrows for ion flux across two nanoslits are clearly longer located near the material surface than those at y=±L. b, Electrical potential (ϕ, blue line) and the derived local resistance (red line) and along the violet dashed line in (a). The local resistance clearly has large positive (R+) and negative (R‒) values in the pink region, while in the cyan region the local resistance is very small. R+ and R‒ result from the sharp slope of ϕ with opposite values in the left and right red regime, due to ion accumulation in overlapped EDL, with a unidirectional current. Note that, although this spatial investigation is only analysed from a snapshot, R+ and R‒ should be time-dependent. c, A schematic diagram showing that the effect of serial connected R+ and R‒ on trans-slit ion transport is equivalent to the sum of Rc and Rd.

Supplementary Fig. 11 | Nanoscopic capacitance of nanoslits and the construction of macroscopic equivalent circuits. a, Nanoscopic capacitance (Cslit) of different nanoslits (represented by i) in the same membrane as a function of time, which all coincide with each other. The slit size (d) is 2 nm. Inset: linear fit of the stored charge (|Qi|) vs. the voltage (|ϕm−ϕi|) in a nanoslit. This shows that Cslit is constant in electrode, both in space and time. b, Cslit of the 2nd nanoslit as a function of time, where d changes from 1 to 5 nm. When d>1 nm, Cslit is a constant over the charging cycle. Inset: Cslit in the middle of the charging cycle as a function of d. c, Nano-circuitry model (NCM, left) and transmission line model (TLM, right) for the half-cell of a supercapacitor. d, CV diagrams by NCM for a membrane-based supercapacitor consisting of 6 layers of 2D materials with d=1.5 nm. The variation of Vm is smoothed here (bottom panel in Fig. 2c). Note that, in order to calculate Rd conveniently for NCM, Qi used in equation (2) could be obtained from mPNP (solid line) or approximated by TLM (hexagon), where the resultant CV diagrams are identical here.

Supplementary Fig. 12 | Impact of nanoconfined ions on the macroscopic performance of supercapacitors, described by the nano-circuitry model (NCM) and the transmission line model (TLM). The supercapacitors are operated at the charging/discharging rates of 20 mV/μs (a-d) and 4 mV/μs (e-h). The value of resistance and capacitance for each circuit element is obtained from previous mPNP studies where d=1.5 nm and γ=0.5. The degree of nanoconfinement effect is weighted by γ in NCM, where γ=0.9 indicates severely confined ions in membrane electrodes (see Supplementary Fig. 7 for more discussion of γ). Note that TLM corresponds to the NCM where γ=0. The membrane electrodes of the supercapacitors consist of 6 (a, e), 10 (b, f), 20 (c, g), and 50 (d, h) layers of 2D materials. The slit size (d) is 1.5 nm. Vm is not smoothed here, as mPNP simulation is not required. These results give two implications at the macroscopic level. (1), Although the nanoconfined ions may only have little effects in membranes with a few layers of 2D materials (e, f), when the number of layer increases, the collective effect of nanoconfined ions increases and it could change the macroscopic behaviour (g, h). (2), The difference between (a, b) and (e, f) implies that the nanoconfinement effect could have higher impact when the charging/discharging rate is high.

Supplementary Fig. 13 | Dynamically varying ion resistance as the mechanism of the asymmetric CV diagram. Charging process is a balance between ion storage and transport. In addition to the general interest on the capacitance and voltage in EDL for ion storage, the limitation of ion supply by resistive transport across nanoslits must also be noted. a, The CV diagrams obtained by TLM (dashed lines) for any values of Rc does not reproduce the asymmetric CV obtained by NCM (dark cyan line), as the TLM-obtained CV is always symmetric. This implies that the nanoscopic ion dynamics described by NCM can be fundamentally different from that described by TLM. Here Rc=5 Ω. The minimum value of Rc+Rd for NCM could reach 0.5 Ω. Purple to orange for TLM: Rc changes from 5, 2, 1, to 0.5 Ω, with the corresponding charging time constants tc=RC varying from 0.4, 0.16, 0.08, to 0.04 μs. Here C=0.08 μF is the capacitance of the electrode. b, The nanoscopic discussion of ion dynamics in NCM, for the interpretation of the asymmetric CV, could be obtained by the time-dependant trans-slit resistance (R=Rc+Rd, bottom panel). There are two perspectives to understand this. (1), Direct discussion of nanoscopic ion transport by R. In nanoslit network, the trans-slit voltage (Δϕi) stimulates ion transport across nanoslits, which can be modulated by R. This modulation changes the trans-slit current which carries ions for storage, and hence changes the total current Im. Here i=2 is demonstrated. At the beginning of charging, Δϕ2 increases rapidly in the positive direction (dark cyan squares in the top panel) to provide enough current for ion storage due to the large resistance (left purple region). As charging proceeds, Δϕ2 decreases as the small value of R requires only a low voltage to supply enough ions for storage (orange region). A small Δϕ2 would induce a large voltage across Cslit in Supplementary Fig. 11c, allowing for storage of more ions. However, as the large R at the beginning of charging limited the storage of ions to a low value, the current must reach a remarkably high value to drastically increase ion storage. At the beginning of discharging, Δϕ2 slowly increase in the negative regime to reverse the charging current to discharging current due to the small value of R. At the end of discharging, Δϕ2 approaches to a value determined by TLM with large R (right purple region). (2), Another perspective to understand the asymmetric CV diagram is through tc, which describes the time needed for the charging/discharging current to reach a steady state. The steady state can be described by a constant value of Im where trans-slit ion transport can steadily supply ions for storage in nanoslits. When t<tc, the resistive trans-slit current provides ions at a low rate to nanoslits for storage, the trans-slit voltage keeps increasing such that ion storage rate increases towards the steady state. However, tc is not constant in NCM due to the varying trans-slit resistance. As charging proceeds, the current described by NCM increases faster than that defined by TLM with large R due to the decreased tc. At the beginning of discharging, the current rapidly reaches a “steady state” due to the small tc. Although tc further decreases during discharging, the current does not change significantly as TLMs with small R are also approaching the “steady state”.

Supplementary Fig. 14 | Nanoscopic evolution of net charge storage in each nanoslit within the membrane electrode of supercapacitors, obtained by transmission line model (a-d, TLM) and nano-circuitry model (e-h, NCM). γ=0.9 for NCM here, all conditions are the same as those for Supplementary Fig. 12. The initial two CV charging/discharging cycles are shown. Net charge stored in the nanoslit with high index (i) near the current collector is clearly smaller than that with low index near the bulk electrolyte, primarily due to slow ion transport6,61,62. Here NCM suggests that, due to the decreased trans-slit ionic resistance or enhanced ion transport under nanoconfinement discussed in Supplementary Fig. 13b, the net charge inside the electrode can increase, for example, the charge stored in the 19th layer described by NCM (9.88 nC) is around 42% higher than that described by TLM (6.95 nC). This results in a better charge storage performance demonstrated by the larger area of CV curve by NCM than that by TLM in Supplementary Fig. 12. Note that these results by both circuit models are obtained within a minute using a laptop computer, in comparison with days or weeks of calculation by mPNP.

Extended Data Table 1 | Parameters used for the molecular dynamics siumation

| Atoms | ϵ (Kcal/mole) | σ (Å) | Charge (e) |
| --- | --- | --- | --- |
| H | 0 | 2.058 | +0.424 |
| O | 0.155 | 3.166 | -0.848 |
| K | 0.087 | 3.143 | +1 |
| Cl | 0.15 | 4.045 | -1 |
| C | 0.068 | 3.407 | 0 (before charging) ±0.041* (charging) |

*Each carbon atom in the left electrode is assigned +0.041, while those in the right -0.041.

Supplementary Fig. 15 | Identification of the dynamically varying resistance (Rd) by evolutionary algorithm (EA). Identification of Rd from the non-linear relation between the time integral of trans-slit current (I2) and voltage (Δϕ2) in the 2nd nanoslit with d=2 nm. The light blue squares are the data directly obtained from mPNP simulation, while the solid curve, along with its explicit mathematical expression [equation (2)], is discovered by EA. Since the resistance is identical in different nanoslits (Supplementary Fig. 6), the obtained Rd can be used throughout all nanoslits in the membrane electrode.

# References

1	Bazant, M. Z., Thornton, K. & Ajdari, A. Diffuse-charge dynamics in electrochemical systems. Phys. Rev. E 70, 021506 (2004).

2	Corry, B., Kuyucak, S. & Chung, S.-H. Tests of Continuum Theories as Models of Ion Channels. II. Poisson-Nernst-Planck Theory versus Brownian Dynamics. Biophys. J. 78, 2364-2381 (2000).

3	Qiao, R. & Aluru, N. R. Ion concentrations and velocity profiles in nanochannel electroosmotic flows. J. Chem. Phys. 118, 4692-4701 (2003).

4	Kilic, M. S., Bazant, M. Z. & Ajdari, A. Steric effects in the dynamics of electrolytes at large applied voltages. II. Modified Poisson-Nernst-Planck equations. Phys. Rev. E 75, 021503 (2007).

5	Pilon, L., Wang, H. & d’Entremont, A. Recent Advances in Continuum Modeling of Interfacial and Transport Phenomena in Electric Double Layer Capacitors. J. Electrochem. Soc. 162, A5158-A5178 (2015).

6	Biesheuvel, P. M. & Bazant, M. Z. Nonlinear dynamics of capacitive charging and desalination by porous electrodes. Phys. Rev. E 81, 031502 (2010).

7	Kondrat, S. & Kornyshev, A. Charging dynamics and optimization of nanoporous supercapacitors. J. Phys. Chem. C 117, 12399-12406 (2013).

8	Wang, H., Fang, J. & Pilon, L. Scaling laws for carbon-based electric double layer capacitors. Electrochim. Acta 109, 316-321 (2013).

9	Zhan, C. et al. Computational insights into materials and interfaces for capacitive energy storage. Adv. Sci. 4, 1700059 (2017).

10	Hollingsworth, S. A. & Dror, R. O. Molecular dynamics simulation for all. Neuron 99, 1129-1143 (2018).

11	Merlet, C. et al. On the molecular origin of supercapacitance in nanoporous carbon electrodes. Nat. Mater. 11, 306-310 (2012).

12	Kondrat, S., Wu, P., Qiao, R. & Kornyshev, A. A. Accelerating charging dynamics in subnanometre pores. Nat. Mater. 13, 387-393 (2014).

13	Pean, C., Rotenberg, B., Simon, P. & Salanne, M. Multi-scale modelling of supercapacitors: from molecular simulations to a transmission line model. J. Power Sources 326, 680-685 (2016).

14	Marconi, U. M. B. & Tarazona, P. Dynamic density functional theory of fluids. J. Chem. Phys. 110, 8032-8044 (1999).

15	Zhan, H. Graphene-Electrolyte Interfaces: Electronic Properties and Applications. (Jenny Stanford Publishing, Singapore, 2020).

16	Kundu, P. K., Cohen, I. M. & Dowling, D. R. Fluid Mechanics. (Academic Press, London, 2015).

17	Haken, H., Wolf, H. C. & Brewer, W. D. The Physics of Atoms and Quanta: Introduction to Experiments and Theory. (Springer, Heidelberg, 2005).

18	Wang, X. et al. Influences from solvents on charge storage in titanium carbide MXenes. Nat. Energy 4, 241-248 (2019).

19	Péan, C. et al. On the dynamics of charging in nanoporous carbon-based supercapacitors. ACS Nano 8, 1576-1583 (2014).

20	Jiang, G., Cheng, C., Li, D. & Liu, J. Z. Molecular dynamics simulations of the electric double layer capacitance of graphene electrodes in mono-valent aqueous electrolytes. Nano Res. 9, 174-186 (2016).

21	Uysal, A. et al. Structural origins of potential dependent hysteresis at the electrified graphene/ionic liquid interface. J. Phys. Chem. C 118, 569-574 (2014).

22	Merlet, C. et al. Simulating supercapacitors: can we model electrodes as constant charge surfaces? J. Phys. Chem. Lett. 4, 264-268 (2013).

23	He, Y., Huang, J., Sumpter, B. G., Kornyshev, A. A. & Qiao, R. Dynamic charge storage in ionic liquids-filled nanopores: insight from a computational cyclic voltammetry study. J. Phys. Chem. Lett. 6, 22-30 (2015).

24	Ferguson, T. R. & Bazant, M. Z. Nonequilibrium thermodynamics of porous electrodes. J. Electrochem. Soc. 159, A1967-A1985 (2012).

25	Zhan, H., Cervenka, J., Prawer, S. & Garrett, D. J. Electrical double layer at various electrode potentials: a modification by vibration. J. Phys. Chem. C 121, 4760-4764 (2017).

26	Bard, A. J. & Faulkner, L. R. Electrochemical Methods: Fundamentals and Applications. (John Wiley & Sons, New York, USA, 2000).

27	Borukhov, I., Andelman, D. & Orland, H. Steric effects in electrolytes: a modified Poisson-Boltzmann equation. Phys. Rev. Lett. 79, 435-438 (1997).

28	Kornyshev, A. A. Double-layer in ionic liquids: paradigm change? J. Phys. Chem. B 111, 5545-5557 (2007).

29	Wang, H. & Pilon, L. Physical interpretation of cyclic voltammetry for measuring electric double layer capacitances. Electrochim. Acta 64, 130-139 (2012).

30	Zhan, H. et al. Solvation-involved nanoionics: new opportunities from 2D nanomaterial laminar membranes. Adv. Mater. 32, 1904562 (2020).

31	Nair, R. R., Wu, H. A., Jayaram, P. N., Grigorieva, I. V. & Geim, A. K. Unimpeded permeation of water through helium-leak–tight graphene-based membranes. Science 335, 442-444 (2012).

32	Cheng, C. et al. Ion transport in complex layered graphene-based membranes with tuneable interlayer spacing. Sci. Adv. 2, e1501272 (2016).

33	Zhan, H. et al. Direct fabrication of 3D graphene on nanoporous anodic alumina by plasma-enhanced chemical vapor deposition. Sci. Rep. 6, 19822 (2016).

34	Jackson, J. D. Classical Electrodynamics. (Wiley, 1999).

35	Pean, C. et al. Confinement, desolvation, and electrosorption effects on the diffusion of ions in nanoporous carbon electrodes. J. Am. Chem. Soc. 137, 12627-12632 (2015).

36	Yang, X., Cheng, C., Wang, Y., Qiu, L. & Li, D. Liquid-mediated dense integration of graphene materials for compact capacitive energy storage. Science 341, 534-537 (2013).

37	Ashford, S. A. & Sitar, N. Effect of element size on the static finite element analysis of steep slopes. Int. J. Numer. Anal. Methods Geomech. 25, 1361-1376 (2001).

38	Bhadauria, R. & Aluru, N. R. Multiscale modeling of electroosmotic flow: effects of discrete ion, enhanced viscosity, and surface friction. J. Chem. Phys. 146, 184106 (2017).

39	Pathria, R. K. & Beale, P. D. Statistical Mechanics. (Elsevier Science, Oxford, 2011).

40	Nosé, S. A molecular dynamics method for simulations in the canonical ensemble. Mol. Phys. 52, 255-268 (1984).

41	Hoover, W. G. Canonical dynamics: Equilibrium phase-space distributions. Phys. Rev. A 31, 1695-1697 (1985).

42	Janezic, D. & Orel, B. Implicit Runge-Kutta method for molecular dynamics integration. J. Chem. Inf. Comput. Sci. 33, 252-257 (1993).

43	Zhan, H. et al. Theoretical discussion for electron-density distribution in multicusp ion source. Appl. Phys. Lett. 98, 121501 (2011).

44	Tuckerman, M., Berne, B. J. & Martyna, G. J. Reversible multiple time scale molecular dynamics. J. Chem. Phys. 97, 1990-2001 (1992).

45	Ryckaert, J.-P., Ciccotti, G. & Berendsen, H. J. C. Numerical integration of the cartesian equations of motion of a system with constraints: molecular dynamics of n-alkanes. J. Comput. Phys. 23, 327-341 (1977).

46	Pollock, E. L. & Glosli, J. Comments on P3M, FMM, and the Ewald method for large periodic Coulombic systems. Comput. Phys. Commun. 95, 93-110 (1996).

47	Koza, J. R., Koza, J. R. & Rice, J. P. Genetic Programming: On the Programming of Computers by Means of Natural Selection. (MIT Press, Cambridge, MA, 1992).

48	Liao, Y.-F., Yau, D.-H. & Chen, C.-L. Evolutionary algorithm to traveling salesman problems. Comput. Math. Appl. 64, 788-797 (2012).

49	Ferreira, C. Gene expression programming: a new adaptive algorithm for solving problems. Complex Syst. 13, 87-129 (2001).

50	Weatheritt, J. & Sandberg, R. A novel evolutionary algorithm applied to algebraic modifications of the RANS stress–strain relationship. J. Comput. Phys. 325, 22-37 (2016).

51	Géron, A. Hands-On Machine Learning with Scikit-Learn and TensorFlow: Concepts, Tools, and Techniques to Build Intelligent Systems. (O'Reilly Media, Sebastopol, CA, 2017).

52	Conway, B. E. & Pell, W. G. Power limitations of supercapacitor operation associated with resistance and capacitance distribution in porous electrode devices. J. Power Sources 105, 169-181 (2002).

53	de Levie, R. On porous electrodes in electrolyte solutions: I. capacitance effects. Electrochim. Acta 8, 751-780 (1963).

54	Raistrick, I. D. Impedance studies of porous electrodes. Electrochim. Acta 35, 1579-1586 (1990).

55	Eikerling, M., Kornyshev, A. A. & Lust, E. Optimized structure of nanoporous carbon-based double-layer capacitors. J. Electrochem. Soc. 152, E24-E33 (2005).

56	Ramadesigan, V. et al. Modeling and simulation of lithium-ion batteries from a systems engineering perspective. J. Electrochem. Soc. 159, R31-R45 (2012).

57	Franco, A. A. Multiscale modelling and numerical simulation of rechargeable lithium ion batteries: concepts, methods and challenges. RSC Adv. 3, 13027-13058 (2013).

58	Qiao, R. & Aluru, N. R. A compact model for electroosmotic flows in microfluidic devices. J. Micromech. Microeng. 12, 625-635 (2002).

59	Mirzadeh, M., Gibou, F. & Squires, T. M. Enhanced charging kinetics of porous electrodes: surface conduction as a short-circuit mechanism. Phys. Rev. Lett. 113, 097701 (2014).

60	Huang, K. Statistical mechanics. (Wiley, New York, 1987).

61	Kontturi, K., Murtomäki, L. & Manzanares, J. A. Ionic Transport Processes: in Electrochemistry and Membrane Science. (Oxford University Press, Oxford, 2008).

62	Feinauer, J. et al. MULTIBAT: Unified workflow for fast electrochemical 3D simulations of lithium-ion cells combining virtual stochastic microstructures, electrochemical degradation models and model order reduction. J. Comput. Sci. 31, 172-184 (2019).