# Supporting information

# Bio-adsorption of heavy metals from aqueous solution using the ZnO-modified date pits

Khalid Khazzal Hummadia,b,*, Lin Zhua, and Songbo Hea,c,*

aJoint International Research Laboratory of Circular Carbon, Nanjing Tech University, Nanjing 211816, PR China

bCollege of Engineering, University of Baghdad, 47024, Aljadria, Baghdad, Iraq

cCoRe Pro BV, 9722NJ Groningen, The Netherlands

*Corresponding authors. E-mails: dr.khalid.hummadi@coeng.uobghdad.edu.iq (K. Hummadi), songbohe@gmail.com (S. He).

Figure S1 Particle size distribution of ZnO on fresh ZnO-modified date pits (MDP).

Figure S2 Photos of date pits (DP) and ZnO-modified date pits (MDP).

Figure S3 Effect of (a) pH, (b) particle size, and (c) shaking speed on the removal of heavy metals by the bio-adsorption on MDP. (Bio-adsorption conditions: adsorption temperature 25 °C, initial concentration of 50 mg L-1, MDP dosing of 2 g L-1solution, adsorption time of 180 min; (a) particle size of 200 µm and shaking speed of 300 rpm; (b) pH of 5 and shaking speed of 300 rpm; (c) pH of 5 and particle size of 200 µm.)

Figure S4 Effect of MDP dosing on the removal of heavy metals by the bio-adsorption on MDP. (Bio-adsorption conditions: adsorption temperature 25 °C, initial concentration of 90 mg L-1, MDP dosing of 0.4-6 g L-1solution, particle size of 200 µm, pH of 5, shaking speed of 300 rpm, and adsorption time of 60 min.)

Figure S5 The equilibrium bio-adsorption of heavy metals on MDP and the corresponding non-linear fitting curves using the Langmuir and the Freundlich isotherm models. (Bio-adsorption conditions: adsorption temperature 25 °C, initial concentration of 90 mg L-1, MDP dosing of 0.4 - 6 g L-1solution, particle size of 200 µm, pH of 5, shaking speed of 300 rpm, and adsorption time of 60 min.)

Table S1 Parameters of the two isotherm models for the bio-adsorption of heavy metals on MDP.

|  | qe exp (mg g-1) | Langmuir isotherm model |  |  |  |  |  | Freundlich isotherm model |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | KLan | RLan | qm (mg g-1) | SSR# | R2 |  | KF | n | SSR# | R2 |
| Cu2+ | 77.5 | 0.359 | 0.03 | 82.4 | 28.6 | 0.964 |  | 28 | 3.37 | 8.28 | 0.980 |
| Ni2+ | 68.2 | 0.279 | 0.03 | 71.9 | 25.2 | 0.939 |  | 23 | 3.19 | 2.09 | 0.940 |
| Zn2+ | 50.5 | 0.194 | 0.04 | 66.3 | 20.5 | 0.878 |  | 17 | 3.00 | 1.08 | 0.910 |

# SSR=∑(qe cal - qe exp)2 / N. SSR (Sum of squares due to regression) is the sum of the differences between the predicted value and the experimental data divided by N (total number of experiments).

Table S2 Parameters of various kinetic models for the bio-adsorption of heavy metals on MDP.

|  | C0 (mg L-1) | qe exp (mg g-1) | Pseudo-first order model |  |  |  | Pseudo-second order model |  |  |  | Intra-particle diffusion model |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | qe cal (mg g-1) | k1 (min-1) | R2 |  | k2 (g mg-1 min-1) | qe cal (mg g-1) | R2 |  | kIP (mg g-1 min-1/2) | C (mg g-1) | R2 |
| Cu2+ | 10 | 4.01 | 4.02 | 0.015 | 0.980 |  | 0.081 | 4.45 | 0.996 |  | 0.187 | 1.97 | 0.938 |
|  | 30 | 12.45 | 12.45 | 0.109 | 0.968 |  | 0.196 | 13.26 | 0.986 |  | 0.365 | 8.71 | 0.999 |
|  | 50 | 23.33 | 23.02 | 0.108 | 0.983 |  | 0.267 | 23.78 | 0.999 |  | 0.608 | 16.66 | 0.999 |
|  | 70 | 32.52 | 32.52 | 0.110 | 0.988 |  | 0.277 | 33.78 | 0.999 |  | 0.842 | 23.71 | 0.999 |
|  | 90 | 42.45 | 42.47 | 0.116 | 0.987 |  | 0.250 | 44.84 | 0.999 |  | 1.084 | 31.26 | 0.999 |
| Ni2+ | 10 | 4.04 | 3.42 | 0.012 | 0.960 |  | 0.065 | 3.62 | 0.962 |  | 0.193 | 1.84 | 0.925 |
|  | 30 | 12.2 | 12.03 | 0.080 | 0.975 |  | 0.231 | 12.61 | 0.999 |  | 0.420 | 7.57 | 0.886 |
|  | 50 | 23.46 | 22.52 | 0.092 | 0.975 |  | 0.200 | 24.04 | 0.999 |  | 0.756 | 14.59 | 0.943 |
|  | 70 | 32.48 | 31.78 | 0.107 | 0.987 |  | 0.314 | 33.11 | 0.999 |  | 0.884 | 22.59 | 0.988 |
|  | 90 | 42.30 | 42.06 | 0.111 | 0.982 |  | 0.364 | 43.67 | 0.999 |  | 1.117 | 30.48 | 0.882 |
| Zn2+ | 10 | 3.49 | 3.48 | 0.044 | 0.979 |  | 0.108 | 3.68 | 0.993 |  | 0.178 | 0.15 | 0.943 |
|  | 30 | 13.08 | 12.49 | 0.089 | 0.954 |  | 0.179 | 13.48 | 0.999 |  | 0.448 | 7.88 | 0.966 |
|  | 50 | 22.08 | 21.50 | 0.095 | 0.975 |  | 0.251 | 22.63 | 0.999 |  | 0.679 | 14.42 | 0.991 |
|  | 70 | 31.45 | 30.86 | 0.084 | 0.991 |  | 0.255 | 32.14 | 0.999 |  | 1.018 | 19.99 | 0.944 |
|  | 90 | 40.95 | 40.16 | 0.110 | 0.991 |  | 0.387 | 41.67 | 0.997 |  | 1.041 | 29.29 | 0.987 |

Table S3 Thermodynamic analysis for the bio-adsorption of heavy metals on MDP.

|  | ΔG (KJ mol-1) |  |  |  |  | ΔH (KJ mol-1) | ΔS (J mol-1 K-1) | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 298 K | 308 K | 318 K | 328 K |  |  |  |  |
| Cu2+ | -9.054 | -6.628 | -5.366 | -4.448 |  | -54.181 | -152.73 | 0.968 |
| Ni2+ | -7.014 | -5.768 | -4.156 | -3.180 |  | -46.152 | -131.46 | 0.991 |
| Zn2+ | -6.006 | -5.432 | -3.574 | -3.003 |  | -38.502 | -108.66 | 0.951 |