Supporting Information for

Superior Activation of Persulfate to Degrade Acetaminophen by MgO incorporated CuO/TiO2: Pivotal Roles of non-redox MgO in the Regulation of Performance, Surface Properties and Nonradical Mechanism

Wang Jiang,a Jawad Ali,b Fang Luo,a Siqi Wang,a Jia Wang,a Zhuwei Liao*c and Zhuqi Chen*a

Affiliation:

a Key Laboratory of Material Chemistry for Energy Conversion and Storage, Ministry of Education; Hubei Key Laboratory of Material Chemistry and Service Failure, School of Chemistry and Chemical Engineering, Huazhong University of Science and Technology, Wuhan 430074, China.

b Wuhan Technology and Business University, School of Environment and Biological Engineering, Wuhan 430065, China.

c Urban Construction Engineering Division, Wenhua College, Wuhan 430074, China.

*Corresponding author:

E-mail address: zqchen@hust.edu.cn (Zhuqi Chen), liaozhuwei@outlook.com (Zhuwei Liao)

List of Tables and Figures

Table S1. EDS spectra data of CuOMgO/TiO2.

Table S2. Changes in solution pH before and after reaction and metal leaching.

Table S3. Metal leaching of different Cu modified catalysts.

Table S4. LC-MS data for ACT and transformation products (TPs).

Figure S1. Element mapping of CuOMgO/TiO2. (a) Cu, (b) Mg, (c) O and (d) Ti.

Figure S2. Pores size distribution curves of CuO/TiO2 and CuOMgO/TiO2.

Figure S3. Optimization of catalyst preparation conditions. (a, b) Mg2+ ion loading, (c, d) calcination temperature.

Figure S4. The pHzpc of CuOMgO/TiO2.

Figure S5. XPS spectra of CuOMgO/TiO2 before and after reaction.

Figure S6. Reusability of CuOMgO/TiO2. (a) ACT degradation over five consecutive runs in CuOMgO/TiO2/PS, (b) XRD spectra of CuOMgO/TiO2 before and after reaction.

Figure S7. Influence of DMSO on the degradation of ACT in CuOMgO/TiO2/PS.

Figure S8. ACT degradation in H2O and D2O.

Figure S9. Influence of K2CrO4 on the degradation of ACT in CuOMgO/TiO2/PS.

Figure S10. Solid EPR spectra of CuO, CuOMgO and CuOMgO/TiO2.

Table S1. EDS spectra data of CuOMgO/TiO2.

| Element | Weight (%) | Atomic (%) |
| --- | --- | --- |
| Cu | 3.71 | 1.01 |
| Mg | 8.05 | 5.73 |
| O | 41.7 | 45.0 |
| Ti | 10.6 | 3.84 |

Table S2. Changes in solution pH before and after reaction and metal leaching.

| Initial pH | pH after reaction | Cu2+ leaching (mg/L) | ACT removal efficiency (%) |  |
| --- | --- | --- | --- | --- |
| 3.0 | 4.68 | 1.9 |  | 17.0 |
| 5.0 | 7.24 | 0.26 |  | 76.3 |
| 7.0 | 7.75 | 0.10 |  | 87.0 |
| 8.44 (unadjusted pH) | 7.58 | 0.34 |  | 93.5 |
| 9.0 | 7.70 | 0.17 |  | 90.8 |
| 10.0 | 8.64 | 0.029 |  | 85.6 |
| 11.0 | 10.47 | 0.030 |  | 25.5 |

Table S3. Metal leaching of different Cu modified catalysts.

| Catalyst | ACT removal efficiency (%) | Cu2+ leaching (mg/L) |
| --- | --- | --- |
| CuO | 1.51 | 0.47 |
| CuOMgO | 55.1 | 0.0060 |
| CuO/TiO2 | 33.1 | 2.5 |
| CuOMgO/TiO2 | 93.5 | 0.34 |
| CuOMgO/Kaolin | 91.2 | 0.090 |
| CuOMgO/SBA-15 | 13.1 | 0.020 |
| CuOMgO/ZnO | 52.5 | 0.050 |
| CuOMgO/Al2O3 | 80.3 | 0.040 |
| CuOMgO/SiO2 | 89.3 | 0.080 |
| CuOMgO/MnO2 | 88.9 | 0.060 |
| CuOMgO/Fe3O4 | 82.8 | 0.23 |

Table S4. LC-MS data for ACT and transformation products (TPs).

| Product | Chemical name |  | Molecular structure | Retention time (min) | Experimental mass (m/z) |
| --- | --- | --- | --- | --- | --- |
|  | Acetaminophen |  |  | 5.27 | 152.07 |
| TP-59 | Acetamide |  |  | 1.86 | 59.05 |
| TP-111 | Hydroquinone |  |  | 0.800 | 111.08 |
| TP-101 | N-acetylacetamide |  |  | 7.15 | 101.13 |
| TP-300 | N,N-(5,6-dihydroxy-[1,1'-biphenyl]-2,3'-diyl)diacetamide |  |  | 9.90 | 300.14 |
| TP-118 | Succinic acid |  |  | 1.34 | 118.02 |
| TP-110 | 4-aminophenol |  |  | 7.70 | 110.05 |
| TP-60 | Acetic acid |  |  | 2.36 | 60.05 |

Figure S1. Element mapping of CuOMgO/TiO2: (a) Cu, (b) Mg, (c) O and (d) Ti.

Figure S2. Pores size distribution curves of CuO/TiO2 and CuOMgO/TiO2.

Figure S3. Optimization of catalyst preparation conditions. (a, b) Mg2+ ion loading, (c, d) calcination temperature.

Reaction conditions: PS 0.4 mM, catalyst 0.04g/L, ACT 20 mg/L, reaction temperature 30 °C.

Figure S4. The pHzpc of CuOMgO/TiO2.

Figure S5. XPS spectra of CuOMgO/TiO2 before and after reaction.

Figure S6. Reusability of CuOMgO/TiO2. (a) ACT degradation over five consecutive runs in CuOMgO/TiO2/PS, (b) XRD spectra of CuOMgO/TiO2 before and after reaction.

Reaction conditions: PS 0.4 mM, catalyst 0.04g/L, ACT 20 mg/L, reaction temperature 30 °C.

Figure S7. Influence of DMSO on the degradation of ACT in CuOMgO/TiO2/PS.

Reaction conditions: PS 0.4 mM, catalyst 0.04g/L, ACT 20 mg/L, reaction temperature 30 °C.

# Figure S8. ACT degradation in H2O and D2O,

Reaction conditions: PS 0.4 mM, catalyst 0.04g/L, ACT 20 mg/L, reaction temperature 30 °C.

Figure S9. Influence of K2CrO4 on the degradation of ACT in CuOMgO/TiO2/PS.

Reaction conditions: PS 0.4 mM, catalyst 0.04g/L, ACT 20 mg/L, reaction temperature 30 °C.

Figure S10. Solid EPR spectra of CuO, CuOMgO and CuOMgO/TiO2.