Microplastics and phthalate esters release from teabags into tea drink: Occurrence, human exposure, and health risks

Fatemeh Sadat Kashfi1#, Azam Mohammadi1#, Farzaneh Rostami2, Arezou Savari2, Gabriel E. De-la-Torre3, Jörg Spitz4, Reza Saeedi5,6, Mohammadreza Kalantarhormozi7, Akram Farhadi7, Sina Dobaradaran1,2,8,9*

1Systems Environmental Health and Energy Research Center, The Persian Gulf Biomedical Sciences Research Institute, Bushehr University of Medical Sciences, Bushehr, Iran

2Department of Environmental Health Engineering, Faculty of Health and Nutrition, Bushehr University of Medical Sciences, Bushehr, Iran

3Biodiversity, Environment, and Society Research Group, San Ignacio de Loyola University, Lima, Peru

4Akademie Für Menschliche Medizin GmbH, Krauskopfallee 27, 65388 Schlangenbad, Germany

5Workplace Health Promotion Research Center, Shahid Beheshti University of Medical Sciences, Tehran, Iran.

6Department of Health, Safety and Environment, School of Public Health and Safety, Shahid Beheshti University of Medical Sciences, Tehran, Iran.

7The Persian Gulf Tropical Medicine Research Center, The Persian Gulf Biomedical Sciences Research Institute, Bushehr University of Medical Sciences, Bushehr, Iran.

8Instrumental Analytical Chemistry and Centre for Water and Environmental Research (ZWU), Faculty of Chemistry, University of Duisburg-Essen, Universitätsstr. 5, Essen, Germany

9Centre for Water and Environmental Research, University of Duisburg-Essen, Universitätsstr. 5, Essen, 45141, German

*Systems Environmental Health and Energy Research Center, Boostan 19 Alley, Imam Khomeini Street, Bushehr, 7514763448, Iran. E-mail addresses sina_dobaradaran@yahoo.com, s.dobaradaran@bpums.ac.ir

# FK and AM should be considered as joint first authors.

Contents

1. PAEs analysis

Table S1. The summary of characteristics of teabag brands.

Table S2. Abbreviation, limit of detection (LOD), limit of quantification (LOQ), and recovery percent (R%) for each examined PAE.

Table S3. Average number of detected MPs in different brands of the Persian (A1-A10) and German (B1-B5) teabags.

Table S4. Size, shapes, and color distribution of detected MPs in different brands of the Persian (A1-A10) and German (B1-B5) teabags.

Table S5. PAEs concentration in different brands of the Persian (A1-A10) and German (B1-B5) teabags.

Table S6. EDI of 6 PAEs congeners for teabag consumers.

Fig. S1. Shape (a) and color (b) of detected MPs in different brands of the Persian (A1-A10) and German (B1-B5) teabag.

Fig. S2. Some detected MPs in teabag samples.

Fig. S3. Spectra Raman of some polymers identified in MPs of the teabag samples.

1. PAEs analysis

An Agilent gas chromatography (GC) model 7890 equipped with triple quadrupole mass spectrometer (MS) model 5975C was applied for PAEs analysis. Isolation was performed via a capillary column of polydimethylsiloxane (HP-5 MS (5% phenyl) -95%) built of silica with a film thickness of 0.25 µm.  Helium with a 99.999% purity was used as carrier gas with a flow rate of 1 mL/min. SIM analysis was used for each of the target species. The samples were injected at 290°C in splitless mode. The temperature of the oven was started from 70°C (maintained for 1 min) and then increased to 300°C at 10°C/min, which was maintained at this temperature for 7 min. The ion source and quadrupole temperatures were 230°C and 150°C, respectively. MSD ChemStation software (version E.02.01.1177) was used for data acquisition.

Table S1. The summary of characteristics of teabag brands.

| Tea brand | Place of production | Place of packaging | Tea type |
| --- | --- | --- | --- |
| A1 | India | Iran | Black tea |
| A2 | India | Iran | Black tea |
| A3 | India | Iran | Black tea |
| A4 | Sri Lanka | Iran | Black tea |
| A5 | Sri Lanka | Iran | Black tea |
| A6 | Iran | Iran | Black tea |
| A7 | Iran | Iran | Black tea |
| A8 | Iran | Iran | Black tea |
| A9 | Iran | Iran | Black tea |
| A10 | Iran | Iran | Black tea |
| B1 | Japan | Germany | Green tea |
| B2 | China | China | Green tea |
| B3 | China | Germany | Green tea |
| B4 | China | Austria | Green tea |
| B5 | China | Germany | Green tea |

Table S2. Abbreviation, limit of detection (LOD), limit of quantification (LOQ), and recovery percent (R%) for each examined PAE.

| PAEs | Abbreviations | LOD (ng/mL) | LOQ (ng/mL) | R2 | Recovery (%) | Precision (%RSD) |
| --- | --- | --- | --- | --- | --- | --- |
| Dimethyl phthalate | DMP | 1.68 | 5.56 | 0.993 | 101.3 | 9.4 |
| Diethyl phthalate | DEP | 0.86 | 2.84 | 0.995 | 103.1 | 6.5 |
| Diisobutyl phthalate | DiBP | 0.06 | 0.21 | 0.999 | 87.8 | 3.4 |
| Dibutyl phthalate | DBP | 0.75 | 2.46 | 0.99 | 101.1 | 2.2 |
| Butyl benzyl phthalate | BBP | 1.67 | 5.50 | 0.992 | 100.2 | 5.2 |
| Diethylhexyl phthalate | BEHP | 0.10 | 0.34 | 0.991 | 104.3 | 1.9 |
| Dioctyl phthalate | DOP | 2.11 | 6.97 | 0.996 | 99.5 | 2.7 |

Table S3. Average number of detected MPs in different brands of the Persian (A1-A10) and German (B1-B5) teabags.

| Country (n= Sample number) | Brand | Average ± SD (items/single teabag) |
| --- | --- | --- |
| Iran (n= 30) | A1 | 164.8 |
|  | A2 | 123.2 |
|  | A3 | 1446.8 |
|  | A4 | 425.6 |
|  | A5 | 1370.4 |
|  | A6 | 262 |
|  | A7 | 109.2 |
|  | A8 | 73.6 |
|  | A9 | 74 |
|  | A10 | 73.6 |
| Average ± SD |  | 412.32 ± 22.92 |
| Germany (n= 15) | B1 | 202.8 |
|  | B2 | 59.6 |
|  | B3 | 55.6 |
|  | B4 | 95.2 |
|  | B5 | 323.2 |
| Average ± SD |  | 147.28 ± 7.09 |
| Total average ± SD |  | 323.97 ± 132.52 |
| p-value* |  | 0.04* |
| *Significant at p-value< 0.05 |  |  |

Table S4. Size, shapes, and color distribution of detected MPs in different brands of the Persian (A1-A10) and German (B1-B5) teabags.

| Characteristics | Category | Teabag brand |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | A1 | A2 | A3 | A4 | A5 | A6 | A7 | A8 | A9 | A10 | B1 | B2 | B3 | B4 | B5 |
| Size | 20-100 µm | 31 | 38 | 290 | 37 | 111 | 13 | 8 | 39 | 2 | 4 | 7 | 15 | 0 | 6 | 26 |
|  | 100-250 µm | 209 | 77 | 1415 | 632 | 1418 | 315 | 97 | 94 | 64 | 51 | 211 | 61 | 17 | 84 | 248 |
|  | 250-500 µm | 93 | 60 | 857 | 193 | 1112 | 179 | 69 | 25 | 60 | 60 | 150 | 30 | 30 | 64 | 256 |
|  | 500-1000 µm | 51 | 78 | 854 | 123 | 609 | 119 | 67 | 20 | 40 | 40 | 108 | 34 | 58 | 59 | 244 |
|  | 1000-5000 µm | 28 | 56 | 201 | 79 | 76 | 29 | 39 | 6 | 19 | 27 | 31 | 9 | 34 | 25 | 34 |
| Shape | Fiber | 412 | 308 | 3615 | 1063 | 3426 | 653 | 273 | 183 | 185 | 184 | 503 | 149 | 139 | 238 | 808 |
|  | Film | 0 | 0 | 2 | 1 | 0 | 2 | 0 | 0 | 0 | 0 | 4 | 0 | 0 | 0 | 0 |
| Color | White/Transparent | 404 | 305 | 2773 | 1062 | 3419 | 641 | 265 | 184 | 177 | 175 | 500 | 145 | 126 | 228 | 803 |
|  | Blue/Purple | 0 | 0 | 0 | 0 | 0 | 2 | 0 | 0 | 0 | 0 | 1 | 0 | 0 | 0 | 0 |
|  | Red/Pink | 0 | 0 | 1 | 1 | 4 | 6 | 4 | 0 | 4 | 2 | 2 | 1 | 3 | 2 | 0 |
|  | Black | 8 | 3 | 10 | 1 | 3 | 6 | 3 | 4 | 4 | 7 | 2 | 3 | 5 | 9 | 5 |
| Total |  | 412 | 308 | 3617 | 1064 | 3426 | 655 | 273 | 184 | 185 | 184 | 507 | 149 | 139 | 238 | 808 |

Table S5. PAEs concentration in different brands of the Persian (A1-A10) and German (B1-B5) teabags.

| Country | Brand | DMP |  | DEP |  | DiBP |  | DBP |  | BBP |  | DEHP |  | DOP |  | ∑7PAEs |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (n= Sample number) |  | mg/g | mg/L | mg/g | mg/L | mg/g | mg/L | mg/g | mg/L | mg/g | mg/L | mg/g | mg/L | mg/g | mg/L | mg/g | mg/L |
| Iran (n= 30) | A1 | 0.22 | 0.37 | 0.002 | 0.003 | 0.19 | 0.31 | 0.49 | 0.82 | 0.01 | 0.01 | 4.55 | 7.55 | 0.03 | 0.04 | 5.49 | 9.11 |
|  | A2 | 0.63 | 1.04 | 0.53 | 0.88 | 0.74 | 1.22 | 0.13 | 0.21 | 0.14 | 0.24 | 0.77 | 1.28 | 0.22 | 1.28 | 3.16 | 5.24 |
|  | A3 | 0.21 | 0.35 | <LOD1 | <LOD | 0.84 | 1.4 | 0.01 | 0.02 | <LOD | <LOD | 0.37 | 0.62 | 0.04 | 0.07 | 1.48 | 2.46 |
|  | A4 | 0.08 | 0.13 | <LOD | <LOD | 0.46 | 0.77 | 0.04 | 0.07 | 0.02 | 0.03 | 1.10 | 1.83 | 0.06 | 0.1 | 1.76 | 2.92 |
|  | A5 | 0.76 | 1.26 | 0.03 | 0.05 | 0.47 | 0.78 | 0.14 | 0.24 | 0.01 | 0.02 | 1.8 | 2.99 | 0.05 | 0.09 | 3.27 | 5.43 |
|  | A6 | 0.5 | 0.83 | <LOD | 0.01 | 1.84 | 3.05 | 0.1 | 0.17 | 0.01 | 0.01 | 0.46 | 0.77 | 0.01 | 0.01 | 2.92 | 4.85 |
|  | A7 | 0.66 | 1.10 | 0.6 | 0.99 | 0.72 | 1.20 | 0.16 | 0.27 | 0.02 | 0.03 | 1.87 | 3.10 | 0.12 | 0.19 | 4.14 | 6.87 |
|  | A8 | 0.64 | 1.06 | 0.01 | 0.01 | 0.54 | 0.9 | 0.2 | 0.33 | 0.01 | 0.02 | 0.79 | 1.31 | 0.06 | 0.1 | 2.25 | 3.74 |
|  | A9 | 0.4 | 0.66 | 0.01 | 0.01 | 0.37 | 0.62 | 0.05 | 0.08 | 0.03 | 0.06 | 0.67 | 1.12 | 0.06 | 0.1 | 1.58 | 2.64 |
|  | A10 | 0.72 | 1.20 | 0.05 | 0.08 | 0.42 | 0.7 | 0.11 | 0.18 | 0.12 | 0.20 | 1.15 | 1.91 | 0.03 | 0.06 | 2.60 | 4.31 |
| Average ± SD |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 2.87 ± 1.18 | 4.76 ± 1.96 |
| Germany (n= 15) | B1 | 0.57 | 0.94 | 0.18 | 0.3 | 0.34 | 0.57 | 0.49 | 0.82 | 0.02 | 0.04 | 2.07 | 3.44 | 0.05 | 0.08 | 3.73 | 6.19 |
|  | B2 | 0.18 | 0.30 | 0.09 | 0.14 | 0.49 | 0.81 | 0.13 | 0.21 | 0.01 | 0.02 | 1.32 | 2.19 | 0.03 | 0.05 | 2.24 | 3.72 |
|  | B3 | 0.4 | 0.66 | 0.2 | 0.33 | 0.09 | 0.15 | 0.01 | 0.02 | 0.07 | 0.12 | 0.53 | 0.87 | 0.02 | 0.03 | 1.32 | 2.19 |
|  | B4 | 0.35 | 0.59 | 0.07 | 0.11 | 0.06 | 0.1 | 0.04 | 0.07 | 0.02 | 0.03 | 0.84 | 1.40 | 0.05 | 0.09 | 1.44 | 2.39 |
|  | B5 | 0.11 | 0.19 | 0.06 | 0.1 | 0.14 | 0.24 | 0.14 | 0.24 | 0.03 | 0.05 | 2.45 | 4.06 | 0.18 | 0.30 | 3.12 | 5.17 |
| Average ± SD |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 2.37 ± 0.94 | 3.93 ± 1.55 |
| Total average ± SD |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 4.93 ± 2.27 | 8.18 ± 3.77 |
| p-value* |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.32 | 0.45 |
| 1Limit of detection *Significant at p-value< 0.05 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

Table S6. Estimated daily intakes (EDI) of 6 PAEs congeners (mg/kg-BW/day) for teabag consumers.

| PAEs Age groups | Teabag brand |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | A1 | A2 | A3 | A4 | A5 | A6 | A7 | A8 | A9 | A10 | B1 | B2 | B3 | B4 | B5 |
| DMP |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Child | 0.007 | 0.02 | 0.006 | 0.002 | 0.02 | 0.01 | 0.02 | 0.02 | 0.01 | 0.02 | 0.017 | 0.005 | 0.01 | 0.01 | 0.003 |
| Teens | 0.002 | 0.007 | 0.002 | 0.0008 | 0.008 | 0.005 | 0.007 | 0.007 | 0.004 | 0.008 | 0.006 | 0.002 | 0.004 | 0.00 | 0.001 |
| adults | 0.0006 | 0.002 | 0.0005 | 0.0002 | 0.002 | 0.001 | 0.002 | 0.002 | 0.001 | 0.002 | 0.001 | 0.0005 | 0.001 | 0.0009 | 0.0003 |
| DEP |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Child | 6.89E-05 | 0.03 | 0 | 0 | 0.001 | 0.0001 | 0.02 | 0.0002 | 0.0002 | 0.001 | 0.005 | 0.003 | 0.006 | 0.002 | 0.002 |
| Teens | 2.48E-05 | 0.01 | 0 | 0 | 0.0004 | 5.35E-05 | 0.006 | 5.9E-05 | 6.42E-05 | 0.0005 | 0.002 | 0.0009 | 0.002 | 0.0007 | 0.0006 |
| adults | 5.96E-06 | 0.003 | 0 | 0 | 8.47E-05 | 1.29E-05 | 0.002 | 1.42E-05 | 1.54E-05 | 0.0001 | 0.0005 | 0.0002 | 0.0005 | 0.0002 | 0.0002 |
| DiBP |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Child | 0.006 | 0.1 | 0.03 | 0.014 | 0.014 | 0.05 | 0.02 | 0.02 | 0.01 | 0.01 | 0.01 | 0.01 | 0.003 | 0.002 | 0.004 |
| Teens | 0.002 | 0.04 | 0.009 | 0.005 | 0.005 | 0.02 | 0.008 | 0.006 | 0.004 | 0.004 | 0.004 | 0.005 | 0.001 | 0.0007 | 0.002 |
| adults | 0.0005 | 0.008 | 0.002 | 0.001 | 0.001 | 0.005 | 0.002 | 0.001 | 0.001 | 0.001 | 0.0009 | 0.001 | 0.0002 | 0.0002 | 0.0004 |
| DBP |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Child | 0.02 | 0.004 | 0.0003 | 0.001 | 0.004 | 0.003 | 0.005 | 0.006 | 0.001 | 0.003 | 0.01 | 0.004 | 0.0003 | 0.001 | 0.004 |
| Teens | 0.005 | 0.001 | 0.0001 | 0.0005 | 0.002 | 0.001 | 0.002 | 0.002 | 0.0005 | 0.001 | 0.005 | 0.001 | 0.0001 | 0.0004 | 0.002 |
| adults | 0.001 | 0.0003 | 2.66E-05 | 0.0001 | 0.0004 | 0.0003 | 0.0004 | 0.0005 | 0.0001 | 0.0003 | 0.001 | 0.000326 | 2.66E-05 | 0.0001 | 0.0004 |
| BBP |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Child | 0.0002 | 0.004 | 4.61E-05 | 0.0005 | 0.0003 | 0.0003 | 0.0005 | 0.0004 | 0.001 | 0.004 | 0.0007 | 0.0003 | 0.002 | 0.0005 | 0.001 |
| Teens | 7.53E-05 | 0.001 | 1.66E-05 | 0.0002 | 0.0001 | 9.45E-05 | 0.0002 | 0.0001 | 0.0004 | 0.001 | 0.0003 | 0.0001 | 0.0008 | 0.0002 | 0.0003 |
| adults | 1.81E-05 | 0.0004 | 3.99E-06 | 4.07E-05 | 2.83E-05 | 2.27E-05 | 4.47E-05 | 3.25E-05 | 8.56E-05 | 0.0003 | 6.21E-05 | 2.86E-05 | 0.0002 | 4.5E-05 | 8.3E-05 |
| DEHP |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Child | 0.14 | 0.41 | 0.01 | 0.03 | 0.05 | 0.01 | 0.06 | 0.02 | 0.26 | 0.03 | 0.06 | 0.04 | 0.02 | 0.03 | 0.07 |
| Teens | 0.05 | 0.15 | 0.004 | 0.01 | 0.02 | 0.005 | 0.02 | 0.008 | 0.09 | 0.01 | 0.02 | 0.01 | 0.006 | 0.009 | 0.03 |
| adults | 0.01 | 0.04 | 0.001 | 0.003 | 0.005 | 0.001 | 0.005 | 0.002 | 0.02 | 0.003 | 0.005 | 0.003 | 0.001 | 0.002 | 0.006 |
| DOP |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Child | 0.0008 | 0.27 | 0.001 | 0.002 | 0.002 | 0.0002 | 0.003 | 0.002 | 0.002 | 0.001 | 0.001 | 0.0009 | 0.0006 | 0.002 | 0.005 |
| Teens | 0.0003 | 0.1 | 0.0005 | 0.0007 | 0.0006 | 6.44E-05 | 0.001 | 0.0007 | 0.0006 | 0.0004 | 0.0005 | 0.0003 | 0.0002 | 0.0006 | 0.002 |
| adults | 6.85E-05 | 0.02 | 0.0001 | 0.0002 | 0.0001 | 1.55E-05 | 0.0003 | 0.0002 | 0.0001 | 8.58E-05 | 0.0001 | 7.65E-05 | 5.33E-05 | 0.0001 | 0.0005 |

a)

b)

Fig. S1. Shape (a) and color (b) of detected MPs in different brands of the Persian (A1-A10) and German (B1-B5) teabags.

Fig. S2. Some detected MPs in teabag samples.

Fig. S3. Spectra Raman of some polymers identified in MPs of the teabag samples.