Supplementary Information for

Quick response auto-coding and recognition via microlaser array

Hongrui Shan1,#, Qiheng Wei1,#, Hailang Dai1,#,*,Xueqian Wang2, Hong Yang1,and Xianfeng Chen1,3*

1 State Key Laboratory of Advanced Optical Communication Systems and Networks, School of Physics and Astronomy, Shanghai Jiao Tong University, Shanghai 200240, China

2State Key Lab of Metal Matrix Composites, Shanghai Key Laboratory for Molecular Engineering of Chiral Drugs, School of Materials Science and Engineering, Shanghai Jiao Tong University, Shanghai 200240, China

3Collaborative Innovation Center of Light Manipulations and Applications, Shandong Normal University, Jinan 250358, China

# These authors contributed equally to this work.

*e-mail: hailangdai@sjtu.edu.cn; xfchen@sjtu.edu.cn;

Fig. S1. The PDMS microfluidic chips in experiment. a The microfluidic chip mounted on a reverted fluorescence microscope. b Internal partial magnified image of the microchannel.

Fig. S2. Information of PS microspheres. a SEM images of uncoated PS microspheres. b SEM images of coated PS microspheres with rosin acid. c, d Particle size distribution of microspheres with and without coating, respectively. Scale bar, 5 μm.

Fig. S3. The sensing ability of WGM lasing based on microsphere. a Comparison of lasing spectra of same microsphere with air and pure alcohol condition. b The spectral intensity difference between alcohol and air in the range of 580-660nm.

Fig. S4. GV-QR codes with change of concentration of a single vapor. The large image on the left corresponds to the initial concentration (DCE: 10%, ISO:10%, TOL:10%, TBP:10%, and BTL:10%). a In the case where the concentration of the other 4 vapors remained constant, the concentration of DEC was 12, 14, 16, 18, 20, 22, 24, 26, 28, and 30respectively. b, c, d, e Same as in case a, but the changing gases are ISO, TOL, TBP, and BTL.

Fig. S5. GV-QR codes with change of concentration of 2 vapors. The change of concentrations of the 5 vapors (DCE, ISO, TOL, TBP, and BTL) corresponding to each GV-QR codes are as follows:

a1	10%	10%	10%	10%	10%

a2	10%	12%	10%	10%	10%

a3	10%	14%	10%	10%	10%

a4	10%	16%	10%	10%	10%

a5	10%	18%	10%	10%	10%

a6	10%	20%	10%	10%	10%

a7	10%	22%	10%	10%	10%

a8	10%	24%	10%	10%	10%

a9	10%	26%	10%	10%	10%

a10	10%	28%	10%	10%	10%

a11	10%	30%	10%	10%	10%

a12	12%	10%	10%	10%	10%

a13	12%	12%	10%	10%	10%

a14	12%	14%	10%	10%	10%

a15	12%	16%	10%	10%	10%

a16	12%	18%	10%	10%	10%

a17	12%	20%	10%	10%	10%

a18	12%	22%	10%	10%	10%

a19	12%	24%	10%	10%	10%

a20	12%	26%	10%	10%	10%

a21	12%	28%	10%	10%	10%

a22	12%	30%	10%	10%	10%

a23	14%	10%	10%	10%	10%

a24	14%	12%	10%	10%	10%

a25	14%	14%	10%	10%	10%

a26	14%	16%	10%	10%	10%

a27	14%	18%	10%	10%	10%

a28	14%	20%	10%	10%	10%

a29	14%	22%	10%	10%	10%

a30	14%	24%	10%	10%	10%

a31	14%	26%	10%	10%	10%

a32	14%	28%	10%	10%	10%

a33	14%	30%	10%	10%	10%

a34	16%	10%	10%	10%	10%

a35	16%	12%	10%	10%	10%

a36	16%	14%	10%	10%	10%

a37	16%	16%	10%	10%	10%

a38	16%	18%	10%	10%	10%

a39	16%	20%	10%	10%	10%

a40	16%	22%	10%	10%	10%

a41	16%	24%	10%	10%	10%

a42	16%	26%	10%	10%	10%

a43	16%	28%	10%	10%	10%

a44	16%	30%	10%	10%	10%

a45	18%	10%	10%	10%	10%

a46	18%	12%	10%	10%	10%

a47	18%	14%	10%	10%	10%

a48	18%	16%	10%	10%	10%

a49	18%	18%	10%	10%	10%

a50	18%	20%	10%	10%	10%

a51	18%	22%	10%	10%	10%

a52	18%	24%	10%	10%	10%

a53	18%	26%	10%	10%	10%

a54	18%	28%	10%	10%	10%

a55	18%	30%	10%	10%	10%

a56	20%	10%	10%	10%	10%

a57	20%	12%	10%	10%	10%

a58	20%	14%	10%	10%	10%

a59	20%	16%	10%	10%	10%

a60	20%	18%	10%	10%	10%

a61	20%	20%	10%	10%	10%

a62	20%	22%	10%	10%	10%

a63	20%	24%	10%	10%	10%

a64	20%	26%	10%	10%	10%

a65	20%	28%	10%	10%	10%

a66	20%	30%	10%	10%	10%

a67	22%	10%	10%	10%	10%

a68	22%	12%	10%	10%	10%

a69	22%	14%	10%	10%	10%

a70	22%	16%	10%	10%	10%

a71	22%	18%	10%	10%	10%

a72	22%	20%	10%	10%	10%

a73	22%	22%	10%	10%	10%

a74	22%	24%	10%	10%	10%

a75	22%	26%	10%	10%	10%

a76	22%	28%	10%	10%	10%

a77	22%	30%	10%	10%	10%

a78	24%	10%	10%	10%	10%

a79	24%	12%	10%	10%	10%

a80	24%	14%	10%	10%	10%

a81	24%	16%	10%	10%	10%

a82	24%	18%	10%	10%	10%

a83	24%	20%	10%	10%	10%

a84	24%	22%	10%	10%	10%

a85	24%	24%	10%	10%	10%

a86	24%	26%	10%	10%	10%

a87	24%	28%	10%	10%	10%

a88	24%	30%	10%	10%	10%

a89	26%	10%	10%	10%	10%

a90	26%	12%	10%	10%	10%

a91	26%	14%	10%	10%	10%

a92	26%	16%	10%	10%	10%

a93	26%	18%	10%	10%	10%

a94	26%	20%	10%	10%	10%

a95	26%	22%	10%	10%	10%

a96	26%	24%	10%	10%	10%

a97	26%	26%	10%	10%	10%

a98	26%	28%	10%	10%	10%

a99	26%	30%	10%	10%	10%

a100	28%	10%	10%	10%	10%

a101	28%	12%	10%	10%	10%

a102	28%	14%	10%	10%	10%

a103	28%	16%	10%	10%	10%

a104	28%	18%	10%	10%	10%

a105	28%	20%	10%	10%	10%

a106	28%	22%	10%	10%	10%

a107	28%	24%	10%	10%	10%

a108	28%	26%	10%	10%	10%

a109	28%	28%	10%	10%	10%

a110	28%	30%	10%	10%	10%

a111	30%	10%	10%	10%	10%

a112	30%	12%	10%	10%	10%

a113	30%	14%	10%	10%	10%

a114	30%	16%	10%	10%	10%

a115	30%	18%	10%	10%	10%

a116	30%	20%	10%	10%	10%

a117	30%	22%	10%	10%	10%

a118	30%	24%	10%	10%	10%

a119	30%	26%	10%	10%	10%

a120	30%	28%	10%	10%	10%

a121	30%	30%	10%	10%	10%

Fig. S6. Tests for detection and identification of 10 sets of mixed gases. The concentration of the input mixed vapors (DCE, ISO, TOL, TBP, and BTL, respectively) is displayed on the right-hand side of each QR code, while the concentration of the output is displayed below. The table contains the errors for the 10 sets of tests.

Table 1 Detailed testing results of 10 sets of mixed vapors

| Test Num. | Input | Output | Error |
| --- | --- | --- | --- |
| T1 | 14.50% 10.60% 10.00% 10.00% 10.00% | 14.35% 10.74% 9.98% 9.93% 9.89% | 0.15% -0.14% 0.02% 0.07% 0.11% |
| T2 | 11.60% 11.20% 10.00% 10.00% 10.00% | 11.77% 11.14% 9.70% 10.07% 9.88% | -0.17% 0.06% 0.30% -0.07% 0.12% |
| T3 | 12.80% 13.60% 10.00% 10.00% 10.00% | 13.05% 13.69% 9.68% 10.08% 10.04% | -0.25% -0.09% 0.32% -0.08% -0.04% |
| T4 | 12.60% 11.60% 10.00% 10.00% 10.00% | 12.55% 11.67% 9.70% 10.02% 9.96% | 0.05% -0.07% 0.30% -0.02% 0.04% |
| T5 | 12.30% 13.10% 10.00% 10.00% 10.00% | 12.14% 12.81% 10.24% 10.09% 9.99% | 0.16% 0.29% -0.24% -0.09% 0.01% |
| T6 | 15.20% 10.00% 10.00% 10.00% 10.00% | 14.78% 9.70% 10.29% 10.04% 9.89% | 0.42% 0.30% -0.29% -0.04% 0.11% |
| T7 | 12.40% 10.00% 10.00% 10.00% 10.00% | 12.07% 9.67% 10.43% 10.03% 9.93% | 0.33% 0.33% -0.43% -0.03% 0.07% |
| T8 | 13.60% 10.00% 10.00% 10.00% 10.00% | 13.75% 10.45% 9.74% 9.93% 9.87% | -0.15% -0.45% 0.26% 0.07% 0.13% |
| T9 | 17.00% 10.00% 10.00% 10.00% 10.00% | 17.14% 9.86% 9.72% 10.10% 9.92% | -0.14% 0.14% 0.28% -0.10% 0.08% |
| T10 | 20.00% 10.00% 10.00% 10.00% 10.00% | 20.24% 10.05% 9.57% 9.97% 9.93% | -0.24% -0.05% 0.43% 0.03% 0.07% |

The artificial neural network

The artificial neural network consists of three layers, the input layer, hidden layer and output layer. A vector of data X1 generated by the GV-QR code is entered into the input layer and dealt with a weight matrix W1.

U1=W1*X1

Then an activation function σ1 is used to generate X2.

X2=σ1(U1)

Finally, with weight matrix W2 and activation function σ2, we can get the gas composition vector Y form the output layer.

U3= W2*X2

Y=σ2(U3)

Other supporting information attachments（separate file）

A1 and A2 The videos titled "A1_One vapor change" and "A2_Two vapors change" show the GV-QR codes undergoing changes in response to the presence of one or two different vapors, respectively.

A3 and A4 Excel files containing two matrices named “A3_Matrix_m” and “A4_Matrix_n”, respectively, which include the results of neural network learning.

Fig. S4_55figures in detail 55 separate images corresponding to Fig. S4

Fig. S5_121figures in detail 121 separate images corresponding to Fig. S5