| BP a c c/a B B’ E0 |  |  |  |
| --- | --- | --- | --- |
| RS (B1) This work WC-GGA | 4.3069 169.5037 3.9588 -733.2159 |  |  |
| LDA PBE-GGA Experiment Calculation | 4.2729 177.7375 4.0579 -731.1849 4.3276 161.9762 4.2345 -733.8020 4.327a 155a2.9800a 4.320b 171b2.82b 4.339c 155c 4.332d 161d 4.32j 156.822j |  |  |
| ZB (B3) This work WC-GGA LDA PBE-GGA Experiment Calculation | 4.5250 169.1176 3.7726 -733.366 4.4946 175.6060 3.7709 -731.3366 4.5523 161.3763 3.7916 -733.9602 4.538e,f , g173e, f, g 4.558d 166d 4d 4.546h 166h 3 h |  |  |
| CsCl (B1) This work WC-GGA | 2.7083 141.7342 3.8937 -733.1026 |  |  |
| LDA PBE-GGA Experiment Calculation | 2.6865 2.7238 | 143.5897 133.5993 | 3.1755 -731.0687 3.3451 -733.6883 |
| NiAs (B8) This work WC-GGA LDA PBE-GGA Experiment Calculation | 3.1993 5.2281 1.6341 169.5081 3.7858 -1466.7305 |  |  |
|  | 3.1420 5.2157 1.6600 170.9170 3.9570 -1468.2217 |  |  |
|  | 3.2168 5.3080 1.6501 165.2083 3.8933 -1450.7702 |  |  |
| Wurtzite This work WC-GGA (B4) LDA PBE-GGA Experiment Calculation | 3.0492 5.0879 1.6686 158.8082 5.2567 -1466.3946 3.0268 5.0326 1.6627 162.1720 6.0124 -1497.2010 3.1055 5.1389 1.6548 159.7136 5.2467 -1459.1236 |  |  |

aRef [30], bRef [56], cRef [13], dRef [39], eRef [57], fRef [16], gRef [17], hRef [18], iRef [58], jRef [59].

Table 1 : The lattice parameters (in Å), the c/a ratio, the internal parameter (in Å), the compressibility modulus (in GPa), its pressure derivative and its equilibrium energy E0 (in Ry) of the different phases considered for compound BP.

| BAs a c c/a B B’ E0 |  |  |
| --- | --- | --- |
| RS (B1) This work WC-GGA LDA PBE-GGA Experiment Calculation | 4.5905 135.0548 3.6802 -4570.6757 4.5502 146.2145 4.1851 -4565.2683 4.6258 124.4247 3.7659 - 4571.7650 4.619a 135a 3.44a 4.583b 143b |  |
| ZB (B3) This work WC-GGA LDA PBE-GGA Experiment Calculation | 4.7765 140.0776 4.0496 -4570.8027 4.8148 131.3025 3.9698 -4571.8985 4.8135 130.7531 4.3923 -4571.8984 4.777c 4.77d, e 145d, e 4.726f 147f 3f 4.784g ,h 145g, h 3g ,h |  |
| CsCl (B1) This work WC-GGA LDA PBE-GGA Experiment Calculation | 2.9170 114.9917 4.3663 -4570.582 |  |
|  | 2.8891 2.9409 | 123.1169 4.3719 -4565.1700 105.1903 4.7145 -4571.6717 |
| NiAs (B8) This work WC-GGA LDA PBE-GGA Experiment Calculation | 3.2536 5.3796 1.6534 134.0138 4.1652 -9141.3223 3.2212 5.3474 1.6602 129.3689 3.9965 -9132.8964 3.2469 5.3534 1.6488 132.3210 4.0369 -9131.8974 |  |
| Wurtzite This work WC-GGA (B4) LDA PBE-GGA Experiment Calculation | 3.3236 5.4740 1.6436 140.1808 4.0894 -9141.6031 3.3036 5.4493 1.6698 138.2215 3.9871 -9141.36985 3.3130 5.4952 1.6587 139.9987 4.0033 -9141.5994 |  |

aRef [56], bRef [18], cRef [39], dRef [30], eRef [57], fRef [60], gRef [58], hRef [59].

Table 2 : The lattice parameters (in Å), the c/a ratio, the internal parameter (in Å), the compressibility modulus (in GPa), its pressure derivative and its equilibrium energy E0 (in Ry) of the different phases considered for compound BAs.

| BN a c c/a B B’ E0 |  |  |
| --- | --- | --- |
| RS (B1) This work WC-GGA LDA PBE-GGA Experiment Calculation | 3.6087 397.0617 3.97 -159.084067 3.4653 418.0691 4.18 -158.239040 3.5096 381.3912 3.81 - 159.135896 3.493a 425.000a 3.493b 425.000b 3.580c 480.000c 3.500d 408.000d |  |
| ZB (B3) This work WC-GGA LDA PBE-GGA Experiment Calculation | 3.6087 397.0617 3.8496 -159.084067 3.4653 418.0691 3.9732 -158.239040 3.5096 381.3912 4.0894 -159.395343 3.493 3.620e 3.615a,f 3.575j 386.0000j 3.576h 397.0000h 3.649i 366.0000i 3.606g 367.0000g 3.623c 365.0000c |  |
| CsCl (B1) This work WC-GGA LDA PBE-GGA Experiment Calculation | 2.3079 255.9973 4.446 -158.538708 |  |
|  | 2.2855 2.3233 | 282.4169 4.496 -157.682225 239.8424 4.871 -158.847755 |
| Wirtzite (B4) This work WC-GGA LDA PBE-GGA Experiment Calculation | 2.4908 4.00621.608 387.2968 4.2642 -318.161482 2.3512 3.9034 1.6602 129.3689 4.3475 -319 .8964 1 3.2769 5.3915 1.6488 132.3210 4.3966 -322.897421 2.536k 4. 19k 1.6522k |  |
| NiAs (8) This work WC-GGA LDA PBE-GG Experiment Calculation | 2.5490 4.208 1.650 387.2968 4.77594 -317.657123 2. 4415 4.0768 1.6698 378.2815 3.9871 -319.369851 2.1965 3.6433 1.6587 359.9977 5.0133 - 320.59942 |  |

aRef [61], bRef [62], cRef [63], dRef [64], eRef[65], fRef[66], gRef [67], hRef [68], iRef[69], jRef [70],kRef [71].

Table 3 : The lattice parameters (in Å), the c/a ratio, the internal parameter (in Å), the compressibility modulus (in GPa), its pressure derivative and its equilibrium energy E0 (in Ry) of the different phases considered for compound BN.

| BBi a c c/a B B’ E0 |  |  |  |
| --- | --- | --- | --- |
| RS (B1) This work WC-GGA LDA PBE-GGA Experiment Calculation | 5.2260 69.5937 3.8868 -43209.8275 5.1775 77.7875 4.0590 -43189.1808 4.3276 61.9762 4.9754 -4333.80208 5.22a 4.918b 5.198 |  |  |
| ZB (B3) This work WC-GGA LDA PBE-GGA Experiment Calculation | 5.4754 86.1176 3.7726 -43209.8795 5.4241 87.6060 3.7709 -43189.2367 5.3523 86.3763 3.7916 -43343.9602 5.392d 5.390e 5.416f 83.99f 4.36f 5.416h 86.27h 4.6h 5.529g 72.209g 4.73g |  |  |
| CsCl (B1) This work WC-GGA LDA PBE-GGA Experiment Calculation | 3.3176 81.2217 3.8937 -43209.7640 |  |  |
|  | 3.2214 3.1987 | 83.5897 80.5993 | 3.9955 -4356.9845 4.0451 -4373.6883 |
| NiAs (B8) This work WC-GGA LDA PBE-GGA Experiment Calculation | 3.7135 6.1156 1.6341 84.3785 3.9921 -43166.7305 3.1420 5.2157 1.6600 82.9170 3.9570 -43468.2217 3.2168 5.3080 1.6501 85.2083 3.8933 -43285.6921 |  |  |
| Wurtzite (B4) This work WC-GGA LDA PBE-GGA Experiment Calculation | 3.8570 6.3487 1.6686 80.8661 5.2567 -86419.7568 3.6542 5.8785 1.6087 81.7654 5.876 -86321.8764 3.7702 6.2328 1.6532 83.1253 5.231 - 86543.9810 |  |  |

aRef[72], bRef [73], cRef [74], dRef [75], eRef[76], fRef[77],  hRef [78].

Table 4 : The lattice parameters (in Å), the c/a ratio, the internal parameter (in Å), the compressibility modulus (in GPa), its pressure derivative and its equilibrium energy E0 (in Ry) of the different phases considered for compound BBi.

Pt (GPa)

Présent travail Autre calcule

BP

B3→B1 130.66 118a, 110b, 160c, 111d B3→B2 183.94 B3→B8 199.74 B1→B4137.96

Bas

B3→B197.89 98a, 93b, 110e, 141f, 105g, 125h(exp) B3→B2 209.79 B3→B8 142.11 B4→B1 98.64 B4→B8 154.72 B4→B2 232.10

BBi B3→B123.86 B3→B243.98 B3→B865.54

BN

B1→B4 0.7587 B1→B8 38.1661 B3→B8 51.0971

aRef [12], bRef [31], cRef [79], dRef [80], fRef[81], gRef [82], hRef [32].

Table 5  : Calculated transition pressures for the studied binary compounds.

Eg

Nos calcules Exp Autre calcules

WC-GGA mBj

BP Zinc blende Γ→∆min 1.103 1.8190 - 1.24b,d(GGA), 1.91b(mBj), 1.831g, 1.87h, 1.85k(mBJ), 1.147k(WC-GGA), 1.863l(mBj) WurtziteΓ→M1.542 2.3162 NaClMétallique Métallique CsCl Métallique Métallique NiAs Métallique Métallique

BAs Zinc blendeΓ→Δmin 1.163 1.690 1.60e 1.21d(GGA), 1.25f, 1.821g(mBj), 1,93e, 1.674i 1.686m(mBJ) , 1.092m Wurtzite Γ→M1.321 2.033 NaClMétallique Métallique CsCl Métallique Métallique NiAs Métallique Métallique

BBi Zinc blende Métallique Métallique 0.35a, 0.949b and Mettalicc Wurtzite Métallique Métallique NaCl Métallique Métallique CsCl Métallique Métallique NiAs Métallique Métallique

BN Zinc blendeΓ→Δmin4.479 5.6131 6.3j 6.31k , 4.19l, 4.40m, 4.38n Wurtzite Γ→K5.844 6.0432 5.81P NaClΓ→K 5.986 6.679 CsCl Métallique Métallique NiAsMétallique Métallique

aRef [90], bRef [91], cRef [37], dRef [14], eRef[92], fRef[18,39 ],  gRef [60], hRef [93] , iRef [94], jRef [38], kRef [95], lRef[96], mRef[97], nRef [98],pRef [100].

Table 6  : Bandgap energy Eg (eV) for binary compounds BBi, BAs, BP and BN using the WC-GGA approximation, mBj.

.

|  | Nos calculs WC-GGA ε1(0) | Autre calculs | Nos Calculs Wc-GGA n(0) | Autre calculs |
| --- | --- | --- | --- | --- |
| BP | 9.5961 | 8.1a | 3.0546 | 3.34a |
| BN | 4.6798 |  | 2.1678 |  |
| BBi | 22.097 |  | 4.6898 |  |
| BAs | 10.216 |  | 3.2198 |  |

aRef [91]

Table 7 :  The static dielectric function ε1(0) and the static refractive index n(0) calculated for the compounds BP, BN, BBi and BAs.