1 The calculation workflow and methodology of the process window

1.1 Melt temperature & Mold temperature

The melt temperature and mold temperature provide during production are usually determined by the material, and the material supplier will provide the recommended melt temperature and mold temperature. In this case, PP 579S was chosen as the material with a recommended melt temperature of 230°C and a mold temperature of 35°C. The field engineers, however, usually make slight adjustments to the temperature due to the challenges posed by variations in mold structure for real molding. Therefore, the temperature window selected in this case is: melt temperature between 220℃ and 240℃, and mold temperature between 25℃ and 45℃.

1.2 Filling balance

Multi-cavity mold is the best means to enhance the economics of injection molding. This multi-cavity technology allows the production of multiple identical parts in a single molding cycle, the core requirement of which is the perfect reproduction of the cavity. Therefore, cavity filling balance tests must be performed to ensure that the product is balanced in terms of weight, shrinkage, warpage and internal stress. Filling balance is tested as follows:

- With "Machine Analysis" selected in Moldex3D, the injection speed is set to the middle value of 50% and the V/P switching position is set to 98% of the product fill volume;

- The packing pressure and packing time are set to 0, and the cooling time is set long enough, in this case it is set to 30s ;

- When 10 consecutive simulations are performed, the weight of each cavity is recorded, and the filling balance is calculated as follows:

δ=∆mmaxmavg×100%

where δ is the filling balance, ∆mmax is the maximum difference in product weight for different cavities, mavg is the average weight of the product.

The simulation test results are listed in Table S1. The average weight of the product mavg is 9.412g. The filling balance of the cavity is 99.97%, which meets the production requirements of the product.

Table S1 Simulation test results

| No. | Cavity 1# /g | Cavity 2# /g | ∆mmax /g |
| --- | --- | --- | --- |
| 1 | 9.411 | 9.413 | 0.002 |
| 2 | 9.409 | 9.412 | 0.003 |
| 3 | 9.409 | 9.410 | 0.001 |
| 4 | 9.413 | 9.410 | 0.003 |
| 5 | 9.411 | 9.412 | 0.001 |
| 6 | 9.411 | 9.412 | 0.001 |
| 7 | 9.414 | 9.413 | 0.001 |
| 8 | 9.412 | 9.413 | 0.001 |
| 9 | 9.412 | 9.413 | 0.001 |
| 10 | 9.412 | 9.413 | 0.001 |

1.3 Injection speed

The non-Newtonian properties of the polymer melt cause the melt viscosity to vary with the injection rate. Filling in the smooth melt viscosity range is an effective way to ensure product quality, and therefore the smooth viscosity range for melt filling is determined by injection speed testing. In this process, the injection speed served as the study variable to record the shear rate of the plastic melt and the peak screw pressure at different injection speeds. After that, the shear rate versus viscosity curve is plotted based on the recorded data. The optimal injection speed corresponding to the smooth viscosity interval is eventually determined. The equations for melt viscosity and shear rate are derived from the Cross equation for polymer flow as follows:

μ=Pp×t×γ

r=1t

Where μ is the melt viscosity; Pp is the peak screw pressure of the injection process; t is the injection time; r is the shear rate; and γ is the enhancement ratio, the value of which is determined according to the type of injection molding machine, γ=1 for all-electric injection molding machine.

The process testing steps are as follows:

- Packing pressure and packing time are set to 0, V/P switchover position is set to 98% of cavity volume;

- Single-stage injection speed is considered to be the optimal process. A single cycle production is executed at the single-stage injection speed, which is set to the maximum injection speed allowed by the machine, and record Pp and t;

- The injection speed is reduced by 10% of the maximum injection speed each time, repeat the above steps and record the data;

- Shear rate versus effective viscosity based on the recorded peak screw pressure and filling time is plotted;

The viscosity versus shear rate curve is shown in Fig S1. When the shear rate exceeds 400 1/s, the melt viscosity reaches a smooth interval and the injection speed has little effect on the viscosity. According to the calculation of equipment parameters, the injection speed should be greater than 55% of the maximum rated injection speed. In order to protect the equipment, the injection speed interval is determined to be 55% to 95% of the maximum nominal injection speed.

Fig. S1 Viscosity versus shear rate curve

1.4 Packing pressure

Injection molding is carried out in two stages, injection and packing pressure, hence packing pressure is also a key factor in determining product quality. Excessive packing pressure can lead to product flutter and residual stress. In contrast, lower packing pressure will cause short shot and shrinkage defects. The packing pressure range is determined by the process window consisting of packing pressure and melt temperature. The magnitude of the packing pressure process window represents the stability of the injection molding process. The larger the window is, the more stable the injection molding process will be, and the products produced within the packing pressure window are defect-free.

The procedure for packing pressure process window testing is as follows:

- The injection speed is set according to the injection speed test results, in this case 75% of the maximum injection speed was set, set V/P switchover position to 98% of cavity volume, the cooling time is set to be long enough, here it is set to 30s;

- The melt temperature is set to the lower limit of the melt temperature, i.e. 220°C;

- The packing pressure is set to 10% of the maximum packing pressure, and gradually increase by 5% for comparison experiments, when the first product without short shot, volume shrinkage and warpage meet the requirements, the packing pressure is recorded and marked as the low temperature - low pressure point in the lower left corner of the packing window;

- Continue to increase the packing pressure for the experiment, the first product with trimming, record the packing pressure and mark it as low temperature-high pressure point; the results of trimming are not directly presented in the simulation software, so it is assumed that trimming occur when the clamping force exceeds the nominal clamping force during the simulated packing process;

- The melt temperature is set to the higher limit of the melt temperature, i.e. 240°C;

- Repeat steps 3 and 4 to mark the high temperature-low pressure point and the high temperature-high pressure point of the packing window;

The packing window is shown in Fig S2. The blue area is the safe area for packing pressure, i.e. the packing pressure range is from 55% to 95% of the maximum packing pressure.

Fig. S2 Packing window

1.5 Packing time

The packing time is determined by the solidification time of the sprue. A proper packing time setting can avoid shrinkage. Sprue solidification time can be determined by the change in product weight. The operation steps are as follows:

- Injection speed is set to 75% of the maximum injection speed, packing pressure is set to 75% of the maximum packing pressure, V/P switchover position is set to 98% of the cavity volume; cooling time is set to 30s;

- The packing time is set to 0 for the simulation, increasing by one second each time, and the weight of the product is recorded for each cycle, as listed in Table S2;

As the packing time increases, the melt continuously enters the cavity causing the product weight to rise. When the packing time exceeds to 6s, the product weight keeps constant, which proves that the gate is solidified at this time. The rate of change of product weight decreases after the packing time exceeds 2s. In conclusion, the range of packing time is determined from 2s to 6s.

Table S2 Relationship between packing time and product weight

| No. | Packing time /s | Weight /g |
| --- | --- | --- |
| 1 | 1 | 26.048 |
| 2 | 2 | 26.550 |
| 3 | 3 | 26.654 |
| 4 | 4 | 26.761 |
| 5 | 5 | 26.866 |
| 6 | 6 | 26.871 |
| 7 | 7 | 26.871 |
| 8 | 8 | 26.871 |
| 9 | 9 | 26.871 |
| 10 | 10 | 26.871 |

Table S3 Taguchi experimental design

| No. | Melt temperature [°C] | Mold temperature [°C] | Injection speed [%] | Packing time [sec] | Packing pressure [%] | Weight of cavity 1# [g] |
| --- | --- | --- | --- | --- | --- | --- |
| 1 . | 220 | 25 | 55 | 2 | 55 | 9.765 |
| 2 . | 220 | 30 | 65 | 3 | 65 | 9.815 |
| 3 . | 220 | 35 | 75 | 4 | 75 | 9.906 |
| 4 . | 220 | 40 | 85 | 5 | 85 | 10.035 |
| 5 . | 220 | 45 | 95 | 6 | 95 | 10.153 |
| 6 . | 225 | 25 | 65 | 4 | 85 | 9.952 |
| 7 . | 225 | 30 | 75 | 5 | 95 | 10.086 |
| 8 . | 225 | 35 | 85 | 6 | 55 | 9.83 |
| 9 . | 225 | 40 | 95 | 2 | 65 | 9.763 |
| 10 . | 225 | 45 | 55 | 3 | 75 | 9.821 |
| 11 . | 230 | 25 | 75 | 6 | 65 | 9.874 |
| 12 . | 230 | 30 | 85 | 2 | 75 | 9.791 |
| 13 . | 230 | 35 | 95 | 3 | 85 | 9.875 |
| 14 . | 230 | 40 | 55 | 4 | 95 | 9.914 |
| 15 . | 230 | 45 | 65 | 5 | 55 | 9.791 |
| 16 . | 235 | 25 | 85 | 3 | 95 | 9.897 |
| 17 . | 235 | 30 | 95 | 4 | 55 | 9.8 |
| 18 . | 235 | 35 | 55 | 5 | 65 | 9.815 |
| 19 . | 235 | 40 | 65 | 6 | 75 | 9.9 |
| 20 . | 235 | 45 | 75 | 2 | 85 | 9.735 |
| 21 . | 240 | 25 | 95 | 5 | 75 | 9.948 |
| 22 . | 240 | 30 | 55 | 6 | 85 | 9.941 |
| 23 . | 240 | 35 | 65 | 2 | 95 | 9.755 |
| 24 . | 240 | 40 | 75 | 3 | 55 | 9.763 |
| 25 . | 240 | 45 | 85 | 4 | 65 | 9.821 |
| 26 . | 230 | 35 | 75 | 4 | 75 | 9.87 |
| 27 . | 230 | 37.5 | 80 | 4.5 | 80 | 9.926 |
| 28 . | 230 | 40 | 85 | 5 | 85 | 9.994 |
| 29 . | 230 | 42.5 | 90 | 5.5 | 90 | 10.054 |
| 30 . | 230 | 45 | 95 | 6 | 95 | 10.104 |
| 31 . | 232.5 | 35 | 80 | 5 | 90 | 10.022 |
| 32 . | 232.5 | 37.5 | 85 | 5.5 | 95 | 10.077 |
| 33 . | 232.5 | 40 | 90 | 6 | 75 | 9.961 |
| 34 . | 232.5 | 42.5 | 95 | 4 | 80 | 9.895 |
| 35 . | 232.5 | 45 | 75 | 4.5 | 85 | 9.918 |
| 36 . | 235 | 35 | 85 | 6 | 80 | 9.985 |
| 37 . | 235 | 37.5 | 90 | 4 | 85 | 9.918 |
| 38 . | 235 | 40 | 95 | 4.5 | 90 | 9.976 |
| 39 . | 235 | 42.5 | 75 | 5 | 95 | 9.984 |
| 40 . | 235 | 45 | 80 | 5.5 | 75 | 9.902 |
| 41 . | 237.5 | 35 | 90 | 4.5 | 95 | 9.995 |
| 42 . | 237.5 | 37.5 | 95 | 5 | 75 | 9.92 |
| 43 . | 237.5 | 40 | 75 | 5.5 | 80 | 9.931 |
| 44 . | 237.5 | 42.5 | 80 | 6 | 85 | 9.982 |
| 45 . | 237.5 | 45 | 85 | 4 | 90 | 9.89 |
| 46 . | 240 | 35 | 95 | 5.5 | 85 | 10.005 |
| 47 . | 240 | 37.5 | 75 | 6 | 90 | 10.012 |
| 48 . | 240 | 40 | 80 | 4 | 95 | 9.907 |
| 49 . | 240 | 42.5 | 85 | 4.5 | 75 | 9.87 |
| 50 . | 240 | 45 | 90 | 5 | 80 | 9.918 |
| 51 . | 220 | 25 | 55 | 2 | 55 | 9.765 |
| 52 . | 220 | 27.5 | 60 | 2.5 | 60 | 9.784 |
| 53 . | 220 | 30 | 65 | 3 | 65 | 9.815 |
| 54 . | 220 | 32.5 | 70 | 3.5 | 70 | 9.856 |
| 55 . | 220 | 35 | 75 | 4 | 75 | 9.906 |
| 56 . | 222.5 | 25 | 60 | 3 | 70 | 9.825 |
| 57 . | 222.5 | 27.5 | 65 | 3.5 | 75 | 9.879 |
| 58 . | 222.5 | 30 | 70 | 4 | 55 | 9.802 |
| 59 . | 222.5 | 32.5 | 75 | 2 | 60 | 9.780 |
| 60 . | 222.5 | 35 | 55 | 2.5 | 65 | 9.786 |
| 61 . | 225 | 25 | 65 | 4 | 60 | 9.812 |
| 62 . | 225 | 27.5 | 70 | 2 | 65 | 9.785 |
| 63 . | 225 | 30 | 75 | 2.5 | 70 | 9.811 |
| 64 . | 225 | 32.5 | 55 | 3 | 75 | 9.825 |
| 65 . | 225 | 35 | 60 | 3.5 | 55 | 9.770 |
| 66 . | 227.5 | 25 | 70 | 2.5 | 75 | 9.819 |
| 67 . | 227.5 | 27.5 | 75 | 3 | 55 | 9.777 |
| 68 . | 227.5 | 30 | 55 | 3.5 | 60 | 9.782 |
| 69 . | 227.5 | 32.5 | 60 | 4 | 65 | 9.812 |
| 70 . | 227.5 | 35 | 65 | 2 | 70 | 9.765 |
| 71 . | 230 | 25 | 75 | 3.5 | 65 | 9.820 |
| 72 . | 230 | 27.5 | 55 | 4 | 70 | 9.829 |
| 73 . | 230 | 30 | 60 | 2 | 75 | 9.786 |
| 74 . | 230 | 32.5 | 65 | 2.5 | 55 | 9.762 |
| 75 . | 230 | 35 | 70 | 3 | 60 | 9.780 |
| 76 . | 225 | 30 | 80 | 4 | 80 | 9.986 |
| 77 . | 225 | 32.5 | 82.5 | 4.25 | 82.5 | 9.965 |
| 78 . | 225 | 35 | 85 | 4.5 | 85 | 10.008 |
| 79 . | 225 | 37.5 | 87.5 | 4.75 | 87.5 | 10.028 |
| 80 . | 225 | 40 | 90 | 5 | 90 | 10.055 |
| 81 . | 227.5 | 30 | 82.5 | 4.5 | 87.5 | 10.010 |
| 82 . | 227.5 | 32.5 | 85 | 4.75 | 90 | 10.043 |
| 83 . | 227.5 | 35 | 87.5 | 5 | 80 | 9.985 |
| 84 . | 227.5 | 37.5 | 90 | 4 | 82.5 | 9.943 |
| 85 . | 227.5 | 40 | 80 | 4.25 | 85 | 9.935 |
| 86 . | 230 | 30 | 85 | 5 | 82.5 | 10.004 |
| 87 . | 230 | 32.5 | 87.5 | 4 | 85 | 9.942 |
| 88 . | 230 | 35 | 90 | 4.25 | 87.5 | 9.978 |
| 89 . | 230 | 37.5 | 80 | 4.5 | 90 | 9.982 |
| 90 . | 230 | 40 | 82.5 | 4.75 | 80 | 9.940 |
| 91 . | 237.5 | 30 | 87.5 | 4.25 | 90 | 9.973 |
| 92 . | 237.5 | 32.5 | 90 | 4.5 | 80 | 9.938 |
| 93 . | 237.5 | 35 | 80 | 4.75 | 82.5 | 9.939 |
| 94 . | 237.5 | 37.5 | 82.5 | 5 | 85 | 9.958 |
| 95 . | 237.5 | 40 | 85 | 4 | 87.5 | 9.895 |
| 96 . | 240 | 30 | 90 | 4.75 | 85 | 9.977 |
| 97 . | 240 | 32.5 | 80 | 5 | 87.5 | 9.973 |
| 98 . | 240 | 35 | 82.5 | 4 | 90 | 9.912 |
| 99 . | 240 | 37.5 | 85 | 4.25 | 80 | 9.887 |
| 100 . | 240 | 40 | 87.5 | 4.5 | 82.5 | 9.913 |

Table S4 Characteristics of the injection molding machine ZHAFIR ZE1200

| Machine Characteristics | Value |
| --- | --- |
| Maximum clamping force | 1200kN |
| Maximum injection volume | 116cm3 |
| Screw diameter | Ø32mm |
| Maximum injection speed | 300mm/s |
| Maximum injection pressure | 250MPa |
| Maximum packing pressure | 200MPa |