Table 1 Optimization of model reaction in the synthesis of 1,4-DHPsa

| Entry | Catalyst | Solvent | Temperature (οC) | Time (min) | Catalyst (g) | Yield (%)b |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | - | Solvent-free | R.T. | 15 | - | - |
| 2 | Magnetic CS-SA | Solvent-free | R.T. | 15 | 0.02 | 30 |
| 3 | Magnetic CS-SA | Toluene | R.T. | 15 | 0.02 | 35 |
| 4 | Magnetic CS-SA | THF | R.T. | 15 | 0.02 | 35 |
| 5 | Magnetic CS-SA | H2O | R.T. | 15 | 0.02 | 40 |
| 6 | Magnetic CS-SA | CH3CN | R.T. | 15 | 0.02 | 45 |
| 7 | Magnetic CS-SA | MeOH | R.T. | 15 | 0.02 | 50 |
| 8 | Magnetic CS-SA | EtOH | R.T. | 15 | 0.02 | 60 |
| 9 | Magnetic CS-SA | EtOH | R.T. | 15 | 0.03 | 75 |
| 10 | Magnetic CS-SA | EtOH | R.T. | 15 | 0.035 | 85 |
| 11 | Magnetic CS-SA | EtOH | 40 οC | 15 | 0.035 | 92 |
| 12 | Magnetic CS-SA | EtOH | 50 οC | 15 | 0.035 | 96 |
| 13 | Magnetic CS-SA | EtOH | 60 οC | 15 | 0.04 | 96 |
| 14 | Magnetic CS-SA | EtOH | 50 οC | 30 | 0.035 | 96 |
| 15 | Fe3O4 | EtOH | 50 οC | 15 | 0.035 | 50 |
| 16 | CS | EtOH | 50 οC | 15 | 0.035 | 45 |
| 17 | CS-SA | EtOH | 50 οC | 15 | 0.035 | 84 |
| a Reaction conditions: Benzaldehyde (1 mmol), ammonium acetate (1 mmol), ethyl acetoacetate (2 mmol), under different conditions and 2 mL of each solvent. b Isolated yield. |  |  |  |  |  |  |

Table 2 Optimization of model reaction for the synthesis of polyhidroquinolinesa

| Entry | Catalyst | Solvent | Temperature (οC) | Time (min) | Catalyst (g) | Yield (%)b |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | - | Solvent-free | R.T. | 15 | - | - |
| 2 | Magnetic CS-SA | Solvent-free | R.T. | 15 | 0.02 | 30 |
| 3 | Magnetic CS-SA | Toluene | R.T. | 15 | 0.02 | 33 |
| 4 | Magnetic CS-SA | THF | R.T. | 15 | 0.02 | 35 |
| 5 | Magnetic CS-SA | H2O | R.T. | 15 | 0.02 | 40 |
| 6 | Magnetic CS-SA | CH3CN | R.T. | 15 | 0.02 | 45 |
| 7 | Magnetic CS-SA | MeOH | R.T. | 15 | 0.02 | 52 |
| 8 | Magnetic CS-SA | EtOH | R.T. | 15 | 0.02 | 60 |
| 9 | Magnetic CS-SA | EtOH | R.T. | 15 | 0.03 | 75 |
| 10 | Magnetic CS-SA | EtOH | R.T. | 15 | 0.035 | 83 |
| 11 | Magnetic CS-SA | EtOH | 40 οC | 15 | 0.035 | 86 |
| 12 | Magnetic CS-SA | EtOH | 50 οC | 15 | 0.035 | 93 |
| 13 | Magnetic CS-SA | EtOH | 60 οC | 15 | 0.04 | 92 |
| 14 | Magnetic CS-SA | EtOH | 50 οC | 30 | 0.035 | 92 |
| 15 | Fe3O4 | EtOH | 50 οC | 15 | 0.035 | 50 |
| 16 | CS | EtOH | 50 οC | 15 | 0.035 | 45 |
| 17 | CS-SA | EtOH | 50 οC | 15 | 0.035 | 80 |
| a Reaction conditions: Benzyaldehyde (1 mmol), ethyl acetoacetate (1 mmol), dimedone (1 mmol), ammonium acetate (1 mmol), under different conditions and 2 mL of each solvent. b Isolated yield. |  |  |  |  |  |  |

Table 3 Formation of diverse derivatives of 1,4-dihydropyridine and polyhydroquinolinea

| Entry | Aldehyde | Product | Time (min) | Yield (%)b | M.p (°C) |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Measured / Reported [Ref] |
| 1 | 1a | 5a | 28 | 92 | 140-142 (144-146) [32] |
| 2 | 1b | 5b | 33 | 88 | 126-128 (127-128) [32] |
| 3 | 1c | 5c | 23 | 90 | 127-129 (127-129) [33] |
| 4 | 1d | 5d | 27 | 89 | 160-163 (163-164) [33] |
| 5 | 1e | 5e | 15 | 96 | 154-157 (157-158) [33] |
| 6 | 1f | 5f | 33 | 92 | 160-162 (160-162) [33] |
| 7 | 1g | 5g | 20 | 87 | 133-135 (134-135) [33] |
| 8 | 1h | 5h | 22 | 90 | 229-232 (230-231) [33] |
| 9 | 1i | 5i | 18 | 88 | 159-162 (160-162) [34] |
| 10 | 1a | 6a | 30 | 87 | 240-243 (242-244) [35] |
| 11 | 1b | 6b | 33 | 85 | 202-204 (200-203) [35] |
| 12 | 1c | 6c | 25 | 88 | 252-254 (252-254) [35] |
| 13 | 1d | 6d | 20 | 89 | 176-178 (176-178) [35] |
| 14 | 1e | 6e | 15 | 93 | 201-204 (202-203) [35] |
| 15 | 1f | 6f | 33 | 92 | 258-261 (259-261) [35] |
| 16 | 1g | 6g | 27 | 85 | 254-256 (255-256) [35] |
| 17 | 1h | 6h | 34 | 85 | 230-232 (231-233) [35] |
| 18 | 1i | 6i | 16 | 90 | 237-240 (238-240) [36] |
| a,b1,4-DHPs (5a-5i): aldehyde (1 mmol), ethyl acetoacetate (2 mmol) and ammonium acetate (1mmol), EtOH (2 mL) and magnetic CS-SA (0.035 g).; polyhydroquinolines (6a-6i): aldehyde (1 mmol), ethyl acetoacetate (1 mmol), dimedone (1 mmol), ammonium acetate (1 mmol), EtOH (2 mL) and magnetic CS-SA (0.035 g). |  |  |  |  |  |