The synergistic effect of degradation and adsorption for emerging pollutants removal from water and real wastewater by using immobilized activated carbon from pomegranate peels

Osamah J. Al-sareji a,b, Mónika Meiczinger a, Raed A. Al-Juboori c,d, Ruqayah Ali Grmasha b,e, Manolia Andredaki f, Viola Somogyi a, Ibijoke A. Idowu f, Csilla Stenger-Kovács e,g, Miklós Jakab h, Edina Lengyel e,g, Khalid S. Hashim f,*

a Sustainability Solutions Research Lab, Faculty of Engineering, University of Pannonia, Egyetem str. 10, Veszprém H, 8200, Hungary

b Environmental Research and Studies Center, University of Babylon, Babylon, Al-Hillah, Iraq

c NYUAD Water Research Center, New York University-Abu Dhabi Campus, Abu Dhabi, P.O. Box 129188, Abu Dhabi, United Arab Emirates

d Water and Environmental Engineering Research Group, Department of Built Environment, Aalto University, P.O. Box 15200, Aalto, FI-00076, Espoo, Finland

e University of Pannonia, Faculty of Engineering, Center for Natural Science, Research Group of Limnology, H-8200 Veszprem, Egyetem u. 10, Hungary

f School of Civil Engineering and Built Environment, Liverpool John Moores University, UK

g ELKH-PE Limnoecology Research Group, H-8200 Veszprém, Egyetem utca 10, Hungary

h Research Centre of Engineering Sciences, Department of Materials Sciences and Engineering, University of Pannonia, P.O. Box 158, H-8201 Veszprém, Hungary

* Corresponding authors: Khalid S. Hashim

Figure S1 EDS for MPPs and LMPPs

| Table S1 the parameter of Langmuir, Freundlich, Pseudo-1st-Order Model and Pseudo-2nd-Order Model |  |  |  |  |
| --- | --- | --- | --- | --- |
| Langmuir | qmax (mg/g) | KL | RL | R2 |
| Amoxicillin | 704.22 | 0.013 | 0.939 | 0.992 |
| Ciprofloxacin | 598.80 | 0.013 | 0.937 | 0.996 |
| Carbamazepine | 606.06 | 0.019 | 0.915 | 0.995 |
| Diclofenac | 704.21 | 0.017 | 0.923 | 0.992 |
| Freundlich | 1/n | Kf | R2 |  |
| Amoxicillin | 0.78 | 12.38 | 0.984 |  |
| Ciprofloxacin | 0.78 | 10.93 | 0.991 |  |
| Carbamazepine | 0.80 | 13.20 | 0.975 |  |
| Diclofenac | 0.79 | 14.58 | 0.988 |  |
| Pseudo-1st-Order Model | qe (mg g-1) | K1 | R2 |  |
| Amoxicillin | 13.08 | 1.8E-05 | 0.995 |  |
| Ciprofloxacin | 4.59 | 1.2E-05 | 0.995 |  |
| Carbamazepine | 2.91 | 1.3E-05 | 0.984 |  |
| Diclofenac | 6.69 | 1.2E-05 | 0.991 |  |
| Pseudo-2nd-Order Model | qe (mg/g) | qe2 | K2 | R2 |
| Amoxicillin | 1.7E+02 | 3.0E+04 | 2.8E-04 | 0.899 |
| Ciprofloxacin | 2.0E+02 | 4.0E+04 | 3.7E-04 | 0.913 |
| Carbamazepine | 1.6E+02 | 2.5E+04 | 1.0E-03 | 0.918 |
| Diclofenac | 2.5E+02 | 6.2E+04 | 5.5E-04 | 0.982 |

| Table S2 Thermodynamic parameters of emerging pollutants adsorption on MPPs |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Pharmaceutical Compound | Temperature (K) | Kl | ΔG° | ΔH° | ΔS° | R2 |
| Amoxicillin | 283 | 6.95 | -4.56 | 9.89 | 50.99 | 0.980 |
|  | 293 | 7.92 | -5.04 |  |  |  |
|  | 303 | 8.85 | -5.49 |  |  |  |
|  | 313 | 10.50 | -6.12 |  |  |  |
| Ciprofloxacin | 283 | 5.88 | -4.17 | 10.18 | 50.83 | 0.950 |
|  | 293 | 7.19 | -4.80 |  |  |  |
|  | 303 | 7.64 | -5.12 |  |  |  |
|  | 313 | 9.14 | -5.75 |  |  |  |
| Carbamazepine | 283 | 6.75 | -4.49 | 14.60 | 67.44 | 0.996 |
|  | 293 | 8.34 | -5.16 |  |  |  |
|  | 303 | 9.97 | -5.79 |  |  |  |
|  | 313 | 12.32 | -6.53 |  |  |  |
| Diclofenac | 283 | 5.30 | -3.96 | 11.38 | 54.30 | 0.968 |
|  | 293 | 6.28 | -4.49 |  |  |  |
|  | 303 | 7.78 | -5.17 |  |  |  |
|  | 313 | 8.43 | -5.54 |  |  |  |

Table S3 Secondary efﬂuent characteristics.

| Parameters | Concentration (mg/L) |
| --- | --- |
| Chemical oxygen demand | 67.2 ±2.3 |
| Biochemical oxygen demand | 26.43 ±1.9 (5 days) |
| Suspended solids | 24.42±1.3 |
| Volatile suspended solids | 18.84± 0.8 |
| Total Phosphorus | 4.9±0.8 |
| Ammonia | 15.93±1.7 (NH3-NH4) |
| Electrical conductivity | 853±5.4 µmoss/cm |
| Total Kjeldahl nitrogen | 11.53 ± 0.7 |
| Nitrate-nitrite | 2.8 ± 0.6 (NO2-NO3) |
| Total solids | 584± 6.7 |
| Total dissolved solids | 498± 3.6 |
| pH | 6.7 |
| Temperature | 26 |