Supporting information

MgO-Based Sorbents for High Pressure CO2 Capture: An Experimental and First-Principles Theoretical Study

Sung Hyun Kwon1,† , Vishwanath Hiremath2,3†, Anshu Nanoti4, Sung Gu Kang5*, Jeong Gil Seo2*, Seung Geol Lee1,6*

1School of Chemical Engineering, Pusan National University, Busan 46241, Republic of Korea

2Department of Chemical Engineering,

Hanyang University, 222 Wangsimni-ro, Seongdong-gu, Seoul 04763, Republic of Korea

3Center for Creative Convergence Education,

Hanyang University, 222 Wangsimni-ro, Seongdong-gu, Seoul 04763, Republic of Korea

4Academy of Scientific and Innovative Research and Adsorption and Membrane Separation Laboratory, Council of Scientific and Industrial Research, Indian Institute of Petroleum Campus (CSIR-IIP), Dehradun 248005, India

5School of Chemical Engineering, University of Ulsan, 93 Daehak-ro, Nam-gu, Ulsan 44610, Republic of Korea

6Department of Organic Material Science and Engineering,

Pusan National University, Busan 46241, Republic of Korea

†These authors contributed equally

Synthesis of MgAl2O4, MgTiO3, and MgSiO3:

MgAl2O4, MgTiO3, and MgSiO3 were synthesized by EISA method reported elsewhere.[1]  In general, 2.3 g of triblock copolymer (EO)20(PO)70(EO)20 (Pluronic P123, SigmaAldrich,) was dissolved in 50 ml of absolute ethanol (94.5%, Samchun Chemicals) under constant stirring for 4 h. Then, appropriate amount of metal precursors (Mg/Al=0.5 for MgAl2O4, Mg/Ti=1.0 for MgTiO3, and Mg/Si=1.0 for MgSiO3) with stoichiometric composition was dissolved followed by the addition of 5 ml of nitric acid (70%, Sigma Aldrich,) for complete hydrolysis. Mg(NO3)2·6H2O, aluminium isopropoxide and TEOS were used as precursors of magnesium oxide (MgO), alumina, and silica, respectively. The stirring was continued till clear solution was obtained (for MgSiO3, white precipitate formed at the bottom). The resultant solution was stirred for 5 h. Further, the self-assembly of the metal precursors was induced via evaporation of the solution at 60 °C for 48 h. The resultant solid was calcined at 550 °C for 5 h. For MgSiO3 similar method was followed except that DI water was used instead of absolute ethanol and 2M HCl was used instead of HNO3.

Synthesis of MgO:

The MgO was obtained by simple calcination of commercial MgO at 400 oC for 2 hr at ramping rate of 5 oC/min.

Characterization

The synthesized samples were characterized by powder X-ray diffraction (PXRD), N2 adsorption-desorption analysis, Thermogravimetric analysis, and Equilibrium Isotherm analysis. PXRD scans were carried out on a Bruker (Germany) advanced diffractometer using Cu Kα radiation in the 2θ range of 20−80o. Surface area and pore-size distribution analysis was carried out on a BELSORP MINI-II analyzer. Prior to analysis, the samples were pre-treated at 100 °C for 6hrs to remove the surface adsorbed contaminants. The equilibrium isotherm measurements were carried out in a gravimetric microbalance unit (Hiden IGA-001). Prior to sorption-desorption analysis the samples were pre-treated at 400 oC under vacuum to activate the sorbents. 100% CO2 was used for the sorption analysis and 100% He was used for the pre-treatment experiment.

Fig. S1. a) XRD patterns, b) N2 adsorption-desorption isotherms for the developed Mg-X composites.

Table S1. The detailed textural properties for the Mg-X composites.

| Sorbent | Specific surface area (m2/g) | Total Pore volume (cm3/g) | Mean Pore diameter (nm) |
| --- | --- | --- | --- |
| MgAl2O4 | 135.7 | 0.4 | 13.31 |
| MgTiO3 | 80.6 | 0.5 | 26.53 |
| MgSiO3 | 242.9 | 0.6 | 10.16 |
| MgO | 3.8 | 0.2 | 21.99 |

Fig. S3. a) The temperature swing CO2 adsorption curves, b) the amount of CO2 sorption for Mg-X composites

References

[1]	V. Hiremath, R. Shavi, J.G. Seo, Controlled oxidation state of Ti in MgO-TiO2 composite for CO2 capture, Chem. Eng. J. 308 (2017) 177–183. doi:10.1016/j.cej.2016.09.052.