Supporting information

Micro flower-like Hierarchical Mo2C/Co@N-C (N-doped carbon) for efficient bifunctional electrocatalyst

Hee Soo Kima,*, Ahyoun Limb, Mino Wooa, Hae In Leea, Yunjang Gua and Dong-Ha Lima,*

aGreen Materials & Processes R&D Group, Korea Institute of Industrial Technology (KITECH), Ulsan, 44413 Republic of Korea

bHydrogen•Fuel Cell Research Center, Korea Institute of Science and Technology (KIST), Seoul 02792, Republic of Korea

* Corresponding Author

*E-Mail: catacylsm@kitech.re.kr (H.S. Kim)

*E-Mail: dongha4u@kitech.re.kr (L-H. Lim)

5um

Fig. S1. SEM image of Mo2C/Co@dopamine polymer before carbonization

Fig. S2. SEM images of Mo2C/Co@N-C (a) and Mo2C@N-C (b and c)

Fig. S3. TGA analysis result of Mo2C/Co@N-C at air condition.

Fig. S4. The element ratio of the Mo2C/Co@N-C catalyst from the XPS scan survey

Fig. S5. CVs of the Mo2C/CO@N-C (a) and Mo2C@N-C (b) measured in a non-faradaic region at different scan rates from 5 to 100 mV/s. Linear plots of capacitive current against scan rate of various electrocatalyst (c). Nyquist plots of the Mo2C@N-C and Mo2C/Co@N-C catalyst at OCV (d)