SUPPLEMENTARY INFORMATION

Levels and composition of microplastics and microfibers in the South Saskatchewan River and stormwater retention ponds in the City of Saskatoon, Canada

Iyanu Kumayon1, Saurabh Prajapati2, Markus Brinkmann2,3,4*, Tara F. Kahan1,4

1 Department of Chemistry, College of Arts and Science, University of Saskatchewan, Saskatoon, Saskatchewan, Canada

2 School of Environment and Sustainability, University of Saskatchewan, Saskatoon, Saskatchewan, Canada

3 Toxicology Centre, University of Saskatchewan, Saskatoon, Saskatchewan, Canada

4 Global Institute for Water Security, University of Saskatchewan, Saskatoon, Saskatchewan, Canada

*Corresponding author:

Markus Brinkmann: markus.brinkmann@usask.ca

Sample Collection, Treatment, and Extraction

a.

b.

c.

Fig. S1: Schematic of the glass separator setup. (a) The cylindrical upper plate (left) with top and bottom ends open, and the lower plate (right) with the top end open and the bottom end sealed. (b) The lower plate and the upper plate stacked into a single unit to hold the solution. (c) The upper half of the device – which is expected to contain the microplastics and other less dense particles – separated from the lower half containing settled denser materials or sediments by sliding the upper plate over the lower plate such that the glass sheet extending from the top of the lower plate acted as a base for the liquid in the upper plate.

Validation of Method

The percent recovery of the instrument based on the density of the polymer samples was validated by extracting six virgin polymer samples (500 μm – 1000 μm) in 1.6 g.cm-3 sodium iodide using the glass separator device. All virgin polymer samples were obtained from the Thermo Fisher Chemical Company, USA, and were used without further purification. Polymers were categorized into two; polymers with densities less than or similar to the density of distilled water (1.00 g.cm-3) namely, nylon,6 (1.08 g.cm-3), polyethylene (PE, 0.925 g.cm-3) and polypropylene (PP, 0.900 g.cm-3). The other category includes those polymers whose densities are greater than the density of distilled water (> 1.00 g.cm-3) which include polyethylene terephthalate (PET, 1.68 g.cm-3), polysulfone (PSF, 1.24 g.cm-3) and polyvinyl chloride (PVC, 1.40 g.cm-3).

The results (Fig. S2) indicate that the glass separator unit shows 100% recovery for polymers with densities less than or close 1.00 g.cm-3, while the recovery of polymers with densities greater than 1.00 g.cm-3 ranges from 98.3% ± 0.6% to 100% ± 0.0% (Overall mean recovery 99.1% ± 0.8%). Analysis of their overall mean recovery rate using t-test, with P > α (p-value = 0.2248, α = 0.05) suggest that there is no significant difference between the overall mean recovery rate of less dense polymer samples and the dense polymer samples when extracted in a dense solution of sodium iodide (NaI) using the small glass density separator device, hence, the method is efficient for recovering both dense and less dense microplastics and anthropogenic fibers from water sample. This result further supports previous finding by Nakajima et al (2019) that there are no significant differences in the mean recovery rate of different polymer type in the same size classification, but the recovery rate increases with increasing polymer sizes (Nakajima et al, 2019).

Fig. S2: Percent recovery of the small glass separator unit. Blue bars indicate polymers with densities less than or similar to the density of distilled water, while green bars indicate polymers which have densities greater than the density of distilled water.

Normalized Intensity

Fig. S3: Reference Raman spectra of some selected polymers obtained for the in-house spectral library.

Films – 4%

Spheres – 3%

Synthetic fibers – 51%

Fragments – 42%

Fig. S4: Optical images of selected microplastics representing the four morphological categories.

1001

1031

1583

1602

1203

3110

2923

Fig. S5: Raman spectrum of polystyrene particle

Table S1: Raman band assignments for polystyrene

|  | Identified peaks (cm-1) | Literature value (cm-1) | Band Assignment |
| --- | --- | --- | --- |
| 1. | 975 | 975 | CH out-of-plane deformation |
| 2. | 1001 | 1001 | Ring breathing mode |
| 3. | 1031 | 1031 | C-H in-plane-deformation |
| 3. | 1156 | 1155 | C-C stretch |
| 4. | 1452 | 1450 | CH2 scissoring |
| 5. | 1583 | 1583 | C=C stretch |
| 6. | 1602 | 1603 | Ring-skeletal stretch |
| 7. | 2923 | 2923 | Methylene C-H backbone |
| 8. | 3110 | 3110 | Aromatic C-H vibration. |

1339

1458

2883

2831

1529

2950

Fig. S6: Raman spectrum of polypropylene particle

Table S2: Raman band assignments for polystyrene

|  | Identified Peaks (cm-1) | Literature value (cm-1) | Band Assignment |
| --- | --- | --- | --- |
| 1. | 808 | 808 | CH2 rocking, C-CH3 and C-C stretching |
| 2. | 841 | 840 | CH3 and CH2 rocking |
| 3. | 974 | 976 | CH3 rocking and C-C stretching |
| 4. | 1152 | 1152 | C-C and C-CH3 stretching, CH bending, and CH3 rocking |
| 5. | 1167 | 1167 | C-C stretching |
| 6. | 1339 | 1338 | CH2 twisting |
| 7. | 1458 | 1459 | CH2 bending |
| 8. | 2832 | 2831 | CH2 sym. Stretching |
| 9. | 2883 | 2444 | CH3 sym. Stretching |
| 10. | 2921 | 2920 | CH2 asym. Stretching |
| 11. | 2950 | 2952 | CH3 asym. Stretching |

706

859

1176

1095

2967

3083

1289

1411

1615

1725

Fig. S7: Raman spectrum of polyethylene terephthalate (PET) particle

Table S3. Raman band assignments for polyethylene terephthalate

|  | Identified peaks (cm-1) | Literature Values (cm-1) | Band Assignment |
| --- | --- | --- | --- |
| 1. | 706 | 706 | Ring -C-C- stretching |
| 2. | 796 | 796 | Ring torsion and C=O stretching |
| 3. | 859 | 857 | Ring mode of C-C and C(O)-O stretching |
| 4. | 1095 | 1096 | Ethylene glycol C-O, C-C stretching, and C-O-C bending |
| 5. | 1125 | 1126 | Ester C(O)-O and ethylene glycol C-C stretching |
| 6. | 1176 | 1178 | Ring in plane C-H bond and C-C stretching |
| 7. | 12 89 | 1290 | C(O)-C stretching |
| 8. | 1308 | 1308 | Ring CH in plane bending |
| 9. | 1411 | 1414 | C-CH bending and OCH bending |
| 10. | 1452 | 1452 | CH2 bending and OCH bending |
| 11. | 1615 | 1615 | Ring mode 8a (in Wilson’s notation) |
| 12. | 1725 | 1726 | C=O stretching |
| 13. | 2895 | 2895 | C-H bond of methylene sequences |
| 14. | 2963 | 2960 | Methylene groups adjacent to oxygen atoms |
| 15. | 2967 | 2967 | C-H stretching |
| 16. | 3080 | 3080 | C-H stretching of ring alkene |

1613

1727

1570

1338

1283

Fig. S8: Raman spectrum of polycotton (blended cotton) fibers. The peak at 1338 cm-1 is typical of cotton material while peaks at 1727, 1613, and at 1283 cm-1 are typical of PET material.

Fig. S9: Raman spectrum of Reactive Black 5 (RB 5) dye observed in some textile fiber samples.

1099

1228

1146

1249

1362

1460

1584

1608

1699

1296

1008

Fig. S10: Raman spectrum of Vat Indigo dye (Natural Blue 1) observed in some textile fiber samples.

1563

1608

1520

1451

1403

1351

1318

1264

1228

Fig. S11: Raman spectrum of Diarylide yellow (Pigment Yellow 83) observed in some textile fiber samples.

1521

1581

1483

1450

1362

1340

1141

947

748

678

591

Fig. S12: Raman spectrum of copper phthalocyanine dye (Pigment Blue 15:0).