Supporting Information

Metal-free graphitic carbon nitride/black phosphorus quantum dots heterojunction photocatalyst for the removal of ARGs contamination

Xinyuan Zhang1,2, Xuan Xu1,2, Chenyu Li1*, Lin Dai2,4,5*, Zhenxin Hao1,2, Jie Yu1,3, Haodong He1,2, Chuanling Si2*, Zhiqiang Shen1, Zhigang Qiu1, Jingfeng Wang1,2*

1Department of Environment and Health, Institute of Environmental and Operational Medicine, Tianjin 300050, China

2State Key Laboratory of Biobased Fiber Manufacturing Technology, Tianjin Key Laboratory of Pulp and Paper, College of Light Industry and Engineering, Tianjin University of Science and Technology, Tianjin 300457, China

3School of Water and Environment, Chang’an University, Xi’an 710064, China

4National Engineering Lab for Pulp and Paper, China National Pulp and Paper Research Institute Co., Ltd, Beijing 100102, China

5Department of Chemical Engineering, University of New Brunswick, Fredericton, New Brunswick E3B 5A3, Canada

*Corresponding authors.

E-mail: nk_lcy710430@hotmail.com (C. Li), dailin@tust.edu.cn (L. Dai), sichli@tust.edu.cn (C. Si) wangjingfeng0116@163.com (J. Wang)

Table of Contents

- Supplementary Text

Text S1. Methods for purification, culture, and preservation of E. coli K12 M1655 and E. coli HB101(RP4).

- Supplementary Figures

Figure S1. Pictures of photocatalytic inactivated E. coli K12 M1655 colony counts of prepared samples.

Figure S2. Pictures of photocatalytic inactivated E. coli HB101(RP4) colony counts of prepared samples.

- Supplementary Tables

Table S1. The qPCR reaction system.

Table S2. The amplification procedure for qPCR.

- Supplementary Experiments

Experiment S1. Methods for purification, culture, and preservation of E. coli K12 M1655 and E. coli HB101(RP4).

The target strains (E. coli K12 M1655 and E. coli HB101(RP4)) already available in the laboratory were cultured in LB liquid medium at 37°C and 150 rpm on a shaker for 12 h. The bacteria solution was dipped in the inoculating ring on the selection medium for plate marking, and then cultured in a constant temperature incubator at 37℃ for 24 h. After the culture, the chromogenic single colonies were selected and cultured in LB liquid medium at 37℃ and 150rpm for 6-8 h (logarithmic growth stage of bacteria). The cells in the logarithmic growth phase were washed three times with PBS, and then stored in 2-8℃ and ultra-low temperature refrigerator using glycerol cryopreservation and inclined plane preservation, respectively.

- Supplementary Figures

Figure S1 Photos of the live E. coli K12 M1655 bacteria colony on solid LB agar plates exposure to different photocatalytic samples for 2 h.

Figure S2 Pictures of the live E. coli HB101(RP4) bacteria colony on solid LB agar plates exposure to different photocatalytic samples for 4 h.

- Supplementary Tables

Table S1 The qPCR reaction system.

| Reagent | Volume (μL) |
| --- | --- |
| P1 | 1 |
| P2 | 1 |
| DNA | 1 |
| Taq Mix | 7 |
| dd H2O | 10 |
| Total volume | 20 |

Table S2 The amplification procedure for qPCR.

| Reaction program |  | Temperature (℃) | Time (min) |
| --- | --- | --- | --- |
| Predegeneration |  | 95 | 5 |
| Cycle (30 pieces) | Denaturation | 95 | 0.5 |
|  | Annealing | 55 | 0.5 |
|  | Extension | 72 | 0.5 |
| Extension |  | 72 | 10 |