# Direct Identification of Two Regimes of Metal Particle Combustion using Condense-luminescence

Quan Tran1, Michelle L. Pantoya1,*, Igor Altman2,*

AFFILIATIONS

1Department of Mechanical Engineering, Texas Tech University, Lubbock, TX, 79424, USA

2Naval Air Warfare Center Weapons Division, China Lake, CA, 93555, USA

* Authors to whom correspondence should be addressed: michelle.pantoya@ttu.edu , igor.altman@navy.mil

Fig. SI. Overlapped XRD patterns of combustion products of write UN-H5 and SQ-H5; UN-H95 and SQ-H95, correspondingly.The insert shows the region of major peaks to highlight the phase composition difference.

The estimate of the relative phase compositions considers the presence of two phases using the ratio of intensities of two peaks originating from these two phases using the following formulas:

R1=kA121+kA12·100%

R2=11+kA12·100%

In the above formulas, A12 is the ratio of areas of peaks corresponding to the considered phases, and k is an instrumental constant depending on the instrument sensitivities to these particular phases at the peak positions, and R1 and R2 are relative fractions of the phases. Although, the precise calculation requires the exact value of k, it is clear that R1 monotonously increases while R2 monotonously decreases with A12 increase. The consistent trend means that the change in the peak area ratios is a qualitative indication of the change of phase fractions regardless of the exact value of the constant of the instrument used for the XRD analysis. For Table 1, we used k=1.25. The Tables S1-S3 below are generated at different k in order to illustrate the qualitative trend in the change of the phase fractions. Note that for our conclusions, we need this trend only, not the exact values of fractions.

Table S1. Relative mass fraction of alumina phases in combustion products recovered after aluminum oxidation in the bomb calorimeter. Data processed at k=1.

|  | UN-H2 | SQ-H2 | UN-H5 | SQ-H5 | UN-H95 | SQ-H95 |
| --- | --- | --- | --- | --- | --- | --- |
| α-alumina, % | 24 | 12 | 12 | 8 | 19 | 11 |
| γ-alumina, % | 76 | 88 | 88 | 92 | 81 | 89 |

Table S2. Relative mass fraction of alumina phases in combustion products recovered after aluminum oxidation in the bomb calorimeter. Data processed at k=1.25.

|  | UN-H2 | SQ-H2 | UN-H5 | SQ-H5 | UN-H95 | SQ-H95 |
| --- | --- | --- | --- | --- | --- | --- |
| α-alumina, % | 29 | 15 | 14 | 10 | 23 | 13 |
| γ-alumina, % | 71 | 85 | 86 | 90 | 77 | 87 |

Table S3. Relative mass fraction of alumina phases in combustion products recovered after aluminum oxidation in the bomb calorimeter. Data processed at k=1.5.

|  | UN-H2 | SQ-H2 | UN-H5 | SQ-H5 | UN-H95 | SQ-H95 |
| --- | --- | --- | --- | --- | --- | --- |
| α-alumina, % | 32 | 17 | 16 | 12 | 26 | 16 |
| γ-alumina, % | 68 | 83 | 84 | 88 | 74 | 84 |

Combustion Experiments

Table S4.  Tabulated run data of Untreated and Super Quenched Aluminum

| UNTREATED (kJ/g) |  |  |  | SUPER QUENCHED (kJ/g) |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Run # | UN H2 | UN H5 | UN H95 | SQ H2 | SQ H5 | SQ H95 |
| 1 | 28.40 | 29.60 | 29.33 | 27.43 | 30.44 | 30.86 |
| 2 | 28.20 | 30.53 | 30.34 | 30.41 | 32.72 | 30.66 |
| 3 | 29.72 | 29.99 | 30.22 | 28.03 | 31.55 | 30.27 |
| 4 | 30.70 | 30.67 | 29.58 | 30.21 | 30.75 | 30.90 |
| 5 | 29.04 | 30.19 | 30.18 | 30.32 | 31.86 | 30.27 |
| 6 | 29.33 | 30.42 | 29.49 | 29.42 | 30.21 | 30.54 |
| 7 | 30.25 | 29.53 | 30.78 | 29.16 | 30.26 | 31.25 |
| 8 | 25.65 | 31.53 | 30.65 | 29.39 | 30.02 | 30.84 |
| 9 | 29.52 | 30.85 | 30.62 | 30.22 | 30.40 | 30.30 |
| 10 | 28.51 | 30.34 | 31.76 | 30.81 | 30.90 | 31.29 |
| 11 | 30.18 | 28.56 | 30.81 | 31.16 | 29.69 | 30.84 |
| 12 | 29.82 | 31.10 | 30.96 | 30.71 | 29.68 | 29.88 |
| 13 | 29.18 | 31.18 | 30.70 | 28.71 | 30.32 | 31.19 |
| 14 | 29.69 | 30.64 | 29.98 | 30.51 | 30.07 | 30.52 |
| 15 | 28.52 | 30.96 | 31.62 | 30.99 | 29.63 | 30.51 |
| 16 | 27.27 | 29.98 | 30.45 | 29.65 | 29.52 | 29.74 |
| 17 | 27.28 | 30.50 | 30.39 | 30.36 | 30.09 | 30.59 |
| 18 | 29.70 | 30.46 | 30.19 | 30.27 | 30.05 | 32.44 |
| 19 | 29.75 | 30.96 | 30.58 | 30.88 | 30.10 | 29.51 |
| 20 | 29.75 | 30.93 | 30.75 | 30.36 | 31.24 | 32.31 |
| AVERAGE | 29.02 | 30.45 | 30.47 | 29.95 | 30.48 | 30.74 |
| STD. DEV | 1.19 | 0.66 | 0.60 | 0.97 | 0.80 | 0.72 |