Amorphous Ni-Mn-O Microspheres with High Energy Density and Ultralong-Term Stability up to 100, 000 Cycles for Aqueous Pseudo-Capacitors

Yingxv Gao #, Qian Ma #, Xiaohong Xia *, Hongbo Liu *

College of Material Science and Engineering, Hunan University, Changsha, Hunan 410082, China

*Corresponding author email: xxh@hnu.edu.cn (Xia X.); hndxlhb@163.com (Liu H.)

# Both the authors contributed equally to this work.

Supplementary equations

For the three-electrode system, Cs (C g−1) was calculated from GCD measurements according to equations S1:

Cs = (i·Δt) / m                (S1)

where m (g) embodies the mass of the active materials on working electrodes, i (A) represents the discharge current and Δt (s) depicts the discharge time.

For two-electrode systems, energy density E (Wh kg−1 ) and power density P (W kg−1 ) were calculated using equations S2 and S3 [1, 2], respectively:

E = ∫ i·V dt / (3.6 M)          (S2)

P = E / (t / 3600)            (S3)

where i (A) represents the discharge current, V (V) conveys the potential, t (s) depicts the discharge time, M (g) embodies the total mass of active materials in both cathode and anode (M = mc + ma). Notably, M is 0.0040 g for SPC.

The formation mechanism of Ni(OH)2 under hydrothermal conditions can be described by equation S4-S6 [3]:

Ni + nH2O → [Ni(H2O)n]2+ + 2e−          (S4)

O2 + 2H2O + 4e− → 4OH−                (S5)

[Ni(H2O)n]2+ + 2OH− → Ni(OH)2 + nH2O    (S6)

Under hydrothermal environment, hydration of Ni occurs at Ni foam surface so that [Ni(H2O)n]2+ and electrons form (equation S4). Then, dissolved O2 adsorbed on the Ni foam surface acquires electrons and react with H2O to form OH− ions (equation S5). Finally, Ni(OH)2 forms by the reaction between [Ni(H2O)n]2+ and OH− ions (equation S6).

Supplementary figures

Fig. S1. SEM images of NF-24@MnO2-C.

Fig. S2. The profile production of NF-24@MnO2-C by FIB

Fig. S3. STEM image of a part of shell in NF-24@MnO2-C with EDX mappings.

Supplementary Tables

| Table S1 Fitting parameters of corresponding equivalent circuit |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Batteries | Rel/Ohm•cm2 | Rs/Ohm• cm2 | Cs/mF• cm−2 | Rct/Ohm•cm2 | Cdl/mF•cm−2 | Zw/Ohm•cm2•s−0.5 | Cint/mF• cm−2 |
| NF-24@MnO2-A //NF-24@MnO2-A | 0.49 | 1.00 | 0.06 | 2.96 | 0.06 | 5.05 | 1.14 |
| NF-24@MnO2-C //NF-24@MnO2-C | 0.08 | 1.36 | 0.01 | 20.15 | 9.34 ×10−5 | 5.01 | 0.61 |

Table S2 The properties of NiMn1.57O4.13 composite electrode were compared with those of similar composites reported in recent years.

| Sample description | Synthesis | Electrolyte | Capacitance F g−1 | Cycle performance | Ref |
| --- | --- | --- | --- | --- | --- |
| NF-24@MnO2-A | electrochemical activation | Ni foam | 1390 F g−1 (5 A g−1) | 106.1 % (100,000 cycles, 5 A g−1) | This work |
| Ni(OH)2-MnO2@C | hydrothermal | Ni foam | 1608 F g−1 (2 mA cm-2) | 93.9 % (5000 cycles, 2 mA cm−2)) | [4] |
| Ni/MnO nanosheet arrays | co-precipitation | Ni foam | 1235.6 F g−1 (0.5 A g−1) | 106 % (15,000 cycles, 10 A g−1) | [5] |
| PC-Ni/MnO2 | calcination | carbon material | 267.34 F g−1 (0.1 A g−1) | 83.6 % (5000 cycles, 1 A g−1) | [6] |
| NiCo2O4 | pulsed laser ablation | Ni foam | 1650 F g−1 (1 A g−1) | 91.78 % (12,000 cycles, 10 A g−1) | [7] |
| NiMoO4 | electrodeposition and hydrothermal | Ni foam | 2813 F g−1 (3 A g−1) | 94 % (5000 cycles, 3 A g−1) | [8] |
| MnO2-CuO | hydrothermal | Ni foam | 279.2 F g−1 (0.5 A g−1) | 91.26 % (10,000 cycles, 0.5 A g−1) | [9] |
| 3D-MnO2/Ni | electrodeposition | Ni foam | 105 F g−1 (0.5 A g−1) | 97 % (10,000 cycles, 7.5 A g−1) | [10] |
| α- MnO2 | hydrothermal | Ni foam | 294.5 F g−1 (2 A g−1) | 84.4 % (5000 cycles, 1 A g−1) | [11] |
| CuS/MnS@NF | solvothermal synthesis | Ni foam | 1517.07 F g−1 (1 A g−1) | 115.6 % (3000 cycles, 10 A g−1) | [12] |
| M-Fe2O3@MnO2 | hydrothermal | Ni foam | 908.5 F g−1 (1 A g−1) | 78.7% (8000 cycles, 1 A g−1) | [13] |
| CoNi2S4-Ni(OH)2NSAs | hydrothermal | Ni foam | 1570.2 F g−1 (1 A g−1) | 97.91% (5000 cycles, 1 A g−1) | [14] |
| NiO nanowires @NiO nanosheets @ NF | microwave-assisted hydrothermal synthesis | Ni foam | 1782 F g−1 (1 A g−1) | 70.33% (5000 cycles, 1 A g−1) | [15] |
| NiO@MnO2 | hydrothermal route | Ni foam | 1227.2 F g−1 (10 A g−1) | 88.77% (10,000 cycles, 10 A g−1) | [16] |

References

[1] B.S. Singu, S.E. Hong, K.R. Yoon, Chemical synthesis of sea-urchin shaped 3D-MnO2 nano structures and their application in supercapacitors, Journal of Nanoscience and Nanotechnology 16(6) (2016) 6093-6101. https://doi.org/10.1166/jnn.2016.12114.

[2] Y. Ouyang, X.F. Xia, H.T. Ye, L. Wang, X.Y. Jiao, W. Lei, Q.L. Hao, Three-dimensional hierarchical structure ZnO@C@NiO on carbon cloth for asymmetric supercapacitor with enhanced cycle stability, Acs Applied Materials & Interfaces 10(4) (2018) 3549-3561. https://doi.org/10.1021/acsami.7b16021.

[3] K.D. Xia, C. Yang, Y.L. Chen, L.L. Tian, Y.Y. Su, J.B. Wang, L. Li, In situ fabrication of Ni(OH)2 flakes on Ni foam through electrochemical corrosion as high sensitive and stable binder-free electrode for glucose sensing, Sensors and Actuators B-Chemical 240 (2017) 979-987. https://doi.org/10.1016/j.snb. 2016.09.077.

[4] J. Li, W. Cao, N. Zhou, F. Xu, N. Chen, Y. Liu, G. Du, Hierarchically nanostructured Ni(OH)2-MnO2@C ternary composites derived from Ni-MOFs grown on nickel foam as high-performance integrated electrodes for hybrid supercapacitors, Electrochimica Acta 343 (2020) 136139. https://doi.org/10.1016/ j.electacta. 2020.136139.

[5] M. Huang, Y. Lin, H. Huang, X. Fan, K. Shi, Z. Yang, W. Zhang, Nickel nanoparticles modified MnO nanosheet arrays for high-performance supercapacitor with long-lasting and sustainable capacitance increase, Electrochimica Acta 383 (2021) 138353. https://doi.org/10.1016/j.electact a.2021.138353.

[6] X. Ji, D. Sun, W. Zou, Z. Wang, D. Sun, Ni/MnO2 doping pulping lignin-based porous carbon as supercapacitors electrode materials, Journal of Alloys and Compounds 876 (2021) 160112. https://doi. org/10.1016/j.jallcom.2021.160112.

[7] R. Bai, X. Luo, D. Zhen, C. Ci, J. Zhang, D. Wu, M. Cao, Y. Liu, Facile fabrication of comb-like porous NiCo2O4 nanoneedles on Ni foam as an advanced electrode for high-performance supercapacitor, International Journal of Hydrogen Energy 45(56) (2020) 32343-32354. https://doi.org/10.1016/j.ijhydene. 2020.08.156.

[8] S. Normohammadi, F. Bahmani, L. Fotouhi, M. Khoshfetrat, Electrodeposited nickel nanocone/ NiMoO4 nanocomposite designed as superior electrode materials for high performance supercapacitor, International Journal of Hydrogen Energy 47(8) (2022) 5220-5229. https://doi.org/10.1016/ j.ijhydene.2021.11.161.

[9] K.M. Racik, A. Manikandan, M. Mahendiran, P. Prabakaran, J. Madhavan, M.V.A. Raj, Fabrication of manganese oxide decorated copper oxide (MnO2/CuO) nanocomposite electrodes for energy storage supercapacitor devices, Physica E: Low-dimensional Systems and Nanostructures 119 (2020) 114033. https://doi.org/10.1016/j.physe.2020.114033.

[10] N. Swain, A. Mitra, B. Saravanakumar, S.K. Balasingam, S. Mohanty, S.K. Nayak, A. Ramadoss, construction of three-dimensional MnO2/Ni network as an efficient electrode material for high performance supercapacitors, Electrochimica Acta 342 (2020) 136041. https://doi.org/10.1016/j.electact a.2020.136041.

[11] S. Jiang, B. Yang, Y. Lu, R. Xia, T. Yu, M. Gao, An aqueous symmetrical supercapacitor with high bulk pseudocapacitance induced by phase transformation of MnO2, Journal of Alloys and Compounds 876 (2021) 160148. https://doi.org/10.1016/j.jallcom.2021.160148.

[12] M. Zhai, Y. Cheng, Y. Jin, J. Hu, Solvothermal synthesis of flower-like structure Cu-Mn bimetallic sulfide on Ni-foam for high-performance symmetric supercapacitors, International Journal of Hydrogen Energy 44(26) (2019) 13456-13465. https://doi.org/10.1016/j.ijhydene.2019.04.021.

[13] Y. Chen, C. Kang, L. Ma, L. Fu, G. Li, Q. Hu, Q. Liu, MOF-derived Fe2O3 decorated with MnO2 nanosheet arrays as anode for high energy density hybrid supercapacitor, Chemical Engineering Journal 417 (2021) 129243. https://doi.org/10.1016/j.cej.2021.129243.

[14] A.K. Yedluri, D.K. Kulurumotlakatla, S. Sangaraju, I.M. Obaidat, H.-J. Kim, Facile synthesis of novel and highly efficient CoNi2S4-Ni(OH)2 nanosheet arrays as pseudocapacitive-type electrode material for high-performance electrochemical supercapacitors, Journal of Energy Storage 31 (2020) 101623. https://doi.org/10.1016/j.est.2020.101623.

[15] A. Ali, M. Ammar, A. Mukhtar, T. Ahmed, M. Ali, M. Waqas, M.N. Amin, A. Rasheed, 3D NiO nanowires@NiO nanosheets core-shell structures grown on nickel foam for high performance supercapacitor electrode, Journal of Electroanalytical Chemistry 857 (2020) 113710. https://doi.org/ 10.1016/j.jelechem.2019.113710.

[16] T.-F. Yi, J. Mei, B. Guan, P. Cui, S. Luo, Y. Xie, Y. Liu, Construction of spherical NiO@MnO2 with core-shell structure obtained by depositing MnO2 nanoparticles on NiO nanosheets for high-performance supercapacitor, Ceramics International 46(1) (2020) 421-429. https://doi.org/10.1016/j.ceramint.20 19.08.278.