Excellent optical, flexible, and mechanical properties of cellulose liquid crystal films induced by carbon quantum dots

Xinyu Zhaoa, Huimin Fenga, Wenjia Kanga, Boying Yanga, Yueer Maa, Xinping Lia, Hui Changb, Shuhua Tongc, Chuanyin Xionga, Zhao Zhanga,＊

a College of Bioresources Chemical and Materials Engineering, Shaanxi University of Science and Technology, Xi'an, 710021, Shaanxi, PR China

b College of Mechanical and Electrical Engineering, Shaanxi University of Science and Technology, Xi'an, 710021, PR China

c Zhejiang Jinchang Special Paper Co., Ltd. Zhejiang, Quzhou, 324404

＊E-mail: zhangzhaoqg@sust.edu.cn

Characterization

Fourier transform-infrared (FT-IR) spectra were recorded using a Bruker Vertex 70 IR spectrometer (Bruker Corp., Billerica, MA, USA) in the spectral range from 4000 to 400 cm-1 using pressed potassium bromide discs. The material was coated with gold to a thickness of ~8 nm and then the fracture surfaces of samples examined by a scanning electron microscope (SEM; S-4800, Hitachi Instruments, Inc., Tokyo, Japan) at an accelerating voltage of 3.0 kV. X-ray diffractograms (XRD) were obtained with a Nihon Reiji Smart diffractometer (Rigaku Corp., Tokyo, Japan), using Cu-Kα radiation and the 2ϴ from 5 to 60o. Structure was recorded by Raman spectroscopy (AVANCE NEO 600 MHz, Bruker Corp.). UV-Vis and fluorescent spectra were recorded using an UV-VIS-NIR spectrometer (Carry 5000 UV, Agilent Technologies, Inc., Santa Clara, CA, USA), a fluorescence spectrometer (FS 5, Edinburgh, UK), respectively. The liquid crystallinity and structure were recorded using a Primotech polarizing light microscope (POM; Carl Zeiss AG, Oberkochen, Germany). Thermal stability curves were recorded using a STA449F-1053-M (Netzsch Instruments North America, Burlington, MA, USA) simultaneous thermal analyzer (TG), Germany, using a 2 × 2 cm size paper fixed on a slide. The laser confocal lens selected to the most suitable excitation wavelength at 400 nm for analysis. The paper was cut into 1 cm width strips and fixed between two ends of a clamp, with the parameters set for mechanical property testing.

Fig.S1 FT-IR spectrum of LC@CQD films

Fig.S2 XRD spectrum of LC and LC@CQD film

Fig.S3 TG spectrums of LC and LC@CQD films

Fig.S4 DTG spectrums of LC and LC@CQD films

Fig.S5 Physical picture of the LC-CQD films under a UV lamp at 365 nm (from left to right, CQD concentration is 0, 5, 10, 15, 20, 25, 30, 100 μL, respectively)