Electronic Supplementary Material

S-doped C@MoSe2(1-x)S2x@MWCNT heterostructure as high-rate and long-cycle stability anodes for Na+ batteries

Yincai Yang, ‡1 Feng Wang, ‡1 Youwen Chen,1,2() Shiguo Zhang,1 Ming Zhang,1 Zhen-Qiang Yu,3() Chak-Tong Au,1 Shuang-Feng Yin1() & Renhua Qiu1() 1 State Key Laboratory of Chemo/Biosensing and Chemometrics, Advanced Catalytic Engineering Research Centre of the Ministry of Education, College of Chemistry and Chemical Engineering, School of physics & Electronics, College of Material Science and Chemical Engineering, Hunan University, Changsha 410082, China. 2 College of Information and Mechatronic Engineering, Hunan International Economics University, Changsha 410082, China. 3 College of Chemistry and Environmental Engineering, Shenzhen University, Shenzhen, China. ‡ These authors contributed equally to this work Supporting information to DOI

Address correspondence to: Dr. Youwen Chen, youwenchen1@hnu.edu.cn; Prof. Z-Q Yu zqyu@szu.edu.cn; Prof. S-F Yin, sf_yin@hnu.edu.cn and Prof. R. Qiu, renhuaqiu1@hnu.edu.cn

Fig. S1. XRD patterns of samples collected at different temperatures: (a) comparison with Se standard card data, (b) comparison with S standard card data.

Fig. S2. Structures of (a) Na2Se0.75S0.25 and (b) Na2Se after geometry optimization [1].

Fig. S3 Initial and final structures of (a, b) MoNa4Se2 and (c, d) GR@MoNa4Se2@CNT upon geometry optimization, respectively [1].

Fig. S4 Diffusion energy barrier for Na atoms in MoSe2 and GR@MoSe2@CNT: top view and side view of Na atoms migration in (a,b) MoSe2 and (d,e) GR@MoSe2@CNT, respectively; (c) and (f) is the energy barrier for Na atoms migration in MoSe2 and GR@MoSe2@CNT, respectively [1].

Fig. S5. (a) SEM, (b) TEM and (c) HRTEM images of C@MoSe2, (d) TEM image and the corresponding EDS elemental mappings (e) C, (f) Mo and (g) Se [1].

Fig. S6. Corresponding TEM-EDX profile of PEG-200-2-C@MoSe2(1-x)S2x@MWCNT.

Table S1. Corresponding TEM-EDX table of PEG-200-2-C@MoSe2(1-x)S2x@MWCNT.

| General spectrogram | Atomic percentage |
| --- | --- |
| C | 72.36 |
| S | 1.82 |
| Se | 13.73 |
| Mo | 12.10 |
| Total | 100.00 |

According to atomic percentage of sulfur and selenium, the ratio between sulfur atoms and selenium atoms is 1.82/13.73, then the x in PEG-200-2-C@MoSe2(1-x)S2x@MWCNT is 0.12, giving the chemical formula PEG-200-2-C@MoSe1.76S0.24@MWCNT.

Fig. S7. XPS analysis of PEG-200-2-C@MoSe2(1-x)S2x@MWCNT anode materials: (a) Survey scan and (b) high-resolution C 1s spectrum.

Fig. S8. TG analysis of C@MoSe2, C@MoSe2(1-x)S2x@MWCNT, PEG200-2-C@ MoSe2(1-x)S2x@MWCNT and PEG200-4-C@MoSe2(1-x)S2x @MWCNT. According to Mo element conservation, the following equation (Eq. S1) is obtained,

mMoSe2(1-x)S2x%=MMoSe2(1-x)S2xMMoO3*mMoO3%               Eq. S1

where MMoSe2(1-x)S2x and MMoO3 stands for the average molecular weight of MoSe2(1-x)S2x and MoO3, respectively, mMoSe2(1-x)S2x% and mMoO3% represents the percentage content of MoSe2(1-x)S2x and MoO3 in the system, respectively. MMoS2=160.06, MMoSe2=253.86 and MMoO3=143.94. According to Table S1 (high-resolution S 2p spectrum), x is 0.12 (0.16), and then MMoSe2(1-x)S2x=MMoSe1.76S0.24(MMoSe1.68S0.32)=242.59 (238.86),  mMoO3% equals 39.3%, 30.8%, 22.7% and 12.1% for C@MoSe2, C@MoSe2(1-x)S2x@MWCNT, PEG200-2-C@MoSe2(1-x)S2x@CNT and PEG200-4-C@MoSe2(1-x)S2x@MWCNT, respectively. Therefore, the estimated MoSe2 mass loading in C@MoSe2 is 69.3%, while the MoSe2(1-x)S2x mass loading in C@MoSe2(1-x)S2x@MWCNT, PEG-200-2-C@MoSe2(1-x)S2x@MWCNT and PEG-200-4-C@MoSe2(1-x)S2x@MWCNT is 51.9% (51.1%), 38.3% (37.7%) and 20.3% (20.1%), respectively.

Fig. S9. SEM of PEG200-2-C@MoSe2(1-x)S2x@MWCNT electrode (a, b) after smeared and (c, d) after 200 cycles with decomposition.

References

[1]	Yang Y., Wang F., Chen Y., Chen C., Zhang S., Yu Z.-Q., Au C.-T., Yin S.-F., Qiu R. Building a PEG-C@MoSe2@CNT heterostructure via in-situ selenidation as highly reversible anodes for Na+ batteries. Sci. China-Chem., 2023, 66(2): 475–491.