Supplementary materials

Theoretical investigation of the structural evolution, electronic and magnetic properties of TMSin− (TM= Mo, W; n = 8-17) clusters

Kai Wang,1 Chengwei Hu2, Zezhao Jia2, Guangjia Yin2, Runyu Wang2, Lei Ma2,a

1 Henan Engineering Research Centre of Building-Photovoltaics, School of Mathematics and Physics, Henan University of Urban Construction, Pingdingshan 467036, China

2Tianjin International Center for Nanoparticles and Nanosystems, Tianjin University, 92 Weijin Road, Nankai District, Tianjin 300072, China

ae-mail: lei.ma@tju.edu.cn (corresponding author)

FIG. S1. The optimized structures of low-lying isomers of TMSi8-17－ (TM = Mo, W) clusters at BP86/def2-TZVP level. For each structure, the symmetry (given inside the bracket) and the total energy difference (eV) respect to the lowest-lying isomer (nA) are provided. Yellow, green, and gray balls represent silicon, molybdenum, and tungsten atoms, respectively.

FIG. S2 Experimental and simulated photoelectron spectra of low-lying isomers of MoSin－ (n = 8-17). The black and blue lines are the experimentally measured and calculated spectra, respectively.1

FIG. S2 Experimental and simulated photoelectron spectra of low-lying isomers of WSin－ (n = 8-17). The black and blue lines are the experimentally measured and simulated spectra, respectively.1

Table S1. Average bond lengths (BL, in Å), bond orders (BO), vertical detachment energy (VDE), HOMO−LUMO gap (EHL, in eV), average binding energies (Eb, in eV), and the second energy differences (Δ2E, in eV) of the ground state structures of TMSin－ (TM= Mo, W; n = 8-17) clusters.

| Size | BL |  | BO |  | VDE | EHL | Eb | Δ2E |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Si-Si | Si-TM | Si-Si | Si-Mo |  |  |  |  |
| MoSi8－ | 2.49 | 2.58 | 0.63 | 1.01 | 2.97 | 0.37 | 3.76 |  |
| MoSi9－ | 2.52 | 2.60 | 0.56 | 0.94 | 3.18 | 0.34 | 3.80 | 0.14 |
| MoSi10－ | 2.42 | 2.64 | 0.49 | 0.86 | 3.03 | 0.35 | 3.81 | -0.78 |
| MoSi11－ | 2.51 | 2.65 | 0.47 | 0.79 | 3.02 | 0.35 | 3.89 | 0.26 |
| MoSi12－ | 2.39 | 2.67 | 0.44 | 0.69 | 2.84 | 0.69 | 3.94 | 0.62 |
| MoSi13－ | 2.49 | 2.70 | 0.41 | 0.67 | 3.45 | 0.30 | 3.93 | -0.99 |
| MoSi14－ | 2.44 | 2.75 | 0.38 | 0.61 | 2.97 | 0.20 | 4.00 | 1.05 |
| MoSi15－ | 2.53 | 2.74 | 0.37 | 0.58 | 2.83 | 0.28 | 3.99 | -0.17 |
| MoSi16－ | 2.44 | 2.83 | 0.39 | 0.52 | 2.80 | 0.32 | 3.99 | 0.39 |
| MoSi17－ | 2.44 | 2.76 | 0.39 | 0.50 | 3.21 | 0.26 | 3.97 |  |
| WSi8－ | 2.52 | 2.64 | 0.63 | 1.00 | 2.55 | 0.46 | 3.87 |  |
| WSi9－ | 2.53 | 2.61 | 0.55 | 0.98 | 3.22 | 0.34 | 3.90 | 0.02 |
| WSi10－ | 2.53 | 2.64 | 0.50 | 0.89 | 3.10 | 0.37 | 3.93 | -0.37 |
| WSi11－ | 2.51 | 2.66 | 0.46 | 0.82 | 3.02 | 0.35 | 3.99 | 0.21 |
| WSi12－ | 2.40 | 2.68 | 0.43 | 0.73 | 2.61 | 0.50 | 4.02 | 0.36 |
| WSi13－ | 2.50 | 2.71 | 0.41 | 0.70 | 3.45 | 0.30 | 4.02 | -0.88 |
| WSi14－ | 2.45 | 2.76 | 0.38 | 0.63 | 2.98 | 0.18 | 4.07 | 1.17 |
| WSi15－ | 2.42 | 2.82 | 0.36 | 0.59 | 3.18 | 0.28 | 4.05 | -0.39 |
| WSi16－ | 2.45 | 2.83 | 0.39 | 0.55 | 2.81 | 0.32 | 4.06 | 0.52 |
| WSi17－ | 2.45 | 2.76 | 0.38 | 0.52 | 3.23 | 0.26 | 4.03 |  |

Table S2. Average binding energies (Eb, in eV)2 of the ground state structures of CrSin－ (n = 14-18) clusters with the zero-point-energy corrections (Eb-ZPE) for comparison.

| Cluster | Eb | Eb-ZPE |
| --- | --- | --- |
| CrSi14－ | 3.84 | 3.79 |
| CrSi15－ | 3.85 | 3.81 |
| CrSi16－ | 3.85 | 3.80 |
| CrSi17－ | 3.83 | 3.78 |
| CrSi18－ | 3.83 | 3.79 |

References

1 M. Ohara, K. Koyasu, A. Nakajima, K. Kaya, Chem. Phys. Lett. 371, 490-497 (2003).

2 K. Wang, H.-Y. Zhao, L. Miao, Z.-Z. Jia, G.-J. Yin, X.-D. Zhu, R. Moro, B. von Issendorff and L. Ma, J. Phys. Chem. A 126 (8), 1329-1335 (2022).