Twin-assisted cracking degradation in sodium layered oxide cathodes

Cheng Chen,1,3∥ Zhen Han,2,∥Chaoping Liang,1,∥ Yiming Feng,1 Peng Wang,*,2 and Weifeng Wei*,1

1State Key Laboratory of Powder Metallurgy, Central South University, Changsha, Hunan 410083, People's Republic of China.

2National Laboratory of Solid State Microstructures, College of Engineering and Applied Sciences, and Collaborative Innovation Center of Advanced Microstructures, Nanjing University, Nanjing, Jiangsu 210093, People’s Republic of China.

3School of Materials Science and Engineering, Guizhou Minzu University, Guiyang, Guizhou 550025, People's Republic of China.

Extended Data Fig. 1 Morphology and chemical information of as-prepared NNCM cathode material. (a) Typical scanning electron microscopy (SEM) images. (b)-(g) STEM-HAADF image and elemental maps taken from cross-sectioned NNCM cathode material.

Extended Data Fig. 2 XRD patterns and refined results. (a) Pristine and (b) cycled NNCM cathode materials.

Extended Data Fig. 3 Electrochemical performance of NNCM cathode. (a) Initial charge and discharge profiles within 1.5-4.0V vs. Na+/Na at 0.1 C. (b) Average cell voltage upon extended cycles. (c) Cyclic voltammetry (CV) curves. (d) Electrochemical cycling properties up to 200 cycles.

Extended Data Fig. 4 Electrochemical performance of NNCM cathode. (a) Charge and discharge profiles during extended cycles. (b) Charge and discharge profiles tested at various C rates (0.1-5 C).

Extended Data Fig. 5 Atomic-resolution STEM images visualizes multiple twins in a single pristine NNCM particle. (a-e) STEM-HAADF images and corresponding reconstructed images of NNCM cathodes, demonstrating that twins widely exist and are stacking along [001] direction in pristine NNCM cathode. The scale bars are 1nm in c-e.

Extended Data Fig. 6 Electronic information of O and TM elements around CTBs using EELS. (a) STEM-ADF images of selected area for EELS acquisition around CTBs. The red and black rectangles indicate the acquisition areas for matrix area and CTBs area, respectively. (b-e) EELS spectra of O-K and TM-L edge acquired at selected areas in (a).

Extended Data Fig. 7 Reconstructed images acquired by 4D STEM techniques of CTBs structure. The bar is 1nm. Na and O atom columns were invisible in HAADF due to weaker scattering of electrons, and contrast of Na and O atom columns were ambiguous in ABF images due to rigorous imaging conditions. The phase reconstructed images, iCOM and dCOM images, showed all atom columns and confirmed the formation of P-type CTBs.

Extended Data Fig. 8 Calculated interlayer distance of Na1-x[NCM211]O2.

Extended Data Fig. 9 Calculated charge density difference of Na1-x[NCM211]O2, (a) x=0; (b) x=0.25

Extended Data Fig. 10 Calculated diffusion barrier for (a) O3 and (b) P2 Na1-x[NCM211]O2