Supplementary material

Table Legends

Table S1. FTIR peak assignments for the PVA/PVP blend and their nanocomposites (cm-1).

Table S2. d-spacing and crystalline index of the polymer blend and polymer blend nanocomposites.

Table S3. Weight % and Atomic% of Ag, Fe elements in prepared composites obtained by EDX.

Table S4. Weight loss of base matrix, monometallic (Ag, Fe) and bimetallic (Ag-Fe) composites at stage I, stage II and stage III.

Table S5. Zone of inhibition values (in mm) of the monometallic (Ag,Fe) and bimetallic (Ag-Fe) composites against two bacterial strains, Staphylococcus aureus (SA), Escherichia coli (EC), and one fungal strain Candida albicans (CA).

Table S1. FTIR peak assignments for the PVA/PVP blend and their nanocomposites (cm-1)

| Type of mode | Matrix | A6 | F6 | A5F1 | A4F2 | A3F3 | A2F4 | A1F5 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| –OH stretching vibration | 3285 | 3265 | 3288 | 3278 | 3304 | 3283 | 3293 | 3294 |
| C-H asymmetric stretching vibration | 2913 | 2916 | 2920 | 2921 | 2938 | 2917 | 2917 | 2917 |
| carbonyl group of PVA | 1720 | 1718 | 1728 | 1730 | 1729 | 1728 | 1716 | 1731 |
| Strong C=O stretching of PVP | 1644 | 1656 | 1651 | 1652 | 1649 | 1652 | 1651 | 1648 |
| N–H stretching | 1460 | - | 1461 | 1460 | 1461 | 1460 | 1460 | 1460 |
| CH2 wagging vibrations | 1421 | 1422 | 1422 | 1422 | 1422 | 1423 | 1423 | 1422 |
| CH2 asymmetric twisting vibrations | 1290 | - | 1290 | 1290 | 1289 | 1290 | 1290 | 1290 |
| C–O Stretching vibration | 1090 | 1090 | 1091 | 1093 | 1092 | 1097 | 1090 | 1088 |
| N–C stretching | 1025 | 1023 | 1023 | 1023 | 1022 | 1025 | 1022 | 1022 |
| C=N stretching vibration | 1493 | 1490 | 1494 | 1494 | 1495 | 1493 | 1493 | 1494 |
| C–O–C stretching vibration | 1243 | 1249 | 1254 | 1248 | 1255 | 1252 | 1251 | 1256 |

Table S2. d-spacing and crystalline index of the polymer blend and polymer blend nanocomposites.

| Sample | Diffraction angle 2θ | d-spacing (Å) | Crystalline index | FWHM |
| --- | --- | --- | --- | --- |
| Matrix | 19.560 | 4.54 | 0.38 | 5.22 |
| A6 | 19.650 | 4.51 | 0.31 | 5.28 |
| F6 | 19.520 | 4.52 | 0.33 | 5.85 |
| A1F5 | 19.580 | 4.52 | 0.29 | 5.73 |
| A2F4 | 19.380 | 4.57 | 0.28 | 5.45 |
| A3F3 | 19.690 | 4.50 | 0.24 | 5.17 |
| A4F2 | 19.430 | 4.56 | 0.28 | 5.28 |
| A5F1 | 19.500 | 4.54 | 0.28 | 5.35 |

Table S3. Weight% and Atomic% of Ag, Fe elements in prepared composites

| PVA/PVP |  |  | A6 |  |  | F6 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Element | Weight% | Atomic% | Element | Weight% | Atomic% | Element | Weight% | Atomic% |
| C K | 56.50 | 63.40 | C K | 63.93 | 73.37 | C K | 56.55 | 64.61 |
| O K | 43.50 | 36.60 | O K | 30.01 | 25.86 | O K | 40.38 | 34.64 |
|  |  |  | Ag L | 6.05 | 0.77 | Fe L | 3.07 | 0.75 |
| A1F5 |  |  | A3F3 |  |  | A4F2 |  |  |
| Element | Weight% | Atomic% | Element | Weight% | Atomic% | Element | Weight% | Atomic% |
| C K | 53.52 | 62.47 | C K | 49.44 | 60.58 | C K | 48.92 | 60.79 |
| O K | 46.17 | 37.50 | O K | 42.18 | 38.02 | O K | 42.03 | 37.70 |
| Fe L | 5.39 | 1.25 | Fe L | 2.93 | 0.71 | Fe L | 2.77 | 0.69 |
| Ag L | 0.31 | 0.04 | Ag L | 5.45 | 0.69 | Ag L | 6.28 | 0.82 |

Table S4. Weight loss of base matrix, monometallic (Ag, Fe) and bimetallic (Ag-Fe) composites at stage I, stage II and stage III.

| Composition | Weight loss at stage – I | Weight loss at stage -II | Weight loss at stage – III | Residue |
| --- | --- | --- | --- | --- |
| Matrix | 8.26 | 38.6 | 45.93 | 7.27 |
| A1F5 | 8.04 | 58.67 | 22.68 | 10.68 |
| A2F4 | 8.27 | 59 | 26.55 | 6.25 |
| A3F3 | 8.16 | 57.1 | 24.88 | 9.92 |
| A4F2 | 8.96 | 52.1 | 33.11 | 5.89 |
| A5F1 | 8.36 | 91.35 | 0.35 | 0 |
| A6 | 7.87 | 64.5 | 15.2 | 12.5 |
| F6 | 8.41 | 48.89 | 34.87 | 7.63 |

Table S5. Zone of inhibition values (in mm) of the monometallic (Ag, Fe) and bimetallic (Ag-Fe) composites against two bacterial strains, Staphylococcus aureus (SA), Escherichia coli (EC), and one fungal strain Candida albicans (CA).

| Name of the bacteria | Sample code |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | F6 | A6 | A1F5 | A3F3 | A5F1 | Amoxicillin |
| Staphylococcus aureus (SA) | 18 ± 0.2 | 12.5 ± 0.38 | 19.5 ± 0.32 | 29.0 ± 0.26 | 22.0 ± 0.45 | 23.5 ± 0.31 |
| Escherichia coli (EC) | 19.5 ± 0.32 | 22.0 ± 0.42 | 23.5 ± 0.36 | 24.5 ± 0.41 | 24.0 ± 0.37 | 25.0 ± 0.46 |
| Candida albicans (CA) | 19.0 ± 0.47 | 18.5 ± 0.41 | 21.0 ± 0.39 | 22.5 ± 0.37 | 21.5 ± 0.18 | 23.0 ± 0.31 |