# Appendix for

Stabilization and solidification of metal and organotin contaminated sediment after electrochemical pretreatment

Anna Noréna,*, Ann-Margret Strömvalla, Sebastien Raucha, Yvonne Andersson-Sköldc,d, Oskar Modina, Karin Karlfeldt Fedjea,b

Addresses

a Department of Architecture and Civil Engineering, Division of Water Environment Technology, Chalmers University of Technology, SE-412 96 Gothenburg, Sweden

b Recovery and Management, Renova AB, Box 156, SE-401 22 Gothenburg, Sweden

c Swedish National Road and Transport Research Institute (VTI), Box 8072, SE-402 78 Gothenburg, Sweden

d Department of Architecture and Civil Engineering, Division of Geology and geotechnics, Chalmers University of Technology, SE-412 96 Gothenburg, Sweden

* Corresponding author, anna.noren@chalmers.se

Table A.1 Typical chemical composition range of Ecocem GGBS (Ecocem, n.d.)

| Compound | Composition range (%) |
| --- | --- |
| SiO2 | 34.15-37.9 |
| Al2O3 | 10.4-13.1 |
| Fe2O3 | 0.64-0.7 |
| CaO | 37.6-43 |
| MgO | 7-8.1 |
| MnO | 0.4 |
| TiO2 | 0.5-0.7 |
| SO | 0.01-0.20 |
| Cl | 0.01-0.03 |
| S2- | 0.7-1.02 |
| Na2Oeqv | 0.51-0.53 |

Table A.2 Average content of compounds in Byggcement Std PK Skövde (Cementa, 2021)

| Compound | Composition (%) |
| --- | --- |
| CaO | 61.2 |
| SiO2 | 18.2 |
| Al2O3 | 5 |
| Fe2O3 | 2.9 |
| MgO | 1.2 |
| Na2O | 0.16 |
| K2O | 1.2 |
| SO3 | 3.6 |
| Cl | 0.03 |

| Cement | GGBS |
| --- | --- |
| Original sediment | Electro sediment |
| Original S/S | Electro S/S |
| Original S/S 28 U-P | Electro S/S 28 U-P |
| Original S/S 28 NaCl | Electro S/S 28 NaCl |
| Original S/S 56 U-P | Electro S/S 56 U-P |
| Original S/S 56 NaCl | Electro S/S 56 NaCl |
| Original S/S 90 U-P | Electro S/S 90 U-P |
| Original S/S 90 NaCl | Electro S/S 90 NaCl |

Fig. A.1 ESEM images of cement, ground granulated blast-furnace slag (GGBS), untreated (original) sediment, electrochemically pretreated (electro) sediment, stabilized original samples (original S/S), and stabilized electrochemically pretreated sediment (electro S/S). The number in the stabilized samples’ image name identifies the time in days after the casting. The curing conditions for the stabilized sediments were either in ultra-pure (U-P) or saline (NaCl) water

Table A.3 Results from the compression tests for electrochemically pretreated stabilized sediment (electro S/S) and untreated stabilized sediment (original S/S) cured in ultra-pure (U-P) or saline (NaCl) water

|  | Electro S/S U-P | Original S/S U-P | Electro S/S NaCl | Original S/S NaCl |
| --- | --- | --- | --- | --- |
| Day | kPa | kPa | kPa | kPa |
| 28 | 1343 | 444 | 973 | 630 |
| 28 | 873 | 965 | 1280 | 800 |
| 28 | 1160 | 913 | 1342 | 751 |
| 56 | 1295 | 1643 | 1215 | 1696 |
| 56 | 1411 | 1681 | 1232 | 1693 |
| 56 | 1355 | 1712 | 1243 | 1720 |
| 56 | 1042 | 1677 | - | - |
| 90 | 442 | 2282 | 1359 | 2557 |
| 90 | 345 | 2153 | 1308 | 2485 |
| 90 | 226 | 2012 | 1280 | 2514 |
| 90 | 351 | 2436 | - | - |

| Electro stabilized sample in ultra-pure water | Original stabilized sample in ultra-pure water |
| --- | --- |
| Electro stabilized sample in saline water | Original stabilized sample in saline water |
| Electro stabilized sample in saline water with DOC |  |

Fig. A.2 DBT leaching from untreated (i.e., original) and electrochemically pretreated (i.e., electro) stabilized sample cured in ultra-pure water, saline water, as well as saline water with dissolved organic carbon (DOC) in the NEN7375 surface diffusion leaching test. e*(n) displays the measured cumulative leaching and e(n) displays the derived cumulative leaching. The slope 0.5 is marked as a reference for identifying diffusion-controlled leaching (see Method and (Environment Agency, 2005))

| Electro stabilized sample in ultra-pure water | Original stabilized sample in ultra-pure water |
| --- | --- |
| Electro stabilized sample in saline water | Original stabilized sample in saline water |
| Electro stabilized sample in saline water with DOC |  |

Fig. A.3 MBT leaching from untreated (i.e., original) and electrochemically pretreated (i.e., electro) stabilized sample cured in ultra-pure water, saline water, as well as saline water with dissolved organic carbon (DOC) in the NEN7375 surface diffusion leaching test. e*(n) displays the measured cumulative leaching and e(n) displays the derived cumulative leaching. The slope 0.5 is marked as a reference for identifying diffusion controlled leaching (see Method and (Environment Agency, 2005))

| Treated stabilized sample in ultra-pure water | Original stabilized sample in ultra-pure water |
| --- | --- |
| Treated stabilized samples in saline water | Original stabilized sample in saline water |

Fig. A.4 Al leaching from untreated (original) and electrochemically pretreated (electro) stabilized sample cured in ultra-pure water and saline water in the NEN7375 surface diffusion leaching test. e*(n) displays the measured cumulative leaching and e(n) displays the derived cumulative leaching. The slope 0.5 is marked as a reference for identifying diffusion-controlled leaching (see Method and (Environment Agency, 2005))

Fig. A.5 Metals released (µg/kg DW) during the granular waste compliance L/S10 leaching test, leached in either ultra-pure water or saline water. Each uniquely colored bar is corresponding to either untreated (i.e., original) or electrochemically pretreated (electro) stabilized samples cured in ultra-pure water (U-P) or saline water (NaCl). The number on the horizontal axis denotes the number of days the samples have been curing when the leaching test was conducted

# References

Cementa, 2021. Typanalys 2020.

Ecocem, n.d. GGBS - Technical data sheet.

Environment Agency, 2005. EA NEN 7375:2004 Leaching characteristics of moulded or monolitic building and waste material. Determination of leaching of inorganic components with diffusion test. "The tank test".