Supplementary information for

SnO2-NiO nanoparticles anchored in ultrathin graphite nanosheets as a high-performance anode material for lithium-ion batteries

Wenbin Ye, Jinxuan Lei, Chaokui Jiang, Zuyong Feng *, Deping Xiong, Miao He

School of Physics and Optoelectronic Engineering, Guangdong University of Technology, Guangzhou, Guangdong 510006, PRC.

*Corresponding author. E-mail address: fengzuyong@foxmail.com (Zuyong Feng)

Fig. S1. Long-term cycling performance of the SnO2-C composite at 1.0 A g-1.

Fig. S2. Long-term cycling performance of SnO2 at 1.0 A g-1.

Fig. S3. CV curves of the SnO2-C composite at various scanning rates.

Fig. S4. The capacitance contribution rates of the SnO2-C composite obtained at various scanning rates from 0.1 to 2.0 mV s-1.

Table S1. Comparison of the specific capacities of previously reported SnO2-based anode materials.

| Samples | Cycling performance Capacity (mAh g−1) /Number (n) /Rate (A g−1) | Rate performance Capacity (mAh g−1) / Rate (A g−1) | Ref |
| --- | --- | --- | --- |
| SnO2@TiO2 | 472.7/800/2.0 518.2/500/0.8 | 388.9/5.0 | [S1] |
| bowl-like SnO2@carbon | 963.0/100/0.4 | 850.0/1.6 | [28] |
| Sandwich-like SnO2/Cu@Carbon | 348.0/1000/1.0 | 289.0/2.0 | [29] |
| SnO2/MoS2(1:3)@ CMK-9 | 1245.0/300/0.1 823.0/1000/1.0 | 740.0/2.0 | [30] |
| W-SnO2-C | 1148.8/500/0.2 1229.5/800/1.0 | 312.3/5.0 | [31] |
| NiO-SnO2/graphene | 826.0/500/1.0 | 721.0/5.0 | [33] |
| Sn@SnO2@C@MoS2 | 841.0/400/1.0 | 458.3/10.0 | [S2] |
| Sn/SnOx@Ti3C2 | 594.2/200/0.05 | 194.5/5.0 | [44] |
| Sn/SnO2@Carbon | 986.3/2000/1.0 | 508.2/5.0 | [56] |
| V2O5-C-SnO2 | 800.0/100/0.2 | 620.0/0.8 | [S3] |
| CNTs@SnO2/SnO/Sn | 394.0/50/0.1 | 200/2.0 | [S4] |
| SnO2/GN | 757.0/500/1.0 | 708.0/1.0 609.0/2.0 | [S5] |
| SnO2-CuO-G | 561.2/150/0.1 | 440.0/1.0 | [S6] |
| SnO2-NiO-C | 1224.3/300/0.2 820.1/1000/1.0 | 507.1/5.0 | This work |

Table S2. Impedance parameters obtained from equivalent circuit model (Fig. 6C) for SnO2-NiO-C, SnO2-C and SnO2 anode materials before cycling.

| Materials | SnO2-NiO-C | SnO2-C | SnO2 |
| --- | --- | --- | --- |
| RΩ/Ω | 1.024 | 2.314 | 4.586 |
| Rct/Ω | 271.8 | 407.8 | 551.4 |

References

[1] Q. Tian, Y. Tian, W. Zhang, J. Huang, Z. Zhang, L. Yang, Impressive lithium storage of SnO2@TiO2 nanospheres with a yolk-like core derived from self-assembled SnO2 nanoparticles, Journal of Alloys and Compounds, 702 (2017) 99-105.

[2] Y.G. Huang, Q.C. Pan, H.Q. Wang, C. Ji, X.M. Wu, Z.Q. He, Q.Y. Li, Preparation of a Sn@SnO2@C@MoS2 composite as a high-performance anode material for lithium-ion batteries, J. Mater. Chem. A 4 (2016) 7185.

[3] L. Zhang, M. Yang, S. Zhang, Z. Wu, A. Amini, Y. Zhang, D. Wang, S. Bao, Z. Lu, N. Wang, C. Cheng, V2O5-C-SnO2 Hybrid Nanobelts as High Performance Anodes for Lithium-ion Batteries, Scientific Reports, 6 (2016).

[4] J. Zhang, Z.S. Ma, W.J. Jiang, Y.L. Zou, Y. Wang, C.S. Lu, Sandwich-like CNTs@SnO2/SnO/Sn anodes on three-dimensional Ni foam substrate for lithium ion batteries, Journal of Electroanalytical Chemistry, 767 (2016) 49-55.

[5] L. Zhan, X.S. Zhou, J. Luo, X.M. Ning, Binder-free multilayered SnO2/graphene on Ni foam as a high-performance lithium ion batteries anode, Ceramics International, 45 (2019) 6931-6936.

[6] B. Lu, H. Wang, R.Z. Hu, L.C. Yang, J. Liu, J.W. Liu, M. Zhu, Enhanced cyclic performance of SnO2-CuO-graphitenano-sheetsas anode for Li-ion battery, Mater.Lett. 185 (2016) 9–12.