Supporting Information

Mechanically robust room-temperature self-healing waterborne polyurethane with antimicrobial properties constructed through multiple dynamic bonds

YuanWang 1, Liang Chen 1, Pingping Jiang 1, Pingbo Zhang 1,*, Yanmin Bao 2, Xuewen Gao 2, Jialiang Xia 2

1 Key Laboratory of Synthetic and Biological Colloids, Ministry of Education, School of Chemical and Material Engineering, Jiangnan University, Wuxi 214122, P. R. China

2 Jiangsu Caihua Packaging Group Company, Kunshan 215321, P. R. China

*Corresponding authors: Pingbo Zhang (E-mail: pingbozhang@126.com)

Fig. S2 1H-NMR of 2,6-diacetylpyridine dioxime.

Fig.S1 Infrared spectra of 2,6-diacetylpyridine dioxime and 2,6-Diacetylpyridine.

Table. S1 Chemical constituents of polyurethane emulsion

Sample a     IPDI/g  PTMG/g  DMPA/g  2,6-DDb/g  TEA/g  CuCl2·2H2O/g

DWPU       2.70     4.95      0.42      0.25     0.31         0

DWPU-Cu0.25  2.70     4.95      0.42      0.25     0.31        0.06

DWPU-Cu0.5  2.70     4.95      0.42      0.25     0.31        0.12

a  The molar ratios of CuCl2⋅2H2O to 2,6-diacetylpyridine doxime were 0.25 and 0.5, respectively, and the corresponding samples were recorded as DWPU-Cu0.25 and DWPU-Cu0.5

b 2,6-diacetylpyridine dioxime is abbreviated as 2,6-DD

Fig. S3 Cu 2p high-resolution XPS spectra of DWPU (a) and DWPU-Cu0.25 (b).