Supplementary material

The Hydroxyapatite Nanowires as High Loading Substrate for Immobilization of Dextranase by Crosslinking Method

Bingnan Sun a,1  Yajie Wang b,1  Haoran Yu a Lei Zhang a*  Weibing Zhang a*

aShanghai Key Laboratory of Functional Materials Chemistry, School of Chemistry & Molecular Engineering, East China University of Science and Technology, Shanghai 200237, P. R. China

bDepartment of Pharmacy, Anhui Medical College, Hefei 230601, P. R. China

*Corresponding authors: leizhang595@ecust.edu.cn; weibingzhang@ecust.edu.cn

Contributing authors: sun98510102@163.com; cactus0926@hotmail.com

These authors contributed equally to this work.

Fig. S1 Effects of the initial concentration of dextranase on the loading capacity of HAPNWs-NH2@dextranase.

Fig. S2 Nitrogen adsorption-desorption isotherms of HAPNWs (a) and BJH desorption pore size distribution curves of HAPNWs (b).

Table S1 Immobilization of dextranase on different substrate.

Table S2 Relative activity of immobilized enzyme at 70°C on different substrate.

Fig. S1 Effects of the initial concentration of dextranase on the loading capacity of HAPNWs-NH2@dextranase.

Fig. S2 Nitrogen adsorption-desorption isotherms of HAPNWs (a) and BJH desorption pore diameter distribution curves of HAPNWs (b).

Table S1 Immobilization of dextranase on different substrate.

| Immobilization method | Substrate | Loading capability（mg·g-1） | Refs. |
| --- | --- | --- | --- |
| Covalent binding | Fe3O4@PDA@GO-PEI | 305.1 | [1] |
| Covalent binding | Fe3O4@SiO2-PEI | 217.2 | [2] |
| Covalent binding | Fe3O4@SiO2-NH2 | 56.55 | [3] |
| Covalent binding | Eupergit C | 16 | [3] |
| Covalent binding | Eupergit C250L | 11 | [3] |
| Covalent binding | Hydroxyapatite | 40 | [4] |
| Adsorption | Mg/Fe-LDH | 1.38 | [5] |

Table S2 Relative activity of immobilized enzyme at 70°C on different substrate.

| Immobilization method | Support | Relative activity (%) | Refs. |
| --- | --- | --- | --- |
| Covalent binding | Fe3O4@SiO2-PEI | 86.43 | [2] |
| Covalent binding | Fe3O4@SiO2-NH2 | 77.68 | [2] |
| Covalent binding | HAP-GA | 92.29 | [4] |
| Embedding | Alginate | 83.12 | [6] |

References

- Y. Wang, Q. Wang, X. Song, and J. Cai, Biochemical Engineering Journal 141, 163 (2019).

- Y. Wang, Q. Wang, X. Song, and J. Cai, New J. Chem. 42, 8391 (2018).

- F. A. Erhardt and H.-J. Jördening, Journal of Biotechnology 131, 440 (2007).

- Y. Ding, H. Zhang, X. Wang, H. Zu, C. Wang, D. Dong, M. Lyu, and S. Wang, Materials 14, 130 (2020).

- Y. Ding, L. Liu, Y. Fang, X. Zhang, M. Lyu, and S. Wang, Nanomaterials 8, 173 (2018).

- F. Shahid, A. Aman, and S. A. U. Qader, International Journal of Polymer Science 2019, 1 (2019).