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Fig. S1. The Epass/log(jpass) (in green) and Epit/log(jpit) (in red) ground truth values (maxima KDE of the distributions determined by the hybrid algorithm) represented as “target” markers. Superimpositions as a function of potential (V) of the: a) conditional mean of the log(j) (with conditional SD and SE); b) the conditional median of the log(j) (with conditional MAD). The estimates provided by the mean and median models are respectively displayed in a) and b) as “dart attempt” markers. Results related to the 0.01 M NaCl (100 mV/s) set.
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Fig. S2. Identical description of the Fig. S1 caption. Results related to the 0.01 M NaCl (50 mV/s) set.
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Fig. S3. Identical description of the Fig. S1 caption. Results related to the 0.05 M NaCl (100 mV/s) set.
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Fig. S4. The top 4 conditional jmax curves as a function of E, for each dataset.
image1.tiff
mean
standard deviation
standard error
Epass (ground truth)
Eve (ground truth)
(mean model)

Eoc (mean model)

median
median absolute deviation
Epass (ground truth)

Epe (ground truth)

Ecass (median model)

Eqe (median model)





image2.tiff
mean
standard deviation
standard error

Epass (ground truth)
Epe (ground truth)

Epess (mean model)

Ev (mean model)

median
median absolute deviation
Epass (ground truth)

Ene (ground truth)

Epass (median model)

Epe (median model)





image3.tiff
mean
standard deviation
standard error
Epess (ground truth)
Eoe (ground truth)
Epess (mean model)
Eoc (mean model)

median
median absolute deviation
Epass (ground truth)

Epe (ground truth)

Epess (median model)

Epe (median model)





image4.tiff
Top 4 conditional jm.x as a function of potential

0.05 M NaCl (50 mV/s)
0.05 M NaCl (100 mV/s)
0.01 M NaCl (50 mV/s)
0.01 M NaCl (100 mV/s)
0.005 M NaCl (100 mV/s)





