Supporting Information

Resorbable Barrier Polymers for Flexible Bioelectronics

Samantha M. McDonald1, Quansan Yang2, Yen-Hao Hsu1, Shantanu P. Nikam1, Ziying Hu2, Zilu Wang3, Darya Ashegali1, Tiffany Yen1, Andrey V. Dobyrnin3, John A. Rogers2,4* and Matthew L. Becker1,5,6,7*

# 1 Department of Chemistry, Duke University, Durham, NC 27708, United States

2 Department of Materials Science and Engineering, Northwestern University, Evanston, IL, 60208 USA

# 3 Department of Chemistry, University of North Carolina-Chapel Hill, Chapel Hill, NC 27599, USA

# 4 Department of Biomedical Engineering and Neurological Surgery, Northwestern University, Evanston, IL, 60208 USA

# 5Thomas Lord Department of Mechanical Engineering and Materials Science, Duke University, Durham, NC 27708, USA

# 6Department of Biomedical Engineering, Duke University, Durham, NC 27708, USA

# 7Department of Orthopedic Surgery, Duke University, Durham, NC 27708, USA

Corresponding Authors

Matthew L. Becker, PhD

Hugo L. Blomquist Distinguished Professor

Duke University

Department of Chemistry, Thomas Lord Department of Mechanical Engineering & Material Science, Department of Biomedical Engineering and Department of Orthopaedic Surgery

308 Research Drive

Durham, NC 27708

(919) 681-3812

matthew.l.becker@duke.edu

John A. Rogers, PhD

Louis Simpson and Kimberly Querrey Professor

Northwestern University

Querrey Simpson Institute for Bioelectronics

Departments of Mechanical Engineering, Material Science and Engineering, Biomedical Engineering

Evanston, IL, 60208, USA

jrogers@northwestern.edu

CONTENTS

Experimental & Methods. Materials ……………………………………………………………..………..…….S3

Experimental & Methods. Synthetic Methods ………………………………………………...…………..…….S4

Experimental & Methods. Instrumental Methods ………………………………………………………..……...S6

Experimental & Methods. Simulation Methods …………………………………………...……………..….….S9

Scheme S1. Proposed Mechanism for Thiol-yne Copolymerization ……………………….……..………..…….S9

Figure S1. The 1H NMR spectrum of 0% Css………………………………………………….….………..…….S10

Figure S2. SEC chromatogram of 0% Css ………………………………………………………….……..…..…S11

Figure S3. The 1H NMR spectrum of 10% Css …………………………………………………….…………….S12

Figure S4. SEC chromatogram of 10% Css ………….…………………………………………..………………..S13

Figure S5. The 1H NMR spectrum of 15% Css .……………………………………………………………....….S14

Figure S6. SEC chromatogram of 15% Css ……………………………………………………………..…….…..S15

Figure S7. The 1H NMR spectrum of 20% Css …………………………………………………..………….…….S16

Figure S8. SEC chromatogram of 20% Css ……………………………………………………………………....S17

Figure S9. The 1H NMR spectrum of 25% Css ……………………………………………………….………….S18

Figure S10. SEC chromatogram of 25% Css …………………………………………………………..………....S19

Figure S11. The 1H NMR spectrum of 30% Css ……………………………………………………….………...S20

Figure S12. SEC chromatogram of 30% Css ………………………………………………………….…………S21

Figure S13. The 1H NMR spectrum of 40% Css ………………………………………………………...………...S22

Figure S14. SEC chromatogram of 40% Css …………………………………………………………..…………S23

Figure S15. The 1H NMR spectrum of 50% Css ………………………………………………………..………...S24

Figure S16. SEC chromatogram of 50% Css ……………………………………………………………..………S25

Figure S17. The 1H NMR spectrum of 60% Css ………………………………………………………….……...S25

Figure S18. SEC chromatogram of 60% Css ……………….………………………………………..……………S27

Figure S19. The 1H NMR spectrum of 100% Css …………………………………………………….…………...S28

Figure S20. SEC chromatogram of 100% Css ……………….……………………………………………………S29

Figure S21. Overlapped TGA data of all synthesized polymers……………………………………………..……S30

Figure S22. Overlapped DSC thermograms of all synthesized polymers ……………………………...…..……S31

Figure S23. Stress vs. strain curves for all synthesized polymers ……………………………………………….S32

Figure S24. Control experiments for Variable Cooling Rate DSC Experiments…..…………………………….S33

Figure S25. In vitro degradation studies………………………………………..…..……………………………S34

Figure S26. Variable cooling rate DSC of 60% Css Css …………………………………………………………S35 Figure S27. VT-WAXS experiments of 60% Css…………………………………………………………………S35

Figure S28. XRD of 10-25% Css…………………………………………………….……………………………S36

Figure S29. Representative Hoffman-Weeks extrapolation………………………………………………………S36

Figure S30.2D Scattering Patterns for 20% Css…………………………………………………………………..S37

Figure S31.Partial Charge Distributions for Monomer Sequences………………………………………...……..S37

Table S1. Simulated Equilibrium Phase Structure for Css Coolymer Melts …………………………….………..S38

Figure S32. Additional Scattering Functions for Other Copolymer Compositions ………………………..……..S38

Figure S33. Variable Temperature WAXS for 20% Css Copolymers ……………………………………..……..S39

Figure S34. DSC Thermograms of Melt-Pressed 20% Css ………//////////////……………………………..……..S40

References……….……………………………………………………………………………...………………..S40

EXPERIMENTAL & METHODS

Materials

# All reagents and solvents were used as received without further purification except 1,10-decanedithiol which was distilled under vacuum before use. The chloroform-d (CDCl3) was purchased from Cambridge Isotopes Laboratories, Inc . Diethyl ether (Et2O), isopropyl alcohol (iPrOH), and dichloromethane (CH2Cl2) were purchased from EMD Millipore. Ethyl acetate (EtOAc), sodium sulfate (Na2SO4), sodium bicarbonate (NaHCO3), ammonium chloride (NH4Cl), propiolic acid, sulfuric acid, 1,8-diazabicyclo[5.4.0]undec-7-ene (DBU), hexanes, butylated hydroxytoluene (BHT), succinic acid, 1,3-propanediol (>98%) were purchased from Sigma-Aldrich. Chloroform (CHCl3) was purchased from VWR Chemicals (99% with amylene as inhibitor) and Fischer Scientific (HPLC grade, 99.5+% with amylene as inhibitor), 3-mercapto-1-propanol (>97%), 1,10-decanedithiol (>98%), were purchased from Tokyo Chemical Industry Ltd.

Synthetic Methods

Synthesis of 1,3-propane diyl dipropiolate (C3A)

The synthetic procedure for C3A was reported previously.20 Briefly, a 500 mL one-neck round bottom flask was charged with 1,3-propanediol (20.000 g, 0.263 mol), propiolic acid (50.000 g, 0.714 mol), and two drops of H2SO4 in approximately 200 mL of toluene. The mixture was heated to reflux (120-130 C) overnight with a Dean-Stark trap to collect the water byproduct. The reaction solution was cooled to ambient temperature and neutralized with a saturated solution of sodium bicarbonate, then extracted into ethyl acetate three times.  The organic phase was collected, dried over magnesium sulfate, gravity filtered, and reduced in volume to dryness. The collected crude product was then purified through silica column chromatography using ethyl acetate: hexanes (1:3, v/v; Rf = 0.45) as an eluent. The first spot was distilled under vacuum (0.02 Torr, 106 C) to yield a colorless oil (39.80 g, 84.0 %). 1H NMR (500 MHz, CDCl3) δ 4.29 (t, J = 10 Hz, 4H), 2.91 (s, 2 H), 2.07 (quint, J = 10 Hz, 2 H).

Synthesis of Bis(3-mercaptopropyl) succinate (Css)

The synthetic procedure for Css was reported previously.18  Succinic acid (15.000 g, 0.127 mol), 3-mercapto-1-propanol (25.000 g, 0.271 mol), and two drops of H2SO4 were added to a round-bottom flask (250 mL) precharged with toluene (180 mL). The mixture was then heated to reflux (120 C) with a Dean-Stark trap overnight to collect the water byproduct. The reaction solution was cooled to ambient temperature and neutralized with a saturated solution of sodium bicarbonate, then extracted into ethyl acetate three times.  The organic phase was collected, dried over magnesium sulfate, gravity filtered, and reduced in volume to dryness.  The collected crude product was then purified through silica column chromatography using ethyl acetate: hexanes (2:3, v/v; Rf = 0.45). The final product was further purified by distillation under high vacuum (0.02 Torr, 150 C) to yield a colorless oil (26.70 g, 79.1 %). 1H NMR (500 MHz, CDCl3) δ 4.20 (t, J = 10 Hz, 4 H), 2.62-2.57 (m, 8 H), 1.93 (quint, J = 10 Hz, 4 H), 1.39 (t, J = 10 Hz, 2 H).

Representative procedure for thiol-yne step-growth polymerization

80% Cis, 20% Css copolymer was synthesized as follows: Css (0.715 g, 0.268 mmol), C3A (2.42 g, 13.4 mmol) and C10S (2.21 g, 10.7 mmol) were added to an oven-dried 100 mL round bottom flask with 25 mL CHCl3. The solution was then cooled to -15 C (ice and sodium chloride mixture) with stirring for 15 min. DBU (20 μL, 0.134 mmol) was diluted in a small amount of CHCl3 and added dropwise due to the exothermicity of the reaction. Additional CHCl3 was added as needed (i.e., following increases in viscosity which rendered the stir bar unable to mix the reaction solution). 5 min after full addition of DBU, the reaction was allowed to warm to room temperature and stirred under ambient conditions for 2 hours. A few drops of C3A was added prior to quenching to cap terminating thiols, then BHT (225 mg, 10.22 × 10-5 mol) was added to quench the catalyst. Polymer was precipitated directly from the reaction mixture with diethyl ether (400 mL) and collected by decanting the supernatant. The pale-yellow polymer was then dried under high vacuum at ambient temperature for 24 h (20% CSS, 8.81 g, 90 %). SEC (CHCl3, based on PS standards) Mn = 32.5 kDa, Mw = 72.8 kDa, ÐM = 2.1. DSC: Tg = -7.3 C, Tc = 30.3 C, Tm = 99.3 C. TGA: Td = 348C. Tensile tests: E0 = 57.2 ± 4.4 MPa, break = 1700 ± 31 %, UTS = 40.5 ± 2.2 MPa.

0% Css: The polymer was prepared by the general procedure described above. 1H NMR (CDCl3, 500 MHz) % cis ~ 80 with 0% Css incorporation. SEC (CHCl3) Mn = 33.1 kDa, Mw = 72.8 kDa, ÐM = 2.2.  DSC: Tg = -6.8 C, Tc = 61.4 C, Tm = 112.4 C. TGA: Td = 351 C. Tensile tests: E0 = 65.8 ± 0.6 MPa, break = 1457 ± 112 %, UTS = 32.2 ± 3.9 MPa.

10% Css: The polymer was prepared by the general procedure described above. 1H NMR (CDCl3, 500 MHz) % cis ~ 80 with 10% Css incorporation. SEC (CHCl3) Mn = 32.1 kDa, Mw = 81.3 kDa, ÐM = 2.5. DSC: Tg = -9.7 C, Tc = 54.0 C, Tm = 102.3 C. TGA: Td = 354 C. Tensile tests: E0 = 105.2 ± 1.4 MPa, break = 1105 ± 67 %, UTS = 26 ± 0.1 MPa.

15% Css: The polymer was prepared by the general procedure described above. 1H NMR (CDCl3, 500 MHz) % cis ~ 80 with 15% Css incorporation. SEC (CHCl3) Mn = 23.6 kDa, Mw = 54.5 kDa, ÐM = 2.3. DSC: Tg = -10.1 C, Tc = 44.1 C, Tm = 95.4 C. TGA: Td = 357 C. Tensile tests: E0 = 93.1 ± 2.1 MPa, break  = 1384 ± 108 %, UTS = 25 ± 0.5 MPa.

25% Css: The polymer was prepared by the general procedure described above. 1H NMR (CDCl3, 500 MHz) % cis ~ 80 with 25% Css incorporation. SEC (CHCl3) Mn = 34.0 kDa, Mw = 89.0 kDa, ÐM = 2.2. DSC: Tg = -9.1 C, Tc = 26.1 C, Tm = 93.1 C. TGA: Td = 359 C. Tensile tests: E0 = 67.2 ± 1.7 MPa, break = 1506 ± 37 %, UTS = 25 ± 3.4 MPa.

30% Css: The polymer was prepared by the general procedure described above. 1H NMR (CDCl3, 500 MHz) % cis ~ 80 with 30% Css incorporation. SEC (CHCl3) Mn = 29.1 kDa, Mw = 60.4 kDa, ÐM = 2.1. DSC: Tg = -7.3 C, Tc = 18.5 C, Tm = 88.9 C. TGA: Td = 349 C. Tensile tests: E0 = 40.9 ± 3.5 MPa, break  = 1638 ± 33 %, UTS = 28.3 ± 1.2 MPa.

40% Css: The polymer was prepared by the general procedure described above. 1H NMR (CDCl3, 500 MHz) % cis ~ 80 with 40% Css incorporation. SEC (CHCl3) Mn = 26.7 kDa, Mw = 57.0 kDa, ÐM = 2.1. DSC: Tg = -7.4 C, Tc = 12.7 C, Tm = 82.5 C. TGA: Td = 349 C. Tensile tests: E0 = 36.2 ± 2.0 MPa, break = 2110 ± 50 %, UTS = 36.2 ± 4.1 MPa.

50% Css: The polymer was prepared by the general procedure described above. 1H NMR (CDCl3, 500 MHz) % cis ~ 80 with 50% Css incorporation. SEC (CHCl3) Mn = 45.4 kDa, Mw = 94.9 kDa, ÐM = 2.1. DSC: Tg = -9.7 C, Tc = 21.5 C, Tm = 74.2 C. TGA: Td = 348 C. Tensile tests: E0 = 36.2 ± 2.0 MPa, break = 1943 ± 155 %, UTS = 37.4 ± 4.5 MPa.

60% Css: The polymer was prepared by the general procedure described above. 1H NMR (CDCl3, 500 MHz) % cis ~ 80 with 60% Css incorporation. SEC (CHCl3) Mn = 29.0 kDa, Mw = 71.7 kDa, ÐM = 2.5. DSC: Tg = -12.2 C. TGA: Td = 342 C. Tensile tests: E0 = 12.0 ± 1.4 MPa, break = 2077 ± 78 %, UTS = 20.5 ± 0.6 MPa.

100% Css: The polymer was prepared by the general procedure described above. 1H NMR (CDCl3, 500 MHz) % cis ~ 80 with 100% Css incorporation. SEC (CHCl3) Mn = 62.0 kDa, Mw = 86.8 kDa, ÐM = 1.4. DSC: Tg = -12.6 C. TGA: Td = 358 C. Tensile tests: E0 = 4.6 ± 0.3 MPa, break = 1886 ± 147 %, UTS = 8.4 ± 1.9 MPa.

Instrumental Methods

Nuclear Magnetic Resonance (NMR) Spectroscopy 1H NMR spectra were acquired on a 500 MHz Bruker NMR spectrometer at 298 K in deuterated chloroform. 16 scans were acquired with a 3-second relaxation delay.

Size Exclusion Chromatography (SEC) Molecular weight was determined by SEC using an EcoSEC HLC-8320GPC (Tosoh Bioscience LLC, King of Prussia, PA) with a TSKgel GMHHR-M mixed bed column, refractive index (RI) detector and poly(styrene) standards. ~3 mg/mL samples were prepared using HPLC grade chloroform for injection with a 0.5 mL/min flow rate at 40 °C.

Thermogravimetric Analysis (TGA) Degradation temperatures for each of the copolymers were determined using TGA on a TA Instruments Discovery TGA550 (TA Instruments – Waters L.L.C, New Castle, DE). Unless otherwise noted, 5 – 10 mg samples were used with a ramp rate of 20°C/min from room temperature to 800°C.  Degradation temperature was determined from the onset of the step transition.

Differential Scanning Calorimetry (DSC) Thermal transitions (Tg, Tm, and Tc) were determined from the centers of the transitions acquired by DSC (first cooling and second heating cycle) on a TA Instruments Discovery DSC250 (TA Instruments – Waters L.L.C., New Castle, DE). Unless otherwise noted, 5 – 10 mg samples were used with a ramp rate of 10 °C/min for both the heating and cooling cycles.

Variable Cooling DSC Variable cooling DSC experiments were performed to investigate the effect of cooling rate on crystallization on samples between 5 – 8 mg. The heating ramp rate was maintained at 10 °C/min across the same temperature distribution for each sample. Then various cooling rates were set to examine how Tc shifted as a result. Three control experiments were performed to establish the validity of these results. The first was a 4 cycle DSC experiment with 10 °C/min heating and cooling rate which confirmed there was no shift in Tc because of thermally cycling the material. The second control experiment was another DSC experiment to establish the reproducibility of the Tc shift. The polymer was cooled at some slow cooling rate followed by a set heating cycle then cooled quickly. After the next heating cycle, it was cooled at the same slow cooling rate to which showed no difference in Tc shift between the two slow cooling cycles. Lastly, SEC was performed on the DSC-cycled samples with an uncycled control to confirm there was minimal thermal degradation. See Appendix C.9

Spin Coating Spin-coating was performed on a Laurell Technologies Corporation HL650Mz-23NPPB spin coater with two 5-second 500 rpm at 500 rpm/s cycles followed by one 3-second 2000 rpm at 1500 rpm/s cycle and finally one 30-second 5000 rpm at 2000 rpm/s cycle. The lower speed cycles were performed to reduce the wobble of the spinning substrate when accelerating.

Compression Molding Melt press films were prepared on a bubble magic 5” x 5” pneumatic heat press (70 psi) between Teflon sheets, poly(acrylic acid) spin-coated Kapton sheets, or Mefine FEP film 10 –  20 °C above their melting temperature (as determined by DSC). Fast cooling was performed by removing pressed film and placing between two cold metal plates on the benchtop until cool. Slow cooling was performed by setting the instrument to room temperature and maintaining pressure until temperature was below 40 °C.

Extrusion Filaments were prepared on a Thermo Scientific HAAKE MiniCTW extruder typically 10 – 20 °C above the polymer’s melting temperature (determined by DSC).

Contact Angle A ramé-hart instrument co. contact angle goniometer was used with DROPimage Pro software to calculate and image the contact angles of 5 L of water, ethylene glycol, and glycerol on the polymer films. DROPimage Pro fits the shape of the droplet on the polymer film and measures the tangent angle between the solid-liquid interface.

Tensile Testing Dogbones were punched from 0.5 mm thick films using a Pioneer Die-tecs die following ASTM D-638-V. Tensile Instron universal testing machine (UTM) at room temperature with a 1 kN load cell at 10 mm/min displacement rate. Young’s Modulus was determined by dividing the stress by the strain % at 5 % strain for each replicate. Ultimate tensile strength was determined from the maximum stress observed, and elongation at break was determined from the strain % observed at break.

X-ray Diffraction (XRD) XRD was performed using a Panalytical X-Pert PRO MRD HR XRD system in a two-theta analysis configuration with a Cu K-alpha source, ½° divergence slit, and Xe proportion detector. The diffraction pattern was collected from 10 – 80° with a 0.05 step size at 1 s/step.

Method for Calculating Lamellar Thicknesses

l=0.9λFWHMcosθ2

Lamellar thicknesses were determined from XRD of 15-25% Css by the Debye-Scherrer equation:

Small-, and Wide-Angle X-ray Scattering (SAXS,  WAXS) SAXS, and WAXS were performed on a SAXSLab Ganesha system with a Cu 50kV Xenocs Genix ULD SL X-ray point source and a 170 m pixel-spaced, single-photon counting Dectris Pilatus 300k 20 Hz detector. This was done in a 2 slit configuration where the distance between the sample and the detector was approximately 101, and 1041 mm for WAXS, and SAXS, respectively. 1D averaging of SAXS data was carried out by averaging across all azimuths with linear x-axis binning. Spectra-by-spectra reduction and corrections for sample transmission, sample thickness and absolute intensity factor were all included as part of 1D averaging using saxsgui software v2.23.33. To accurately determine the momentum transfer corresponding to the peak intensities in SAXS/WAXS spectrums the patterns were modeled using Fityk software. A spline was used to flatten the baseline and gaussian distributions (7 for WAXS, 2 for SAXS) were used to model the pattern by minimizing the residual. Degree of crystallinity was determined from this fitting by taking dividing the crystalline guassian areas by the crystalline and amorphous guassian areas.

Atomic Force Microscopy (AFM) AFM was performed in tapping mode with Budget Sensors Tap300GD-G tips (resonant frequency = 300 kHz, force constant = 40 N/m) on an Asylum Cypher ES Environmental atomic force microscope.

Dynamic Vapor Sorption (DVS) DVS was performed on a TA Q5000 SA sorption analyzer with 5-20 mg of polymer film at 25°C and 0% relative humidity (RH) for 10 minutes. RH was then ramped at 25°C 0.5% min-1  from 0% RH to 97.5% RH. 97.5% RH was maintained for 120 minutes after this point. PET control was provided by TA instruments with DHR relative humidity accessory.

Molecular Dynamics Simulations Methods

All simulations were performed as follows:

- Randomly paced Nchain copolymer chains inside a cubic simulation box with size L=200

- Changed all non-bonded interactions between coarse-grained beads into WCA potential (LJ=1.0 kBT and rcut=21/6 followed by the system relaxation under NVT ensemble conditions (a1) for duration 10000τLJ.

- Gradually decreased the simulation box to achieve the density 0.1 and relaxed the system for another 1000 τLJ.

- Changed nonbonded interaction between coarse-grained beads to the parameters shown in Table 2, and increased the system temperature to 2.0 in energy units followed by the system relaxation lasting 1000 τLJ.

- Switched to  NPT ensemble (a2) with the temperature T=2.0 and relaxed the system for additional 5000 τLJ.

- After the system was fully relaxed at T=2.0 under NPT ensemble conditions, we performed series of annealing cycles to reach an equilibrium. In each annealing cycle, the simulation temperature T was decreased from Tmax=2.0  to Tmin=1.0 during simulation run lasting 10000 τLJ. After the first annealing cycle was completed, the second cycle began with Tmax=1.9 and then repeat the cycle until Tmin=1.0.

- After completing the annealing cycles, a simulation run at T=1.0 was performed for data collection.

Scheme S1. Proposed mechanism as suggested previously which accounts for the high cis content observed for the DBU-catalyzed thiol-yne click polymerizations.1-3 Shown is one addition cycle which would be repeated many times randomly between C3A species with either C10s or Css.

Figure S1. The 1H NMR spectra of 0% CSS shows the 81% cis content for the thiol-yne step-growth polymer. Cis- content can be calculated by the J coupling constants of the respective resonances. Resonance f, g, h, i, and j are from the dithiol monomer (C10S) and resonance a, b, and c are from the 1,3-propane dipropiolate monomer (C3A). The polymer reveals cis %/ trans % = 81 %: 19 % in CHCl3 with 1 mol% DBU (CDCl3, 500 MHz).

Figure S2. SEC chromatogram of 0% CSS of thiol-yne step-growth polymer; Mn = 32.5 kDa, Mw = 72.8 kDa, ÐM = 2.24 (SEC CHCl3, based on PS standards).

Figure S3. The 1H NMR spectra of 10% CSS shows the 80% cis content for the thiol-yne step-growth copolymer with 10% incorporation of CSS in CHCl3 with 1 mol% DBU. The ratio of resonance n (from CSS) to resonance h (from C10S) displays 10%: 90% that affords a polymer 10% incorporation of CSS (CDCl3, 500 MHz).

Figure S4. SEC chromatogram of 10% CSS of thiol-yne step-growth polymer; Mn = 32.1 kDa, Mw = 81.3 kDa, ÐM = 2.51. (SEC CHCl3, based on PS standards).

Figure S5. The 1H NMR spectra of 15% CSS shows the 80% cis content for the thiol-yne step-growth copolymer with 15% incorporation of CSS in CHCl3 with 1 mol% DBU. The ratio of methylene resonance n (from CSS) to methylene resonance h (from C10S) displays 15%: 85% that affords polymer 15% incorporation of CSS (CDCl3, 500 MHz).

Figure S6. SEC chromatogram of 15% CSS of thiol-yne step-growth polymer; Mn = 23.6 kDa, Mw = 54.5 kDa, ÐM = 2.30. (SEC CHCl3, based on PS standards).

Figure S7. The 1H NMR spectra of 20% CSS shows the 80% cis content for the thiol-yne step-growth copolymer with 20% incorporation of CSS in CHCl3 with 1 mol% DBU. The ratio of methylene resonance n (from CSS) to methylene resonance h (from C10S) displays 20%: 80% that affords polymer with 20% incorporation of CSS (CDCl3, 500 MHz).

Figure S8. SEC chromatogram of 20% CSS of thiol-yne step-growth polymer with 20% incorporation of CSS; Mn = 32.6 kDa, Mw = 68.6 kDa, ÐM = 2.10 (SEC CHCl3, based on PS standards).

Figure S9. The 1H NMR spectra of 25% CSS shows the 80% cis content for the thiol-yne step-growth copolymer with 25% incorporation of CSS in CHCl3 with 1 mol% DBU. The ratio of methylene resonance n (from CSS) to methylene resonance h (from C10S) displays 25%: 75% that affords polymer with 25% incorporation of CSS (CDCl3, 500 MHz).

Figure S10. SEC chromatogram of 25% CSS of thiol-yne step-growth polymer; Mn = 34.0 kDa, Mw = 89.0 kDa, ÐM = 2.62. (SEC CHCl3, based on PS standards).

Figure S11. The 1H NMR spectra of 30% CSS shows the 80% cis content for the thiol-yne step-growth copolymer with 30% incorporation of CSS in CHCl3 with 1 mol% DBU. The ratio of methylene resonance n (from CSS) to methylene resonance h (from C10S) displays 30%: 70% that affords polymer with 30% incorporation of CSS (CDCl3, 500 MHz).

Figure S12. SEC chromatogram of 30% CSS of thiol-yne step-growth polymer with 30% incorporation of CSS; Mn = 29.1 kDa, Mw = 60.4 kDa, ÐM = 2.08 (SEC CHCl3, based on PS standards).

Figure S13. The 1H NMR spectra of 40% CSS shows the 80% cis content for the thiol-yne step-growth copolymer with 40% incorporation of CSS in CHCl3 with 1 mol% DBU. The ratio of methylene resonance n (from CSS) to methylene resonance h (from C10S) displays 40%: 60% that affords polymer with 40% incorporation of CSS (CDCl3, 500 MHz).

Figure S14. SEC chromatogram of 40% CSS of thiol-yne step-growth polymer with 40% incorporation of CSS; Mn = 26.7 kDa, Mw = 57.0 kDa, ÐM = 2.13 (SEC CHCl3, based on PS standards).

Figure S15. The 1H NMR spectra of 50% CSS shows the 80% cis content for the thiol-yne step-growth copolymer with 50% incorporation of CSS in CHCl3 with 1 mol% DBU. The ratio of methylene resonance n (from CSS) to methylene resonance h (from C10S) displays 49%: 51% that affords polymer with 49% incorporation of CSS (CDCl3, 500 MHz).

Figure S16. SEC chromatogram of 50% CSS of thiol-yne step-growth polymer with 50% incorporation of CSS; Mn = 45.4 kDa, Mw = 94.9 kDa, ÐM = 2.09 (SEC CHCl3, based on PS standards).

Figure S17. The 1H NMR spectra of 60% CSS shows the 80% cis content for the thiol-yne step-growth copolymer with 60% incorporation of CSS in CHCl3 with 1 mol% DBU. The ratio of methylene resonance n (from CSS) to methylene resonance h (from C10S) displays 60%: 40% that affords polymer with 60% incorporation of CSS (CDCl3, 500 MHz).

Figure S18. SEC chromatogram of 60% CSS of thiol-yne step-growth polymer with 60% incorporation of CSS; Mn = 29.0 kDa, Mw = 71.7 kDa, ÐM = 2.47 (SEC CHCl3, based on PS standards).

Figure S19. The 1H NMR spectra of 100% CSS shows the 80% cis content for the thiol-yne step-growth copolymer with 100% incorporation of CSS in CHCl3 with 1 mol% DBU.

Figure S20. SEC chromatogram of 100% CSS of thiol-yne step-growth polymer with 100% incorporation of CSS; Mn = 62.0 kDa, Mw = 86.8 kDa, ÐM = 1.4 (SEC CHCl3, based on PS standards).

Figure S21. Overlapped data of thermogravimetric analysis (TGA) of all synthesized polymers were performed to determine the degradation temperature and profile for each species.

Figure S22. Differential scanning calorimetry (DSC) thermograms of all synthesized polymers to determine glass transition, melting, and crystalline temperature for each species by 2 cycles of heating. Shown is the second heating cycle (A) and first cooling cycle (B).

Figure S23. Stress vs. strain curves for (co)polymers for all synthesized copolymers tested at 10 mm/min. Data for 3 samples are shown to illustrate the reproducibility.

Figure S24. Investigation into the effect of cooling rate on crystallization of 20% Css. A. Cooling DSC thermograms from the variable cooling rate DSC experiments outlined previously B. SEM image of DSC cooled 20% Css C. DSC thermogram of 20% Css cycled four times to confirm stability throughout cycling D. SEC chromatogram of uncycled and cycled 20% Css to confirm minimal molecular weight loss after cycling E. DSC thermogram to confirm the reproducibility of the Tc shift

Figure S25. In vitro degradation studies under accelerated (5M NaOH) and physiological conditions (PBS) for a subset of Css copolymers.

Figure S26. Variable cooling rate DSC experiment of 60% Css showing that a “melt”-like transition at the Tg dependent on cooling rate and could be attributed to molecular relaxation of the polymer from stresses/order introduced to it through slow cooling.4

Figure S27. VT-WAXS experiments of 60% Css showing changes in the short-range order as a result of heating

Figure S28. X-ray diffraction of 10-25% Css showing that 20% Css is the most crystalline copolymer.

Figure S29. Representative Hoffman-Weeks extrapolation for Tm° shown in Table 2

Figure S30. 2D SAXS (left) and WAXS (right) Scattering Patterns of 20% Css copolymer

Figure S31. Partial charge distribution for selected monomer sequences. Magnitudes of the partial charges are shown by color coding (from red to green).

Table S1. Overview of the equilibrium states of the copolymer melt system.

| x | y | Ntotal | L [σ] | Phase Structure (phase A) |
| --- | --- | --- | --- | --- |
| 6 | 6 | 153,600 | 56.2 | Lamella |
| 6 | 9 | 192,000 | 61.0 | Perforated Lamella |
| 6 | 12 | 230,400 | 65.0 | Gyroid |
| 6 | 18 | 307,200 | 71.7 | Thread/Cylinder |
| 6 | 36 | 268,800 | 68.8 | Spherical/Island |

Figure S32. Self-assembly in block copolymer systems: A. Scattering function S(q) for five self-assembled structures (lamellae, perforated lamellae, gyroid, cylinder, sphere). Inset shows the largest peak height of S(q). Largest peak height corresponds to the gyroid structure. B. Equilibrium structures of the block copolymers with different compositions.  (A and B microphases are shown separately for clarity). C. X-ray diffraction of 10 – 25% Css showing that the 20% Css copolymer exhibits the greatest amount of crystallinity.

Figure S33. Wide Angle X-Ray Scattering (WAXS) and Compiled Crystalline Properties of 15-25% Css Copolymers. A. WAXS of slow cooled 15-25% Css. B. WAXS of 20% Css self-nucleated by DSC, and melt-pressed with slow and fast cooling showing larger dimensional feature for both controlled cooling methods. C. VT-WAXS pattern of 20% Css showing crystal growth via stepped (slow) cooling where the temperatures indicate the temperature at which the scan was taken. D. VT-WAXS pattern of 20% Css showing crystal growth via fast cooling where the temperatures indicate the temperature at which the scan was taken. Greater crystallinity is observed in the slow cooled sample.

Figure S34. DSC Thermograms for the Slow-Cooled and Fast-Cooled Melt-Pressed 20% Css Copolymers The first-heating cycle was used to observe the thermal properties imparted from the melt-processing method used to prepare the tested films. The slow-cooled sample exhibits one polymorph as indicated by the single distribution observed as the Tm curve. The fast-cooled sample shows one dominant polymorph but two overall as demonstrated by the bimodal Tm distribution.

REFERENCES

1.	Worch, J. C.;  Stubbs, C. J.;  Price, M. J.; Dove, A. P., Click Nucleophilic Conjugate Additions to Activated Alkynes: Exploring Thiol-yne, Amino-yne, and Hydroxyl-yne Reactions from (Bio)Organic to Polymer Chemistry. Chem Rev 2021, 121 (12), 6744-6776.

2.	Daglar, O.;  Gunay, U. S.;  Hizal, G.;  Tunca, U.; Durmaz, H., Extremely Rapid Polythioether Synthesis in the Presence of TBD. Macromolecules 2019, 52 (9), 3558-3572.

3.	Truong, V. X.; Dove, A. P., Organocatalytic, regioselective nucleophilic "click" addition of thiols to propiolic acid esters for polymer-polymer coupling. Angew Chem Int Ed Engl 2013, 52 (15), 4132-6.

4.	C.Thomas, L., Interpreting Unexpected Events and Transitions in DSC Results. Instruments, T., Ed. Vol. TA039.