# Title

High-throughput deformation potential and electrical transport calculations

# Authors

Yeqing Jin1, Xiangdong Wang1,3, Mingjia Yao1, Di Qiu1,2, Jinyang Xi1,2, Lili Xi1,2*, Jiong Yang1,2*

# Affiliation

1. Materials Genome Institute, Shanghai University, Shanghai 200444, China

2. Zhejiang Laboratory, Hangzhou, Zhejiang 311100, China

3. School of Physics and Electronic Science, East China Normal University, Shanghai 200241, China

# Corresponding authors:

Lili Xi(lilyxi@t.shu.edu.cn)

Jiong Yang(jiongy@t.shu.edu.cn)

Figure S1 Comparison of deformation potentials with different methods

ref1[1]: They construct the supercell, then stretch and compress both ends of the supercell. They get the deformation potential in a lattice direction.

ref2[2][3]: They set the 1s energy level of an atom as a reference level.

ref3[4]: They stretch the structure slightly, and ignore the effect of the reference level.

ref4[5]: They use pressure as a variable.

- Wang, S. et al. Absolute volume deformation potentials of inorganic ABX3 halide perovskites: the chemical trends. Adv. Theory Simul. 4, 2100060 (2021).

- Li, X. et al. TransOpt. A code to solve electrical transport properties of semiconductors in constant electron-phonon coupling approximation. Comput. Mater. Sci. 186, 110074 (2021).

- Xi, L. et al. Discovery of high-performance thermoelectric chalcogenides through reliable high-throughput material screening. J. Am. Chem. Soc. 140, 10785-10793 (2018).

- Fan, T. & Oganov, A. AICON2: A program for calculating transport properties quickly and accurately. Comput. Phys. Commun. 266, 108027 (2021).

- Gueddim, A., Bouarissa, N. & Villesuzanne, A. Energy levels and deformation potentials for rocksalt MgO. Optik 124, 2670-2673 (2013).

Figure S2 The fitting of deformation potentials under different determination coefficients We show R2 at 1.0, 0.99, 0.97, 0.95, 0.94, 0.93. The fitting parameter we choose in this work is above 0.95.

Figure S3 Deformation potentials of magnetic materials at (a) VBM and (b) CBM.

Figure S4 Distribution of band gap deformation potentials for (a) all non-magnetic materials (b) half-Heusler.

Figure S5 Electrical transport properties at 700 K for MatHub3d-84609-TiCoSb. (a) and (d) present the p-type and n-type Seebeck coefficients, respectively. (b) and (e) present the electrical conductivities. (e) and (f) depict the corresponding power factors.

Figure S6 Distribution of PF under Seebeck 180 mV/K at 300K.

Figure S7 Relationship of PF and absolute value of deformation potential at 300K. (a) p-type (b) n-type

Figure S8 Normalized Eband numerical statistics. (a) VBM. (b) CBM. The red star indicates the Eband of KSbSn.

Table S1 Thermoelectric performance information for 156 materials

| ID-compound | Band gap (eV) | DP (eV) VBM | DP (eV) CBM | s (S/m) n-type | Seebeck(mV/K) n-type | PF (mWcm-1K-2) n-type | PF/ke (10-4K-1) n-type | s (S/m) p-type | Seebeck (mV/K) p-type | PF (mWcm-1K-2) p-type | PF/ke (10-4K-1) p-type |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| MatHub3d-7317-Bi5La1O9 | 1.62 | 2.683 | 2.565 | 527812.02 | -179.79 | 170.61 | 30.17 | 163351.38 | 179.63 | 52.71 | 105.66 |
| MatHub3d-11011-Cl2Rh2Te2 | 1.34 | -2.034 | -1.57 | 541180.35 | -179.84 | 175.04 | 33.08 | 190797.32 | 179.51 | 61.48 | 89.19 |
| MatHub3d-19407-Gd4O4Se4Ti1 | 0.82 | 2.259 | 2.582 | 487158.79 | -180.22 | 158.22 | 53.47 | 755983.13 | 179.83 | 244.48 | 70.96 |
| MatHub3d-7574-Br2Mo2Te8 | 0.88 | 1.561 | 0.936 | 1608658.00 | -180.17 | 522.18 | 89.08 | 159995.01 | 179.70 | 51.67 | 66.63 |
| MatHub3d-22759-K2O2Tl2 | 1.39 | 0.599 | 0.501 | 4969737.00 | -179.57 | 1602.52 | 33.27 | 1480429.0 | 180.10 | 480.17 | 57.73 |
| MatHub3d-13754-Cs4S4Te2 | 1.16 | 0.714 | -1.04 | 466422.63 | -180.25 | 151.53 | 32.87 | 295043.43 | 180.17 | 95.77 | 55.24 |
| MatHub3d-7747-Br6Cs2Pt1 | 1.39 | 1.064 | -0.572 | 1315284.00 | -179.59 | 424.21 | 33.37 | 160871.51 | 180.01 | 52.13 | 52.45 |
| MatHub3d-7318-Bi5O9Tb1 | 1.77 | -1.829 | -2.048 | 680816.58 | -179.87 | 220.27 | 36.05 | 307797.11 | 179.82 | 99.53 | 50.26 |
| MatHub3d-7356-Bi8I4Ru2 | 0.53 | -0.762 | -0.987 | 743528.62 | -179.74 | 240.21 | 28.08 | 2579217.0 | 179.75 | 833.33 | 48.95 |
| MatHub3d-6976-Bi2Cu2O2Se2 | 0.54 | -0.527 | -2.886 | 294359.85 | -179.70 | 95.06 | 24.67 | 6303171.0 | 180.26 | 2048.24 | 44.30 |
| MatHub3d-7259-Bi4La2O9 | 1.83 | 2.243 | 2.552 | 455029.32 | -179.68 | 146.90 | 32.28 | 256740.19 | 179.94 | 83.13 | 43.34 |
| MatHub3d-16082-Eu6P8 | 0.67 | 0.91 | 2.437 | 199357.83 | -180.37 | 64.86 | 30.28 | 748618.00 | 179.90 | 242.29 | 43.27 |
| MatHub3d-20889-Hf6N6O3 | 1.97 | 2.334 | 0.983 | 969892.79 | -180.24 | 315.10 | 31.29 | 332008.25 | 180.04 | 107.62 | 42.77 |
| MatHub3d-27596-O2Rb1Tl1 | 0.83 | 0.535 | -2.259 | 538786.41 | -180.31 | 175.17 | 22.75 | 3983448.0 | 179.72 | 1286.63 | 42.65 |
| MatHub3d-28557-P4Pb4Se12 | 1.75 | 0.878 | -0.565 | 5931906.00 | -180.47 | 1931.96 | 59.41 | 588735.37 | 179.55 | 189.79 | 42.23 |
| MatHub3d-28793-Pd1Rb2 | 0.63 | 0.862 | 0.502 | 1273940.00 | -180.27 | 413.99 | 27.12 | 665365.17 | 179.72 | 214.90 | 39.66 |
| MatHub3d-7703-Br4Nb1O1Tl1 | 1.44 | 1.551 | 2.443 | 247826.46 | -179.36 | 79.72 | 48.98 | 598729.74 | 180.28 | 194.59 | 39.64 |
| MatHub3d-7223-Bi4Br2O9Te2 | 0.91 | -0.958 | -2.189 | 301881.24 | -180.02 | 97.83 | 27.36 | 1561606.0 | 179.92 | 505.48 | 38.29 |
| MatHub3d-14824-Cu4Gd4Se8 | 1.04 | 1.96 | 1.798 | 298950.08 | -179.94 | 96.79 | 40.68 | 170219.44 | 180.34 | 55.36 | 38.12 |
| MatHub3d-13742-Cs4O2 | 0.54 | 0.577 | -0.915 | 326348.75 | -180.28 | 106.07 | 23.14 | 278365.01 | 179.78 | 89.97 | 38.11 |
| MatHub3d-14420-Cu2La2O2Te2 | 1.69 | 2.03 | 3.168 | 202597.88 | -180.48 | 65.99 | 32.33 | 384190.06 | 180.29 | 124.88 | 37.13 |
| MatHub3d-2810-As2Ba2Cd2F2 | 1.02 | 1.735 | 1.097 | 493330.75 | -180.21 | 160.21 | 26.79 | 595048.35 | 180.31 | 193.46 | 37.07 |
| MatHub3d-541-Ag2Ba2F2Te2 | 1.81 | 1.27 | -1.077 | 326091.57 | -180.27 | 105.97 | 31.19 | 636383.56 | 179.79 | 205.59 | 36.71 |
| MatHub3d-663-Ag2F2Sr2Te2 | 1.59 | 1.833 | -0.737 | 1266480.00 | -179.85 | 409.67 | 32.75 | 664266.13 | 179.54 | 214.13 | 36.54 |
| MatHub3d-22800-K2Pt1Se2 | 1.27 | 0.795 | -0.569 | 4641637.00 | -180.26 | 1508.19 | 33.63 | 736189.68 | 180.20 | 239.07 | 36.30 |
| MatHub3d-1912-Al2K2Te4 | 1.70 | 0.664 | -0.862 | 467784.78 | -180.31 | 152.09 | 23.42 | 1133093.0 | 179.76 | 366.15 | 36.21 |
| MatHub3d-21700-I6Pb5S2 | 1.87 | 0.796 | 0.785 | 642825.75 | -180.49 | 209.42 | 35.72 | 195754.22 | 180.46 | 63.75 | 36.09 |
| MatHub3d-888-Ag2Se4Y2 | 1.04 | 2.03 | 1.199 | 559911.64 | -180.18 | 181.77 | 22.58 | 363302.22 | 179.51 | 117.08 | 35.89 |
| MatHub3d-6753-Bi1I1Te1 | 1.32 | -0.742 | -1.051 | 290266.17 | -180.02 | 94.07 | 29.09 | 906896.59 | 180.19 | 294.45 | 35.84 |
| MatHub3d-14518-Cu2Nd2O2Te2 | 1.56 | 1.992 | 2.953 | 184723.02 | -180.44 | 60.14 | 33.68 | 541178.56 | 179.64 | 174.64 | 35.82 |
| MatHub3d-553-Ag2Bi2K4 | 0.61 | 1.509 | -1.019 | 165976.37 | -179.79 | 53.65 | 26.10 | 208034.21 | 179.80 | 67.25 | 35.81 |
| MatHub3d-29989-Sb2Sn1Te4 | 0.38 | -1.578 | -0.834 | 1931074.00 | -180.23 | 627.30 | 23.81 | 616544.97 | 179.71 | 199.13 | 35.71 |
| MatHub3d-19789-Ge2Se6Tl4 | 1.13 | -1.452 | -2.053 | 217336.41 | -180.48 | 70.79 | 42.26 | 236522.25 | 179.74 | 76.41 | 35.63 |
| MatHub3d-7193-Bi3Br1O4 | 0.98 | -0.791 | -1.082 | 4581467.00 | -179.85 | 1481.86 | 27.46 | 3085096.0 | 179.80 | 997.38 | 35.34 |
| MatHub3d-6942-Bi2Cl1Ho1O4 | 1.44 | 1.763 | -2.003 | 1954179.00 | -180.12 | 633.98 | 28.43 | 377189.68 | 180.08 | 122.32 | 35.02 |
| MatHub3d-877-Ag2S4Tm2 | 1.48 | 1.674 | 0.732 | 775506.48 | -180.00 | 251.27 | 26.64 | 566669.27 | 180.01 | 183.62 | 34.96 |
| MatHub3d-648-Ag2Er2S4 | 1.47 | 1.591 | 0.708 | 828293.29 | -180.05 | 268.51 | 26.01 | 621666.46 | 179.54 | 200.40 | 34.90 |
| MatHub3d-649-Ag2Er2S4 | 1.36 | 1.421 | 0.633 | 988658.56 | -180.39 | 321.70 | 27.32 | 900506.66 | 180.51 | 293.42 | 34.77 |
| MatHub3d-3925-Au2K2Se2 | 1.89 | 0.668 | -1.399 | 366328.58 | -180.18 | 118.92 | 33.90 | 583593.41 | 180.21 | 189.53 | 34.76 |
| MatHub3d-6938-Bi2Cl1Dy1O4 | 1.43 | 2.088 | -1.705 | 2666445.00 | -180.32 | 867.00 | 28.45 | 258584.52 | 180.24 | 84.01 | 34.72 |
| MatHub3d-30130-Se2Sn1 | 0.80 | -1.12 | -2.613 | 354209.55 | -179.92 | 114.67 | 29.06 | 1221872.0 | 180.29 | 397.18 | 34.71 |
| MatHub3d-23146-La2O2Te1 | 1.90 | 2.9 | 2.382 | 394604.7 | -180.08 | 127.96 | 35.16 | 517141.11 | 179.63 | 166.87 | 34.42 |
| MatHub3d-19778-Ge2S6Tl4 | 1.77 | -1.248 | -1.919 | 237083.93 | -179.72 | 76.58 | 40.31 | 284442.11 | 179.79 | 91.95 | 34.39 |
| MatHub3d-7048-Bi2In2S6 | 1.36 | -1.061 | -1.358 | 413987.11 | -179.72 | 133.72 | 27.26 | 935488.17 | 179.97 | 302.99 | 34.33 |
| MatHub3d-16028-Eu4Ge2Se8 | 1.19 | -0.914 | -3.68 | 186465.78 | -180.18 | 60.54 | 37.63 | 494030.89 | 180.27 | 160.54 | 34.11 |
| MatHub3d-796-Ag2Lu2S4 | 1.41 | 1.604 | 0.624 | 1006948.00 | -180.21 | 327.02 | 27.39 | 773563.86 | 179.52 | 249.29 | 34.07 |
| MatHub3d-16029-Eu4Ge2Se8 | 1.20 | -0.892 | -3.676 | 173825.42 | -179.81 | 56.20 | 36.65 | 513886.03 | 179.65 | 165.86 | 33.99 |
| MatHub3d-3458-As8Eu6 | 0.45 | 1.387 | 1.808 | 272290.11 | -179.92 | 88.15 | 26.06 | 235705.12 | 180.26 | 76.59 | 33.92 |
| MatHub3d-21172-Hg4Mo2O8 | 1.87 | 0.848 | -1.742 | 1460000 | -180 | 473 | 58.17 | 1150000 | 180 | 372 | 33.80 |
| MatHub3d-6899-Bi2Br1Nd1O4 | 1.27 | 2.058 | 1.836 | 2110418.00 | -179.84 | 682.53 | 28.22 | 223635.74 | 179.96 | 72.43 | 33.62 |
| MatHub3d-5643-Ba2Cd2F2Sb2 | 0.36 | 1.556 | 1.0 | 687755.62 | -180.07 | 223.01 | 29.19 | 832078.66 | 180.15 | 270.03 | 33.61 |
| MatHub3d-6949-Bi2Cl1O4Tb1 | 1.39 | 2.222 | -1.538 | 3274086.00 | -179.83 | 1058.86 | 28.21 | 219912.52 | 180.07 | 71.30 | 33.50 |
| MatHub3d-6901-Bi2Br1O4Sm1 | 1.31 | 2.215 | 1.922 | 1958495.00 | -180.38 | 637.23 | 28.57 | 210759.27 | 180.37 | 68.57 | 33.46 |
| MatHub3d-15517-Er1K1Te2 | 1.37 | 0.549 | 2.517 | 155640.20 | -179.79 | 50.31 | 28.24 | 1430784.0 | 180.43 | 465.80 | 33.42 |
| MatHub3d-6941-Bi2Cl1Gd1O4 | 1.36 | 2.311 | -1.424 | 3774346.00 | -180.34 | 1227.46 | 28.28 | 196947.42 | 179.87 | 63.72 | 32.88 |
| MatHub3d-6994-Bi2Eu4O1 | 0.39 | -1.046 | 1.005 | 290156.15 | -179.89 | 93.89 | 28.90 | 567962.34 | 180.29 | 184.62 | 32.86 |
| MatHub3d-27622-O2Se1Tm2 | 1.94 | 0.5 | -1.808 | 1450000 | -180 | 469 | 30.94 | 2.24E+07 | 180 | 7300 | 32.79 |
| MatHub3d-6658-Bi1Br1Te1 | 1.33 | -0.555 | -0.718 | 877920.58 | -179.86 | 284.02 | 30.46 | 1534787.0 | 179.78 | 496.05 | 32.48 |
| MatHub3d-27369-O1Sb2Yb4 | 0.62 | -0.763 | 1.616 | 247480.73 | -180.08 | 80.26 | 29.91 | 1203180.0 | 179.57 | 387.96 | 32.43 |
| MatHub3d-6896-Bi2Br1Gd1O4 | 1.34 | -1.014 | -1.379 | 3909173.00 | -180.24 | 1269.93 | 28.62 | 1057775.0 | 180.19 | 343.46 | 32.41 |
| MatHub3d-6902-Bi2Br1O4Tb1 | 1.36 | -1.096 | -1.492 | 3353023.00 | -180.14 | 1088.10 | 28.69 | 930295.20 | 180.43 | 302.85 | 32.35 |
| MatHub3d-6893-Bi2Br1Dy1O4 | 1.37 | -1.248 | -1.67 | 2709583.00 | -179.89 | 876.79 | 28.66 | 745814.61 | 180.36 | 242.61 | 32.14 |
| MatHub3d-14280-Cu2Gd4Rb2Se8 | 1.07 | 0.611 | 1.885 | 293088.51 | -180.30 | 95.28 | 31.29 | 905932.25 | 180.38 | 294.78 | 32.13 |
| MatHub3d-5892-Ba2Hf2N4 | 1.27 | 2.653 | 3.31 | 409412.53 | -180.23 | 132.99 | 27.46 | 334037.58 | 180.12 | 108.37 | 32.03 |
| MatHub3d-27586-O2Pr2Te1 | 1.66 | 2.849 | 2.514 | 443231.69 | -180.41 | 144.27 | 38.87 | 619852.45 | 180.04 | 200.91 | 31.96 |
| MatHub3d-6897-Bi2Br1Ho1O4 | 1.39 | -1.454 | -1.939 | 2017590.00 | -180.03 | 653.93 | 28.79 | 567722.69 | 180.26 | 184.47 | 31.92 |
| MatHub3d-19258-Gd1S2Tl1 | 1.66 | 0.607 | 2.02 | 332075.19 | -179.81 | 107.37 | 28.20 | 2197220.0 | 180.03 | 712.15 | 31.74 |
| MatHub3d-15256-Dy1S2Tl1 | 1.54 | 0.862 | 2.36 | 166666.92 | -180.09 | 54.05 | 25.35 | 1205382.0 | 179.78 | 389.58 | 31.73 |
| MatHub3d-21539-I10In2Pb4 | 1.85 | 0.51 | 1.523 | 254746.19 | -179.72 | 82.28 | 26.36 | 830075.72 | 179.99 | 268.92 | 31.44 |
| MatHub3d-28688-Pb1Sb2Te4 | 0.61 | -0.803 | -0.757 | 2772524.00 | -179.89 | 897.24 | 31.32 | 1621365.0 | 180.41 | 527.71 | 31.31 |
| MatHub3d-3118-As2O1Yb4 | 0.94 | -1.465 | 0.595 | 2254604.00 | -179.56 | 726.96 | 32.20 | 341341.48 | 180.02 | 110.62 | 31.24 |
| MatHub3d-20735-Hf1Se2 | 0.56 | 1.89 | 3.738 | 194325.68 | -179.94 | 62.92 | 30.56 | 904097.39 | 179.95 | 292.76 | 31.22 |
| MatHub3d-13975-Cu1Lu1Se2 | 1.48 | 2.03 | 3.885 | 239376.47 | -179.75 | 77.34 | 32.02 | 243685.07 | 180.29 | 79.21 | 31.17 |
| MatHub3d-6904-Bi2Br1O4Y1 | 1.38 | 2.282 | 1.857 | 2157098.00 | -180.11 | 699.75 | 28.76 | 219743.44 | 179.82 | 71.06 | 31.11 |
| MatHub3d-26751-Nd2O2Te1 | 1.58 | 2.858 | 2.543 | 497089.60 | -180.21 | 161.43 | 39.05 | 654514.78 | 179.58 | 211.08 | 31.06 |
| MatHub3d-175-Ag1Bi1S2 | 0.80 | -1.583 | -1.639 | 458673.78 | -180.06 | 148.70 | 22.91 | 1460042.0 | 179.79 | 471.93 | 30.94 |
| MatHub3d-20838-Hf3N4 | 1.07 | 2.824 | 1.729 | 1415766.00 | -180.26 | 460.02 | 27.59 | 279537.22 | 179.66 | 90.23 | 30.90 |
| MatHub3d-7629-Br3Cs1Ge1 | 0.77 | -1.649 | -2.9 | 170420.97 | -180.04 | 55.24 | 25.75 | 206979.77 | 180.40 | 67.36 | 30.88 |
| MatHub3d-7037-Bi2I1O4Tm1 | 1.39 | 1.073 | -0.632 | 11863240.00 | -180.10 | 3847.84 | 31.82 | 2286266.0 | 179.91 | 739.99 | 30.82 |
| MatHub3d-14124-Cu1Se2Tm1 | 1.43 | 1.987 | 3.754 | 194069.05 | -180.26 | 63.06 | 32.46 | 243232.40 | 180.08 | 78.87 | 30.77 |
| MatHub3d-6985-Bi2Er1I1O4 | 1.36 | 0.553 | -1.081 | 4121748.00 | -180.40 | 1341.43 | 31.72 | 8304970.0 | 179.59 | 2678.60 | 30.72 |
| MatHub3d-7038-Bi2I1O4Y1 | 1.35 | 3.242 | 1.529 | 2067413.00 | -179.53 | 666.35 | 31.19 | 226919.57 | 179.59 | 73.19 | 30.68 |
| MatHub3d-21388-Ho2O2Te1 | 0.58 | -1.073 | -0.502 | 5814382.00 | -179.67 | 1876.95 | 23.69 | 3149817.0 | 179.86 | 1018.95 | 30.67 |
| MatHub3d-84433-Co1Nb1Sn1 | 0.91 | 2.389 | 1.722 | 276770.04 | -180.19 | 89.86 | 27.32 | 185207.14 | 180.26 | 60.18 | 30.62 |
| MatHub3d-174-Ag1Bi1S2 | 0.78 | -1.536 | -1.614 | 479531.73 | -180.34 | 155.96 | 23.57 | 1520480.0 | 179.61 | 490.49 | 30.60 |
| MatHub3d-13796-Cu1Er1Se2 | 1.40 | 1.884 | 3.65 | 170898.05 | -180.29 | 55.55 | 32.31 | 265105.37 | 179.93 | 85.83 | 30.59 |
| MatHub3d-27635-O2Sm2Te1 | 1.42 | 3.01 | 2.797 | 452024.19 | -179.55 | 145.72 | 37.45 | 639904.31 | 179.90 | 207.09 | 30.56 |
| MatHub3d-7035-Bi2I1O4Sm1 | 1.29 | 3.211 | 1.588 | 1970820.00 | -180.30 | 640.68 | 30.87 | 192609.88 | 179.65 | 62.16 | 30.49 |
| MatHub3d-30022-Sb4Te8Yb2 | 0.56 | 1.331 | 1.608 | 400046.99 | -180.22 | 129.93 | 33.89 | 473973.16 | 180.20 | 153.91 | 30.44 |
| MatHub3d-20736-Hf1Se4Te1 | 0.99 | 1.649 | 2.143 | 339537.25 | -179.83 | 109.80 | 25.80 | 505907.98 | 179.78 | 163.51 | 30.42 |
| MatHub3d-19096-Ga4Te4 | 0.36 | -2.505 | -2.407 | 173630.54 | -179.81 | 56.13 | 28.01 | 196372.95 | 180.07 | 63.68 | 30.35 |
| MatHub3d-15338-Dy2O2Te1 | 1.09 | -0.968 | -0.776 | 6572370.00 | -180.26 | 2135.59 | 33.32 | 6910324.0 | 179.65 | 2230.19 | 30.23 |
| MatHub3d-7033-Bi2I1Nd1O4 | 1.25 | 3.076 | 1.493 | 2194493.00 | -179.88 | 710.11 | 30.54 | 189650.55 | 180.06 | 61.48 | 30.21 |
| MatHub3d-15580-Er1Rb1Se2 | 1.99 | 0.798 | 2.329 | 214962.5 | -180.24 | 69.84 | 28.22 | 853879.62 | 180.24 | 277.40 | 30.18 |
| MatHub3d-20778-Hf2N2S1 | 0.88 | 2.039 | 2.745 | 556748.18 | -180.04 | 180.47 | 29.86 | 424838.96 | 180.04 | 137.71 | 30.16 |
| MatHub3d-21999-In2Na2Te4 | 0.65 | 0.563 | -0.739 | 550167.74 | -179.90 | 178.05 | 21.71 | 1848597.0 | 179.59 | 596.20 | 30.15 |
| MatHub3d-14277-Cu2Gd4K2Se8 | 1.05 | 0.778 | 2.114 | 263175.94 | -179.89 | 85.16 | 31.83 | 611271.85 | 179.89 | 197.82 | 30.15 |
| MatHub3d-19325-Gd2O2Te1 | 1.25 | -1.98 | -1.998 | 794897.90 | -180.49 | 258.96 | 34.53 | 1553153.0 | 179.74 | 501.79 | 30.13 |
| MatHub3d-27645-O2Tb2Te1 | 1.17 | -1.463 | -1.392 | 1838891.00 | -180.13 | 596.66 | 33.79 | 2940010.0 | 179.56 | 947.87 | 30.04 |
| MatHub3d-14278-Cu2Gd4K2Se8 | 1.05 | 0.765 | 2.12 | 263847.68 | -179.60 | 85.10 | 31.72 | 632770.90 | 179.88 | 204.73 | 30.04 |
| MatHub3d-20753-Hf2I2N2 | 1.02 | 0.745 | 2.573 | 374492.11 | -180.48 | 121.98 | 33.99 | 3529170.0 | 180.24 | 1146.48 | 30.04 |
| MatHub3d-14782-Cu3Te4V1 | 0.72 | 1.557 | 1.618 | 163119.98 | -179.63 | 52.63 | 30.92 | 253303.66 | 179.83 | 81.92 | 30.04 |
| MatHub3d-13787-Cu1Dy1Se2 | 1.37 | 1.76 | 3.447 | 175945.25 | -180.44 | 57.29 | 32.28 | 294023.02 | 179.57 | 94.81 | 29.98 |
| MatHub3d-25548-Mo1Se2 | 1.34 | 1.505 | 0.955 | 1487537.00 | -179.58 | 479.74 | 33.01 | 727327.65 | 180.03 | 235.74 | 29.95 |
| MatHub3d-7034-Bi2I1O4Pr1 | 1.23 | 3.052 | 1.495 | 2172076.00 | -180.05 | 704.17 | 30.47 | 178948.44 | 179.68 | 57.78 | 29.91 |
| MatHub3d-3189-As2Yb1Zn2 | 0.68 | 1.373 | 2.474 | 520041.49 | -180.27 | 169.00 | 28.99 | 773048.88 | 179.82 | 249.97 | 29.83 |
| MatHub3d-21311-Ho1Rb1Se2 | 1.97 | 0.84 | 2.305 | 215736.44 | -180.0 | 69.90 | 28.16 | 765461.59 | 179.88 | 247.67 | 29.75 |
| MatHub3d-7726-Br4Sn2 | 1.66 | -1.613 | 0.584 | 4988732.00 | -179.60 | 1609.22 | 29.62 | 235621.64 | 180.16 | 76.48 | 29.50 |
| MatHub3d-25627-Mo2Se4 | 1.35 | 1.568 | 0.994 | 1347177.00 | -180.03 | 436.65 | 33.17 | 660539.63 | 179.64 | 213.15 | 29.44 |
| MatHub3d-7986-C1Hf1 | 0.29 | 2.303 | 3.707 | 436299.77 | -179.76 | 140.98 | 23.82 | 578131.34 | 180.18 | 187.70 | 29.39 |
| MatHub3d-19430-Gd6O6Sb2 | 0.46 | -2.829 | -2.066 | 268003.51 | -180.43 | 87.24 | 54.67 | 596284.22 | 179.96 | 193.11 | 29.14 |
| MatHub3d-29370-Rb1Se2Tb1 | 1.94 | 0.93 | 2.269 | 214701.99 | -179.71 | 69.34 | 28.08 | 610769.49 | 179.87 | 197.60 | 29.02 |
| MatHub3d-7117-Bi2O3 | 1.14 | -1.859 | -2.396 | 978827.75 | -180.14 | 317.62 | 29.03 | 747264.73 | 180.07 | 242.30 | 28.84 |
| MatHub3d-19248-Gd1Rb1Se2 | 1.93 | 0.984 | 2.266 | 208814.73 | -180.41 | 67.96 | 28.32 | 540272.94 | 180.07 | 175.18 | 28.56 |
| MatHub3d-84411-Hf1Rh1Sb1 | 0.97 | -1.55 | -2.885 | 198827.46 | -180.41 | 64.71 | 30.03 | 356168.88 | 179.64 | 114.93 | 28.46 |
| MatHub3d-7319-Bi6Br2Se8 | 1.02 | -0.554 | -0.773 | 1782150.00 | -180.02 | 577.56 | 44.56 | 1199656.0 | 179.67 | 387.28 | 28.46 |
| MatHub3d-25629-Mo2Te4 | 0.90 | 2.154 | 1.461 | 484941.70 | -179.58 | 156.38 | 30.60 | 249835.68 | 179.85 | 80.81 | 28.30 |
| MatHub3d-14352-Cu2Ho4K2Se8 | 1.10 | 0.666 | 2.016 | 307250.05 | -180.38 | 99.97 | 32.32 | 866246.76 | 180.34 | 281.72 | 28.30 |
| MatHub3d-5245-Ba1Cd2P2 | 0.74 | 1.945 | -1.335 | 613025.51 | -180.06 | 198.76 | 27.37 | 235641.27 | 179.70 | 76.10 | 27.89 |
| MatHub3d-14174-Cu2Er4K2Se8 | 1.12 | 0.592 | 2.028 | 312621.31 | -179.84 | 101.11 | 32.19 | 1127740.0 | 179.62 | 363.83 | 27.77 |
| MatHub3d-7260-Bi4Li4Sr4 | 0.57 | 0.904 | 1.222 | 308226.37 | -179.85 | 99.70 | 27.09 | 377614.34 | 179.78 | 122.05 | 27.72 |
| MatHub3d-29166-Pt1Si1Ti1 | 1.05 | 3.324 | 1.593 | 328174.92 | -179.64 | 105.90 | 27.87 | 202592.70 | 179.77 | 65.47 | 27.56 |
| MatHub3d-7351-Bi8Br4Ru2 | 0.65 | -0.75 | -1.07 | 599347.84 | -179.85 | 193.86 | 29.87 | 4199301.0 | 180.29 | 1365.00 | 27.52 |
| MatHub3d-15458-Dy6O6Sb2 | 0.41 | -1.757 | -1.086 | 1067119.00 | -180.66 | 348.29 | 54.48 | 1597962.0 | 180.03 | 517.94 | 27.44 |
| MatHub3d-21494-Ho6O6Sb2 | 0.38 | -1.234 | -0.94 | 1582490.00 | -180.85 | 517.56 | 45.32 | 3490121.0 | 179.75 | 1127.70 | 27.06 |
| MatHub3d-19526-Ge1Pt1Ti1 | 0.92 | 3.169 | 1.723 | 217528.21 | -180.25 | 70.67 | 29.54 | 183152.74 | 180.00 | 59.34 | 26.75 |
| MatHub3d-29171-Pt1Sn1Ti1 | 0.73 | 2.936 | 1.819 | 156896.31 | -179.95 | 50.81 | 28.29 | 204505.19 | 179.57 | 65.94 | 26.64 |
| MatHub3d-24415-Lu1O2Tl1 | 1.22 | 2.023 | 1.592 | 1497302.00 | -179.68 | 483.38 | 26.63 | 444821.37 | 180.16 | 144.38 | 26.60 |
| MatHub3d-27660-O2Tl1Tm1 | 1.33 | 1.593 | 1.064 | 3375443.00 | -179.99 | 1093.53 | 27.91 | 671684.21 | 179.80 | 217.14 | 26.57 |
| MatHub3d-15551-Er1O2Tl1 | 1.40 | 1.302 | 0.74 | 7042430.00 | -180.33 | 2290.07 | 28.85 | 983342.95 | 179.76 | 317.76 | 26.56 |
| MatHub3d-30159-Se4Sn4 | 0.58 | -1.213 | -0.695 | 3704033.00 | -180.02 | 1200.39 | 21.18 | 488296.17 | 180.08 | 158.36 | 26.52 |
| MatHub3d-7307-Bi4Se8 | 0.71 | -0.521 | -2.031 | 561160.18 | -179.86 | 181.52 | 33.33 | 5747442.0 | 180.02 | 1862.56 | 26.30 |
| MatHub3d-15847-Eu1Mg2Sb2 | 0.75 | 1.843 | 3.006 | 175857.62 | -179.89 | 56.91 | 28.99 | 190009.32 | 179.71 | 61.36 | 26.15 |
| MatHub3d-28725-Pb2S2 | 1.67 | -1.144 | -0.586 | 8201157.00 | -180.16 | 2661.83 | 26.09 | 552312.73 | 180.36 | 179.66 | 25.68 |
| MatHub3d-84450-Ru1Sb1Ta1 | 0.66 | -1.525 | -0.91 | 825791.06 | -179.75 | 266.82 | 29.00 | 379497.93 | 180.14 | 123.15 | 25.63 |
| MatHub3d-24858-Mg2Sb2Yb1 | 0.70 | 1.954 | 2.91 | 166222.60 | -179.99 | 53.85 | 28.59 | 155965.24 | 180.29 | 50.70 | 25.03 |
| MatHub3d-84449-Pt1Sn1Ti1 | 0.79 | 2.669 | 1.687 | 157899.52 | -180.15 | 51.24 | 24.44 | 156957.93 | 179.95 | 50.83 | 24.94 |
| MatHub3d-29177-Pt1Ta1Tl1 | 0.76 | 2.354 | 1.824 | 187873.44 | -179.82 | 60.75 | 28.79 | 203000.81 | 180.02 | 65.78 | 24.91 |
| MatHub3d-84560-Pt1Ta1Tl1 | 0.98 | 2.15 | 1.454 | 246235.44 | -179.76 | 79.57 | 26.14 | 235614.27 | 179.92 | 76.27 | 24.71 |
| MatHub3d-20854-Hf4N4O2 | 1.40 | 1.222 | 2.272 | 1172412.00 | -180.43 | 381.70 | 31.95 | 2500038.0 | 180.18 | 811.60 | 24.51 |
| MatHub3d-84503-Pb1Pt1Ti1 | 0.55 | 2.265 | 1.245 | 286708.30 | -179.94 | 92.83 | 30.34 | 178302.96 | 179.73 | 57.60 | 24.35 |
| MatHub3d-19557-Ge1Te1 | 0.39 | -1.573 | 1.836 | 2173091.00 | -180.15 | 705.24 | 21.82 | 2262677.0 | 180.30 | 735.54 | 23.97 |
| MatHub3d-19539-Ge1Ru2Ti1 | 0.50 | 1.634 | 1.12 | 695152.12 | -179.85 | 224.85 | 23.96 | 247687.96 | 179.69 | 79.98 | 23.96 |
| MatHub3d-19559-Ge1Te1 | 0.39 | -1.557 | 1.84 | 2154073.00 | -179.74 | 695.87 | 21.60 | 2312520.0 | 180.13 | 750.35 | 23.84 |
| MatHub3d-22811-K2Sb2Sn2 | 0.28 | 0.55 | -0.509 | 3670430.00 | -179.92 | 1188.11 | 25.29 | 1420729.0 | 180.17 | 461.19 | 23.63 |
| MatHub3d-29645-Ru1Sb1Ta1 | 0.88 | -1.182 | -0.754 | 862913.34 | -180.20 | 280.21 | 28.29 | 651672.16 | 179.89 | 210.88 | 23.29 |
| MatHub3d-84485-Bi1Rh1Ti1 | 0.74 | 2.324 | 1.496 | 194773.88 | -180.19 | 63.24 | 23.95 | 164870.54 | 179.75 | 53.27 | 23.21 |
| MatHub3d-7091-Bi2Na2Se4 | 0.67 | -1.516 | -0.547 | 19378100.00 | -179.71 | 6258.28 | 33.76 | 344191.11 | 180.14 | 111.69 | 23.21 |
| MatHub3d-3254-As4Cd2Eu4 | 0.75 | 1.212 | -0.755 | 777181.13 | -179.94 | 251.63 | 26.71 | 213271.84 | 180.00 | 69.10 | 23.00 |
| MatHub3d-7118-Bi2O3 | 1.77 | -1.271 | -1.237 | 1627907.00 | -179.96 | 527.20 | 28.14 | 783998.63 | 179.98 | 253.96 | 22.64 |
| MatHub3d-19556-Ge1Te1 | 0.72 | -1.296 | 0.72 | 6168315.00 | -179.87 | 1995.61 | 22.11 | 1837063.0 | 179.89 | 594.50 | 22.31 |
| MatHub3d-7154-Bi2Pb1Te4 | 0.60 | -0.962 | -0.742 | 1470538.00 | -179.65 | 474.62 | 23.56 | 999552.75 | 180.13 | 324.32 | 21.81 |
| MatHub3d-29426-Rb4Sn2Te10 | 0.72 | 0.791 | -1.148 | 897574.39 | -180.08 | 291.07 | 27.54 | 891374.49 | 179.90 | 288.49 | 21.75 |
| MatHub3d-28726-Pb2S2 | 1.67 | -1.168 | -0.573 | 4658124.00 | -179.66 | 1503.49 | 25.72 | 1263615.0 | 179.69 | 408.00 | 21.12 |
| MatHub3d-28724-Pb2S2 | 1.66 | -1.193 | -0.605 | 7504205.00 | -179.62 | 2421.24 | 26.19 | 2273154.0 | 179.79 | 734.80 | 21.05 |
| MatHub3d-7185-Bi2Te3 | 0.43 | -1.179 | -1.068 | 473988.43 | -180.03 | 153.62 | 27.22 | 622731.80 | 179.82 | 201.36 | 20.20 |