Methods

Test of line heating rate/DSC

The thermal properties of CaC2O4·H2O were investigated by differential scanning calorimeter (DSC3+, 1780, METTLER TOLEDO, Switzerland) and all samples were placed in an Al (40 µL) crucible and capped. The sample mass was 6-8 mg, the line heating rate was 5, 10 and 15 K·min-1, respectively. The temperature range was 30-300°C. The high purity Ar gas with a flow rate of 50 mL·min-1 and 20 mL·min-1 was employed as the purging gas and protective gas, respectively.

The isothermal TGA experiments

The thermal properties of CaC2O4·H2O were investigated by thermogravimetry-differential scanning calorimeter (TGA/DSC, METTLER TOLEDO, Switzerland) and all samples were placed in an Al2O3 (70 µL) crucible and capped. The sample mass was 6-8 mg. The heating rate was 10 K·min-1 and the temperature was up to and kept at 150, 180, 210 and 240°C for 3h, respectively. The high purity Ar gas with a flow rate of 50 mL·min-1 and 20 mL·min-1 was employed as the purging gas and protective gas, respectively.

The isothermal DSC experiments

The thermal properties of CaC2O4·H2O were investigated by thermogravimetry-differential scanning calorimeter (TGA-DSC, STA449C, NETZSCH, Germany) and all samples were placed in an Al2O3 (85 µL) crucible and capped. The sample mass was 6-7 mg. The heating rate was 10 K·min-1 and the temperature was up to and kept at 120 and 140°C for 360 min, respectively. The high purity Ar gas with a flow rate of 50 mL·min-1 was employed as the purging gas and protective gas, respectively.

The specific heat capacity of CaC2O4∙H2O

The specific heat capacity of CaC2O4∙H2O was investigated by differential scanning calorimeter (DSC3+, 1780, METTLER TOLEDO, Switzerland). The sample of 11.02 mg was placed in an Al (40 µL) crucible and capped. The sample was first stored at 20 °C for 10 min, then heated up to 260 °C with a heating rate of 10 K·min-1 and finally kept at 260 °C for 10 min. The high purity Ar gas with a flow rate of 50 mL·min-1 and 20 mL·min-1 was employed as the purging gas and protective gas, respectively. Two blank experiments, Sapphire experiment (22.5 mg), and sample testing were performed using the same crucible.

Calculation:

Q=nC∆T=nT1T2fTdT

Q=nC∆T=nT1T20.0009T+0.5322dT=128*(0.00045T2+0.5322T)|T1T2=128*0.00045*1252-252+0.5322*125-25=7676.16

Q=nC∆T=nT1T20.0009T+0.5322dT=128*(0.00045T2+0.5322T)|T1T2=128*0.00045*1252-252+0.5322*125-25=7676.16