Supporting Information

Interfacial self-healing polymer electrolytes for ultralong-life solid-state lithium-sulfur batteries

Fei Pei, Lin Wu, Yi Zhang, Yaqi Liao, Qi Kang, Yan Han, Huangwei Zhang, Yue Shen, Henghui Xu, Zhen Li* & Yunhui Huang*

State Key Laboratory of Materials Processing and Die & Mould Technology

School of Materials Science and Engineering

Huazhong University of Science and Technology

Wuhan 430074, China

*Corresponding authors

E-mail: li_zhen@hust.edu.cn; huangyh@hust.edu.cn

Methods

Materials. All reagents were commercially available and used as supplied without further purification. Dimethylacetamide (DMAc), dichloromethane, PEO, polytetrahydrofuran (PTMG, 2000 g mol-1), hexamethylene diisocyanate (HDI) and 2-Hydroxyethyl disulfide (BHDS) and dibutyltin dilaurate (DBTDL) catalyst were purchased from Alfa Aesar. Lithium bis(fluorosulfonyl)imide (LiFSI) were purchased from Aldrich.

Material Characterization

The SEM analyze was carried out on FEI Nova NanoSEM450 microscope operated at 10 kV. FTIR spectra were measured using a Nicolet iS50 FT/IR Spectrometer (Thermo Fisher) with a diamond attenuated total reﬂectance attachment. Mechanical testing was carried out on an Instron 5565 testing stain using a strain rate of 5 cm min-1. Powder X-ray diffraction (PXRD) analysis was characterized by X-ray powder diffraction (XRD, Cu Ka radiation, Rigaku Ultima IV) with a scanning rate of 2o min-1. XPS tests were performed on ThermoFisher Thermo Scientific KAlpha+. 1H NMR spectra was recorded on a Bruker 500 NMR MHz spectrometer at room temperature. Gel permeation chromatography (GPC) was carried out in DMF on two PolyPore columns (Agilent) connected in series with a DAWN multiangle laser light scattering (MALLS) detector.

Electrochemical Characterizations

The ionic conductivities of the solid composite electrolytes at different temperatures were measured by sandwiching the SPEs between two steel sheets in CR2032 cells and the frequency range was 0.1-106 Hz. The ionic conductivity σ was calculated by the equation σ = L/(RS), where R was the total resistance of solid electrolyte, L was the sample thickness, and S was the area of solid electrolyte. The Li+ transference number (tLi+) was obtained using a symmetric Li||Li cell by a chronoamperometry test with a DC voltage amplitude of 50 mV. The EIS tests were taken before and after DC polarization. The tLi+ can be calculated according to tLi+ = Is(ΔV−R0I0)/[I0(ΔV−RsIs)], where I0 and Is are the initial and steady-state DC current, respectively; R0 and Rs are the initial and steady-state interfacial resistances, respectively. The electrochemical stability of the SPEs are evaluated a scan rate of 10 mV s-1 from 0 to 6 V at room temperature.

DFT calculation

Density Functional Theory (DFT) calculations were carried out to better understand the electrolyte. This simulation calculation was carried out on Material studio software. All computations of electrolytes were calculated by using the DMol3 module. The exchange correlation functional was treated by the generalized-gradient-approximation (GGA) with the Perdew-Burke-Ernzerhof (PBE) functional1. For the geometry optimization, convergence energy was set to 1.0 × 10-5 Ha for energy, 0.001 Ha/Å for force, and 0.005 Å for displacement.

The binding energy (Eb) was computed in the following equation2:

ΔEb = Etotal - ELi+ - EPolymer

where ΔEb is the binding energy between the Li+ ion and polymer. Etotal is the DFT total energy of the corresponding system with adsorbed Li+. ELi+ and Es represent the Gibbs energies of a Li+ ion and the corresponding polymer substrates, respectively.

Supplementary Fig. 1 Digital photographs of the PTMG-HDI-BHDS films in various states.

Supplementary Fig. 2 Top-view SEM images of PEO, PTMG-HDI and PTMG-HDI-BHDS films.

Supplementary Fig. 3 Photographs of the stress-strain measurement of PEO film.

Supplementary Fig. 4 Photographs of before and after rhodamine B was added in the colorless PTMG-HDI-BHDS gel solution.

Supplementary Fig. 5 Optical microscopy images of the scratch on the PTMG-HDI-BHDS film before and after healing for 15 min at 30 oC.

Supplementary Fig. 6 FTIR spectra of PTMG-HDI and PTMG-HDI-BHDS films.

Supplementary Fig. 7 1H NMR spectrum of the synthesized PTMG-HDI in CDCl3 (500 MHz).

Supplementary Fig. 8 1H NMR spectrum of the HDI in CDCl3 (500 MHz).

Supplementary Fig. 9 N 1s XPS spectrum of PTMG-HDI-BHDS film.

Supplementary Fig. 10 ElS measurements of the (a) PTMG-HDI/LiFSI and (b) PEO/LiFSI at different temperatures.

Supplementary Fig. 11 Cross-sectional SEM images of the PTMG-HDI-BHDS/LiFSI film teared off from SS|PTMG-HDI-BHDS|SS cell.

Supplementary Fig. 12 Digital photographs of the conventional (a, b) laminated Li|PEO|Li pouch cell and (c, d) integrated Li|PTMG-HDI-BHDS|Li pouch cell.

Supplementary Fig. 13 Galvanostatic cycling of Li|PEO|Li pouch cells at the current density of 0.2 mA cm−2.

Supplementary Fig. 14 The SPEs solution were introduced on the Li anodes through casting infiltration, the integrated Li@SPE were formed by the subsequent solvent evaporation.

Supplementary Fig. 15 Galvanostatic cycling of Li|PTMG-HDI-BHDS|Li pouch cells at the current density of 0.2 mA cm−2.

Supplementary Fig. 16 Digital photograph of the integrated Li@SPE before drying.

Supplementary Fig. 17 Top view SEM images of the cycled Li anodes detached from Li|PEO|Li (a), Li|PTMG-HDI|Li (b) and Li|PTMG-HDI-BHDS|Li cells (c).

Supplementary Fig. 18 Cross-sectional SEM images of the cycled Li anodes detached from (a) Li|PEO|Li, (b) Li|PTMG-HDI|Li and (c) Li|PTMG-HDI-BHDS|Li cells.

Supplementary Fig. 19 Digital photographs of the integrated (a) SPAN@SPE and (b) Li@SPE.

Supplementary Fig. 20 The cross-sectional SEM images of SPAN cathode.

Supplementary Fig. 21 The cross-sectional SEM images of integrated SPAN@SPE cathode.

Supplementary Fig. 22 Charge/discharge curves of the SPAN|PTMG-HDI-BHDS|Li cell at 0.3 C.

Supplementary Fig. 23 Digital photograph of the large-scale preparation of SPAN@SPE.

Supplementary Fig. 24 Digital photograph of the integrated SPAN|PTMG-HDI-BHDS|Li pouch cell.

Supplementary Fig. 25 Charge/discharge curves of the S@CB|PTMG-HDI-BHDS|Li cell at 0.3 C.

Supplementary Fig. 26 EIS plots of the Laminated SPAN|PTMG-HDI-BHDS|Li and Integrated SPAN|PTMG-HDI-BHDS|Li cells.

Supplementary Table 1. The cycling stabilities of the solid-state Li|SPEs|Li symmetric cells.

| Electrolytes | Current density/capacity (mA cm-2/mAh cm-2) | Cycling time (h) | Rate capability (mA cm-2) | References |
| --- | --- | --- | --- | --- |
| PVFH-VEC-SN | 0.2/0.2 (26 oC) | 1500 | 1 | Adv. Mater. 2022, 34, 2202143 |
| PVDF-hfp/SiO2 | 0.2/0.2 (25 oC) | 3000 | 0.5 | Adv. Mater. 2022, 34, 2205575 |
| PAN/Li1.4Al0.4Ti1.6(PO4)3/PEO-LiTFSI | 0.2/0.2 (60 oC) | 1000 | 0.2 | JACS 2019, 141, 9165-9169 |
| PEO/LLZTO-LiTFSI | 0.2/0.1 (55 oC) | 600 | 0.2 | Adv. Energy Mater. 2019, 9, 1804004 |
| PEO-LiFTFSI | 0.1/0.2 (70 oC) | 200 | 0.1 | JACS 2018, 140, 9921-9933. |
| PEGMEA-Li7La3Zr2O12 LiTFSI | 0.1/0.1 (55 oC) | 3200 | 0.1 | JACS 2018, 140, 82-85 |
| PEO/PMA | 0.1/0.1 (65 oC) | 336 | 0.1 | Adv. Mater. 2019, 31, 1805574 |
| PEO/Li3/8Sr7/16Ta3/4Zr1/4O3-LiTFSI | 0.1/0.1 (45 oC) | 700 | 0.6 | PNAS 2019, 116, 18815-18821. |
| PE/PEGMEA | 0.1/0.1 (60 oC) | 1500 | 0.45 | Adv. Mater. 2021, 2100353 |
| PI/DBDPE/PEO -LiTFSI | 0.1/0.1 (60 oC) | 300 | 0.1 | Nano Lett. 2020, 20, 1686-1692 |
| PI/PEO-LiTFSI | 0.1/0.1 (60 oC) | 1000 | 0.1 | Nat. Nanotechnol. 2019, 14, 705-711. |
| PEGDA-LiTFSI/LiBOB | 0.05/0.05 (30 oC) | 1300 | 0.05 | Joule, 2018, 2, 1838-1856. |
| PE/PEO-LiTFSI | 0.1/0.1 (60 oC) | 1500 | 0.1 | Adv. Energy Mater. 2019, 1902767 |
| PTMG-HDI-BHDS | 0.2/0.2 (30 oC) | 5500 | 1 | This work |

Supplementary Table 2. Comparison of cycling performance of solid-state Li-S batteries.

| Electrolytes | S cathode | S loading (mg cm-2) | Capacity after the cycling test (mAh g-1) | Ref. |
| --- | --- | --- | --- | --- |
| PE/PEO-LiTFSI | S | 1.0 (26 oC) | ~625 mAh gS-1 (30th cycle at 0.1 C) | Adv. Energy Mater. 2019, 1902767 |
| Poly(DOL)/PEG/SiO2-LiTFSI | SPAN | 0.5 (60 oC) | ~500 mAh gS-1 (100th cycle at 0.1 C) | Adv. Mater. 2022, 34, 2110333 |
| PEO/PVDF-LiTFSI | S | ~1.0 (55 oC) | ~650 mAh gS-1 (60th cycle at 0.1 C) | Adv. Funct. Mater. 2021, 31, 2001812 |
| PEO/LGPS-LiTFSI | SPAN | ~1.0 (60 oC) | ~588 mAh gS-1 (50th cycle at 0.1 C) | Adv. Funct. Mater. 2020, 30, 1910123 |
| PEO/CNT/GO-LiTFSI | S | 0.5 (60 oC) | 800 mAh gS-1 (50th cycle at 0.2 C) | Adv. Funct. Mater. 2021, 31, 2104863 |
| PEO/LLZO-LiClO4 | S | 0.6-0.9 (37 oC) | ~800 mAh gS-1 (200th cycle at 0.08 C) | Nano Lett. 2017, 17, 2967-2972 |
| PEO-PIM-LiTFSI | S | 1.0 (26 oC) | ~720 mAh gS-1 (100th cycle at 0.5 C) | Adv. Funct. Mater. 2021, 31, 2104830 |
| PEO-LiFTFSI | S | ~1.0 (70 oC) | ~750 mAh gS-1 (60th cycle at 0.1 C) | JACS. 2018, 140, 9921−9933 |
| PEO-PAN-LiTFSI | S | ~1.0 (70 oC) | ~752 mAh gS-1 (75th cycle at 0.1 C) | Adv. Funct. Mater. 2022, 32, 2203272 |
| PIN/SN-LiTFSI | S | ~1.0 (70 oC) | ~420 mAh gS-1 (50th cycle at 1 C) | Nano Lett. 2019, 19, 2343-2349 |
| LLZO/PEO-LiTFSI | S | 0.41 (45 oC) | 820 mAh gS-1 (50th cycle at 0.073 C) | Energy Environ. Sci., 2019, 12, 2496-2506 |
| PTMG-HDI-BHDS | SPAN S | 2 (30 oC) 2 (30 oC) | 745 mAh gSPAN-1 (700th cycle at 0.3 C) 782 mAh gS-1 (350th cycle at 0.3 C) | This work |

References:

- Perdew, J. P., Burke, K. & Ernzerhof M. Generalized gradient approximation made simple. Phys. Rev. Lett. 77, 3865 (1996).

- Wang, H. et al. Electrolytes enriched by crown ethers for lithium metal batteries. Adv. Funct. Mater. 31, 2002578 (2021).