Supplementary information

Heteropolyacid supported on on ionic liquid decorated hierarchical faujasite zeolite as an efficient catalyst for glycerol acetalization to solketal

Samahe Sadjadia1, Sara Tarighi*1, Motahareh Delangiza1, Majid Heravi*2

Materials

To synthesize HR/Y-F127-IL-HPMo catalyst, the following reagents and solvents were utilized: phosphomolybdic acid (H3[PMo12O40], HPMo), silicotungstic acid (H4[W12SiO40], HW), phosphotungstic acid (H3[PW12O40], HPW), triethanolamine (TEA), (3chloropropyl)triethoxysilane (CPTES), sodium hydroxide (NaOH), sodium aluminate (NaAlO2), acetic acid, ammonium hydroxide (NH4OH), ammonium nitrate (NH4NO3),  Pluronic®F-127, ludox AS-30 colloidal silica, toluene, ethanol (EtOH), all was provided from Sigma-Aldrich. The used glycerol for the acetalization was purchased from Merck Co., while acetone was provided from Sigma-Aldrich.

Instruments

Characterization of HR/Y-F127-IL-HPMo catalyst was fulfilled via Fourier transform infrared (FT-IR) spectroscopy using KBr pellet (PERKIN-ELMER‐Spectrum 65 with scan time of 1 s and spectral resolution of 2 cm-1), X-ray powder diffraction (XRD) analysis (Inel, EQUINOX 1000 X-ray diffractometer), Scanning electron microscopy (SEM) and elemental mapping analyses (VEGAII TESCAN scanning electron microscope, equipped with QX2, RONTEC energy dispersive X-ray analyzer), thermo gravimetric (TG) analysis (METTLER TOLEDO device, under O2 atmosphere within the range of 25-800 ºC and heating rate of 10 °C/min). The acidity of the as-prepared samples was evaluated by the temperature programmed desorption of ammonia (NH3-TPD(, Chemisorption Analyzer, NanoSORD (made by Sensiran Co., Iran), the heating ramp rate was 20 °C/min, in the temperature range of 25-800 °C). To measure the specific surface area (SBET) and total pore volume (VP) of the catalyst, Brunauer-Emmett-Teller (BET) method (BELSORP MINI II, BEL apparatus) was applied. The catalyst pre-heating step was done at 150 °C for 3 h. Average pore diameter (DP), micropore volume (Vmicro) and mesopore volume (Vmeso) were obtained via BJH and t-plot methods.

To identify the reaction products and calculate their yields, GC analysis (Shimadzu GC 17A apparatus, equipped with flame ionization detector (FID) and fitted with a Carbowax capillary column) was employed. In this analysis, the temperature of detector and injector were fixed on 280 and 250 ºC, respectively.

B

Figure S1. A: EDS and B: elemental mapping analyses of the catalyst.

Figure S2. NH3-TPD profiles of HR/Y-F127 and HR/Y-F127-IL-HPMo

Figure S3. N2-adsorption-desorption isotherms of HR/Y-F127 and HR/Y-F127-IL-HPMo

Figure S4. The results of recyclability of HR/Y-F127-IL-HPMo for the acetalization of glycerol under optimum condition.

Figure S5. The proposed mechanism for glycerol acetalization to DDM.

Table S1. Comparison of the activity of HR/Y-F127-IL-HPMo with other catalysts

| No. | Catalyst | G: A* | Temp. (ºC) | Time (h) | Conv. (%) | DDM selectivity (%) | DDM yield (%) | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | HR/Y-F127-IL-HPMo | 1:20 | 55 | 2 | 100 | 98 | 98 | - workwork |
| 2 | HPW | 1:20 | r.t. | 2 | 83 | 98 | 81.3 | 1 |
| 3 | NaY zeolite | 1:20 | 50 | 2 | 44.5 | 22.5 | 10.0 | 2 |
| 4 | HR/Y | 1:20 | 50 | 2 | 92.7 | 77.9 | 72.3 | 2 |
| 5 | Y-W20a | 1:20 | 50 | 2 | 75.9 | 68.8 | 52.2 | 2 |
| 6 | HR/Y-W20b | 1:20 | 50 | 2 | 98.1 | 96.4 | 94.6 | 2 |
| 7 | Nb15-HUSYc | 1:2 | 70 | 3 | 58 | 98 | 57 | 3 |

*Molar ration of glycerol to acetone

a: Faujasite zeolite-supported HPW (20 wt.%)

b: Hierarchical faujasite zeolite-supported HPW

c: H-form of Ultrastable Y zeolite-supported niobium pentoxide

References

1	da Silva, M. J., Julio, A. A. & Dorigetto, F. C. S. Solvent-free heteropolyacid-catalyzed glycerol ketalization at room temperature. RSC Adv. 5, 44499-44506, doi:10.1039/C4RA17090C (2015).

2	Talebian-Kiakalaieh, A. & Tarighi, S. Hierarchical faujasite zeolite-supported heteropoly acid catalyst for acetalization of crude-glycerol to fuel additives. J. Ind. Eng. Chem. 79, 452-464, doi:https://doi.org/10.1016/j.jiec.2019.07.021 (2019).

3	Ferreira, C. et al. Y zeolite-supported niobium pentoxide catalysts for the glycerol acetalization reaction. Microporous Mesoporous Mater. 271, 243-251, doi:https://doi.org/10.1016/j.micromeso.2018.06.010 (2018).