Supplementary material

Table S.1. Models used for the evaluation of adsorption of Ni(II) and Cd(II) ions in PAB.

| Isotherm |  |  |
| --- | --- | --- |
| Model | Equation | Parameters |
| Langmuir | qeq=qmaxKLCeq1+KLCeq | qeq (mg/g): Sorption capacity at equilibrium qmax (mg/g): Maximum sorption capacity |
|  | RL=1(1+KLCo) | KL (L/mg): Langmuir’s constant Ceq (mg/L): concentration at equilibrium RL: separation factor Co (mg/L): higher initial concentration |
| Freundlich | qeq=KFCeq1n | KF (mg/g)(L/mg)1/n: Freundlich’s constant n: heterogeneity factor |
| Kinetic |  |  |
| Model | Equation | Parameters |
| Pseudo first-order | lnln qeq-qt =lnln qeq- k1t | qt (mg/g): sorption capacity at time t k1 (1/min): pseudo first-order’s constant rate |
| Pseudo second-order | 1qt=1k2qeq2+1qeqt | k2 (1/min): pseudo second-order’s constant rate |
| Intraparticle diffusion | qt=kdt0,5+C | kd (mg/min1/2g): instraparticle diffusion’s parameter C (mg/g): intercept |
| Thermodinamyc |  |  |
| Equation |  | Parameters |
| ∆G°=∆H°-T∆S° | Enthalpy change (∆H°) and entropy change (∆S°) can be obtained from the plot of log(qece) vs. 1/T. | ΔG°: Gibbs free energy T: Temperature (K) qe= amount of metal adsorbed by unit mass of adsorbent (mg/g) ce= Equilibrium metal concentration (mg/L) |

Table S.2. Operational parameters for column biosorption studies

| Column adsorption |  |  |
| --- | --- | --- |
| Operational parameter | Equation/Description | Parameters |
| C/C0 Máx | - | C = concentração final (mg/L); C0 = Initial concentration (mg/L) |
| tb (min) | Time at C/C0 = 0,05 | tb = Breakthrough time (min) |
| tx (min) | Time at C/C0 = 0,95 | tx = Exhaust time (min) |
| Vb (mg/L) | Volume at C/C0 = 0,05 | Vb = Breakthrough volume (mg/L) |
| Vx (mg/L) | Volume at C/C0 = 0,95 | Vx = Exhaust volume (mg/L) |
| δ (cm) | δ=1-quqt*h | δ= Height of ZTM; qu = Amount of metal removed until the breakthrough point (mg); qt = Total amount of metal removed (mg); h = Height of fixed bed adsorption (cm) |
| %sat | %S = 1+δf-1h*100 | %S = Column saturation percentage; δ = Height of ZTM (cm); f = Adsorbent capacity fractional in the adsorption zone to continue removing solute after the breakthrough point; h = Height of fixed bed adsorption (cm). |

Table S.3. Analysis of variance for removed Ni(II) and Cd(II) using PAB

| Metal ion |  | Source | Sum of squares (SS) | Degrees of freedom (df) | Mean square (MS) | F | Ftab |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Ni(II) |  | Regression (R) | 0,762858 | 3 | 0,254286 | 14,91 | 4,35 |
|  |  | Residual (r) | 0,119312 | 7 | 0,017045 |  |  |
|  |  | Lack of fit | 0,038192 | 2 | 0,019096 |  |  |
|  |  | Pure error | 0,000072 | 2 | 0,000036 |  |  |
|  |  | Total SS | 0,882170 | 10 |  |  |  |
| Cd(II) |  | Regression (R) | 0,557341 | 3 | 0,185780 | 5,48 | 4,35 |
|  |  | Residual (r) | 0,237146 | 7 | 0,033878 |  |  |
|  |  | Lack of fit | 0,028471 | 2 | 0,014235 |  |  |
|  |  | Pure error | 0,000176 | 2 | 0,000088 |  |  |
|  |  | Total SS | 0,794487 | 10 |  |  |  |

Fig. S.1. XRD pattern of the PAB

Fig S.2. Effects of factors on (a) Ni(II) (b) Cd(II) removal using PAB