New modified heterocyclic-magnetite chitosan nanocomposite for efficient alizarin red dye removal: adsorption analysis and antibacterial activity.

Asmaa Abuessawy,1,2 Amr Fouda 3, Adel A.-H. Abdel-Rahman1, Mohamed A. Hawata1 Nora A. Hamad*1

1Chemistry Department, Faculty of Science, Menofia University, Shebin El-Kom, 32511 Egypt

2Basic Science Department, Higher Institute of Engineering and Technology, Menoufia, Egypt

3 Botany and Microbiology Department, Faculty of Science, Al-Azhar University, Nasr City, Cairo 11884, Egypt

| Name | Email | ORCID |
| --- | --- | --- |
| Asmaa Abuessawy | a.abuessawy@science.menofia.edu.eg | 0000-0003-2264-3552 |
| Amr Fouda | amr_fh83@azhar.edu.eg | 0000-0003-3840-7837 |
| Adel A-H. Abdel-Rahman | adelnassar63@yahoo.com | 0000-0003-3319-8191 |
| Mohamed A. Hawata | drmohamedhawata@gmail.com | 0000-0001-6859-5133 |
| Nora A. Hamad | nhamad059@gmail.com | 0000-0002-4195-6215 |

*Corresponding author: Nora A. Hamad

https://orcid.org/0000-0002-4195-6215

E–mail address: nhamad059@gmail.com; Tel: +2-010-9587-6887

Scheme S1. The preparation steps of AOC.

Scheme S2. The preparation steps of MC-Cl.

### Characterization of 4,6- di methyl-2-oxo-1,2- di hydropyridine-3-carbonitrile (1):

- IR (KBR) cm-1νmax: 3353 cm-1 (ν NH), 2921, 2856 cm-1 (ν CH-Aliphatic), 2218 cm-1 (ν CN), 1641 cm-1 (ν C=O, C=C Ar).

Fig.S1: FTIR spectrum of compound 1.

- ¹H-NMR (DMSO) δ: 2.107, 2.147 (s, 6H, 2CH), 4.326) Brs, 1H, NH), 5. 921 (s, 1H, C-H).

Fig.S2: ¹H -NMR spectrum of compound 1.

### Characterization of Ethyl 2-(3-cyano-4,6-dimethyl -2- oxopyridine-1(2H)-yl)acetate (2):

- IR (KBR) cm-1νmax: 3022 cm-1 (ν CH-Aromatic), 2967, 2917cm-1 (ν CH-Aliphatic), 2218 cm-1 (ν CN), 1732, 1638 cm-1 (ν 2 C=O), 1605 cm-1 (ν C=C Ar).

Fig.S2: FTIR spectrum of compound 2.

- ¹H-NMR (DMSO) δ: 1.213(t, 3H, CH), 2.218, 2.295 (d, 6H, 2CH), 4.156 (q, 2H, CH), 4.822(s, 2H, CH), 6.154(s, 1H, CH).

Fig.S4: ¹H -NMR spectrum of compound 2.

### Characterization of 1-((4-amino-5-thioxo-4,5-dihydro-1H-1,2,4-triazole-3-yl)methyl)-4,6-dimethyl-2-oxo-1,2-dihydropyridine-3-carbonitrile (3) OAC:

- IR (KBR) cm-1νmax: 3425 cm-1 (ν NH2), 3071 cm-1 (ν NH), 3026 cm-1 (ν CH-Aromatic),   2924, 2854 cm-1 (ν CH-Aliphatic), 2223 cm-1 (ν CN), 1634 cm-1 (ν C=O, C=C Ar), 1522 cm-1 (ν C=N), 1309 cm-1 (ν C=S).

Fig.S5: FTIR spectrum of compound 3 (AOC).

- ¹H-NMR (DMSO) δ: 2.372, 2.434 (d, 6H, 2CH₃), 3.673(s, 2H, CH₂), 5.027(brs, 2H, NH₂), 10 (brs, 1H, NH).

Fig.S6: ¹H -NMR spectrum of compound 3.

### Characterization of MC-Cl (4):

- IR (KBR) cm-1νmax: 3449cm-1 (ν OH), 3385 cm-1 (ν NH), 2856, 2925 cm-1 (ν CH-Aliphatic), 1152 cm-1 (ν C-C), 1064 cm-1 (ν C-O), 800 cm-1 (ν C-CL), 581cm-1 (ν Fe-O).

Fig.S7: FTIR spectrum of compound MC-Cl.

Fig.S8: Effect of AR concentration on sorption process at pH 1→7;

a) 100 ppm Befor adding sorbent and b) 100 ppm after adding sorbent.

Fig.S9: Effect of AR concentration on sorption process at pH 1→7;

a) 200 ppm Befor adding sorbent and b) 200 ppm after adding sorbent.

Fig.S10: Effect of AR concentration on sorption process at pH 1→7;

a) 300 ppm Befor adding sorbent and b) 300 ppm after adding sorbent.

Fig.S11: Effect of AR concentration on sorption process at pH 1→7;

a) 400 ppm Befor adding sorbent and b) 400 ppm after adding sorbent.