Electronic Supporting Information

Hyperbranched 5-sulfosalicylic acid-TDI-chitosan decorated by Fe3O4 nanoparticles: a highly efficient solid acid organocatalyst for the synthesis of quinazoline derivatives under green conditions

Reyhaneh Peyvasteh sourkouhi, Mohammad G. Dekamin*, Ehsan Valiey, Najmeh Hassanzadeh,  Mohammad Dohendou

Pharmaceutical and Biologically-Active Compounds Research Laboratory, Department of Chemistry, Iran University of Science and Technology, Tehran 16846-13114, Iran

Tel: +98-21-77240640-50; fax: +98-21-73021584; e-mail: mdekamin@iust.ac.ir

| Page | Content |
| --- | --- |
| S1 | Title page |
| S2 | Synthesis of 2,3-dihydroquinazolin-4(1H)-one derivatives catalyzed by CS-TDI-SSA-Fe3O4 (1) |
| S3 | Fig S1. FTIR spectra of the commercial Chitosan (a), (CS-TDI-SSA- Fe3O4 1, b) |
| S3 | Fig S2. The EDX spectrum of the CS-TDI-SSA-Fe3O4 (1) |
| S4 | Fig S3. FESEM images of the CS-TDI-SSA-Fe3O4 (1) |
| S5 | Fig S4. XRD patterns of the CS-TDI-SSA-Fe3O4 (1) |
| S5 | Fig S5. VSM pattern of CS-TDI-SSA-Fe3O4 (1) |
| S6 | Fig S6. TGA curve of the CS-TDI-SSA-Fe3O4 (1) |
| S6 | Fig S7. Reusability of the CS-TDI-SSA-Fe3O4 organocatalyst (1) in the model reaction to afford 5a |
| S7 | Table S1 Optimization of the ternary reaction of isatoic anhydride (2) with ammonium acetate (3a) and 4-chlorobenzaldehyde (4a) under different conditions.a |
| S8 | Table S2 Calculation of GC metrics for compound 5a. |
| S9 | Table S3 Comparative synthesis of compound 5a using the reported heterogeneous catalysts versus the present method. |
| S10 | Scheme 2 The proposed mechanism for the synthesis of 2,3-dihydroquinazoline derivatives 5 catalyzed by the biobased multifunctional CS-TDI-SSA-Fe3O4 solid acid nanocomposite (1). |
| S11 | Fig S8. FTIR spectrum of 2‑(4‑Chlorophenyl)-2,3‑dihydroquinazolin‑4(1H)-one (5a) |
| S11 | Fig S9. 1H-NMR spectrum of 2‑(4‑Chlorophenyl)‑2,3‑dihydroquinazolin‑4(1H)‑one (5a) |
| S12 | Fig S10. FTIR spectrum of 2‑(4‑Methylphenyl)-2,3‑dihydroquinazolin‑4(1H)-one (5c) |
| S12 | Fig S11. 1H-NMR spectrum of 2‑(4‑Methylphenyl)-2,3‑dihydroquinazolin‑4(1H)-one (5c) |
| S13 | Fig S12. FTIR spectrum of 2‑phenyl‑2,3‑dihydroquinazolin‑4(1H)-one (5j) |
| S13 | Fig S13. 1H-NMR spectrum of 2‑phenyl‑2,3‑dihydroquinazolin‑4(1H)-one (5j) |

Scheme S1. Synthesis of 2,3-dihydroquinazolin-4(1H)-one derivatives catalyzed by CS-TDI-SSA-Fe3O4 (1)

Characterization of the CS-TDI-SSA-Fe3O4 (1)

(b)

(b)

(a)

(a)

Fig S1. FTIR spectra of the commercial Chitosan (a), (CS-TDI-SSA- Fe3O4 1, b).

Fig S2. The EDX spectrum of the CS-TDI-SSA-Fe3O4 (1).

Fig S3. FESEM images of the CS-TDI-SSA-Fe3O4 (1)

Fe3O4

Fe3O4

chitosan

chitosan

5-Sulfosalicylic acid

5-Sulfosalicylic acid

Fig S4. XRD patterns of the CS-TDI-SSA-Fe3O4 (1).

Fig S5. VSM pattern of CS-TDI-SSA-Fe3O4 (1).

Fig S6. TGA curve of the CS-TDI-SSA-Fe3O4 (1)

Fig S7. Reusability of the CS-TDI-SSA-Fe3O4 organocatalyst (1) in the model reaction to afford 5a.

Table S1 Optimization of the ternary reaction of isatoic anhydride (2) with ammonium acetate (3a) and 4-chlorobenzaldehyde (4a) under different conditions.a

| Entry | Catalyst (g) | Solvent | T (°C) | Time(min) | Yield (%) |
| --- | --- | --- | --- | --- | --- |
| 1 | - | EtOH | 70 | 1440 | 20 |
| 2 | 0.02 | EtOH | Reflux | 20 | 91 |
| 3 | 0.007 | EtOH | 70 | 35 | 78 |
| 4 | 0.003 | EtOH | 70 | 45 | 55 |
| 5 | 0.02 | Solvent-Free | Reflux | 130 | 71 |
| 6 | 0.02 | H2O | Reflux | 60 | 87 |
| 7 | 0.02 | MeOH | Reflux | 30 | 75 |
| 8 | 0.02 | CH2Cl2 | Reflux | 35 | 54 |
| 9 | 0.02 | C6H5CH3 | Reflux | 50 | 45 |
| 10 | 0.02 | THF | Reflux | 100 | 40 |
| 11 | 0.02 | CH3CN | Reflux | 40 | 55 |
| 12 | 0.02 | EtOH | Room temperature | 70 | 53 |
| 13 | 0.02 | EtOH | 50 | 55 | 78 |
| 14 | 0.02 | EtOH | 60 | 45 | 82 |

aReaction conditions: isatoic anhydride (2, 0.5 mmol), ammonium acetate (3a, 1mmol), 4-chlorobenzalaldehyde (4a, 0.5 mmol), CS-TDI-SSA-Fe3O4 (1) and solvent (2.0 mL). isolated yields.

Table S2 Calculation of GC metrics for compound 5a.

|  | Parameters | Characteristics | Formula | Ideal Value | Calculated value for compound 5a |
| --- | --- | --- | --- | --- | --- |
| 1 | Environmental (E) factor | E-factor signifies the total amount of waste generated in a chemical reaction. | [Total mass of raw materials - the total mass of product]/ mass of product | 0 | [(81.566 + 77.083 +70.285)-117.71]/ 117.71 = 0.945 |
| 2 | Atom economy (AE%) | Atom economy signifies the percentage of atoms wasted in chemical reaction. Higher the value of AE, greener is the reaction. Maximum value of atom economy is 100% which indicates that all the atoms present in reactants lies in the product. | [MW of product] ÷ Σ(MW of stoichiometric reactants) × 100 | 100% | [(117.71)/ (81.566 + 77.083 +70.285)] ×100 = 51.42% |
| 3 | Carbon efficiency (CE%) | CE signifies the percentage of carbons in the reactants that is left in the product. | [Amount of carbon in product/ Total carbon present in reactants] x 100 | 100% | [0.455 x 14 / (1.0 x2+ 0.5x 7 + 0.5 x 8)]x 100 = [ 6.37 / (2 + 3.5 +4)] x 100 = 67.05% |
| 4 | Process mass intensity (PMI) | PMI takes into account reaction efficiency, stoichiometry, amount of solvent and all reagent used in the chemical reaction. | Σ (mass of stoichiometric reactants)/[mass of stoichiometry product] | 1 | (81.566 + 77.083 +70.285)/ 117.71 = 1.945 |
| 5 | Reaction mass efficiency (RME %) | RME accounts into atom economy, chemical yield and stoichiometry. | [mass of product/Σ (mass of stoichiometric reactants)] × 100 | 100% | [117.71/ (81.566 + 77.083 +70.285)] × 100 = 51.42% |

Table S3 Comparative synthesis of compound 5a using the reported heterogeneous catalysts versus the present method.

| Entry | Catalyst | Catalyst Loading | Condition reaction | Time(min) | Yield (%) | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Silica sulfuric acid | 20 mol% | Solvent –free | 300 | 80 | (ref. [28]) |
| 3 | Sulfamic acid | 10 mol% | H2O | 35 | 89 | (ref. [29]) |
| 4 | Cobalt aluminat (CoAl2O 4) | 0.02 gr | EtOH | 130 | 82 | (ref. [39]) |
| 6 | CS-TDI-SSA-Fe3O4 | 0.02 gr | EtOH | 20 | 91 | This work |

Scheme S2 The proposed mechanism for the synthesis of 2,3-dihydroquinazoline derivatives 5 catalyzed by the biobased multifunctional CS-TDI-SSA-Fe3O4 solid acid nanocomposite (1).

Selected spectral data

2‑(4‑Chlorophenyl)‑2,3‑dihydroquinazolin‑4 (1 H)‑one (5a):

White solid, melting point: 196-197 °C. 1HNMR  (500MHz, CDCl3): δ(ppm) 7.95 (dt, J = 7.8, 1.4 Hz, 1H), 7.58-750 (m, 3H), 7.43 (dd, J = 8.4, 1.3 Hz, 2H), 7.0-732 (m, 1H), 6.92 (t, J = 7.6 Hz, 1H), 6.68 (d, J = 8.1 Hz, 1H), 5.90 (s, 1H), 5.85 (s, 1H); FTIR (KBr) ν (cm−1): 3447, 3306, 3187, 1656,  1509.

Fig S8 FTIR spectrum of 2‑(4‑Chlorophenyl)-2,3‑dihydroquinazolin‑4(1H)-one (5a).

Fig S9 1H NMR spectrum of 2‑(4‑Chlorophenyl)‑2,3‑dihydroquinazolin‑4(1H)‑one (5a)

2‑(4‑Methylphenyl)‑2,3‑dihydroquinazolin‑4 (1 H)‑one (5c):

White solid, melting point: 227– 228 °C. 1HNMR (500 MHz, CDCl3):

δ(ppm) 7.95 (d, J = 7.8 Hz, 1H), 7.48 (d, J = 7.6 Hz, 2H), 7.34 (t, J = 7.6 Hz, 1H), 7.27 (s, 3H), 6.91 (t, J = 7.6 Hz, 1H), 6.67 (d, J = 8.1 Hz, 1H), 5.87 (s, 1H), 5.79 (s, 1H), 2.4 (s,3H); FTIR (KBr) ν (cm−1): 3450, 3312,3192, 2924, 1658, 1510, 1295.

Fig S10 FTIR spectrum of 2‑(4‑Methylphenyl)-2,3‑dihydroquinazolin‑4(1H)-one (5c).

Fig S11 1H NMR spectrum of 2‑(4‑Methylphenyl)-2,3‑dihydroquinazolin‑4(1H)-one (5c).

2‑phenyl‑2,3‑dihydroquinazolin‑4 (1 H)‑one (5j):

White solid, melting point: 215-217 °C. 1HNMR  (500MHz, CDCl3): δ(ppm) 8.00 – 7.94 (m, 1H), 7.62 (dd, J = 6.7, 3.0 Hz, 2H), 7.50 – 7.44 (m, 3H), 7.41 – 7.32 (m, 1H), 6.93 (t, J = 7.6 Hz, 1H), 6.70 (d, J = 8.1 Hz, 1H), 5.92 (d, J = 10.0 Hz, 2H), 4.43 (s, 1H). FTIR (KBr, cm−1) ν =3300, 3184, 2928, 1656, 1512

Fig S12 FTIR spectrum of 2‑phenyl‑2,3‑dihydroquinazolin‑4(1H)-one (5j).

Fig S13 1H NMR spectrum of 2‑phenyl‑2,3‑dihydroquinazolin‑4(1H)-one (5j).

.