Table 1 Optimization of the ternary reaction of isatoic anhydride (2) with ammonium acetate (3a) and 4-chlorobenzaldehyde (4a) under different conditionsa

| Entry | Catalyst (mg) | Solvent | T (°C) | Time (min) | Yieldb(%) |
| --- | --- | --- | --- | --- | --- |
| 1 | - | EtOH | 70 | 1440 | 20 |
| 2 | 20 | EtOH | Reflux | 20 | 91 |
| 3 | 7 | EtOH | 70 | 35 | 78 |
| 4 | 3 | EtOH | 70 | 45 | 55 |
| 5 | 20 | Solvent-Free | Reflux | 130 | 71 |
| 6 | 20 | H2O | Reflux | 60 | 87 |
| 7 | 20 | MeOH | Reflux | 30 | 75 |
| 8 | 20 | CH2Cl2 | Reflux | 35 | 54 |
| 9 | 20 | C6H5CH3 | Reflux | 50 | 45 |
| 10 | 20 | THF | Reflux | 100 | 40 |
| 11 | 20 | CH3CN | Reflux | 40 | 55 |
| 12 | 20 | EtOH | Room temperature | 70 | 53 |
| 13 | 20 | EtOH | 50 | 55 | 78 |
| 14 | 20 | EtOH | 60 | 45 | 82 |
| aReaction conditions: isatoic anhydride (2, 0.5 mmol), ammonium acetate (3a, 1.0 mmol), 4-chlorobenzalaldehyde (4a, 0.5 mmol), CS-TDI-SSA-Fe3O4 (1) and solvent (2.0 mL). bIsolated yields. |  |  |  |  |  |

Table 2 Synthesis of DHQ derivatives (5a–j) through the three-component condensation of aldehyde derivatives (4a–j) isatoic anhydride (2), and ammonium acetate (3a) in the presence of CS-TDI-SSA-Fe3O4 organocatalyst (1).

| Entry | Aldehyde | Product | Time (min) | Yield (%) | M.P. (°C) Observed | M.P. (°C) (Reported) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 4a | 5a | 20 | 91 | 196-197 | 196-197110,111 |
| 2 | 4b | 5b | 25 | 88 | 190-193 | 192-193112 |
| 3 | 4c | 5c | 20 | 86 | 227-228 | 227-22897 |
| 4 | 4d | 5d | 20 | 90 | 198-200 | 199-200113 |
| 5 | 4e | 5e | 18 | 88 | 349-351 | 350-351114 |
| 6 | 4f | 5f | 20 | 86 | 214-216 | 213-215115 |
| 7 | 4g | 5g | 25 | 84 | 216-218 | 216-21796 |
| 8 | 4h | 5h | 20 | 90 | 201-204 | 202-204116 |
| 9 | 4i | 5i | 30 | 86 | 165-168 | 165-167117 |
| 10 | 4j | 5j | 20 | 88 | 215-217 | 216-218118 |

Table 4 Calculation of GC metrics for compound 5a.

|  | Parameters | Characteristics | Formula | Ideal Value | Calculated value for compound 5a |
| --- | --- | --- | --- | --- | --- |
| 1 | Environmental (E) factor | E-factor signifies the total amount of waste generated in a chemical reaction. | [Total mass of raw materials - the total mass of product]/ mass of product | 0 | [(81.566 + 77.083 +70.285)-117.71]/ 117.71 = 0.945 |
| 2 | Atom Economy (AE%) | Atom economy signifies the percentage of atoms wasted in chemical reaction. Higher the value of AE, greener is the reaction. Maximum value of atom economy is 100% which indicates that all the atoms present in reactants lies in the product. | [MW of product] ÷ Σ(MW of stoichiometric reactants) × 100 | 100% | [(117.71)/ (81.566 + 77.083 +70.285)] ×100 = 51.42% |
| 3 | Carbon Efficiency (CE%) | CE signifies the percentage of carbons in the reactants that is left in the product. | [Amount of carbon in product/ Total carbon present in reactants] x 100 | 100% | [0.455 x 14 / (1.0 x2+ 0.5x 7 + 0.5 x 8)]x 100 = [ 6.37 / (2 + 3.5 +4)] x 100 = 67.05% |
| 4 | Process mass intensity (PMI) | PMI takes into account reaction efficiency, stoichiometry, amount of solvent and all reagent used in the chemical reaction. | Σ (mass of stoichiometric reactants)/[mass of stoichiometry product] | 1 | (81.566 + 77.083 +70.285)/ 117.71 = 1.945 |
| 5 | Reaction mass efficiency (RME %) | RME accounts into atom economy, chemical yield and stoichiometry. | [mass of product/Σ (mass of stoichiometric reactants)] × 100 | 100% | [117.71/ (81.566 + 77.083 +70.285)] × 100 = 51.42% |