SUPPLEMENTARY MATERIAL

Improving the adsorption capacity of graphene oxide. Effect of Ca2+ on tetracycline retention

Florencia M. Onaga Medinaa, Marcelo J. Avenab, María E. Paroloa

aCentro de Investigaciones en Toxicología Ambiental y Agrobiotecnología del Comahue (CITAAC), Facultad de Ingeniería, CONICET-Universidad Nacional del Comahue. Buenos Aires 1400, 8300 Neuquén, Argentina.

bInstituto de Química del Sur (INQUISUR), Departamento de Química, CONICET-Universidad Nacional del Sur. Av. Alem 1253, 8000 Bahía Blanca, Argentina.

* Corresponding author. E-mail address: maria.parolo@fain.uncoma.edu.ar

Structural and textural properties of graphite and graphene oxide

Table S.1. Textural properties of Gr and GO.

| Material | Gr | GO |
| --- | --- | --- |
| BET Surface area | 14 m2 g-1 | 30 m2 g-1 |
| Pore Volume (BJH) | 0.04 cm3 g-1 | 0.03 cm3 g-1 |
| Pore Size (BJH) | 10.1 nm | 5.6 nm |
| Slurry pH | 6.7 | 3.8 |

Table S.2. XRD parameters of Gr and GO

| Material | FWHM | d002 (nm) | Lc (nm) | Number of layers (Nc) |
| --- | --- | --- | --- | --- |
| Gr | 0.38 | 0.34 | 21.49 | 65 |
| GO | 0.66 | 0.95 | 12.06 | 13 |

Fig. S1 UV-visible spectra: A) Gr and GO dispersions of 500 mg L-1. B) GO dispersions of 500 mg L-1 at pH 2-11. C) Photograph of GO (left) and Gr (right) dispersions. D) photograph of GO dispersions at different pH.