Supplementary Information

[(EtO)3Si(CH2)3NH3+][CH3COO-] functionalized on magnetic silica: a novel magnetically recyclable nanocatalyst for synthesis of new (phenylsulfonyl)dihydropyrido[2,3-d]pyrimidine derivatives

Farhad Shirzaei, Hamid Reza Shaterian*

Department of Chemistry, Faculty of Science, University of Sistan and Baluchestan, PO Box:987-98155, Postal Code: 98197-45845, Zahedan, Iran Tel: 0098-54-33447010, Fax: 0098-54-33431067; E-mail: hrshaterian@chem.usb.ac.ir

Title Page.................................................................................................................................S1

Preparation of Fe3O4@SiO2.....................................................................................................S2

Preparation and characterization of Fe3O4@SiO2@[(CH2)3NH3+][CH3COO-]...................... S3

General Experimental Details..................................................................................................S9

FT-IR, spectra of compounds 4A……...................................................................................S10

FT-IR, 1H NMR and 13C NMR spectra of compounds 4B....................................................S11

FT-IR, 4C-4H.................................................................................................................S13-S18

FT-IR, 1H NMR and 13C NMR spectra of compounds 4I......................................................S19

FT-IR, 1H NMR and 13C NMR spectra of compounds 4J.....................................................S21

FT-IR, 1H NMR and 13C NMR spectra of compounds 4K....................................................S23

FT-IR, 1H NMR and 13C NMR spectra of compounds 4L.....................................................S25

FT-IR, 1H NMR and 13C NMR spectra of compounds 4M...................................................S27

FT-IR, 4N-4O.................................................................................................................S29-S30

FT-IR, 1H NMR and 13C NMR spectra of compounds 4P.....................................................S31

1. Preparation of Fe3O4@SiO2

Fe3O4 magnetic nanoparticles were prepared by dissolving FeCl3·6H2O (20 mmol) and FeCl2·4H2O (10 mmol) in deionized H2O (100 mL) with vigorous stirring (800 rpm), and then dropwise adding NH4OH (25% aq, 30 mL) at room temperature until the pH increased to 11. The resulting black dispersion was continuously stirred for 1h at room temperature, and then the mixture was refluxed for 1h. EtOH (40 mL) was added to the nanoparticles and the mixture was heated for 1 h at 40 °C. Tetraethyl orthosilicate (10 mL) was then added and the mixture was continuously stirred for 24 h. The silica-coated nanoparticles were collected by using an external magnet, washed with EtOH and Et2O (2×5 mL), and then dried in a vacuum at 100 °C for 12 h

Fe3O4. IR (KBr) (νmax/cm−1): 3391, 2923, 1622, 1020, 586.

Fe3O4@SiO2. IR (KBr) (νmax/cm−1): 3416, 1618, 1095, 954, 800, 632, 471.

2. Preparation and characterization of Fe3O4@SiO2@[(CH2)3NH3+][CH3COO-]

In a two-necked flask equipped with a dropping funnel and reflux condenser in the ice bath, APTES ((3-aminopropyl) triethoxy silane) (30 mmol) was added. Then, acetic acid (30 mmol) added dropwise to the flask slowly. Stirring was continued at room temperature for 24 hours. After 24 h, ionic liquid [(EtO)3Si(CH2)3NH3+][CH3COO-] was obtained as a yellow viscous liquid. The ionic liquid [(EtO)3Si(CH2)3NH3+][CH3COO-] can be stored for 6 months without any decomposition. [(EtO)3Si(CH2)3NH3+][CH3COO-] (6.0 g) was added to Fe3O4@SiO2 (3.0 g) nanoparticles at room temperature in about 15 minutes. The mixture was then refluxed in toluene (30 mL) as solvent for 24 hours. Finally, Fe3O4@SiO2@[(CH2)3NH3+][CH3COO-] nanoparticles were separated using an external magnet. Then nanoparticles first washed with toluene (2×3 mL), and then washed with EtOH (2×5 mL), subsequently, nanoparticles dried at 80 °C for 6 h in an oven.

[(EtO)3Si(CH2)3N+H3][CH3COO-]. Yellow oil. IR (KBr) (νmax/cm−1): 2974, 2920, 2174, 1888, 1710, 1617, 1569, 1403, 1334, 1295, 1225, 1166, 1079, 1007, 964, 885, 774, 650, 617, 498, 1H NMR (300 MHz, DMSO-d6): δH (ppm) 1.06 (9H, t, J=6.9 Hz, CH3), 1.75 (3H, s, CH3), 1.79 (2H, s, CH2), 2.73 (2H, s, CH2), 3.45 (6H, q, J1=7.2 Hz, J2=6.91 Hz, CH2), 3.75 (2H, t, J=3.6 Hz, CH2), 7.26 (3H, s, NH3), 13C NMR (75 MHz, DMSO-d6): δC (ppm) 18.39, 18.49, 18.81, 24.26, 41.78, 56.45, 175.51.

General procedure for the synthesis of (phenylsulfonyl)dihydropyrido[2,3-d]pyrimidine derivatives over Fe3O4@SiO2@[(CH2)3NH3+][CH3COO-] and ionic liquid [(EtO)3Si(CH2)3NH3+][CH3COO-] catalysts.

In a 50 mL round bottom flask, added Arylaldehydes (1 mmol), Benzenesulfonylacetonitrile (1 mmol), 6-Amino-1,3-dimethyluracil (1 mmol), and nanocatalyst Fe3O4@SiO2@[(CH2)3NH3+][CH3COO-] 0.015 g were stirred under stirring in ethanol as solvent (3 mL) conditions at reflux for the specific time. TLC monitored the progress of the reaction (ethyl acetate / petroleum benzene: 3 / 1). The solid crude product was separated easily. Fe3O4@SiO2@[(CH2)3NH3+][CH3COO-] was separated by an external magnet after adding sufficient ethanol to the solid and heat mixture. The nanocatalyst was dried after three washing with ethanol. The hot ethanol solution containing the crude product was cooled to precipitate the pure product.

In a 50 mL round bottom flask, added arylaldehydes (1 mmol), benzenesulfonylacetonitrile (1 mmol), 6-Amino-1,3-dimethyluracil (1 mmol), and [(EtO)3Si(CH2)3NH3+][CH3COO-] 30 mol% were added under stirring in ethanol as solvent (3 mL) conditions at reflux for the specific time. TLC monitored the progress of the reaction (ethyl acetate / petroleum benzene: 3 / 1). After completion of the reaction, the mixture was cooled, the ionic liquid was dissolved in ethanol but the desired product was precipitated in ethanol. The ethanolic solution containing the ionic liquid as catalyst was separated from solid crude product, and the resulting solid crude product was subsequently recrystallized in ethanol to give the final pure solid desired product. The products were identified by FT-IR, 1H NMR and 13CNMR spectroscopy.

7-Amino-1,3-dimethyl-5-phenyl-6-(phenylsulfonyl)-6,8a-dihydropyrido[2,3-d]pyrimidine-2,4-(1H,3H)-dione (4A), M.p: >280 °C.; IR (KBr) (νmax/cm−1): 3417, 3350, 1653, 1626 ,  1567, 1490, 1445, 1370, 1273, 1263, 1192, 1137, 1110, 1091, 1063, 1038, 1021, 945, 877, 811, 772, 754, 696, 686, 638, 625, 576, 517.

7-Amino-1,3-dimethyl-5-(2-nitrophenyl)-6-(phenylsulfonyl)-6,8a-dihydropyrido[2,3-d]pyrimidine-2,4-(1H,3H)-dione (4B), M.p: >280 °C.; IR (KBr) (νmax/cm−1): 3621, 3478, 3380, 3317, 3227, 3066, 2925, 1683, 1638, 1586, 1530, 1475, 1446, 1407, 1348, 1313, 1279, 1243, 1216, 1175, 1078, 1020, 986, 947, 915, 874, 863, 809, 778, 754, 705, 686, 648, 627, 609, 584, 534, 486, 475.; 1HNMR (300 MHz, DMSO-d6): δH (ppm) 2.9 (3H, s, CH3), 3.0 (3H, s, CH3), 4.5 (1H, s, C-H), 5.0 (1H, s, C-H), 7.0 (1H, d, J = 7.2 HZ, Ar-H), 7.5-7.7 (7H, m, Ar-H), 8.0 (1H, d, J = 7.5 HZ, Ar-H), 8.4 (1H, s, NH2), 8.8 (1H, s, NH2); 13CNMR (75 MHz, DMSO-d6): δC (ppm) 27.6, 29.6, 32.5, 39.1, 39.4, 39.7, 40.0, 40.2, 40.5, 40.8, 66.8, 87.6, 125.2, 129.0, 129.2, 129.7, 129.8, 133.5, 134.3, 134.8, 136.8, 148.8, 151.4, 154.7, 159.6, 160.8.

7-Amino-1,3-dimethyl-5-(3-nitrophenyl)-6-(phenylsulfonyl)-6,8a-dihydropyrido[2,3-d]pyrimidine-2,4-(1H,3H)-dione (4C), M.p: >280 °C.; IR (KBr) (νmax/cm−1): 3413, 3299, 3271, 3148, 2939, 1693, 1652, 1622, 1527, 1491, 1447, 1394, 1352, 1326, 1280, 1252, 1223, 1172, 1084, 1025, 898, 854, 818, 794, 775, 751, 705, 689, 679, 597, 500, 471.

7-Amino-1,3-dimethyl-5-(4-nitrophenyl)-6-(phenylsulfonyl)-6,8a-dihydropyrido[2,3-d]pyrimidine-2,4-(1H,3H)-dione (4D), M.p: 276-277 °C.; IR (KBr) (νmax/cm−1): 3625, 3551, 3431, 3389, 3321, 3088, 2930, 1680, 1668, 1616, 1581, 1555, 1524, 1482, 1446, 1419, 1364, 1371, 1336, 1325, 1309, 1278, 1248, 1218, 1079, 1058, 1055, 1010, 985, 964, 903, 889, 860, 842, 810, 775, 762, 752, 728, 687, 632.

7-Amino-5-(2-chlorophenyl)-1,3-dimethyl-6-(phenylsulfonyl)-4a,7-dihydropyrido[2,3-d]pyrimidine-2,4(1H,3H)-dione (4E), M.p: >280 °C.; IR (KBr) (νmax/cm−1): 3442, 3265, 3137, 2921, 1693, 1675, 1625, 1564, 1476, 1446, 1412, 1365, 1336, 1319, 1309, 1282, 1254, 1243, 1213, 1178, 1138, 1080, 1049, 1030, 968, 891, 851, 818, 773, 755, 708, 688, 644, 608, 574, 557, 535, 449.

7-Amino-5-(2,6-dichlorophenyl)-1,3-dimethyl-6-(phenylsulfonyl)-6,8a-dihydropyrido[2,3-d]pyrimidine-2,4-(1H,3H)-dione (4F), M.p: >280 °C.; IR (KBr) (νmax/cm−1): 3392, 3223, 3029, 2919, 1682, 1656, 1614, 1557, 1449, 1429, 1346, 1322, 1282, 1244, 1211, 1161, 1081, 858, 826, 708, 567, 479.

7-Amino-5-(4-chlorophenyl)-1,3-dimethyl-6-(phenylsulfonyl)-6,8a-dihydropyrido[2,3-d]pyrimidine-2,4-(1H,3H)-dione (4G), M.p: >280 °C.; IR (KBr) (νmax/cm−1): 3639, 3376, 3207, 2934, 1168, 1665, 1622, 1581, 1554, 1479, 1446, 1423, 1324, 1307, 1262, 1252, 1215, 1174, 1139, 1081, 1035, 1015, 997, 898, 852, 839, 810, 773, 767, 727, 720, 689, 635, 535, 506, 486, 458.

7-Amino-5-(4-bromophenyl)-1,3-dimethyl-6-(phenylsulfonyl)-6,8a-dihydropyrido[2,3-d]pyrimidine-2,4-(1H,3H)-dione (4H), M.p: >280 °C.; IR (KBr) (νmax/cm−1): 3373, 3196, 2935, 1678, 1661, 1622,1570, 1609, 1483, 1448, 1413, 1387, 1324, 1306, 1288, 1249, 1223, 1177, 1138, 1081, 1036, 894, 861, 833, 804, 789, 758, 598, 571, 556, 501, 438.

7-Amino-5-(3-hydroxyphenyl)-1,3-dimethyl-6-(phenylsulfonyl)-4a,7-dihydropyrido[2,3-d]pyrimidine-2,4(1H,3H)-dione (4I), M.p: >280 °C.; IR (KBr) (νmax/cm−1): 3639, 3376, 3207, 2934, 1680, 1665, 1622, 1581, 1554, 1479, 1423, 1370, 1262, 1252, 1215, 1174, 1139, 1081, 1035, 1015, 997, 898, 862, 839, 810, 773, 757, 727, 708, 689, 635, 535, 506, 486, 456.; 1HNMR (300 MHz, DMSO-d6): δH (ppm) 3.03 (3H, s, CH3), 3.04 (3H, s, CH3), 4.33 (1H, s, C-H), 4.45 (1H, s, C-H), 6.42-6.69 (2H, m, NH2), 6.47 (1H, dd, J1 = 6.0 HZ, J2 = 1.8 HZ, Ar-H), 7.09 (1H, t, J = 7.8 HZ, Ar-H), 7.50-7.55 (2H, m, Ar-H), 7.64-7.71 (3H, m, Ar-H), 8.35 (1H, s, NH2), 8.72 (1H, s, NH2); 9.42 (1H, s, OH).; 13CNMR (75 MHz, DMSO-d6): δC (ppm) 27.61, 29.52, 39.14, 39.41, 39.69, 39.97, 40.25, 40.52, 40.80, 68.07, 87.84, 113.89, 114.82, 117.65, 129.04, 129,09, 130.45, 134.73, 136.50, 141.91, 151.44, 153.48, 158.18, 159.05, 161.07.

7-Amino-5-(2,3-dimethoxyphenyl)-1,3-dimethyl-6-(phenylsulfonyl)-6,8a-dihydropyrido[2,3-d]pyrimidine-2,4-(1H,3H)-dione (4J), M.p: >280 °C ; IR (KBr) (νmax/cm−1): 3405, 3348, 3238, 3208, 3093, 3001, 2975, 2927, 2828, 1683, 1658, 1641, 1567, 1517, 1479, 1462, 1447, 1430, 1390, 1366, 1320, 1308, 1287, 1266, 1248, 1209, 1180, 1167, 1138, 1070, 1029, 942, 915, 892, 851, 812, 759, 717, 685, 627, 611, 588, 541, 530, 497.; 1HNMR (300 MHz, DMSO-d6): δH (ppm) 0.3 (3H, s, CH3), 3.1 (3H, s, CH3), 3.4 (3H, s, CH3), 3.8 (3H, s, CH3), 4.3 (1H, s, C-H), 4.9 (1H, s, C-H), 6.2 (2H, d, J = 7.2 HZ, Ar-H), 6.86-6.96 (2H, m, Ar-H), 7.5 (2H, m, Ar-H), 7.7 (3H, m, Ar-H), 8.3 (1H, s, NH2), 8.6 (1H, s, NH2).; 13CNMR (75 MHz, DMSO-d6): δC (ppm) 26.6, 30.8, 39.03, 39.0, 39.3, 39.6, 39.9, 40.1, 40.1, 40.4, 40.7, 56.1, 60.4, 66.9, 87.4, 112.7, 119.3, 124.4, 129.0, 129.2, 133.2, 134.9, 149.1, 151.6, 153.0, 154.3, 159.1, 161.0.

7-Amino-5-(3,4-dimethoxyphenyl)-1,3-dimethyl-6-(phenylsulfonyl)-6,8a-dihydropyrido[2,3-d]pyrimidine-2,4-(1H,3H)-dione (4K), M.p: >280 °C ; IR (KBr) (νmax/cm−1): 3379, 3321, 3234, 3206, 2961, 2934, 2837, 1683, 1633, 1560, 1511, 1443, 1415, 1307, 1235, 1210, 1172, 1134, 1080, 1022, 862, 841, 796, 770, 757, 704, 686, 642, 626, 608, 578, 533, 516, 488, 441, 426, 413.; 1HNMR (300 MHz, DMSO-d6): δH (ppm) 3.02 (3H, s, CH3), 3.05 (3H, s, CH3), 3.70 (3H, s, CH3), 3.73 (3H, s, CH3), 4.41 (1H, s, C-H), 4.45 (1H, s, C-H), 6.48-6.84 (3H, m, Ar-H), 7.50-7.54 (2H, m, Ar-H), 7.64-7.67 (3H, m, Ar-H), 8.34 (1H, s, NH2), 8.73 (1H, s, NH2).; 13CNMR (75 MHz, DMSO-d6): δC (ppm) 27.62, 29.53, 39.14, 39.41, 39.69, 39.97, 40.25, 40.52, 40.80, 56.00, 68.12, 88.27, 111.00, 112.49, 118.95, 128.98, 129.09, 132.64, 134.66, 136.62, 148.66, 149.44, 151.44, 153.36, 159.23, 161.17.

پیوست

7-Amino-1,3-dimethyl-6-(phenylsulfonyl)-5-(3,4,5-trimethoxyphenyl)-4a,7-dihydropyrido[2,3-d]pyrimidine-2,4(1H,3H)-dione (4L), M.p: >280 °C ; IR (KBr) (νmax/cm−1): 3425, 3313, 3220, 3200, 2952, 1700, 1624, 1561, 1487, 1444, 1416, 1326, 1294, 1244, 1206, 1167, 1127, 1078, 1030, 991, 860, 823, 800, 777, 754, 727, 710, 682, 630, 596, 562, 528, 512, 493, 447, 419, 400.; 1HNMR (300 MHz, DMSO-d6): δH (ppm) 3.02 (3H, s, CH3), 3.06 (3H, s, CH3), 3.62 (3H, s, CH3), 3.72 (6H, s, CH3), 4.47 (1H, s, C-H), 4.54 (1H, s, C-H), 6.63 (2H, s, Ar-H), 7.50-7.53 (2H, m, Ar-H), 7.65-7.68 (3H, m, Ar-H), 8.39 (1H, s, NH2), 8.80 (1H, s, NH2).; 13CNMR (75 MHz, DMSO-d6): δC (ppm) 27.64, 29.57, 39.10, 39.38, 39.65, 39.93, 40.21, 40.49, 40.77, 56.37, 60.40, 67.78, 88.12, 104.39, 129.00, 129.10, 134.68, 136.35, 136.55, 137.31, 151.45, 153.49, 153.56, 159.43, 167.28.

7-Amino-5-(2,5-dimethoxyphenyl)-1,3-dimethyl-6-(phenylsulfonyl)-4a,7-dihydropyrido[2,3-d]pyrimidine-2,4(1H,3H)-dione (4M), M.p: >280 °C ; IR (KBr) (νmax/cm−1): 3534, 3459, 3323, 3203, 3063, 3025, 2937, 2839, 1655, 1620, 1562, 1496, 1462, 1419, 1368, 1316, 1280, 1239, 1212, 1178, 1135, 1076, 1050, 1016, 944, 847, 800, 768, 757, 717, 683, 620, 536, 513, 491, 461, 428, 413.; 1HNMR (300 MHz, DMSO-d6): δH (ppm) 3.09 (6H, s, CH3), 3.58 (3H, s, CH3), 3.75 (3H, s, CH3), 4.33 (1H, s, C-H), 4.84 (1H, s, C-H), 6.17 (1H, s, Ar-H), 6.76-6.96 (2H, m, Ar-H), 7.54-7.59 (2H, m, Ar-H), 7.69-7.71 (3H, m, Ar-H), 8.34 (1H, s, NH2), 8.61 (1H, s, NH2).; 13CNMR (75 MHz, DMSO-d6): δC (ppm) 27.69, 29.64, 39.11, 39.39, 39.66, 39.94, 40.22, 40.49, 40.77, 55.66, 56.29, 65.97, 86.66, 111.86, 112.32, 115.20, 127.78, 129.05, 129.19, 134.59, 137.15, 150.87, 151.67, 153.50, 154.56, 159.37, 161.08.

7-Amino-1,3-dimethyl-6-(phenylsulfonyl)-5-(m-tolyl)-4a,7-dihydropyrido[2,3-d]pyrimidine-2,4(1H,3H)-dione (4N), M.p: >280 °C ; IR (KBr) (νmax/cm−1): 3365, 3208, 2924, 1684, 1660, 1619, 1551, 1464, 1446, 1364, 1323, 1311, 1279, 1244, 1200, 1174, 1137, 1100, 1083, 1037, 999, 924, 880, 853, 803, 775, 758, 712, 700, 688, 612, 570, 540, 532, 510, 484.

7-Amino-1,3-dimethyl-6-(phenylsulfonyl)-5-(p-tolyl)-4a,7-dihydropyrido[2,3-d]pyrimidine-2,4(1H,3H)-dione (4O), M.p: >280 °C ; IR (KBr) (νmax/cm−1): 3652, 3524, 3345, 3201, 2931, 1682, 1666, 1617, 1554, 1477, 1446, 1420, 1387, 1337, 1319, 1280, 1248, 1212, 1173, 1137, 1079, 1023, 997, 889, 861, 842, 809, 796, 757, 707, 685, 631, 572, 553, 538, 497, 481.

7-Amino-5-(5-bromo-2-hydroxyphenyl)-1,3-dimethyl-6-(phenylsulfonyl)-4a,7-dihydropyrido[2,3-d]pyrimidine-2,4(1H,3H)-dione (4P), M.p: >280 °C ; IR (KBr) (νmax/cm−1): 3469, 3334, 1651, 1622, 1565, 1514, 1446, 1393, 1373, 1334, 1259, 1185, 1129, 1190, 1056, 1022, 965, 942, 880, 822, 811, 776, 756, 725, 686, 635, 612, 584, 556.; 1HNMR (300 MHz, DMSO-d6): δH (ppm) 3.01 (3H, s, CH3), 3.08 (3H, s, CH3), 4.38 (1H, s, C-H), 4.89 (1H, s, C-H), 6.61 (1H, s, Ar-H), 6.82-7.25 (2H, m, Ar-H), 7.51-7.54 (2H, m, Ar-H), 7.64-7.66 (3H, m, Ar-H), 8.41 (1H, s, NH2), 8.63 (1H, s, NH2), 10.26 (1H, s, OH).; 13CNMR (75 MHz, DMSO-d6): δC (ppm) 27.70, 29.61, 39.09, 39.37, 39.65, 39.93, 40.21, 4048, 40.76, 65.88, 86.38, 110.59, 117.92, 127.57, 128.90, 129.16, 129.86, 131.63, 134.52, 137.08, 151.57, 154.52, 154.68, 159.59, 161.11.