| Table 1 Optimal reaction conditions for the synthesis of 7-amino-1,3-dimethyl-5-phenyl-6-(phenylsulfonyl)-6,8a-dihydropyrido[2,3-d]pyrimidine-2,4(1H,3H)-dionea by [(EtO)3Si(CH2)3NH3+][CH3COO-]. |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Entry | Catalyst | Amount of catalyst (mol %) | Solvent (3 ml) | Temp. (°C) | Time (min) | Yield (%)b |
| 1 | - | - | - | r.t. | 24 h | - |
| 2 | - | - | - | 100 | 24 h | - |
| 3 | - | - | H2O | r.t. | 24 h | - |
| 4 | - | - | H2O | Reflux | 24 h | Trace |
| 5 | - | - | EtOH | r.t. | 24 h | - |
| 6 | - | - | EtOH | Reflux | 24 h | Trace |
| 7 | - | - | Acetonitrile | Reflux | 24 h | - |
| 8 | - | - | Toluene | Reflux | 24 h | - |
| 9 | - | - | DMF | Reflux | 24 h | - |
| 10 | [(EtO)3Si(CH2)3NH3+][CH3COO-] | 30 mol% | H2O | r.t. | 24 h | - |
| 11 | [(EtO)3Si(CH2)3NH3+][CH3COO-] | 30 mol% | H2O | Reflux | 6 h | 43 |
| 12 | [(EtO)3Si(CH2)3NH3+][CH3COO-] | 30 mol% | - | r.t. | 6 h | Trace |
| 13 | [(EtO)3Si(CH2)3NH3+][CH3COO-] | 30 mol% | Solvent-Free | 100 | 60 | 94 |
| 14 | [(EtO)3Si(CH2)3NH3+][CH3COO-] | 30 mol% | DMF | Reflux | 6 h | 41 |
| 15 | [(EtO)3Si(CH2)3NH3+][CH3COO-] | 30 mol% | Toluene | Reflux | 6 h | - |
| 16 | [(EtO)3Si(CH2)3NH3+][CH3COO-] | 30 mol% | Acetonitrile | Reflux | 6 h | 37 |
| 17 | [(EtO)3Si(CH2)3NH3+][CH3COO-] | 30 mol% | EtOH | r.t. | 2 h | 28 |
| 18 | [(EtO)3Si(CH2)3NH3+][CH3COO-] | 30 mol% | EtOH | 50 | 90 | 46 |
| 19 | [(EtO)3Si(CH2)3NH3+][CH3COO-] | 30 mol% | EtOH | 60 | 75 | 61 |
| 20 | [(EtO)3Si(CH2)3NH3+][CH3COO-] | 30 mol% | EtOH | 70 | 40 | 84 |
| 21 | [(EtO)3Si(CH2)3NH3+][CH3COO-] | 30 mol% | EtOH | Reflux | 25 | 96 |
| 22 | [(EtO)3Si(CH2)3NH3+][CH3COO-] | 10 mol% | EtOH | Reflux | 65 | 90 |
| 23 | [(EtO)3Si(CH2)3NH3+][CH3COO-] | 20 mol% | EtOH | Reflux | 45 | 92 |
| 24 | [(EtO)3Si(CH2)3NH3+][CH3COO-] | 40 mol% | EtOH | Reflux | 15 | 89 |
| aBased on the reaction of benzaldehyde (1 mmol), Benzenesulfonylacetonitrile (1 mmol), and 6-Amino-1,3-dimethyluracil (1 mmol).; bYields refer to isolated product after purification. |  |  |  |  |  |  |

| Table 2 Optimal reaction conditions for the synthesis of 7-amino-1,3-dimethyl-5-phenyl-6-(phenylsulfonyl)-6,8a-dihydropyrido[2,3-d]pyrimidine-2,4(1H,3H)-dionea by Fe3O4@SiO2@[(CH2)3NH3+][CH3COO-]. |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Entry | Catalyst | Amount of catalyst (g) | Solvent (3 ml) | Temp. (°C) | Time (min) | Yield (%)b |
| 1 | Fe3O4@SiO2@[(CH2)3NH3+][CH3COO-] | 0.015 | H2O | r.t. | 6 h | - |
| 2 | Fe3O4@SiO2@[(CH2)3NH3+][CH3COO-] | 0.015 | H2O | Reflux | 6 h | 55 |
| 3 | Fe3O4@SiO2@[(CH2)3NH3+][CH3COO-] | 0.015 | DMF | Reflux | 6 h | 61 |
| 4 | Fe3O4@SiO2@[(CH2)3NH3+][CH3COO-] | 0.015 | Toluene | Reflux | 6 h | - |
| 5 | Fe3O4@SiO2@[(CH2)3NH3+][CH3COO-] | 0.015 | Acetonitrile | Reflux | 6 h | 54 |
| 6 | Fe3O4@SiO2@[(CH2)3NH3+][CH3COO-] | 0.015 | Solvent-Free | r.t. | 3 h | Trace |
| 7 | Fe3O4@SiO2@[(CH2)3NH3+][CH3COO-] | 0.015 | Solvent-Free | 100 | 3 h | 19 |
| 8 | Fe3O4@SiO2@[(CH2)3NH3+][CH3COO-] | 0.015 | EtOH | r.t. | 2 h | 39 |
| 9 | Fe3O4@SiO2@[(CH2)3NH3+][CH3COO-] | 0.015 | EtOH | 50 | 65 | 47 |
| 10 | Fe3O4@SiO2@[(CH2)3NH3+][CH3COO-] | 0.015 | EtOH | 60 | 40 | 63 |
| 11 | Fe3O4@SiO2@[(CH2)3NH3+][CH3COO-] | 0.015 | EtOH | 70 | 30 | 82 |
| 12 | Fe3O4@SiO2@[(CH2)3NH3+][CH3COO-] | 0.015 | EtOH | Reflux | 20 | 95 |
| 13 | Fe3O4@SiO2@[(CH2)3NH3+][CH3COO-] | 0.008 | EtOH | Reflux | 30 | 90 |
| 14 | Fe3O4@SiO2@[(CH2)3NH3+][CH3COO-] | 0.025 | EtOH | Reflux | 15 | 92 |
| 15 | Fe3O4@SiO2@[(CH2)3NH3+][CH3COO-] | 0.035 | EtOH | Reflux | 10 | 89 |
| 16 | Fe3O4@SiO2@[(CH2)3NH3+][CH3COO-] | 0.05 | EtOH | Reflux | 5 | 81 |
| 17 | Fe3O4 | 0.015 | EtOH | Reflux | 2 h | 45 |
| 18 | Fe3O4@SiO2 | 0.015 | EtOH | Reflux | 2 h | 52 |
| 19 | [(EtO)3Si(CH2)3NH3+][CH3COO-] | 30 mol% | EtOH | Reflux | 25 | 96 |
| aBased on the reaction of Benzaldehyde (1 mmol), Benzenesulfonylacetonitrile (1 mmol), and 6-Amino-1,3-dimethyluracil (1 mmol).; bYields refer to isolated product after purification. |  |  |  |  |  |  |

| Table 3 Synthesis of (phenylsulfonyl)dihydropyrido[2,3-d]pyrimidinea in the presence of Fe3O4@SiO2@[(CH2)3NH3+][CH3COO-] and [(EtO)3Si(CH2)3NH3+][CH3COO-] as catalysts. |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Entry | Product | Catalyst (A) |  | Catalyst (B) |  | M.P (°C) (reported) | M.P (°C) (observed) |
|  |  | Time (min) | Yield (%)b | Time (min) | Yield (%)b |  |  |
| 1 | 4A | 20 | 95 | 25 | 96 | >280 | 306-307 [30] |
| 2 | 4B | 10 | 97 | 15 | 95 | >280 | New compound |
| 3 | 4C | 15 | 92 | 20 | 94 | >280 | 281-282 [30] |
| 4 | 4D | 10 | 96 | 10 | 96 | 276-277 | 277-278 [30] |
| 5 | 4E | 15 | 93 | 20 | 91 | >280 | 288-289 [30] |
| 6 | 4F | 10 | 89 | 15 | 93 | >280 | New compound |
| 7 | 4G | 10 | 94 | 20 | 97 | >280 | 290-291 [30] |
| 8 | 4H | 20 | 91 | 25 | 92 | >280 | 282-283 [30] |
| 9 | 4I | 35 | 88 | 45 | 90 | >280 | New compound |
| 10 | 4J | 40 | 90 | 50 | 95 | >280 | New compound |
| 11 | 4K | 45 | 88 | 45 | 86 | >280 | New compound |
| 12 | 5L | 50 | 98 | 55 | 97 | >280 | New compound |
| 13 | 4M | 40 | 96 | 55 | 93 | >280 | New compound |
| 14 | 4N | 55 | 92 | 60 | 95 | >280 | 284-285 [30] |
| 15 | 4O | 50 | 91 | 55 | 94 | >280 | 281-282 [30] |
| 16 | 4P | 30 | 96 | 35 | 94 | >280 | New compound |
| aReaction conditions: arylaldehydes (1 mmol), benzenesulfonylacetonitrile (1 mmol), and 6-Amino-1,3-dimethyluracil (1 mmol). bIsolated yields after purification. |  |  |  |  |  |  |  |

.

| Table 4 Comparison result of Fe3O4@SiO2@[(CH2)3NH3+][CH3COO-] and [(EtO)3Si(CH2)3NH3+][CH3COO-] with other reported catalysts in the literature for preparation of (phenylsulfonyl)dihydropyrido[2,3-d]pyrimidinea. |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Entry | Catalyst | Amount of catalyst | Solvent | Temp (°C) | Time (min) | Yield (%)[b] | Ref |
| 1 | Triethylamine | 8 mL | Ethanol | Reflux | 4 h | 79 | [30] |
| 2 | glycerol | 5 mL | glycerol | 80 | 120 | 90 | [31] |
| 3 | [(EtO)3Si(CH2)3NH3+][CH3COO-] | 0.04 g | Ethanol | Reflux | 25 | 96 | - |
| 4 | Fe3O4@SiO2@[(CH2)3NH3+][CH3COO-] | 0.015 g | Ethanol | Reflux | 20 | 95 | - |
| a Based on the reaction of benzaldehyde (1 mmol), Benzenesulfonylacetonitrile (1 mmol), and uracil (1 mmol).; b Yields refer to isolated product after purification. |  |  |  |  |  |  |  |